## Slide 1: Beam Screen and Cold Bore Temperatures
V. Baglin
32nd HL-LHC TC
03-12-2015

## Slide 2: Outline
LHC cases
HL-LHC cases with ”high” temperature beam screen
Conclusions

## Slide 3: 1. LHC Cases

## Slide 4: LHC arc & IT: case 1
Cold bore (CB) operates at 1.9 K
Beam screen (BS) operates in the 5-20 K window
A monolayer
C. Benvenuti, R. Calder, G. Passardi
J.Vac.Sci. 13(6), Nov/Dec 1976, 1172-1182
H2 adsorption isotherm on stainless steel
During machine operation, the gas load, induced by the interaction of the beam with the vacuum chamber wall, increase with time
This gas load, can be as large as 10 1015 H2/cm2
As a result, the gas condense on the surface with a given vapour pressure
On the CB, the H2 vapour pressure is negligible:
  < 10-19 mbar
  the vapour pressure of the other gases in even much lower
On the BS, the H2 vapour pressure increase with operation time …..
….. and can be much larger than 10-6 mbar when more than one monolayer are condensed !
Operation time
4.2 K
2.3 K
10-6
10-12

## Slide 5: LHC arc & IT: solution to the H2 vapour pressure issue
A perforated beam screen as demonstrated by SSC studies in 1994
V.V. Anashin et al. J. Vac.Sci.Technol. A. 12(5) , Sep/Oct 194
No perforations
With perforations
The beam screen holes defines the pumping speed
The 1.9 K cold bore temperature provide the capacity (infinite)
10-7
10-9

## Slide 6: LHC SAM: case 2
Cold bore (CB) operates at 4.5 K
Beam screen (BS) operates in the 5-20 K window
  During gas load production, H2 accumulates on the CB reaching the 4.5 K saturated vapour pressure of 2 10-5 mbar
  the CB does not provide enough pumping capacity anymore
  a cryosorber is needed: a woven carbon fiber was selected during LHC design
X 25
X 10 000
V. Anashin et al. Vacuum 75 (2004) 293-299
Required performances (for installation of 200 cm2/m):
  Operates from 5 to 20 K
  Capacity larger than 1018 H2/cm2
  Capture coefficient larger than 15 %

## Slide 7: Carbon fiber cryosorbers
Capacity
Capacity at 10-8 mbar :
  1018 H2/cm2 at 6 K
  1017 H2/cm2 at 30 K
Sticking prob.
Sticking probability at 1018 H2/cm2 :
  15 % at 22 K
  > 15 % below 22 K
V. Baglin et al. EPAC’04, Luzern 2004.
The cryosorbers installed onto the back of the BS provide the required capacity and pumping speed for H2. They are located in cryoelements operating with 4.5 K cold bores
The cryosorbers installed in D2, D3, D4, Q4, Q5 and Q6 of the LSS require a regeneration during the shutdown for removing the H2
During normal operation of the LHC machine, a regeneration is not foreseen
The cryosorber is regenerated at ~ 80 K
While regenerating, the beam is OFF and the BS should be warmed up to more than 80 K and the CB held at more than 20 K (emptying cold mass)
While the H2 is liberated from the cryosorbers, it is pumped by an external pumping system.
Principle of operation

## Slide 8: 2. HL-LHC Cases with “High” Temperature Beam Screen

## Slide 9: HL-LHC: case 1
Cold bore (CB) operates at 1.9 K
Beam screen (BS) operates in the 40-60 K range
The perforated beam screen together with the 1.9 K cold bore provides the H2 pumping speed and capacity
Particularity of a-C coated beam screen:
40 K
50 K
R. Salemme
Physisorbed / condensed H2 is released from 400 nm thick a-C coating in the 40-50 K temperature range !
 The temperature window 40-60 K is not appropriated
 TBC in the coming year(s) if 50–70 K is an alternative
H2 adsorption isotherm
a-C coating is a cryosorber !
At 10 K:
  capacity ~ 100 Cu
  but less than the LHC cryosorber
Characterisation with different gases and temperatures to be continued in 2016 and later
Increasing T

## Slide 10: HL-LHC: case 2
Cold bore (CB) operates at 4.5 K
Beam screen (BS) operates in the 40-60 K range
A cryosorber is needed with a perforated beam screen to provide the H2 pumping speed and capacity
No cryosorber is evidenced above 5-20-30 K working temperature
LHC cryosorber:
  H2 is not pumped above 40 K
  Regeneration above 80 K

## Slide 11: 3. Conclusions

## Slide 12
Conclusions
Perforation on the beam screen provides pumping speed
Operating the cold bore at 1.9 K provides H2 capacity
A cold bore operating at 4.5 K do not provides H2 capacity: a cryosorber is needed
Actual (known) cryosorber can operate in the range 5-20 K but cannot operate above ~ 40 K
Finding a cryosorber operating above 40 K is one of the main challenge for the FCC study !
Evidencing such a cryosorber in the HL-LHC time frame seems unrealistic

## Slide 13: Thank you for your attention

## Slide 15: Reserve slides

## Slide 16: LHC : Examples of temperature transients
Cold bore (CB) operates at 1.9 K
Beam screen (BS) operates in the 5-20 K but with excursion outside the temperature window
Fill 2177, 1st October 2011
During beam injection:
  T => 22 K
     P ~ 10-8 mbar
Fill 4332, 8th September 2015
During end of fill:
  T => 22 K
     P ~ 3 10-8 mbar