## Slide 1: Bruker Energy & Supercon Technologies (BEST)
EUCARD2 status by Bruker HTS
CERN, 01.12.2015
Notes: Title picture can be exchanged in the masterslide.

## Slide 2: Outline
New production site
First Ic-s in PLD600
PLD 300
12mm production Cu, Ag, 50µm substrate tests,
EUCARD2 plan
Gustaaf Van Tendeloo
Alexander Meledin,
Uni Antwerpen
2
EUCARD2 , Bruker HTS, CERN, 01-12- 2015

## Slide 3: HTS PILOT-LINE PRODUCTION Actual Status
Page 3
3
RELOCATION OF BHTS IN Q3 2015
  current site
  new site
Page 3

## Slide 4: Bruker HTS: new site
Gustaaf Van Tendeloo
Alexander Meledin,
Uni Antwerpen
4
Provided by U. Betz
EUCARD2 , Bruker HTS, CERN, 01-12- 2015

## Slide 5: First short tapes with Ic =800 - 1000A at 4.2K, 5T, B//c; w=4mm
Gustaaf Van Tendeloo
Alexander Meledin,
Uni Antwerpen
5
EUCARD2 , Bruker HTS, CERN, 01-12- 2015

## Slide 6
6
Bruker 14017-2-1-905 tape in LHe
B, T
Comparison Ic(4K; B): FSU + BHTS, 2015
1-905N3
1-905N4
309 A at 31 T
D. Abraimov, D. Larbalestier, … Nov 2014
PLD600, new site, Oct 2015
EUCARD2 , Bruker HTS, CERN, 01-12- 2015

## Slide 7
Page 7
7

## Slide 8: CC/module production: HR-PLD
6 beam HR-PLD
MB-PLD machine with deposition area of 0.13m2
Laser beam guide
Deposition chamber
Optical system
PLD2 = PLD300.

## Slide 9: Available parts of PLD300
Gustaaf Van Tendeloo
Alexander Meledin,
Uni Antwerpen
9

## Slide 10
Gustaaf Van Tendeloo
Alexander Meledin,
Uni Antwerpen
10
Units of PLD300

## Slide 11
Gustaaf Van Tendeloo
Alexander Meledin,
Uni Antwerpen
11
New Chamber of PLD300: Pfeiffer Vacuum says few days needed to accomplish chamber
EUCARD2 , Bruker HTS, CERN, 01-12- 2015

## Slide 12: PLD 300: assembling (time-plan) status 2015-12-01 Chamber: CW50 Optics: CW51 (laser port) CW1 (BDS, chamber) Assembling starts: CW51 Heater: CW52 Power suppls delivered Target unit: CW2 Chamber accessories: CW2 Motors, drives: CW1 System control: CW4
Gustaaf Van Tendeloo
Alexander Meledin,
Uni Antwerpen
12

## Slide 13: EUCARD2: 12mm production Cu, Ag, 50µm substrate tests

## Slide 14: Additional protection of tape after punching at KIT
Confidential
Confidential
Two new defects were introduced to the 36m long tape: one from low-current end (delta x = 1.5 m from the end). Other defect was at distance 21 (?) m. Reason: errors in tape handling (not during plating step!)
Suppression of dog boning is implemented. This suppression is found to be dependent on quality of punching.

## Slide 15: EUCARD2: SS+Ag tapes recently punched by KIT
Confidential
Confidential

## Slide 16: Newest progress in suppression of dog-boning: is important in case of meander-punched tapes
Cu thickness: 27µm in the middle 38µm at the edge
35 µm
Confidential
Confidential

## Slide 17: First 610m long tapes (w=4mm) processed in PLD600 (May-June 2015)
17
Confidential
EUCARD2 , Bruker HTS, CERN, 01-12- 2015

## Slide 18: EUCARD2 plan in WP10 + suppl. order Jan 150m Feb 250m Mar 280m Apr 280m May 280m
Gustaaf Van Tendeloo
Alexander Meledin,
Uni Antwerpen
18

## Slide 19: WP10: REBCO Tapes: Cern specs Nov. 2015
Tape parameters
  Tape width: 12 mm
  Tape thickness: 0.1 mm (SP, SuperOX, Sunam) … 0.14 (BHTS) mm
  Electrodeposited copper layer (after punching): 2 x 20 mm
  Engineering current density (20 T, 4.2 K) > 400 A/mm2 (target 600 A/mm2 )
  Critical current (20 T, 4.2 K) > 500 A (target 670 A)
  Unit length: minimum 50 m (> 30 m needed for magnet construction)
    UL for Aligned Blocks: 20 m (1.2 mm thick cable) to 28 m (0.8 mm thick cable)
    UL for Cos Theta: 17 m (1.2 mm thick cable)

## Slide 20: Cut tape geometry
Optimal geometry as defined by KIT
t
g
p
a
t = 5.9 mm
g = 0.2 mm
α = 30 °
p = 300 mm
R = 1...2 mm
R
R

## Slide 21: Summary
BHTS is transferred by 100% to new building. Installation works with equipment are in progress. Installation and commisioning is practically completed. Fine tuning of process parameters: 2015
New equipment for 12 mm tape is ordered in the end of August. New PLD300 will be assembled in 2015; will be put in operation in the beginning of 2016.
Suppression of dog boning is implemented. This suppression is found to be dependent on quality of punching.
Confidential
EUCARD2 , Bruker HTS, CERN, 01-12- 2015

## Slide 22: 12mm wide tape technology for EUCARD2 CERN VISIT POSTER 3A-WT-P-02.03
Page 22
22
BHTS manufactured several 12mm wide tapes for EUCARD2, CERN
  The high field performance (18T) was checked, a minimum Je of 400 A/mm2 @ 4.2K/18T is required for the C12 tapes

## Slide 23
Innovation with Integrity
Copyright © 2014 Bruker Corporation. All rights reserved. www.bruker.com
Notes: No pictures on last slide!

## Slide 24: Supporting foils:
EUCARD2 , Bruker HTS, CERN, 01-12- 2015

## Slide 25
Page 25
25
Ic(B) in different piece lengths (4.2K, B//c)
Ic(B) at B perpendicular to tape surface measured in liquid He. Coated tapes are 4 mm wide tape with 45 µm thick Cu plating. YBCO thickness corresponds to 1.5-2 µm. Fractions of the 22 m long batch of best quality was measured in wide field range at FSU/NHFML, Tallahassee (D. Abraimov, 2014). Measurements of fractions of 120-230 m long batches of average quality were performed by Bruker HTS/Bruker EAS, Alzenau/Hanau. The n-values measured were in between 42 and 52.