## Slide 1: HTS insert for a particle accelerator using a twisted stacked cable
John Himbele, Arnaud Badel, Pascal Tixador

## Slide 2: Outline of contents
HTS twisted stacked magnet design
  - 2D magnet cross-section
  - 3D magnet ends
Current distribution analysis
Future aspects
Conclusions

## Slide 3: 2D HTS twisted stacked design
Parameter | Value
Center field B0 | 17 T
Current density Jop | 650 MA/m²
Operating current Iop | 10.4 kA
Conductor area | 1472 mm²
Field quality B3/ B5 | 1.5/ 0.78 units
Inner/ external tube | 2/ 4 mm
46-turns HTS insert
Main highlights of twisted stacked design
4 x 4 mm block-coil consisting 20 ReBCO stacked tapes of 4 mm wide achieves required Iop = 10 kA with 46-turns HTS stacked cable.
Three or four block-coils are assembled and aligned in horizontal to facilitate the mechanical architecture and winding.
Good field quality as possible within range of Jop = 600 – 700 A/mm².
17 T

## Slide 4: Winding topology
360° twist
180° twist
Racetrack coil (above beam tube)
180° twist one side
0° on the other
Flared-ends coil (below beam tube)
180° twist one side
360° twist on the other
Flared-ends coil
Straight part
90º twist
ew + 90º twist
Winding head
2D magnet ends cross-section at twist part

## Slide 5: 3D magnet ends
Layer-jump side
Transposition side
Main highlights of 3D HTS coil-ends
Hardway bend: > 2 m
Easyway bend > 10 mm
Twist pitch = 1.8 º/mm
46-turns HTS insert is consist of six double pancakes. Three coils at top and at bottom are the racetrack and flared-ends coils, respectively.
Double pancake is connected with layer jump. Layer jump is done with twist + ew bending or with hw bending.
40 cm
40 cm
- Total length of straight part: 15 m
- Total length of magnet ends: 0.8 m
- Total length of stack cable
in magnet ends: 22 m

## Slide 6: Outline of contents
HTS twisted stacked magnet design
  - 2D magnet cross-section
  - 3D magnet ends
Current distribution analysis
Future aspects
Winding test
Conclusions

## Slide 7: Current distribution 〜 Introduction 〜
Twisted stacked cable (TSC) has only one twist per turn out of 15m long insert.
Stacked tapes are insulated each other in order not to allow the current sharing.
Current distribution of TSC depends on contact resistance.
20 stacked tapes

## Slide 8: Current distribution 〜 Numerical setup 〜
Time [s]
Current [A]
Field [T]
Ramp current
External field
0 T → 1 T
0 A → 0.65*Je
(= Jop)
Rsc + Rcontact
Engineering current density Je | 1000 MA/m2
n-value | 20
Specification for HTS tape
Operating condition

## Slide 9: Current distribution 〜 Numerical setup 〜
H. Gonzáles-Jorge et al., “Evidence of current stabilization after long-time decay in High-Tc superconductors”, Cryogenics, 2004
Chart: Time (s)
Using the right E-J characteristics for the material

## Slide 10: Current distribution 〜 1st step 〜
Ba = 1T, Ia = 0A
Ia = 10.4 kA
Current [A]
Time [s]
Tapes at edges
Tapes in middle
(3) Homogenization
15 m long magnet + Constant contact resistance R = 1000 nW
Current remains zero during the external field. (Twist transposition)
Tapes at edges have more current due to a shielding current in middle.
Current equilibrates depending on total resistance and inductance.
(1)
(2)

## Slide 11: Current distribution 〜 2nd step 〜
Ba = 1T, Ia = 0A
Ia = 10.4 kA
Current [A]
Time [s]
Homogenization
15 m long magnet + Random contact resistance R (= R’ + DR’)
DR’ = aR’
a1: 0.38
a2: 0.4
a3: 0.43
a4: 0.04
a5: 0.2
a6: 0.13
a7: 0.4
a8: 0.22
a9: 0.46
a10: 0.09
a11: 0.13
a12: 0.07
a13: 0.07
a14: 0.43
a15: 0.29
a16: 0.27
a17: 0.07
a18: 0.43
a19: 0.31
a20: 0.18
Tapes at edges
Tapes in middle
R’ = 1000 nW
a = 0 – 0.5

## Slide 12: Current distribution 〜 2nd step 〜
Ba = 1T, Ia = 0A
Ia = 10.4 kA
Current [A]
Time [s]
Homogenization
15 m long magnet + Random contact resistance R (= R’ + DR’)
DR’ = aR’
a1: 0.38
a2: 0.4
a3: 0.43
a4: 0.04
a5: 0.2
a6: 0.13
a7: 0.4
a8: 0.22
a9: 0.46
a10: 0.09
a11: 0.13
a12: 0.07
a13: 0.07
a14: 0.43
a15: 0.29
a16: 0.27
a17: 0.07
a18: 0.43
a19: 0.31
a20: 0.18
Tapes at edges
Tapes in middle
R’ = 1000 nW
a = 0 – 0.5
Next step
Long period analysis
Smaller R’ with less variation a
Anisotropic dependency
Divide all block into 20 tapes

## Slide 13: Outline of contents
HTS twisted stacked magnet design
  - 2D magnet cross-section
  - 3D magnet ends
Current distribution analysis
Future aspects
Conclusions

## Slide 14: Test for current distribution
Electrical joints (MIT)
Twist part
<Plan>
Test at 77 K in Grenoble
December/ 2015
Test under external field
January or February/ 2016
Fresca 10 T test station ?
Pick-up coil
Hole sensor
<Objective>
To see the current distribution of twisted stacked cable
with the ramp current. And to see the behavior after the
end of the ramp current (Long period test).
Current
Time
Ramp current
0.5 Ic

## Slide 15: Conclusion
46-turns HTS twisted stacked design achieved a field of 5 T with Je = 650 MA/m2 and a good field quality. Large Je is needed as the background filed penetrate into c-axis at twist part. The relative magnet ends’ positions of HTS insert and LTS outsert may maintain the large Je.
Twisted stacked cable needs to be insulated because there is only one twist per turn out of 15 m long HTS insert. Therefore, the current distribution is determined by the contact resistance. Further analysis is ongoing.
Current distribution test of twisted stacked cable is planed to especially see after the end of the ramp current.