## Slide 1: ECC
Clément Lorin – Maria Durante
Acknowledgements: Fresca2 team

## Slide 2: Foundations
Context:
  16 T dipole – 4.5 K – ~10% LL margin – Nb3Sn – 50 mm aperture
  No-grading leads to too much conductors: >20,000 tons (4800 dip, 15 m, d = 8.7)
  Preliminary graded cos-theta designs: ~12,000 tons (not protectable!)
Grading needed for block (as well!)
  An efficient grading: extremes strand dimensions (1.1 mm – 0.7 mm)
  Number of coils (manufacturing): large current, big cable (40 strands)
  Cables:
    1.1 mm, 26 strands, 15 mm, 2 mm (~125 tons per turn)
    0.7 mm, 40 strands, 15 mm, 1.25 mm (~75 tons per turn)
Mechanical support: 6 mm
  Fresca2 = 8 mm, 15 T @ 1.9 K not optimized
Fresca2

## Slide 3: Grading 1 – (reference)
Splice room = Large cable thickness (>2.3 mm)
Cu/nonCu = 1.0 both cable
Protectable (50 ms, hotspot < 300 K)
19/146 turns -> 13,600 tons (217 cm²)
Iop = 8395 A
Gap closed 15/148 turns -> 13,300 tons (212 cm²)
FCC quad remark [Ezio]:
1% less dipole field is 8 outer turns (~quantity of conductors needed for the FCC quad)

## Slide 4: Grading 2 – (Cu/nonCu reduction 0.6)
Splice room = Large cable thickness (>2.3 mm)
Cu/nonCu = 0.6 inner 1.0 outer
Protectable (50 ms, hotspot < 300 K)
17/122 turns -> 11,500 tons (184 cm²)
Iop = 9700 A
Gain ~2000 tons (~3 times the quantity of conductors for the quadrupoles!)

## Slide 5: Grading 3 – (Cu/nonCu 0.6 + 48 str. 0.5 mm)
No splice room
Cable
    1.1 mm, 22 strands, 12.7 mm, 2 mm
    0.5 mm, 48 strands, 12.7 mm, 0.9 mm
Cu/nonCu = 0.6 inner 1.4 outer
15 + 10 ms, hotspot ~ 350 K
45/98 turns -> 9,300 tons (149 cm²)
Iop = 8840 A
About the same quantity of conductor as GL Sabbi, same time to react*
*Design study of a 16 T block-dipole for FCC» to be published in IEEE TAS

## Slide 6: Grading 4 – (Cu/nonCu 0.6 + 40 str. 0.6 mm)
No splice room
Cable
    1.1 mm, 22 strands, 12.7 mm, 2 mm
    0.6 mm, 40 strands, 12.7 mm, 1.1 mm
Cu/nonCu = 0.6 inner 1.5 outer
20 + 20 ms, hotspot ~ 300 K
37/108 turns -> 9,999 tons (159 cm²)
Iop = 8760 A

## Slide 7: Grading 5 – (Cu/nonCu 0.6 + 34 str. 0.7 mm)
No splice room
Cable
    1.1 mm, 22 strands, 12.7 mm, 2 mm
    0.7 mm, 40 strands, 12.7 mm, 1.25 mm
Cu/nonCu = 0.6 inner 1.5 outer
20 + 30 ms, hotspot < 300 K
33/116 turns -> 11,000 tons (177 cm²)
Iop = 8620 A

## Slide 8
Magnet ID | 1 | 2 | 3 | 4 | 5
Cables [mm] | 26x1.1 ; 40x0.7 | 26x1.1 ; 40x0.7 | 22x1.1 ; 48x0.5 | 22x1.1 ; 40x0.6 | 22x1.1 ; 34x0.7
Cu/nonCu [-] | 1 ; 1 | 0.6 ; 1 | 0.6 ; 1.4 | 0.6 ; 1.5 | 0.6 ; 1.5
Turns [-] | 19 ; 146 | 17 ; 122 | 45 ; 98 | 37 ; 108 | 33 ; 116
Iop [A] | 8395 | 9700 | 8840 | 8760 | 8620
Time [ms] | 20+30 | 20+30 | 15+10 | 20+20 | 20+30
HotSpot [K] | < 300 | < 300 | ~350 | ~300 | < 300
Weight [tons] | 13,600 | 11,500 | 9,300 | 9,999 | 11,000
Area 2 ap. [cm²] | 217 | 184 | 149 | 159 | 177
-Is a ‘perfect’ cable the better solution for a ‘perfect’ magnet?
-Why do we operate at 4.5 K instead of 4.2 K?
-Where do we make the splices? And how?

## Slide 9: From FRESCA2
No specific feedback about grading from FRESCA2
  Ungraded coils
  No Grading options from the beginning
Feedback on use of 40 strands, 1 mm in diameter :
  no special issues for winding (R min 45 mm)
  to be confirmed by coil/magnet test…
Feedback on coil and tools design:
  Preliminary winding tests with special tools to study/define head configuration (length, angle, …), layer jump -- >
  Cable behavior studies relative to heat treatment : to be done as soon as possible with final cable, bare and insulated
FRESCA2 splices: 2 mm thick copper box (U + wedge)

## Slide 10: Splice requirements
Min splice length = cable twist pitch
Need space on each side of cables pair for:
  Copper stabilizer
    U shape + wedge
  Insulation
Need supports to:
  Guide the cables to splice position
  Block the cables ends during winding (and reaction?)
  Support replaced after reaction by copper stabilizer, insulation and soldering tools

## Slide 11: Splice options
In the straight section
  Gap between the two conductors blocks (4 x cable thickness?)
  Gap between layers
In the heads
  Experience on bended splices ?
  Small radius  short length  need for longer (flared) heads  bigger outer diameter
External splices/connections

## Slide 12: Extra – Fresca2

## Slide 13: Extra – D20

## Slide 14: Extra – HD2