## Slide 1: Longitudinal Halo from NEA and PEA Photocathodes
ERL 2017 – 19.06.2017 Geneva
Monika Dehn
K. Aulenbacher, V. Bechthold, F. Fichtner
FKZ 05K12UM1

## Slide 2: Motivation
Knowledge of shape, structure, and length of electron bunches out of a photoemission gun under different photo excitation conditions
Beginning of the project as a collaboration between HZB, HZDR, JGU, MSU, and SPSPU
Now collaboration between HZB, HZDR, DESY, University of Siegen, JGU, and the additional support through University of Rostock, University of Wuppertal, and TU Darmstadt
time
intensity
acceptance
unwanted beam
(longitudinal halo)
laser pulse
pulse response

## Slide 3: Outline
Some fundamentals
  Semiconducting photocathodes
  Photoemission process
Time response measurements
  Experimental setup
  Measuring principles
  Measuring results
Conclusion and Outlook

## Slide 4: Fundamentals Semiconducting photocathodes
CsO:GaAs
  Single crystalline structure
  Negative electron affinity (NEA)
K2CsSb
  Multi crystalline structure
  Positive electron affinity (PEA)
EVal
EC
optical pumping
e-
transport
tunneling
e-
thermalization
EV
solid
vacuum
χ
E
valence band
x
EVal
EC
optical pumping
e-
thermalization
e-
emission
no emission
EV
solid
vacuum
χ
E
x
valence band

## Slide 5: Fundamentals CsO:GaAs – Influences of the Photon Energy
E
x
p-doped solid
vacuum
valence band
5 nm
conducting band
EC
EV
EF
BBR
Penetration depth
  ca. 1250 nm @ 800 nm (Eγ = 1.55 eV)
  ca. 15 nm @ 400 nm (Eγ = 3.10 eV)
Band bending region (BBR) causes an electric field
  Electrons near the surface get accelerated
Parameter | Value
band gap (at 300 K) | 1.42
absorption coefficient 800 nm | 0.8
absorption coefficient 400 nm | 67.1
diffusion constant | 20
doping level | 2.8 ± 1.2 x 1019
layer thickness | 10
Parameter | Value
band gap (at 300 K) | 
absorption coefficient 800 nm | 
absorption coefficient 400 nm | 
diffusion constant | 
doping level | 
layer thickness | 

## Slide 6: Time Response Measurements Principles
Active Phase Stabilization
≈
RF Master
Solid State Amplifier
Deflector
Cavity
:32
Freq. Divider
Cathode
DBM
76MHz-Filter/ Photodetector
Phase Shifter
Laser
Slit
YAG Screen
Detector/
Channeltron
CCD Camera
Beamsplitter
ϕ
Conversion of the longitudinal profile into transverse profile by TM110 RF Deflector Cavity
Electron bunches must be emitted synchronously to RF Master
Longitudinal profile directly visible on the screen (intensity) or can be sampled by a Channeltron Detector

## Slide 7: Time Response Measurements Experimental Setup at PKAT
e- Bunch
Laser
Deflector Cavity
YAG Screen/
Slit
RF Deflection
700 mm
Channeltron
Generation of short electron bunches:
Laser pulse (red), Electron bunch (green), synchronous with RF
Electron Gun
100 keV DC
Double Solenoid

## Slide 8: Time Response Measurements Some Technical Details
Verdi 10G
Pump laser
(CW)
Modelocked Ti:Sapphire Laser (MIRA 900)
Pulsed (~150 fs) or CW
tunable
Repetition rate (32nd subharmonic of master)
at pulsed
HarmoniXX SHG
Frequency doubler (Second Harmonic Generation)
RF system:
  2.45 GHz master oscillator
  2.45 GHz solid state amplifier (developed in house)
  Electronic phaseshifter with 400° range (developed in house)
  TM110 deflector cavity
Laser system:
400 mm

## Slide 9: Time Response Measurements Measurements with CsO:GaAs
Beam profile YAG-screen
CW-beam (integrated over 25 x 106 bunches)
Bunch charge < 0.01 fC
Intensity distribution equals the convolution of
  the transverse beam profile of deflection plane and the time response
  time of flight effects because of energy distribution within the bunch
  laser pulse length
  laser spot size
Without RF
With RF
Time structure
Transverse structure

## Slide 10: Time Response Measurements Results at 400 nm and 800 nm with CsO:GaAs
Measurements
Simulations with the diffusion model
After 10 ps the intensity at 400 nm is about 2 orders of magnitudes smaller.
Quantum efficiency
    QE800 = 0.05%
    QE400 = 0.5%
Simulation with a diffusion model
Describes the pulse response only qualitatively not quantitatively
The signals do not fall as fast as in the measurements
  E.g. unknown doping level
  Electrons at 400 nm do not follow a diffusion

## Slide 11: Time Response Measurements Production of K2CsSb Photocathodes
Victor Bechthold, DPG spring meeting 2017, Dresden
Further information:
Poster
Victor Bechthold
MOPSPP004
Used for measurements

## Slide 12: Time Response Measurements Comparison of CsO:GaAs and K2CsSb
Red and blue line: NEA
Black line: PEA
  Pulse response faster than NEA
  Variation of the intensity in the tail: between a factor of 2 (left) and 10 (right)
  QE = 1 %

## Slide 13: Conclusion and Outlook
Conclusion
  Pulse response measurements with CsO:GaAs photocathodes at 800 nm and 400 nm
  Lower contribution to unwanted beam at 400 nm due to higher concentration to electrons at the surface
  Pulse response measurements with K2CsSb photocathodes at 400 nm
  Pulse response of K2CsSb is faster than CsO:GaAs, and lower contribution to unwanted beam even to CsO:GaAs
  Actually, the measurements with K2CsSb show the lowest limit of our time resolution with σ = 0.9 ps
Outlook
  Analysis of the different types of jitter during the measurements
  Time resolved measurements with other types of GaAs photocathodes (thin layers)
  Investigations in the differences of the tail intensities of K2CsSb

## Slide 14
for your
attention.
Thank you

## Slide 15: Time Response Measurements Limits of the Resolution
Different effects
  Real transverse spot size only by the emittance
  High voltage power supply: jitter
  Beam spot: jitter
  RF phase: jitter
  Laser bunch length: jitter
  Electrons: different starting energies
  Electrons: different transverse momenta
  Channeltron: hum of the mains
  Water cooling: drifts

## Slide 16: Time Response Measurements Limits of the Resolution
Limits by the Experimental Setup
  Phase Stability (Jitter and Drift of the RF Cavity)
    Jitter (fast) mainly due to the Laser Systems
    Drifts (slow) by thermal effects
     depends on measurement time
  Finite transversal size of the electron bunch
    “Deflection speed“ on the screen ~400µm/ps at minimum transversal size of ~190µm 
    Size of Laser spot on Cathode affects bunch size (Emittance)   
  
Physical Limits (beam transport)
  Longitudinal dispersion caused by distribution of kinetic energy at emission
  

## Slide 17: Time Response Measurements Long Phaseshift
Phase shift: 200°
Pulse repeats after 169°
11°
180°
Cavity simulation
  E.g. a beam deviation of 5mrad through the cavity shows an additional phase shift and an intensity modulation.
Source: Kirsch, E.: Johannes Gutenberg Universität Mainz, Diplomarbeit, 2014

## Slide 18: Fundamentals Semiconducting photocathode GaAs
undotiert
p-dotiert
CsO2 Schicht (NEA)

## Slide 19: Fundamentals Photoemission from Semiconductors
Absorption
  Condition:
  Absorption coefficient:
Diffusion model for GaAs-photocathodes
  Electron motion only by diffusion, not by scattering: And the solution
  Emitted current: with und

## Slide 20: Time Response Measurements Some Calibrations
Phase modulation
37.906° = 18.617 mm
450 Pixel = 23 mm
18.617mm
23mm
Electronical phaseshifter
Source: Bechthold, V.: Johannes Gutenberg Universität Mainz, internal notes, 2016