## Slide 1
Mattia Checchin
Performance frontier group, SRF sector, TD
ERL 2017
20 June 2017
High-Q R&D at FNAL

## Slide 2: Superconducting RF resonators
EM field resonates efficiently with very low dissipation
Performance defined by the first hundreds of nanometers form the RF surface (), where the current flows
High minimization of and

## Slide 3: Why high-Q?
courtesy of A. Grassellino
8 GeV CW SRF Linac

## Slide 4
High studies at FNAL
N-doping & N-infusion

## Slide 5: High treatments studied at FNAL
N-doping
  High T treatment in HV with
  injection done at T = 800 – 1000 C for 2 – 20 min
  Successfully implemented on large scale production (LCLS-II)
N-infusion
  Low T treatment in HV with
  injection done at T = 120 – 160 C for 48 – 96 h
  Being deeply investigated
N-infusion
N-doping

## Slide 6: High treatments studied at FNAL
N-doping
  High T treatment in HV with
  injection done at T = 800 – 1000 C for 2 – 20 min
  Successfully implemented on large scale production (LCLS-II)
N-infusion
  Low T treatment in HV with
  injection done at T = 120 – 160 C for 48 – 96 h
  Being deeply investigated
N-infusion
N-doping

## Slide 7: N-doping: reversal of BCS surface resistance
A. Grassellino et al., Supercond. Sci. Technol. 26 102001 (2013) - Rapid Communications
A. Romanenko and A. Grassellino, Appl. Phys. Lett. 102, 252603 (2013)
M. Martinello et al., App. Phys. Lett. 109, 062601 (2016)
Anti-Q-slope emerges from the BCS surface resistance decreasing with RF field

## Slide 8: High treatments studied at FNAL
N-doping
  High T treatment in HV with
  injection done at T = 800 – 1000 C for 2 – 20 min
  Successfully implemented on large scale production (LCLS-II)
N-infusion
  Low T treatment in HV with
  injection done at T = 120 – 160 C for 48 – 96 h
  Being deeply investigated
N-infusion
N-doping

## Slide 9: N-infusion: a larger parameter space to be explored
at !
A. Grassellino et al., arXiv:1701.06077 (submitted to SUST)
at

## Slide 10: 120 C N-infusion: high at high gradients
Higher Q-factor at higher field may allow for higher duty-cycles and therefore higher luminosity!
Single-cell
9-cells
2 times higher!
A. Grassellino et al., arXiv:1701.06077 (submitted to SUST)

## Slide 11: Nitrogen role in N-infusion
data courtesy of Y. Trenikhina
No nitrides formation at the RF surface
Higher N2 background than not infused samples
Small () N2 enriched layer below native oxide
SIMS data suggest that performances are related to the first nm from the RF surface
Being investigated with subsequent HF rinsing experiment
A. Grassellino et al., arXiv:1701.06077 (submitted to SUST)

## Slide 12
preservation
Understanding the trapped flux
surface resistance

## Slide 13: Trapped flux surface resistance
⇒ intrinsic residual resistance
⇒ trapped magnetic flux surface resistance:
If pinned, vortices may survive in the Meissner state introducing dissipation
—flux trapping efficiency
—trapped flux sensitivity
—external magnetic field
H. F. Hess et al., Phys. Rev. Lett. 62, 214 (1989)
Cooldown
Pinning points
Trapped vortices
Normal conducting

## Slide 14: Trapped flux surface resistance contributions
can be reduced by minimizing these contributions:
𝐵
Magnetic shielding and hygiene
𝜂_𝑡
Fast cooling / pinning
𝑆
Optimizing mean free path
Magnetic shielding and hygiene
Fast cooling / pinning
Optimizing mean free path
Flux Trapping Efficiency
Trapped Flux Sensitivity
External Magnetic Field

## Slide 15: Trapped flux surface resistance contributions
can be reduced by minimizing these contributions:
𝐵
Magnetic shielding and hygiene
𝜂_𝑡
Fast cooling / pinning
𝑆
Optimizing mean free path
Magnetic shielding and hygiene
Fast cooling / pinning
Optimizing mean free path
Flux Trapping Efficiency
Trapped Flux Sensitivity
External Magnetic Field

## Slide 16: Minimization of remnant field in the cryomodule
Demagnetization
Empty vacuum vessel
Assembled Cryomodule
Coils for magnetic field demagnetization
Demagnetization
data courtesy of S. Chandrasekaran

## Slide 17: Trapped flux surface resistance contributions
can be reduced by minimizing these contributions:
𝐵
Magnetic shielding and hygiene
𝜂_𝑡
Fast cooling / pinning
𝑆
Optimizing mean free path
Magnetic shielding and hygiene
Fast cooling / pinning
Optimizing mean free path
Flux Trapping Efficiency
Trapped Flux Sensitivity
External Magnetic Field

## Slide 18: Magnetic field redistribution after SC transition
after complete Meissner effect
(COMSOL simulation)
after full flux trapped
Before the SC transition:
B = Bnc
After the SC transition:
Field completely expelled
Field completely trapped
: trapped magnetic field
: expulsion ratio
Bsc
Bsc
fluxgate magnetometers to measure external field

## Slide 19: Fast cooldown helps flux expulsion
Fast cool-down: large thermal gradients
  efficient flux expulsion
Slow cool-down: small thermal gradients
  poor flux expulsion
T1
T2
A. Romanenko et al., Appl. Phys. Lett. 105, 234103 (2014)
A. Romanenko et al., J. Appl. Phys. 115, 184903 (2014)
D. Gonnella et al., J. Appl. Phys. 117, 023908 (2015)
M. Martinello et al., J. Appl. Phys. 118, 044505 (2015)
S. Posen et al., J. Appl. Phys. 119, 213903 (2016)
S. Huang et al., Phys. Rev. Accel. Beams 19, 082001 (2016)
Bsc/Bnc

## Slide 20: Thermodynamic force during cooldown
We can define the thermodynamic force acting on the vortex as:
The Gibbs free energy density defines the stability of vortices in the SC:
Meissner State
Mixed State
Meissner State
Mixed
State
  M. Martinello, M. Checchin et al., to be published

## Slide 21: Critical thermal gradient
The minimum thermal gradient needed to expel vortices is the critical thermal gradient :
The pinning force acting against the expulsion is defined in terms of critical current density :
Meissner State
Mixed State
Pinning point
  M. Martinello, M. Checchin et al., to be published

## Slide 22: Statistical model for the expulsion ratio
Cavity name | 
CBMM | 0.3
ACC002 | 1.6
Cavity name | 
CBMM | 0.3
ACC002 | 1.6
The model predicts in agreement with literature1,2:
M. Martinello, M. Checchin et al., to be published
Data: S. Posen et al., J. Appl. Phys. 119, 213903 (2016)
1 G. Park et al., Phys. Rev. Lett. 68, 12 (1992)
2 L. H. Allen and J. H. Claassen, Phys. Rev. B 39, 4 (1989)
Let’s define a probability density function for flux expulsion:
the probability of expelling vortices with the thermal gradient is , hence the expulsion ratio is:
Lower
For TESLA shape

## Slide 23: Trapped flux surface resistance contributions
can be reduced by minimizing these contributions:
𝐵
Magnetic shielding and hygiene
𝜂_𝑡
Fast cooling / pinning
𝑆
Optimizing mean free path
Magnetic shielding and hygiene
Fast cooling / pinning
Optimizing mean free path
Flux Trapping Efficiency
Trapped Flux Sensitivity
External Magnetic Field

## Slide 24: Light doping to minimize trapped flux sensitivity
Trapped flux sensitivity:
Bell-shaped trend of as a function of mean free path
N-doping cavities present higher sensitivity than standard treated cavities
Light doping is needed to minimize trapped flux sensitivity
M. Martinello et al., App. Phys. Lett. 109, 062601 (2016)
D. Gonnella et al., J. Appl. Phys. 119, 073904 (2016)
2/6 N-doping

## Slide 25: Single vortex equation of motion
The pinning potential assumed is a 2D Lorentzian function
  parabolic approximation along
The pinning constant is depth-dependent
  flexible vortex line
Multiple pinning centers can be considered
The solution is valid from to
  M. Checchin et al., Supercond. Sci. Technol. 30, 034003 (2017)
Pinning Center
Pinning Center
The motion equation has form:

## Slide 26: Sensitivity vs mean-free-path
Pinning
regime
Flux-flow
regime
  M. Checchin et al., Supercond. Sci. Technol. 30, 034003 (2017)
  Data: M. Martinello et al., App. Phys. Lett. 109, 062601 (2016)
Small – pinning regime :
  increases with and , decreases with the increasing of
Large – flux-flow regime :
  decreases with , independent on and
Pinning

## Slide 27: Sensitivity vs frequency
Small – pinning regime :
  increases with
Large – flux-flow regime :
  independent on
The higher the higher the sensitivity peak
Lower frequencies are favorable to minimize the sensitivity
Pinning
regime
Flux-flow
regime
Increasing
frequency
  M. Checchin et al., Supercond. Sci. Technol. 30, 034003 (2017)

## Slide 28
Summary
State-of-the-art surface treatment for
high at 1.3 GHz

## Slide 29: in condition of full flux-trapping @ 1.3 GHz
12
15
M. Martinello et al., App. Phys. Lett. 109, 062601 (2016)

## Slide 30: in condition of full flux-trapping @ 1.3 GHz
12
15
LCLS-II N-doping is better than standard treatments as long as the field trapped is
M. Martinello et al., App. Phys. Lett. 109, 062601 (2016)

## Slide 31: LCLS-II prototype cryomodule test at FNAL
Cavity | Usable Gradient* [MV/m] | Cryomodule Q0 @16MV/m** Fast Cool Down
TB9AES021 | 18.2 | 2.6e10
TB9AES019 | 18.8 | 3.1e10
TB9AES026 | 19.8 | 3.6e10
TB9AES024 | 20.5 | 3.1e10
TB9AES028 | 14.2 | 2.6e10
TB9AES016 | 16.9 | 3.3e10
TB9AES022 | 19.4 | 3.3e10
TB9AES027 | 17.5 | 2.3e10
Average | 18.2 | 3.0e10
Total Voltage | 148.1 MV | 
* Radiation <50 mR/h
** TB9AES028 Q0 was at 14 MV/m
Acceptance = 128 MV
LCLS-II spec: at
courtesy of G. Wu

## Slide 32: Frequency dependence study
We are now extending the same study to different frequencies and many surface treatments (EP, 120 C bake, N-doping and N-infusion)….
The initial results are extremely interesting….STAY TUNED!

## Slide 33
Conclusions

## Slide 34: Conclusions
Thank you for the attention
N-doping and N-infusion both increases
can be minimized by:
  Efficient magnetic field shielding (low )
  Fast cooling, minimize pinning (low )
  Decreasing as much as possible the sensitivity (low )
Two different regimes of vortex dissipation
  Small , pinning regime: increases if , and
  Large , flux-flow regime: decreases if , but independent on and
Only by understanding N-doping could be successfully implemented to mass production
  LCLS-II cryomodule specification exceeded

## Slide 35
Back-up slides

## Slide 36: N-infusion thermal process
Bulk electro-polishing
High T furnace with caps to avoid furnace contamination:
  3h @ 800C in HV
  48h @ 120-160 C with N2 (25 mTorr)
  Optional annealing 48h @ 120-160 C
NO chemistry post furnace
HPR, VT assembly
Protective caps and foils are BCP’d prior to every furnace cycle and assembled in clean room, prior to transporting the cavity to furnace area
120 C
25 mTorr
800 C
A. Grassellino et al., arXiv:1701.06077 (submitted to SUST)

## Slide 37: Statistical definition of trapping efficiency
The probability of expelling vortices with the thermal gradient is
The trapping efficiency is function of :
The trapped field is then:
  M. Martinello, M. Checchin et al., to be published
For TESLA shape

## Slide 38: Double-peaked probability density function
Double distribution of pinning centers (e.g. dislocations + grain boundaries)
finite probability that vortices are not pinned
First plateau defined by the ratio of the two peaks’ area
Complete flux expulsion reached when is larger enough so that
  M. Martinello, M. Checchin et al., to be published

## Slide 39: High T baking effects
M. Martinello, M. Checchin et al., to be published
Data: S. Posen et al., J. Appl. Phys. 119, 213903 (2016)
After 1000 C
baking
High T baking effects:
Decreases the number of pinning points
  pdf narrowing
Smaller

## Slide 40: Pdf before/after 1000 C annealing example
  M. Martinello, M. Checchin et al., to be published

## Slide 41: Pinning potential
The smaller , the steeper the potential:
  M. Checchin et al., Supercond. Sci. Technol. 30, 034003 (2017)

## Slide 42: Vortex surface impedance
The complex resistivity of the vortex line follows from the calculation of the apparent power (active plus reactive power) :
The vortex surface impedance (using the classic definition of ) is then:
Number of vortices
Vortex impedance weighted over normal distributions of pinning positions and strengths
  M. Checchin et al., Supercond. Sci. Technol. 30, 034003 (2017)

## Slide 43: Pinning strength dependence
Lower pinning strength
Higher pinning strength
1.4 nΩ/mG
0.2 nΩ/mG
M. Checchin et al., Supercond. Sci. Technol. 30, 034003 (2017)
The higher the pinning force, the more constrained the oscillation
Dirtier or more defective materials (e.g. thin films) have larger pining strength
Lower sensitivity!
By increasing the pinning force of one order of magnitude the sensitivity is 7 times smaller!

## Slide 44: Sensitivity vs pinning site depth
Vortex dissipation is a near-surface property
The pinning site distance from the surface determines the resistance
For instance, if :
    sensitivity is the lowest
    constant sensitivity
    bulk pinning does not affect the vortex oscillation!
  M. Checchin et al., Supercond. Sci. Technol. 30, 034003 (2017)
Pinning
Pinning
is a near surface property!