## Slide 1
Tohoku Univ. N. Nishimori
QST R. Nagai, M. Sawamura, R. Hajima
Development of a multialkali photocathode DC gun
for high current operation

## Slide 2: Outline
Development of a photoemission DC gun at QST
Fabrication of Cs3Sb photocathode with QE of 5%
mA beam generation from the gun
Summary

## Slide 3: Application of high current DC gun
800MeV ERL-FEL
10kW EUV light sources
Smith-Purcell FEL
Compact THz light source
N. Nakamura, Tudesday Talk
J. Gardelle et al., PRSTAB12, 110701 (2012)
Charge | en (mm) | Ipeak (A) | Iave. (mA)
60 pC | 0.60 | 30 | 10
Injector specifications after merger
CEA-CESTA, France

## Slide 4: Development of a photoemission DC gun at QST
1. alkali photocathode preparation chamber
2. photoemission DC gun (250kV-50mA max.)
3. beamline
cathode electrode
drive laser
beding magnet
beam profile
monitor
3m

## Slide 5: 1. Development of an alkali photocathode preparation chamber (2013~)
f) tungsten heater
a) transfer rod
b) thickness monitor
CRTS-4 (ULVAC)
c) puck holder
on ratating table
a)
c)
d) NEG pump
d)
e) AS-6-Cs-415-V
(ALVATEC)
Mo boat
Sb 99.9999%
e)
Follow Cornell’s system,
L. Cultera, “Fabrication, characterization and use of alkali antimonides in a dc gun”, P3 Workshop 2012.
MBE chamber
b)
Alkali photocathode preparation chamber

## Slide 6: Fabrication of Cs3Sb photocathode
10-9
10-8
vacuum (Pa)
0
2
3
time (hrs.)
10-7
10-6
1
4
0
2.0
1.5
1.0
0.5
0
200
150
50
QE (%)
T(degC)
10-5
Mo puck
(cERL compatible)
Si(100) substrate
33 mm in diam.
15 mm
in height
Sb
Cs evaporation
10-9
10-8
vacuum (Pa)
0
4
time (min.)
10-7
10-6
8
0
4
3
2
1
QE (%)
10-5
QE increased
2 days later.

## Slide 7: 2. Development of a photoemission DC gun
R. Nagai et al., Proc. Of PAC09, 545 (2009)
R. Nagai et al., RSI 83, 123303 (2012)
Gun development started in 2006.
180kV-1mA beam generation with GaAs photocathode
250kV-50 mA HV power supply
SF6 insulator gas tank
GaAs preparation system

## Slide 8: HV test with cathode electrode in place
0
250
200
150
100
50
0
200
150
100
50
HV (kV)
HVPS current (uA)
10-9
10-8
vacuum (Pa)
0.0
0.5
0.4
0.2
0.1
radiation (uSv/h)
0
4
8
12
time (hrs.)
0.3
cathode electrode

## Slide 9: 3. Beamline
beding magnet
beam profile
solenoid
differential pump
beam profile
monitor
beam dump

## Slide 10: mA beam generation
0
250
200
100
50
0
50
40
20
10
HV (kV)
Beam dump current (mA)
10-8
10-7
Gun, beam dump vacuum (Pa)
0
0.2
time (hrs.)
10-5
10-4
0.6
10-9
0.4
150
30
10-6
0
1.0
532nm laser power (mW)
0
10
8
4
2
QE (%)
0
50
40
20
10
30
6
2.0
Beam dump current (mA)

## Slide 11: mA beam generation
0
200
532nm laser power (mW)
0
5
4
2
1
QE (%)
0
5
4
2
1
3
3
600
Beam dump current (mA)
0
250
200
100
50
0
5
4
2
1
HV (kV)
Beam dump current (mA)
10-8
10-6
0
0.2
time (hrs.)
100
10+2
0.6
10-10
0.4
0.8
300
6
1.8mA with 200 mW laser
4.3mA with 500 mW laser
150
3
10-4
10-2
400
Gun, beam dump vacuum (Pa)

## Slide 12: Vacuum incident during beam transport
0
250
200
100
50
0
5
4
2
1
HV (kV)
Beam dump current (mA)
10-8
10-6
0
0.2
time (hrs.)
100
10+2
0.6
10-10
0.4
0.8
300
6
vacuum incident
150
3
10-4
10-2
Gun, beam dump vacuum (Pa)
1.5mA with 200 mW laser
3.6mA with 500 mW laser

## Slide 13: Summary
Fabricated Cs3Sb photocathode with QE of 5 %.
Generated 150kV - 4.3 mA beam from the photocathode.
Future work
Fix the vacuum issue and perform baking, HV conditioning, photocathode fabrication to restart the gun development.
Acknowledgement
This work is partially supported by JSPS Grants-in-Aid for Scientific Research in Japan (15K13412).