## Slide 1: Graphene – Quantum dot Hybrid photodetector technology for CMOS compatible high performance photodetectors from the UV to Short-wave Infrared
G. Navickaite1, S. Goossens1, I. Nikitskiy1, E. Puma 1, T. Galan1, S. Gupta1, M. Montagut1, C. Monasterio1, F. H. L. Koppens1,2 , G. Konstantatos1,2
1 ICFO - Institut de Ciències Fotòniques, Mediterranean Technology Park, 08860 Castelldefels, Barcelona, Spain
2 ICREA – Institució Catalana de Reçerca i Estudis Avançats, Barcelona, Spain
Gerasimos.Konstantatos@icfo.es, Frank.koppens@icfo.es

## Slide 2
Consumer market: digital imaging, surveillance, remote sensing
The automotive industry (thermal, passive night vision)
The biomedical industry (x-ray imaging, NIR biomedical imaging and diagnostics),
Environmental monitoring (Infrared, UV and multispectral imaging),
Safety (x-ray imaging, explosives and threat detection),
Metrology (scientific metrology, space applications etc.)
Wearable devices (pulse- oxymetry, and other kinds of health monitoring).
Process Monitoring (agro-, food- pharmaceutical inspection)
Machine vision (industrial manufacturing, AUVs, Drones)
Market Applications

## Slide 3
Existing technology roadblocks
Technology Fragmentation
Non Monolithic Solutions
InGaAs Photodiode
Array Chip
Si ROIC Chip
InP
Si
Dramatically High cost beyond Si-coverage:
in SWIR (>20K€)
In FLIR (>50K€)
Low Pixel Resolution
Complex and High cost multispectral systems
Non-flexible platforms (rigid substrates)

## Slide 4
+
Colloidal Quantum Dots
Graphene
ICFO´s Approach

## Slide 5
+
Colloidal Quantum Dots
Graphene
ICFO´s Approach
Ultra small nanocrystals based on PbS
Absorption wavelengths tunable by changing size, exciton peak 600 nm – 2000 nm
Strong light absorber
Solution processed
CMOS Compatible
Vary diameter
Atomically thin carbon layer
High mobility
Low 1/f noise
Transparent and flexible
Grown by chemical vapour deposition (CVD)
CMOS Compatible

## Slide 6
G. Konstantatos et al., Nature Nanotech. 7, 363-368 (2012) .
First Generation of a Graphene-QD photodetector
Gain 106 - 107
EQE 25%
Time response 10 – 100 ms
Linear Dynamic Range 60 dB

## Slide 7
Second Generation of a Graphene-QD photodetector
Nikitskiy et al., Nature Comm. (2016)
Gain 105 - 106
EQE 80%
Time response 0.1 – 1 ms
Linear Dynamic Range 110 dB

## Slide 8
Second Generation of a Graphene-QD photodetector
Nikitskiy et al., Nature Comm. (2016)
Gain 105 - 106
EQE 80%
Time response 0.1 – 1 ms
Linear Dynamic Range 110 dB

## Slide 9
2D (MoS2)-QD photodetector
Kufer et al., Adv. Materials. (2014)
Kufer et al. ACS Photonics (2016)