## Slide 1
Study of the New Glass and Glass Ceramic
Stoichiometric and Gd3+-loaded
BaO*2SiO2:Ce (DSB:Ce)
Scintillation Material for Future Calorimetry
R. W. Novotnya, K.-T. Brinkmana, A. Borisevichb, V. Dormeneva, M. Korjikb, D. Kozlovb, P. Orsichb, H.-G. Zaunicka, and S. Zimmermanna
aJustus-Liebig-Universität Giessen ,II. Physikalisches Institut, Giessen, Germany
bInstitute for Nuclear Problems, Bobruiskaya11, 220030, Minsk, Belarus
and for the Crystal Clear Collaboration
motivation: severe radiation damage due to hadrons
properties of the new material DSB:Ce
characterization of bulk and fiber material
radiation hardness
heavy loading with Gd3+
summary and outlook

## Slide 2
motivation: calorimetry limited by severe hadronic radiation damage
Francesca Nessi-Tedaldi
(ETH, Zürich, Switzerland)
change of optical transmission due to 150MeV protons
1.8 x 1013p/cm2
@KVI
24 GeV protons
3.6·1013 p/cm2
creation of macro defects
highly ionizing fission products
ion displacements
lower Z material required
sampling calorimetry
cheap for mass production

## Slide 3
properties
phase diagram of the BaO*SiO2 system
T / oC
weight % SiO2
nano-sized particles of Ba2SiO5
improve scintillation!
Ba-Si system allows to incorporate
trivalent ions: Lu, Gd, Yb
technology: glass production combined with
successive thermal annealing
(800 – 900oC)
SEM image of recrystallized BaO*2SiO2
at 950oC
1µm

## Slide 4
Investigation of the creation of scintillation centers
in collaboration with D. Rinaldi, SIMAU, Ancona
Characterization of doped and un-doped DSB
at different annealing temperatures:
characterization of crystallization
measurement of light yield and radiation hardness
XRD:
HRSEM: 1.6% Ce 1.93% Ce
samples containing Ce show earlier crystallization

## Slide 5
Irradiation and recovery studies:
Quality
of samples:
@RT, integration 4µs
dLY:/dT: +0.05%/oC
LY @ RT: 110 phe/MeV (4µs)
Irradiation with 60Co, 2Gy/min
Spontaneous and
stimulated recovery

## Slide 6
irradiation and recovery studies: with 150MeV protons
BaO x 2SiO2
(mother glass)
flux ≤ 2x1011 p/s cm2
integral fluence = 5x1013 p/cm2
BaO x 2SiO2 : Ce
(without thermal treatment)
DSB: Ce
(after thermal treatment)

## Slide 7
DSB:Ce fibers: 200 mm long
0.7 < Ø < 1.2 mm
several macro defects
short attenuation length
SP
SP
optical transmission
excitation with LASER @ 325nm
SP

## Slide 8
excitation with UV-LED @ 365nm
SP
SP
DSB:Ce fiber

## Slide 9
response of a single DSB:Ce fiber to electrons (90Sr)
coincidences with
a plastic scintillator
~ 1.5 p.e.

## Slide 10
100 p.e.
200 p.e.
amplitude /a.u.
counts
DSB:Ce testmatrix: 4 x 5
composed of: 20 fiber (1mmØ), 50mm
Mo - structure
response to cosmics
PMT 1
PMT 2
matrix
PMT 1
PMT 2

## Slide 11
DSB:Ce large volume 23 x 23 x 120 mm3
light yield
137Cs
optical transmission
transmission / %
longitudinal
transversal

## Slide 12
DSB:Ce large volume 23 x 23 x 120 mm3
radiation hardness: 100Gy 60Co

## Slide 13
the luminescence
properties
BaO*2SiO2):Ce
BaO*2SiO2):Ce
Gd-loaded
DSB:Ce
excitation @ 380nm
excitation @ 350nm
Gd3+-loaded glass appears
not to change the scintillation
created by the Ce3+ centers

## Slide 14
Scintillation properties:
Material | Decay constants and their fractions in the kinetics |  | 
 | Fast ns (%) | Middfast ns (%) | Slow ns (%)
(BaO*2SiO2):Ce glass | 22 (12) | 72(50) | 450(38)
(BaO*2SiO2):Ce glass loaded with 7 weight% of Gd oxide |  | 86(40) | 330(60)
(BaO*2SiO2):Ce glass loaded with 20 weigth% of Gd oxide | 50(19) | 120(39) | 400(40)
kinetics
Leads to significant increase of light output measured with a 22Na g-source
(BaO*2SiO2):Ce
glass
(BaO*2SiO2):Ce
7 weight%
of Gd oxide
(BaO*2SiO2):Ce
20 weigth%
of Gd oxide

## Slide 15
Light yield as a function
of gate length
response to 137Cs-source (662keV
Scintillation property
of 2 selected
Gd-loaded samples
#1: 10 weight% Gd2O3
#2: 20 weight% Gd2O3
both: 0.5 weight% Ce
disturbed stoichiometry leads to additional traps and slows down the scintillation

## Slide 16
radiation hardness

## Slide 17
DSB:Ce / Gd loaded large volume 23 x 23 x 120 mm3
longitudinal transmission
macro defects

## Slide 18
DSB:Ce / Gd loaded large volume 23 x 23 x 120 mm3
response to low energy g-sources
137Cs
response to
cosmic muons

## Slide 19
summary and outlook:
DSB:Ce appears to be a promising material
loading with Gd3+ helps to increase sensitivity to em probes
wide spectrum of shapes
detailed understanding of scintillation centers and the
process of thermal annealing
properties of large volume blocks
need for optimization of Ce3+ concentration and Gd/Ce ratio
improvement of fiber production free of cracks
cutting of fibers from blocks
to do list: