## Slide 2: Proposal 1602 – Cable Stack HiRadMat Technical board
V. Raginel, D. Kleiven, D. Wollmann
CERN TE-MPE

## Slide 3: Outline
Scientific motivation
Goals of the “Cable Stack” experiment in HiRadMat
Overview of the experimental layout
Operational aspects- Beam Pulse list
Radiological risk
Removal and Post mortem analysis
Risk Assessment

## Slide 4: Determination of damage limit of sc. magnets for instantaneous beam impact
Original motivations coming from HL-LHC failure cases (injection, extraction)
Several experiments planned without beam and with beam:
  Heat stacks of cables in an oven to different peak temperatures and measure dielectric strength of the insulation
  Heat insulation by a short current pulse and measure dielectric strength
  Heat a single strand by a current pulse and measure critical current
  Expose stacks of cables to radiation in HiRadMat at RT and measure dielectric strength and critical current
  Expose stacks of cables to radiation in HiRadMat at cryogenic temperatures and measure dielectric strength and critical current

## Slide 5: Objectives
Measure the degradation of the insulation
Measure the degradation of critical current of Nb-Ti
Check structural integrity of stainless steel plate to validate design of future HiRadMat experiment (cryostat)

## Slide 6: Experimental Design Concept
Six Cu/Nb-Ti cable stacks under compression in stainless steel moulds
  200 mm long cables
  Mould: 60 x 85 x 120 mm3 (~ 4kg)
Aluminium container
  Air tight (to be tested up to 2 atm)
  Filed with Argon (1.1 atm)
  250 x 300 x 600 mm3
Stainless steel plate (thickness = 5 mm)
Vertically movable table (reusing from HRMT24) stroke of 500 mm
Diamond detector to be fixed on the container
Stainless steel plate
Beam
Sc. cable stacks
600 mm
300 mm
500 mm

## Slide 7: Peak Temperature – Design choice
Peak temperatures to be reach in sample based on results of experiments without beam
Peak Temperature (C) | Energy Density in Cu/Nb-Ti (kJ/cm3)
950 | 3.2
800 | 2.8
650 | 2.4
500 | 1.6
400 | 1.2
300 | 0.6

## Slide 8: Energy Deposition and Temperature rise
Beam characteristics FWHM x = y = 0.5 mm, E = 440 GeV
Max. Temp in 3rd cable stack, stainless steel plate and container

## Slide 9: Operational process - Beam Pulse list
Single bunches for alignment (diamond detector)
After each “high” intensity pulse, the target is moved vertically (moving the target ~1 to 2 minutes
Estimated beam time: 1 shift

## Slide 10: Radiological risks – residual dose in proximity of the container
Figures show spatial distribution of the residual dose rates in the horizontal plane
Total intensity ~ 240 bunches, 1.15E11 p/b
After 1 day
After 1 week
After 6 months
After 1 month
Cooling Period | Maximum residual dose rate at 40 cm (µSv/h) | Maximum residual dose rate at contact (µSv/h)
1 day | < 200 | 1.4 x 104
1 week | < 30 | 4.5 x 102
1 month | < 10 | 1.3 x 102
6 months | < 1 | 3.5 x 101

## Slide 11: Radiological risks – residual dose rate within/at contact with the cable stack
Figures show spatial distribution of the residual dose rates in the horizontal plane
½ of the total intensity (120 bunches, 1.15E11 p/b)
After 1 day
After 1 week
After 6 months
After 1 month
Cooling Period | Maximum residual dose rate within cable stack (µSv/h)
1 day | 8.1 x 104
1 week | 9.4 x 103
1 month | 2.6 x 103
6 months | 4.8 x 102

## Slide 12: Removal and disposal
After an appropriate cool down time to be defined in accordance with RP:
In BA7
Removal of the container from the table
Table will be left on the HiRadMat experimental table (to be used in future experiments)
  Transport container to an appropriate controlled area in B867 or in Radioactive WS (B109)
  In Building 867/ Radioactive WS
  Opening of the container and removal of the cable stacks (procedure to be define with RP experts)
  Container to be stored as a single object in an appropriate controlled area – can be reused for future experiment. Request to be performed
  Cable stacks and stainless steel plate package in boxes for further analysis.

## Slide 13: Post mortem analysis
Procedure for post mortem analysis will be defined with RP
Cable stacks:
High Voltage test to be conduct either in building 867 or in the high voltage lab building 112
Critical current measurement to be perform in external lab (to be perform)
Stainless steel plate:
Structural analysis to be done in Microscopic Lab (B599) –(similar procedure as for the LPROT post mortem analysis)
After analysis the cable stacks, mould and the stainless steel plate become RP waste – request to be perform

## Slide 14: Risk Assessment
Melting of the samples
  No contamination risk in HiRadMat
Melting of the container due to too many bunches send on the target
  Contamination risk
  Low probality due to pre pulsing in the SPS
Polyimide Film burning due to air contamination
  Air tight test of the container at 2 atm.
High Voltage for the Diamond detectors (100V DC)
  The handling of high voltage equipment will be performed by trained CERN personnel.
Radiological Risk
  The experiment has been designed to include as little material as possible.

## Slide 15
Thanks you for your attention!

## Slide 16: Stress in Aluminium
# of bunches | ΔT (K) | σ (MPa)
6 | 26.5 | 43.2
12 | 53 | 86.4
24 | 106 | 172.8
with the coefficient of thermal expansion (2.5E-5 K-1)
the young modulus (71 GPa)
the temperature rise
Yield stress of aluminium 90 to 280 MPa

## Slide 17: Pressure in container due to beam pulse
Energy stored in 24 bunches @ 440 GeV = 200 kJ
Temperature rise in all volume less than 3 K
Pressure rise < 0.1 mbar