## Slide 2: Damage levels of superconducting magnet components
Status of studies and first experimental results
V. Raginel, D. Kleiven, K. Kulesz, D. Wollmann

## Slide 3: Outline
Motivations and goals
Damage mechanisms and consequences
Experimental road map
Experimental Results
Next experiments

## Slide 4: Motivations from HL-LHC ultra-fast failure Ultra-fast failure < 270 us (3 LHC turns)
Studies of injection and extraction failures with HL-LHC bunch intensities show that despite beam absorber a peak energy density up to ~ 100 J/cm3 in sc. magnets can be reached. Is it safe?
What is the damage limit of sc. magnets in case of ultra-fast beam losses?
What are the damage mechanisms?

## Slide 5: Reduction of cable Ic due to thermo-mechanical stress
  Plastic deformation of Copper Matrix inducing permanent stress on the Nb-Ti filaments. Critical current (Ic) of Nb-Ti has a low dependency to stress.
  Nb-Ti filaments breaking leading to a reduction of the Ic of the sc. cable
* J.W. Ekin, F.R. Fickett, A. F. Clark, Effect of Stress on the Critical Current of NbTi Multifilamentary composite wire, Proc. Int. Cryogenic Materials Conf., 1975; (1977), Adv. Cryog. Eng., 22:449
  Beam losses  Fast heating  Mechanical stress
Sc. Filaments
Sc. strands
Sc. cable
Notes: When do we break NbTi filaments due to energy depositions?

## Slide 6: Reduction of cable Ic induced by temperature
Melting of copper matrix (~6 kJ/cm3).
Variation of the α-Ti precipitate size (T>400 °C for several minutes).
Variation of the Nb-Ti/Cu strand magnetization (ΔM) at 4.2 K in magnetic field up to 6 T after different HT’s (a) and relative flux pinning reduction vs. annealing temperature at different magnetic field (b).
C. Scheuerlein
Notes: When do we break NbTi filaments due to energy depositions?

## Slide 7: Insulation degradation due to temperature
Reduction of the dielectric strength of polyimide films for T > ~400°C
Courtesy A. Siemko
Failure modes:
  inter-turn short (fatal for magnet in case of quench)
  short to ground (prevent operation and require most probably a replacement of the damage magnet)
Notes: When do we break NbTi filaments due to energy depositions?

## Slide 8: Experimental plan
Insulation degradation due to temperature
  Heat stacks of cables in furnace (hours)
  Heat insulation by a short current pulse in a heater (ms)
Sc. strand degradation due to temperature
  Heat a single strand by a current pulse and measure critical current. (ms)
  Experiments with beam (all degradation mechanisms – μs to ms)
  Expose stacks of cables and strands to a proton beam, at room temperature.
  Expose stacks of cables and coils to a proton beam at cryogenic temperatures.
Nb-Ti strands (1 mm ø)
10 cm
Stack of 6 Nb-Ti cables
25 cm

## Slide 9: Degradation of insulation due to temperature
Cable stacks heated in furnace between 200 C and 600 C in an inert atmosphere.
Measurement of the breakthrough voltage cable to cable after heat treatment
Temperature profiles of the cable stacks during
the heat treatment in an oven filled with Argon
5 hours

## Slide 10: Experimental results
Side view of the cable stacks before and after the heat treatment with different peak temperatures
Results of the dielectric strength measurements
after heat treatments at different peak temperature
Significant degradation of polyimide insulation when heating > 400 C
Lowest breakthrough voltage considered as worst case scenario.

## Slide 11: Correlation of dielectric strength degradation and weight loss
A model of the weight loss model has been developed:
is the reaction rate
is the weight loss after a full degradation,
is the ideal gas constant,
is the temperature in Kelvin
, and are fitting parameters
Extrapolation from long heating time (hours) to short heating time (us, ms)
950°C heating for ms time scale is equivalent to heating at 500°C for several hours.

## Slide 12: Beam experiment at room temperature
In the HiRadMat facility shooting a 440 GeV proton beam on:
  LHC Nb-Ti Cable stacks to study the degradation of the insulation
  Nb-Ti and Nb3Sn strands to study the degradation of sc. properties
  Samples are within an inert atmosphere.
Nb-Ti & Nb3Sn strands
30 Nb-Ti cables
~ 5 cm

## Slide 13
Second Picture with the tank open
Experimental setup and peak temperatures
Nb-Ti cable stacks
in steels moulds
Nb-Ti and Nb3Sn strands fixed on a steel plate
Beam pulse list: 6 x 6x1011 protons, 6 x 1.3x1011 protons, 6 x 2.6x1012 protons
p+
230°C
250°C
70°C
180°C
220°C
200°C
150°C
6x1011 p
p+
630°C
725°C
150°C
510°C
675°C
630°C
410°C
2.6x1012 p
800°C – Nb3Sn
p+
460°C
450°C
110°C
320°C
410°C
370°C
285°C
1.3x1011 p
620°C - Nb3Sn

## Slide 14: Post irradiation analysis
From December 2016
High voltage tests on the cables stacks – degradation of insulation (CERN – b.112)
Magnetization measurements on the single strands – degradation of the sc. properties. (University of Geneva)

## Slide 15: Conclusions
The project aims to identify critical magnet component, to understand the damage mechanisms and to measure the damage limit of superconducting magnet components.
Furnace experiment show a clear degradation of the insulation above 400°C in the hours timescale
The beam experiment at room temperature had successfully been performed.
  Peak temperature of 750°C in cable stacks and 630°C/ 800°C in the strands.
  Analysis on the results on going. Measurements on the sample to be done in the coming months.
More experiments are planned:
  Current discharge experiments to measure degradation of insulation and critical current in the ms timescale – (end 2016/beginning 2017)
  Beam experiment at 4 K with coil samples (end 2017)

## Slide 16: Extra slides

## Slide 17: Superconducting magnets ? Instantaneous beam impact ?
LHC Nb-Ti magnets: Main Dipoles, Quadrupoles, Correctors… but also Nb3Sn
Instantaneous beam impact: ultra-fast beam losses in µs time (e.g. injection and extraction failure cases).
Despite efficient absorber, beam can impact sc. magnets leading to temperature rise and thermo-mechanical stresses.

## Slide 18: Example of failure cases - injection
B1 (inj)
B1 (circ)
Injection Kicker (MKI) kicks the circulating beam
Beam intensity : 2.2x1011 p per bunch (HL-LHC
Maximum energy density ~100 J/cm3 (> 100 K – include design margins) in separation dipole (D1)
A. Lechner et all, Protection of superconducting magnets in case of accidental beam losses during HL-LHC injection, In Proceedings of IPAC15

## Slide 19: Example of failure cases – extraction
Asynchronous beam dumps
Beam intensity : 2.2x1011 p per bunch (HL-LHC
Maximum energy density ~100 J/cm3 in Q5
B1
B2
B. Auchmann et all, Quench and Damage Levels for Q4 and Q5 Magnets near Point 6, CERN EDMS 1355063, 2014

## Slide 20: Known limits
Lower bound
Accidental beam losses during injection in 2011.
Peak energy density in D1 coils ~ 6 J/cm3
Upper bound
Disintegration of polyimide insulation foils for T > ~400°C
Melting of copper with energy densities of 6 kJ/cm3
Courtesy A. Lechner
D1
Q3
Q2
Q1
Beam

## Slide 21
    Current discharge (t~ 20 ms) in sc. strands to achieve peak temperature rise from 250°C to 1000°C
    Magnetization measurement on ~18 strands (before and after discharge)
    Experiment planned for December 2016
CLIQ, 40 mF
Nb-Ti strand
Degradation of sc. properties due to temperature - ms timescale

## Slide 22
Stack of cable with a steel strip inserted between cable.
Fast current discharge (~100 ms) in strip inducing a fast heat pulse into the insulation in inert atmosphere.
    Measure I and V during the discharge to deduce the temperature of the strip
High voltage tests after the discharge to measure the degradation of the insulation.
Degradation of insulation due to temperature - ms timescale

## Slide 23: Beam experiment in cryogenic environment
At the HiRadMat facility shooting a 440 GeV proton beam on cable stacks, strands and test coils.
  Cryogenic conditions (4.2K)
  On-line monitoring of the coils (electrical integrity and critical current)
Goals:
  Extend the results of the previous beam experiment to cryogenic temperature (LHC environment).
  Test on sample coils to investigate other damage mechanisms (mechanical stability, ...)
Liquid He
Instrumentation:
Voltage tabs, temperature probes, hall probes
p+
Insulation vacuum
Heater
Cable stacks
Test Coils
Support Table

## Slide 24: Cable stacks as pre-experiment for SextSc
The experiment at room temperature will give essential inputs to optimize the following experiment planned to be done at cryogenic temperature.
Simpler setup at room temperature.
Energy deposition in μs time scales and verification of damage models.
Optimization (number of shots and samples).
Extension to environment as in LHC (cryogenic) required.