## Slide 1: FCC protection studies within the EuroCirCol project
Marco Prioli, L. Bortot, M. Maciejewski, A. Fernandez
B. Auchmann, A. Verweij
CERN, TE-MPE

## Slide 2: EuroCirCol workshop 2016
7-9 November 2016, ALBA Synchrotron
Link to the EuroCirCol web page

## Slide 3: EuroCirCol project
WP1: management and coordination (M. Benedikt, CERN)
WP2: arc design (A. Chance, CEA)
WP3: experimental insertion region design (A. Seryi, UOXF)
WP4: cryogenic beam vacuum system (P. Francis, ALBA)
WP5: high-field accelerator magnet design (D. Tommasini, CERN)
  5.6: Devise quench protection concept (TUT, INFN, CERN)
Link to the EuroCirCol web page

## Slide 4: The FCC layout
From C. Cook, FCC week 2016 (link)
Half arc (L=8km)

## Slide 5: Dipole magnet designs
Cos-theta 14% LL, 1.9K
Block coil 14% LL, 1.9K
Common coil 14% LL, 1.9K
Cos-theta 18% LL, 4.2K
Block coil 18% LL, 4.2K
Common coil 18% LL, 4.2K

## Slide 6: Effect of load line margin and temperature
Chart: Critical current [A/mm2] as a function of peak field [T]
| 10 | 10.5 | 11 | 11.5 | 12 | 12.5 | 13 | 13.5 | 14 | 14.5 | 15 | 15.5 | 16 | 16.5 | 17 | 17.5 | 18 | 18.5 | 19 | 19.5
Jc (4.5) | 4862.8164 | 4436.6993 | 4043.0288 | 3678.8411 | 3341.5857 | 3029.0518 | 2739.3107 | 2470.6704 | 2221.6378 | 1990.8891 | 1777.2447 | 1579.6495 | 1397.1551 | 1228.9066 | 1074.13 | 932.1224 | 802.2436 | 683.9087 | 576.5817 | 479.7701
Jc (1.9) | 6310.4553 | 5825.153 | 5374.7185 | 4955.8858 | 4565.8471 | 4202.1717 | 3862.7416 | 3545.7005 | 3249.4124 | 2972.4286 | 2713.4597 | 2471.3532 | 2245.0752 | 2033.6941 | 1836.3677 | 1652.3324 | 1480.8929 | 1321.415 | 1173.3182 | 1036.0697
LL margin, 1.9K
LL margin, 4.2K

## Slide 7: Main achievements: cos-theta
Bladder & key configuration
Rectangular steel pad, cut vertically, 20-60 mm thick.
Circular iron yoke, cut at 45o, 133-175 mm thick.
Rectangular shaped steel pad and horizontal and vertical keys allow to decouple x and y component of pre-stress.
Courtesy of Barbara Caiffi. Link to the presentations

## Slide 8: Main achievements: block coil
= v20ar
margin drop
bore tip decrease
Courtesy of Clement Lorin. Link to the presentations

## Slide 9: Main achievements: common coil
Courtesy of Fernando Toral. Link to the presentations
We have studied different configurations of the ancillary coils.

## Slide 10: Main achievements: canted cos-theta
Courtesy of Bernhard Auchmann. Link to the presentations
Rendering taken from Berkeley Lab
Cos-theta can pack more x-section “turns” on the innermost layer.
CCT has to use higher currents to achieve similar ampere-turns.
CCT outer-layer conductor length grows with radial position.
CCT tilted-helix winding increases SC use by ~10%.
CCT has larger stored energy  needs more copper.
  Note the field pattern. CT field lines more compact  lower energy.
  Roughly same peak fields.

## Slide 11: Magnet protection
Circuit protection aspects
  Circuit protection @ FCC week 2016
  Circuit layouts for the latest magnet designs
The STEAM project
  New perspectives for circuit and quench simulations
  Main STEAM features
  First results of CLIQ simulations
Simulation of Transient Effects in Accelerator Magnets

## Slide 12: Magnet protection
Circuit protection aspects
  Circuit protection @ FCC week 2016
  Circuit layouts for the latest magnet designs
The STEAM project
  New perspectives for circuit and quench simulations
  Main STEAM features
  First results of CLIQ simulations
  Simulation of Transient Effects in Accelerator Magnets

## Slide 13: Circuit protection @ FCC week 2016*
Definition of the FCC powering sector (PS)
PC 1
PC 2
PS 1
PS 2
HalfArc 1
8km
PC 1
PS 1
Sector 1
3km
LHC
FCC
Description | LHC PS | FCC PS | FCC MiniArc | Units
Powering sector (PS) length | 3000 | 4000 | 3200 | [m]
Number of PS in the accelerator | 8 | 16 | 4 | -
Filling factor | 74% | 77% | 77% | -
Number of dipole magnets per PS | 154 | 215 | 172 | -
Inductance per PS | 15 | 272 | 218 | [H]
Stored energy per PS | 1 | 10 | 8 | [GJ]
20 PS in total
*Concepts for magnet circuit powering and protection (M. Prioli) (Link)

## Slide 14: Circuit protection @ FCC week 2016*
A
B
C
D
E
Option | τdischarge | Energy | EE position | Circuit complexity
A |  |  |  | 
B |  |  |  | 
C |  |  |  | 
D |  |  |  | 
E |  |  |  | 
Example for N=5
*Concepts for magnet circuit powering and protection (M. Prioli) (Link)

## Slide 15: Circuit protection @ FCC week 2016*
A string of magnets can always be protected, for any magnet design and given constraints, by adapting the number of circuits, so by subdividing a powering sector in multiple circuits
Magnets can be compared analysing the resulting circuit complexity
  Number of circuits N in one Powering Sector (PS)
  20N circuits for the entire machine
Example for N=5
*Comparison of magnet designs from a circuit protection point of view (A. Verweij)
(Link)

## Slide 16: New magnets parameters
 | Load line margin | Current @ Bnom [kA] | Differential inductance (2 apertures) [mH] | Stored energy @ Inom (2 apertures) [MJ]
Cos-theta 28b38 v.5 | 18% | 10.275 | 734 | 39
Cos-theta v22b | 14% | 11.23 | 566 | 38
Block coil v26cmag | 18% | 8.47 | 1265 | 45
Block coil v20ar | 14% | 10.99 | 571 | 36
Common coil v1h_intgrad | 18% | 9.025 | 1824 | 74
Common coil v1h2_1ac1 | 14% | 16.80 | 287 | 43
Canted cos-theta | 14% | 18 | 254 | 44
Cos-theta v22b
Block coil v20ar
Common coil v1h2_1ac1

## Slide 17: Circuits layouts for Cos-theta 18% LL*
N. of circuits per PS | 1 | 2 | 3 | 4 | 6 | 8
N. of circuits entire FCC | 20 | 40 | 60 | 80 | 120 | 160
Magnets per circuit | 215 | 108 | 72 | 54 | 36 | 27
Inductance per circuit [H] | 158 | 79 | 53 | 39 | 26 | 20
Stored energy per circuit [GJ] (<1.6) (>3) | 8.3 | 4.2 | 2.8 | 2.1 | 1.4 | 1.0
Ramp time [min] | 20 | 20 | 20 | 20 | 20 | 20
VPC [V] (<500) (>1000) | 1352 | 676 | 451 | 338 | 225 | 169
VFPA,max [kV] | 1.0 | 1.0 | 1.0 | 1.0 | 1.0 | 1.0
VFPA,max,fault [kV] | 3.3 | 2.6 | 2.4 | 2.3 | 2.2 | 2.2
τcirc [s] (<150) (>250) | 811 | 406 | 270 | 203 | 135 | 101
MIITS [A2s]*109 (<10) (>20) | 43 | 21 | 14 | 11 | 7 | 5
Abusbar [mm2], ΔT=300K | 550 | 390 | 310 | 270 | 220 | 190
*Comparison of magnet designs from a circuit protection point of view (A. Verweij)
(Link)

## Slide 18: Circuits layouts for Cos-theta 14% LL
N. of circuits per PS | 1 | 2 | 3 | 4 | 6 | 8
N. of circuits entire FCC | 20 | 40 | 60 | 80 | 120 | 160
Magnets per circuit | 215 | 108 | 72 | 54 | 36 | 27
Inductance per circuit [H] | 122 | 61 | 41 | 30 | 20 | 15
Stored energy per circuit [GJ] (<1.6) (>3) | 8.1 | 4.1 | 2.7 | 2.0 | 1.4 | 1.0
Ramp time [min] | 20 | 20 | 20 | 20 | 20 | 20
VPC [V] (<500) (>1000) | 1139 | 570 | 380 | 285 | 190 | 142
VFPA,max [kV] | 1.0 | 1.0 | 1.0 | 1.0 | 1.0 | 1.0
VFPA,max,fault [kV] | 3.3 | 2.6 | 2.4 | 2.3 | 2.2 | 2.2
τcirc [s] (<150) (>250) | 684 | 342 | 228 | 171 | 114 | 85
MIITS [A2s]*109 (<10) (>20) | 43 | 22 | 14 | 10 | 7 | 5
Abusbar [mm2], ΔT=300K | 550 | 390 | 320 | 270 | 220 | 190

## Slide 19: Circuits layouts for Block coil 18% LL*
N. of circuits per PS | 1 | 2 | 3 | 4 | 6 | 8
N. of circuits entire FCC | 20 | 40 | 60 | 80 | 120 | 160
Magnets per circuit | 215 | 108 | 72 | 54 | 36 | 27
Inductance per circuit [H] | 272 | 136 | 91 | 68 | 45 | 34
Stored energy per circuit [GJ] (<1.6) (>3) | 9.7 | 4.9 | 3.2 | 2.4 | 1.6 | 1.2
Ramp time [min] | 20 | 20 | 20 | 20 | 20 | 20
VPC [V] (<500) (>1000) | 1920 | 960 | 640 | 480 | 320 | 240
VFPA,max [kV] | 1.0 | 1.0 | 1.0 | 1.0 | 1.0 | 1.0
VFPA,max,fault [kV] | 3.3 | 2.6 | 2.4 | 2.3 | 2.2 | 2.2
τcirc [s] (<150) (>250) | 1152 | 576 | 384 | 288 | 192 | 144
MIITS [A2s]*109 (<10) (>20) | 41 | 21 | 14 | 10 | 7 | 5
Abusbar [mm2], ΔT=300K | 540 | 380 | 310 | 270 | 220 | 190
*Comparison of magnet designs from a circuit protection point of view (A. Verweij)
(Link)

## Slide 20: Circuits layouts for Block coil 14% LL
N. of circuits per PS | 1 | 2 | 3 | 4 | 6 | 8
N. of circuits entire FCC | 20 | 40 | 60 | 80 | 120 | 160
Magnets per circuit | 215 | 108 | 72 | 54 | 36 | 27
Inductance per circuit [H] | 123 | 61 | 41 | 31 | 20 | 15
Stored energy per circuit [GJ] (<1.6) (>3) | 7.8 | 3.9 | 2.6 | 1.9 | 1.3 | 1.0
Ramp time [min] | 20 | 20 | 20 | 20 | 20 | 20
VPC [V] (<500) (>1000) | 1124 | 562 | 375 | 281 | 187 | 141
VFPA,max [kV] | 1.0 | 1.0 | 1.0 | 1.0 | 1.0 | 1.0
VFPA,max,fault [kV] | 3.3 | 2.6 | 2.4 | 2.3 | 2.2 | 2.2
τcirc [s] (<150) (>250) | 674 | 337 | 225 | 169 | 112 | 84
MIITS [A2s]*109 (<10) (>20) | 41 | 20 | 14 | 10 | 7 | 5
Abusbar [mm2], ΔT=300K | 540 | 380 | 310 | 270 | 220 | 190

## Slide 21: Circuits layouts for Common c. 18% LL*
N. of circuits per PS | 1 | 2 | 3 | 4 | 6 | 8
N. of circuits entire FCC | 20 | 40 | 60 | 80 | 120 | 160
Magnets per circuit | 215 | 108 | 72 | 54 | 36 | 27
Inductance per circuit [H] | 392 | 196 | 131 | 98 | 65 | 49
Stored energy per circuit [GJ] (<1.6) (>3) | 16.0 | 8.0 | 5.3 | 4.0 | 2.7 | 2.0
Ramp time [min] | 20 | 20 | 20 | 20 | 20 | 20
VPC [V] (<500) (>1000) | 2952 | 1476 | 984 | 738 | 492 | 369
VFPA,max [kV] | 1.0 | 1.0 | 1.0 | 1.0 | 1.0 | 1.0
VFPA,max,fault [kV] | 3.3 | 2.6 | 2.4 | 2.3 | 2.2 | 2.2
τcirc [s] (<150) (>250) | 1771 | 886 | 590 | 443 | 295 | 221
MIITS [A2s]*109 (<10) (>20) | 72 | 36 | 24 | 18 | 12 | 9
Abusbar [mm2], ΔT=300K | 710 | 500 | 410 | 360 | 290 | 250
*Comparison of magnet designs from a circuit protection point of view (A. Verweij)
(Link)

## Slide 22: Circuits layouts for Common c. 14% LL
N. of circuits per PS | 1 | 2 | 3 | 4 | 6 | 8
N. of circuits entire FCC | 20 | 40 | 60 | 80 | 120 | 160
Magnets per circuit | 215 | 108 | 72 | 54 | 36 | 27
Inductance per circuit [H] | 62 | 31 | 21 | 15 | 10 | 8
Stored energy per circuit [GJ] (<1.6) (>3) | 9.2 | 4.6 | 3.1 | 2.3 | 1.5 | 1.1
Ramp time [min] | 20 | 20 | 20 | 20 | 20 | 20
VPC [V] (<500) (>1000) | 863 | 432 | 288 | 216 | 144 | 108
VFPA,max [kV] | 1.0 | 1.0 | 1.0 | 1.0 | 1.0 | 1.0
VFPA,max,fault [kV] | 3.3 | 2.6 | 2.4 | 2.3 | 2.2 | 2.2
τcirc [s] (<150) (>250) | 518 | 259 | 173 | 130 | 86 | 65
MIITS [A2s]*109 (<10) (>20) | 73 | 37 | 24 | 18 | 12 | 9
Abusbar [mm2], ΔT=300K | 720 | 510 | 410 | 360 | 290 | 250

## Slide 23: Circuits layouts for CCT 14% LL
N. of circuits per PS | 1 | 2 | 3 | 4 | 6 | 8
N. of circuits entire FCC | 20 | 40 | 60 | 80 | 120 | 160
Magnets per circuit | 215 | 108 | 72 | 54 | 36 | 27
Inductance per circuit [H] | 55 | 27 | 18 | 14 | 9 | 7
Stored energy per circuit [GJ] (<1.6) (>3) | 9.6 | 4.8 | 3.2 | 2.4 | 1.6 | 1.2
Ramp time [min] | 20 | 20 | 20 | 20 | 20 | 20
VPC [V] (<500) (>1000) | 819 | 409 | 273 | 205 | 136 | 102
VFPA,max [kV] | 1.0 | 1.0 | 1.0 | 1.0 | 1.0 | 1.0
VFPA,max,fault [kV] | 3.3 | 2.6 | 2.4 | 2.3 | 2.2 | 2.2
τcirc [s] (<150) (>250) | 491 | 246 | 164 | 123 | 82 | 61
MIITS [A2s]*109 (<10) (>20) | 80 | 40 | 27 | 20 | 13 | 10
Abusbar [mm2], ΔT=300K | 750 | 530 | 430 | 370 | 300 | 260

## Slide 24: Circuit protection aspects: conclusions
For all magnet designs:
  Reduction in the circuit complexity
  The layout with 6 circuits per powering sector fulfils the largest number of constraints
 | Cos-theta | Block coil | Common coil | Canted cos-theta
Circuit complexity |  |  |  | 
Circuit energy |  |  |  | 
Ramp-up, VPC |  |  |  | 
FPA, τcirc |  |  |  | 
FPA, MIITS |  |  |  | 

## Slide 25: Magnet protection
Circuit protection aspects
  Circuit protection @ FCC week 2016
  Circuit layouts for the latest magnet designs
The STEAM project
  New perspectives for circuit and quench simulations
  Main STEAM features
  First results of CLIQ simulations
  Simulation of Transient Effects in Accelerator Magnets

## Slide 26: Outlook for circuit and quench simulations
To understand if this proposal is feasible, circuit simulations are needed
  Quenching magnet
  CLIQ protection system
  Lumped element model of the other magnets in the chain
  Other components (e.g. Power Converter (PC), nonlinear switches)
  … Quench protection system, controller of Power Converter
CLIQ introduces a coupling between circuit and quench simulations
Lfilt
PC
Rfilt
Cfilt
REE
M1
M2
M18
M36
M35
M19
Mn
CLIQ
Example: magnets powered with Ncircuits per PS = 6

## Slide 27: Field-circuit coupling
PC
Rfilt
Cfilt
REE
M1
M2
M18
M36
M35
M19
Mn
CCLIQ
M
Cadence PSpice
Circuit model
2D Electro-thermal Field model
Lfilt
I
φ, R
L1
ΔU1
R1
L2
ΔU2
R2

## Slide 28: Field-circuit coupling
Coupling scheme: Waveform Relaxation – Gauss-Siedel scheme
Advantages
  Multiple solvers with individual adaptive time stepping
  No assumptions about current decay
  No assumptions about field and inductance evolution
  Convergence error under control
Circuit solver
Field solver
t + Δt
tend
t
* Courtesy of M. Maciejewski
*
φ, R
I
φ, R
I

## Slide 29
Field and Circuit automated workflows
400 FEM domains* for common coil
User’s Input Magnet features
FEM model
Solver
(COMSOL)
Material Properties C-functions
API
Model Builder
Potentially 5000 elements for circuit (slide 15)
User’s Input List of elements
Circuit model
Solver (PSpice)
Model Builder
Circuit Libraries
Netlist
* Element with assigned geometry, materials and physical laws

## Slide 30
2D Electrothermal
Electrical Circuit
Simulations Coupling Interface (Java / MpCCI)
1D Electrothermal
2D Mechanical
Power Converter Controller
Network solvers
Motivation for simulation coupling:
Multi-physics
  Multiple coupled physical domains
Multi-rate
  Time constants ranging from μs to minutes
Multi-scale
  Geometrical dimensions differ by several orders of magnitude μm to km
PSpice
PSIM
  FEM solvers
PID
yref
-
+
STEAM architecture

## Slide 31: CLIQ simulations Cos-theta v22b
ltp [mm] | 14
ρ0 [ohm*m] | 1.334e-10
ρ1 [ohm*m/T] | 4.2e-11
L1
ΔU1
R1
L2
ΔU2
R2
CCLIQ
PC
CCLIQ=20 mF, UCLIQ=2 kV

## Slide 32: CLIQ simulations Cos-theta v22b
Coupling losses [W/m3]
Current [A] and resistance [Ω] evolution
CCLIQ=20 mF, UCLIQ=2 kV
−
+
+
−
+
+
−
−

## Slide 33: CLIQ simulations Cos-theta v22b
Voltage to ground [V]
Temperature [K]
Hot-spot 312 K
Peak voltage to ground @ 120ms
CCLIQ=20 mF, UCLIQ=2 kV

## Slide 34: CLIQ simulations Block coil v20ar
Coupling losses [W/m3]
Current [A] and resistance [Ω] evolution
CCLIQ=20 mF, UCLIQ=2 kV
−
+
+
−

## Slide 35: CLIQ simulations Block coil v20ar
Hot-spot 338 K
Peak voltage to ground @ 110ms
Voltage to ground [V]
Temperature [K]
CCLIQ=20 mF, UCLIQ=2 kV

## Slide 36: CLIQ simulations Common coil v1h2
Coupling losses [W/m3]
Current [A] and resistance [Ω] evolution
2 × CCLIQ=20 mF, UCLIQ=2 kV
−
+
+
−
−
−
−

## Slide 37: CLIQ simulations Common coil v1h2
Hot-spot 354 K
Peak voltage to ground @ 130ms
Voltage to ground [V]
Temperature [K]
2 × CCLIQ=20 mF, UCLIQ=2 kV

## Slide 38: Conclusions and future work
A new tool for circuit and quench protection simulations
First fully consistent CLIQ simulations
Flexibility enables study of complex circuits/magnets without additional effort
Next steps
  Analyse a magnet quench in the full FCC circuit
  Test new ideas for magnet powering: e.g. separate circuits for inner and outer layers, or subdivision diodes
  Build two apertures model for all magnet designs
  Optimize CLIQ configuration considering different current levels
  Include heaters model
  Share the tool with TAMPERE colleagues