## Slide 1: CLICpix2 and C3PD Bump Pads
E. Santin, P. Valerio, I. Kremastiotis &
R. Ballabriga Sune
CLICdp Vertex Meeting
CERN, February 12th 2016

## Slide 2: Motivation
Define the bump pads layout for the C3PD chip (based on the CLICpix2 bump pads)
Summarize (and get feedback of, if any) the final bump pads layouts for both chips: CLICpix2 & C3PD

## Slide 3: Topological cross-section of 1st prototype
C3PD bump pad
CLICpix1 bump pad
via
Ctotal
Cp1
Cp2
Cp3
Cp4
Cpx = undesirable caps
 crosstalks
Aim: Maximize Ctotal and minimize Cpx

## Slide 4: An approximate study…
Assume M6 of TSMC 65nm as the C3PD bump pad
 some limitations wrt the actual scenario:
Different dielectric height
Different dielectric material
Different (M6-approximated) C3PD pad thickness
 “absolute” values shown next do not match the reality
AP layer of TSMC 65nm as the CLICpix2 bump pad
ASSUMPTIONS
TSMC 65nm cross-section
Ctotal
M6
AP

## Slide 5: Accurate 3D field solver
layout
Calibre xACT 3D
Extracted parasitics

## Slide 6: Coupling capacitances without GRs
2,2
2,1
2,3
1,2
1,1
1,3
3,2
3,1
3,3
C2,2BOTtoTOP =11.5 fF
C2,2BOTto2,1BOT = 0.14 fF
C2,2BOTto2,3BOT = 0.12 fF
C2,2BOTtoOTHERS < 0.07 fF
15µm
15µm
C2,2BOT
C2,2TOP
Without guard rings (GRs), there are capacitive couplings from C2,2BOT (i.e. C3PD bump pad) to all other bump pads (i.e. adjacent C3PD and CLICpix2 pads). The couplings to the CLICpix2 pads are, however, very small.
create signal crosstalks
we want to minimize this phenomenon
C3PD
CLICpix2

## Slide 7: Coupling capacitances with GRs
2,2
2,1
2,3
1,2
1,1
1,3
3,2
3,1
3,3
C2,2BOTtoTOP =11.2 fF
C2,2BOTtoVSSA = 2.5 fF
15µm
15µm
2µm
4µm
4µm
With guard rings (GRs) around the C3PD bump pads, the capacitive coupling from C2,2BOT to other adjacent bump pads are negligible. On the other hand, there is a fixed capacitance between the pads and the analog ground, Vssa, which is not a problem.
not a problem
Guard rings are a good solution to minimize undesirable crosstalks!

## Slide 8: Final CLICpix2 bump pads layout
Bump pad size is 240 µm2
Vias adjacent to the bump pad openings to comply with foundry DRC rules
12µm
14µm
25µm
22.5µm
bump pad
via
8µm
10µm
6µm

## Slide 9: Final C3PD bump pads layout
15µm
15µm
2µm
4µm
25µm
bump pad
guard ring
Bump pad size is about 15 x 15 µm2
Guard rings around the bump pads are connected to the same low-noise, low-impedance voltage (i.e. Vssa) and they minimize inter-pad (capacitive) coupling

## Slide 10: Conclusion
CLICpix2 bump pad final size is imposed by the power distribution grid and technology constraints (i.e. via)
C3PD bump pad final size is imposed by the “shielding” guard rings (to minimize crosstalks)
Open question: Is it possible to avoid the passivation layer on the C3PD chip to increase Ctotal (i.e. the intended coupling capacitance between C3PD and CLICpix2 bump pads)?

## Slide 11: Thank you for your attention!

## Slide 12: Backup slides

## Slide 13: Capacitance between two plates
http://maxwell.ucdavis.edu/~electro/dc_circuits/images/cap_fields.jpg
Ctotal = Carea + Cfringe
Ctotal
Total capacitance is a result of two components: area capacitance, Carea, and fringe capacitance, Cfringe
Question: Which one of the two dominates in the CLICpix2 and C3PD bump pads arrangement?

## Slide 14: Extracted coupling capacitances (using TSMC 65nm back-end layers as an approximation)
Ctotal=15.1 fF
Ctotal=10.7 fF (-29%)
Ctotal=16.3 fF (+8%)
CLICpix2 bump pad vs three C3PD bump pad layouts
Case 2 should favor the fringe capacitance component, but since the Ctotal is smaller than the other two cases it tells us that the area capacitance component dominates in these three scenarios
  But, do not ignore the analysis limitations mentioned on slide 4
Case 1
Case 2
Case 3