## Slide 1
Conceptual Design Review of the
Magnet Circuits for HL-LHC
21-23 March 2016 , CERN
SC Links
A. Ballarino
21/03/2016

## Slide 2
Contributions from:
WP6 contributors:
S. Giannelli, G. Montenero, A. Jacquemod, J. Hurte, R. Betemps, B. Bordini and V. Parma (CERN)
Y. Yang and the team at the Univ. of Southampton
LHC Cryogenics:
U. Wagner and S. Claudet (CERN)
Integration studies:
P. Fessia and S. Maridor (CERN)

## Slide 3
System overview
Cryogenic layout
Electrical components
Integration
Protection
Milestones and schedule
Conclusions
A. Ballarino, 21/03/2016

## Slide 4
System overview
Cryogenic layout
Electrical components
Integration
Protection
Milestones and schedule
Conclusions
A. Ballarino, 21/03/2016

## Slide 5
A. Ballarino, 21/03/2016
Machine Interface Cryo-assembly - DF
SC Link - DSH
Interconnection Cryo-assembly - DFH
SC Current Leads
Cold Powering System (WP6)
Function: transfer the current from the
power converters to the Hi-Luminosity magnet circuits
Integration in LHC: during LS3
Nb-Ti
Bus-Bar
SC Link: a component of
the Cold Powering system

## Slide 6
A. Ballarino, 21/03/2016
Distribution Feedbox and current leads in LHC Tunnel

## Slide 7
A. Ballarino, 21/03/2016
Cold Powering System WP6 - WBS
WP9
WP7
WP6

## Slide 8
Hi-Lumi Triplets and Matching Section
+ Q5 and Q6
A. Ballarino, 21/03/2016

## Slide 9
Baseline Powering Layout: MQXF quadrupoles
18 kA/20 V
18 kA/20 V
 0.12 kA/  10 V
 2 kA/  10 V
All other magnets are individually powered
Trim
Trim
Proposals for different powering layouts being discussed, i.e. MQXF quadrupole magnets all in series and D1 in series with D2, can/will be taken into account by the Cold Powering System (see next slides)
A. Ballarino, 21/03/2016

## Slide 10
Changes in operating current (2015)
Q1/Q3 – Q2a/Q2b
D2, D1
Q4, Q5, Q6
Orbit correctors Q3 and Q2, Trim on Q3
Orbit correctors D2 and Q4
CP,
Correctors Q5 and Q6, Trim on Q2
20 kA
Q4 16 kA
2 kA
DC Current  70 kA per IP
NB 2015 Baseline
A. Ballarino, 21/03/2016

## Slide 11
A. Ballarino, 21/03/2016
Number of Leads and of SC cables, Current Rating
Triplets, D1 and CP – per IP Side
Matching Sections – per IP Side
6  18 kA
13  2 kA
 0.2 kA
1 0.12 A
38 Units
268.5 kA
2  13 kA
12  6 kA
16  0.6 kA
18  0.12 kA
48 Units
254.8 kA
Per IP side : 2123 kA , 86 Leads/SC Cables
Hi-Luminosity Upgrade: 2492 kA, 344 Leads/SC Cables
Type | N_IPside
18 kA | 6
13 kA | 4
6 kA | 12
2 kA | 13
0.6 kA | 16
0.2 kA | 18
0.12 kA | 19
NB 2015 Baseline

## Slide 12
Number of Cold Powering Systems
Two Cold Powering Systems per IP Side at LHC P1 and P5 (one for the Matching Section and one for the Triplets + D1)
 eight Cold Powering Systems in total
Two types of Cold Powering Systems (two powering
layouts, one for MSs and one for Triplets):
2 Types of DF Cryo-assemblies (DFX and DFM)
2 Types of Superconducting Links (DSHX and DSHM)
2 Types of DFH Cryo-assemblies (DFHX and DFHM)
Series of leads at different current ratings
A. Ballarino, 21/03/2016

## Slide 13
Inputs for design of Cold Powering System
SC cables and current leads designed for operating in DC mode at the rated (maximum) current of the associated power converters
Insulation voltages to ground and between electrical components of  1 kV -1.5 kV in nominal operating conditions
Capability of enabling discharge of the magnet circuits with time constants of 3 s (MQXF circuit)
CLIQ, if used for magnets protection, fed by its own system – to avoid EM coupling issues in the SC cables
In case of quench/resistive transition of any component of the Cold Powering System, discharge of the circuit with time constants in the range from 3 s to 6 s
A. Ballarino, 21/03/2016

## Slide 14
Cold Powering System - Concept
1. Current leads
3. Electrical interconnection box
2. Superconducting link
Concept initially developed for LHC P7 and
proposed also for LHC P1 and P5
MgB2
HTS
A. Ballarino, 21/03/2016

## Slide 15
System overview
Cryogenic layout
Electrical components
Integration
Protection
Milestones and schedule
Conclusions
A. Ballarino, 21/03/2016

## Slide 16
T < 20 K
THe < 35 K (Mixing of He gas)
Qcold_mass  0.3 W/m
Qth_shield  2.5 W/m
TLead = 40 K-50 K
LHe
THe = 20 K
Room Temperature
MgB2
Bi-2223 or YBCO
1
2
3
Cryogenic layout : present baseline
A. Ballarino, 21/03/2016

## Slide 17
T < 20 K
THe < 35 K (Mixing for LHC P1 and P5)
Qcold_mass  0.3 W/m
Qth_shield  2.5 W/m
TLead = 40 K-50 K
LHe
THe = 20 K
Room Temperature
MgB2
Bi-2223 or YBCO
1
2
3
Under evaluation
Shorter superconducting Lines (from  300 m to  100 m):
Possible elimination of thermal shield cooling (and mixing)
A. Ballarino, 21/03/2016

## Slide 18
U. Wagner et al.
CERN-ACC-2014-0065 (2014)
A. Ballarino, 21/03/2016
LHe from QRL in the tunnel
GHe at 20 K from line D
Cryogenic layout : present baseline

## Slide 19
System overview
Cryogenic layout
Electrical components
Integration
Protection
Milestones and schedule
Conclusions
A. Ballarino, 21/03/2016

## Slide 20
Superconducting Material
Use of Nb barrier
wire = 1 mm
37 MgB2 filaments
Twisted filaments (LT=100 mm)
eq_MgB2 = 56 m
ACu  5 % Awire (th=30 m)
Cu plating
Sn coating of Cu surface
Ic(25 K, 0.9 T) > 186 A
3.60.67 mm2
Product commercial at Columbus when the
project started: MgB2 tape
Launched procurement of 80 km of wire
Unit lengths  500 m
60 km at CERN
20 km to be delivered before end of April 2016
Launched development of MgB2 round wire
A. Ballarino, 21/03/2016

## Slide 21
Hi-Lumi Triplets and D1
ext  65 mm
Mass  11 kg/m
Superconducting Cable Assembly
ext  220 mm
A. Ballarino, 21/03/2016

## Slide 22
A. Ballarino, 21/03/2016
Hi-Lumi Triplets and D1
ext  65 mm
Mass  11 kg/m
Superconducting Cable Assembly
Six high-current (18 kA) cables:
MQXF and D1

## Slide 23
A. Ballarino, 21/03/2016
H  4 m
L = 20 m
ext = 163 mm
Test station at CERN

## Slide 24
Imax Power Converter
I = 20 kA
T = 24 K
Bp = 1 T
=19.5 mm
Hcable =3.7 H
Record in current for MgB2
High Current Cable
A. Ballarino, 21/03/2016

## Slide 25
Thermal stability and quench studies
At 3 kA NPVZ = 7.3-12.6 cm/s for T = 5K -25 K
Measurements @ CERN
Measurements @ SOTON
Twisted-Pair MgB2 Cables
Study for LHC P7
J = Normalized Current Density
Thermal stability
Quench propagation
in He gas
4 Joule !
A. Ballarino, 21/03/2016

## Slide 26
Measurement performed at 15 K, 3000 A
Max hot-spot temperature reached Ths~340 K with no degradation of cable performance
25 K, 3 kA, 100 mV detection threshold  15 MIITS of “quench capital” before detection  final Tmax  150 K within 3 s
Effect of radial quench propagation among cables
Quench propagation and thermal coupling
Quench Propagation in Helium-Gas-Cooled MgB2 Cables, S. Giannelli , G. Montenero, A. Ballarino , IEEE Febr. 2016

## Slide 27
System overview
Cryogenic layout
Electrical components
Integration
Protection
Milestones and schedule
Conclusions
A. Ballarino, 21/03/2016

## Slide 28
Integration baseline till mid 2015
 80 m
LHC P1

## Slide 29
Integration: new baseline
Point 1
DFH
DFH
DFH
DFH
S. Maridor, CERN
Presentation by P. Fessia on Friday, WP6 Session
A. Ballarino, 21/03/2016

## Slide 30
Integration of Cold Powering System
Leads assembled and tested before integration
SC Link assembled and tested before integration
    Bending radius  1.5 m
      300 mm
    DF and DFH cryostats assembled and tested before integration
A. Ballarino, 21/03/2016
Splicing in the tunnel

## Slide 31
A. Ballarino, 21/03/2016
System overview
Cryogenic layout
Electrical components
Integration
Protection
Milestones and schedule
Conclusions

## Slide 32
Protection
Room Temperature
MgB2
Bi-2223 or YBCO
1
2
3
Resistive part of each lead
Superconducting part of each lead
Superconducting cables in the
link (each cable)
LHe
Joints MgB2/Nb-Ti
Joints MgB2/HTS
A. Ballarino, 21/03/2016

## Slide 33
A. Ballarino, 21/03/2016
Resistive part of each lead
As for LHC: voltage detection. Detection threshold  100 mV
Long integration times permitted
Superconducting part of each lead
As for LHC: voltage detection. Detection threshold  1-5 mV
Integration times of  100 ms (depending on final choice of material)
Superconducting cables in the link cryostat
Long ( 100 m) cables. Work on-going. Aiming at detection thresholds in the range from 50 mV-100 mV, with  of the circuits of up to 3 s
Protection

## Slide 34
A. Ballarino, 21/03/2016
Protection
Electrical joints (MgB2 to Nb-Ti and HTS to MgB2)
Required availability of individual signals for post-quench analysis (need to identify location - and circuit – for interventions in case of performance degradation).
The design of the cold powering system takes as boundary condition the need of accessing and repairing individual joints at the level of the electrical interconnection box (MgB2-HTS) or at the magnets interface (MgB2 – Nb-Ti)

## Slide 35
Temperature Interlocks
Room Temperature
MgB2
Bi-2223 or YBCO
1
2
3
LHe
Joints MgB2/Nb-Ti
Joints MgB2/HTS
Joint RT Cables/Lead
As in the LHC
Warmer end of HTS in each Lead
As in the LHC (cryo)
Warmer end of MgB2 cable (cryo)
A. Ballarino, 21/03/2016

## Slide 36
System overview
Cryogenic layout
Electrical components
Integration
Protection
Milestones and schedule
Conclusions
A. Ballarino, 21/03/2016

## Slide 37
A. Ballarino, 21/03/2016
Till beg. 2018: Construction and test of prototype Cold Powering Systems (Phase 1)
      80 m long SC Link, horizontal test in SM-18 (Triplets)
      80 m long SC Link, horizontal test in SM-18 (MSs)
2018-2021: Series production (Phase 2)
2021-2023: Test of Series production (Phase 3)
Program and schedule
From Cost & Schedule Review, March 2015

## Slide 38
A. Ballarino, 21/03/2016
From Cost & Schedule Review, March 2015
Prototype production

## Slide 39
First installation and test: a pair of 18 kA leads, full SC Link
MgB2 wire procured
MgB2 cabling: DO being prepared for cabling in industry
HTS cables procured
SC Link cryostat – 60 m long - being procured (DO issued, received offers from four companies)
Leads: internal production at CERN in the Main Workshop (together with production of lead for SM-18 test stations). DO for manufacturing of two 18 kA components launched
DFH cryostat: design completed. Production launched in Main Workshop
A. Ballarino, 21/03/2016
Prototype production - by end 2016

## Slide 40
From Cost & Schedule Review, March 2015
A. Ballarino, 21/03/2016
Series Production
Components for String
End of production
Delivery of components
304 units
 3000 km
304 unit lengths
8 units
8 SC Links
8+8 Cryo-Modules
FC Dec 2017
FC March 2018
FC March 2018
FC Dec 2017
FC June 2018

## Slide 41
A. Ballarino, 21/03/2016
Procurement strategy
Contracts:
  Procurements based on build to print CERN design: Current leads, SC Cables (as for LHC)
  Procurements based on technical specification: MgB2 and HTS conductor (as for LHC)
  Procurement based on technical specification: Cryostat of SC Link (DSH)
  Integration of SC cables in DSH cryostat: in industry or at CERN
  Procurement of sub-components with in-house cryostating assembly: DFH and DF cryo-assemblies

## Slide 42
A. Ballarino, 21/03/2016
Conclusions
Significant activity (design , test, procurement,…) made/being made on the design/test of the Cold Powering system for Hi-Lumi (Triplets and D1)
First prototype system planned to be available at CERN by end 2016
Detailed study of interfaces in tunnel to be launched as well as integration of the system in the tunnel
Needed “final” circuits configuration (voltages, time constants,..) for definition of system and validation of the on-going development/test program

## Slide 43
Thanks for your attention !