## Slide 2: SEY meeting: SPS-aC activities
By M. Van Gompel

## Slide 3
Overview
Introduction
  Magnets to coat in situ
Cathodes
  MBB
  QF
Quality assurance
  Before coating
  During coating
  After coating -> SEY
Future activities

## Slide 4
Overview
Introduction
  Magnets to coat in situ
Cathodes
  MBB
  QF
Quality assurance
  Before coating
  During coating
  After coating -> SEY team
Future activities

## Slide 5
Introduction: Magnets to coat in situ
Low SEY:
Secondary
Electron
Yield

## Slide 6
Cathodes: MBB cathode
Main train is 2 m
Robust and easy to repair/assemble
Coat 2 MBB dipoles in series (13.28 m): Total cathode length of 13.43

## Slide 7
QF cathode
Follows contour of QF tube surface
Wider cathode since larger surface needs coating
Triangular cells
1.7 meter cathode (2 trains)

## Slide 8
Introduction: Magnets to coat in situ

## Slide 9
QA: SEY examples
First test of 2 MBB tubes in series with pumping group on right side
4.5 hour coating
Left (13.2 m)
Middle (6.6 m)
Right (0 m): injection
and pumping

## Slide 10
Left (13.2 m)
Middle (6.6 m)
Right (0 m): injection
and pumping
QA: SEY examples
First test of 2 MBB tubes in series with pumping group on right side
24 hour coating

## Slide 11
Introduction: Magnets to coat in situ

## Slide 12
QA: SEY examples
First test of coating a QF tube
24h coating

## Slide 13
QA: SEY examples
First test of coating a QF tube
24h coating
Middle (SEM: 415±8 nm)
Edge (SEM: 205±65 nm)

## Slide 14
Future activities with support from you
Coat 2 MBB dipoles in series
Coat a QF quadrupole
Optimise deposition time of MBB and QF
Coat MBB by hollow cathode sputtering with triangular cells
Help with EYETS!
XPS analysis on Ozone etched samples

## Slide 15
Risk assessment
After coating ( endoscope + IR)
  Sooth
  Peel off
  SEYMBB < 1.10 and SEYQF< 1.05
  Inhomogeneous coating (Discoloration, transverse thickness variations, uncoated regions)

## Slide 16
Future activities with support from you
Coat 2 MBB dipoles in series
Coat a QF quadrupole
Optimise deposition time of MBB and QF
Coat MBB by hollow cathode sputtering with triangular cells
Help with EYETS!
XPS analysis on Ozone etched samples