## Slide 1: Task 5.3: Develop dipole magnet cost model: Distribution of the work and status
D. Schoerling
February 19th, 2016

## Slide 2
Distribution of the work
CERN | CIEMAT | CEA
Coordination Parameter studies Extrapolating of cost from LHC magnet cost Scaling for cos-theta (see this presentation + aperture vs cost) | Analytical model of a “typical” FCC-hh high-field magnet (cost of individual components as a function of magnet size & design, cost of conductor as a function of magnet design relevant input parameters (Cu/Non-Cu, diameter, etc.)) Scaling for common-coil | Assembly cost Scaling for block design

## Slide 3
Status - Introduction
Goal: Provide preliminary estimates of the cost of the dipole magnets as a function of field and temperature based on cross-sections scaled from the EuroCirCol 16 T dipole design and from LHC magnet cost
Reference parameters: 50 mm aperture, 4578 magnets, 14.3 m long, 16 T

## Slide 4
Cost of magnet
Cost of LHC dipole magnet taken as reference
LHC dipole cost was around 1 MCHF/dipole, 2000 (around 660 kEUR/dipole, 2000).
The conductor cost was around 200 kEUR/dipole, 2000
Assuming 2% inflation over 16 years for the dipoles one finds 900 kEUR/dipole, 2015
The cost of the LHC dipole without conductor is 630 kEUR/dipole, 2015
Manufacturing process involves more steps due to heat treatment, different insulation technique, etc., but number of units is larger (detailed study started with CEA & CIEMAT)

## Slide 5
Cost of conductor
Target cost for FCC is set to 5 EUR/kA.m at 16 T and 4.2 K (CERN-ACC-2015-0021)
With Jc(4.2 K, 16 T) = 1500 A/mm2 and Cu/Non-Cu = 1:1 => 500 EUR/kg
Remark: considering what above, the Cu placed in the conductor becomes expensive!
Source:
Ian Pong (ipong@lbl.gov), Dan Dietderich, Lance Cooley, Arup Ghosh: Cost and Performance of Nb3Sn for the Next Big Project

## Slide 6
Estimate of conductor amount
Assumptions:
Cos-theta magnet based on a schematized EuroCirCol INFN design (two double pan-cake, two-layer grading), simplified for the purpose of this study
Jcu ≤ 1200 A/mm2 (magnet protection at short sample) and Cu/Non-Cu ≥ 1:1(optimized strand production)
Field quality (b3 ≤ 100 units), non-optimized, no insulation, NOGRAD, LSELF
Cable without keystoning, 0% degradation
Calculation of required conductor mass for FCC-hh: 2 x Area x 140 dm/unit x 4578 unit x 8.7 kg/dm3

## Slide 7
Conductor Jc-fit
Chart: B in T
Where:
with Bp peak field on the conductor
Tc0 = 16 K, Bc20 =29.4 T, α = 0.96, C0 = 270 kA/mm2 T.
Cable degradation: 0%.

## Slide 8
Conductor amount vs field @ 1.9 K
Conductor amount is sensitive to the operational field and margin!
Chart: Temperature 1.9 K
| 16 | 15.600000000000001 | 15.12 | 13.92 | 13.12 | 12.08
20% | 12399.9177 | 10846.443 | 9349.8435 | 6759.232 | 5478.9815 | 4353.7439
15% | 12399.9177 | 10846.443 | 9349.8435 | 6759.232 | 5478.9815 | 4353.7439
10% | 12399.9177 | 10846.443 | 9349.8435 | 6759.232 | 5478.9815 | 4353.7439
 | 15 T | 16 T
10% | 6 | 7
15% | 7 | 9
20% | 9 | 12
Conductor amount in kt

## Slide 9
Conductor amount vs field @ 4.2 K
Conductor amount is very sensitive to the operational field and margin!
kt | 15 T | 16 T
10% | 7 | 10
15% | 10 | 16
20% | 15 | >25
Chart: Temperature 4.2 K
| 15.52 | 15.040000000000001 | 14.719999999999999 | 14.32 | 13.92 | 13.280000000000001 | 12.240000000000002
20% | 20381.4098 | 15524.7103 | 12094.3527 | 10413.7451 | 9078.8497 | 6926.5122 | 5376.3831
15% | 20381.4098 | 15524.7103 | 12094.3527 | 10413.7451 | 9078.8497 | 6926.5122 | 5376.3831
10% | 20381.4098 | 15524.7103 | 12094.3527 | 10413.7451 | 9078.8497 | 6926.5122 | 5376.3831
Conductor amount in kt

## Slide 10
Conductor amount vs field
Assuming the copper in excess of 1:1 can be added for the material price of copper, savings can be achieved
Chart: 4.2 K
| 19.399999999999999 | 18.8 | 18.399999999999999 | 17.899999999999999 | 17.399999999999999 | 16.600000000000001 | 15.3
Cable mass | 20381.4098 | 15524.7103 | 12094.3527 | 10413.7451 | 9078.8497 | 6926.5122 | 5376.3831
Non-Cu/Cu 1:1 | 18949.492 | 13790.5731 | 10523.0347 | 8787.7823 | 7576.6742 | 5303.895 | 3619.9418
Chart: 1.9 K
| 20 | 19.5 | 18.899999999999999 | 17.399999999999999 | 16.399999999999999 | 15.1
Cable mass | 12399.9177 | 10846.443 | 9349.8435 | 6759.232 | 5478.9815 | 4353.7439
Non-Cu/Cu 1:1 | 10344.6026 | 9006.3617 | 7288.9524 | 4857.8147 | 3457.1225 | 2379.8385
Ex: For a magnet with an operating field of 16T with 15% of margin around 2000 t of conductor cost (~25%) can be saved if the Non-Cu/Cu is limited to 1:1.
Ex: For a magnet with an operating field of 16T with 10% of margin around 1500 t of conductor (~15%) can be saved if the Non-Cu/Cu is limited to 1:1.

## Slide 11
Conductor amount vs operating temperature
We assume the enthalpy margin is meaningful to compare the margin to quench
In terms of enthalpy margin 10% on the load at 4.2 K corresponds to ~15% at 1.9 K
The same cross section with a margin on the loadline of 10% at 4.2 K gives a margin of 18% at 1.9 K (due to the different critical curves)
Under these assumptions we gain ~3% of margin on the loadline from 4.2 K to 1.9 K or with the same margin we can gain some conductor mass
Chart: Operational field in T
| 17 | 16.574999999999999 | 16.064999999999998 | 14.79 | 13.939999999999998 | 12.834999999999999
1.9 K | 12399.9177 | 10846.443 | 9349.8435 | 6759.232 | 5478.9815 | 4353.7439
4.2 K | 20381.4098 | 15524.7103 | 12094.3527 | 10413.7451 | 9078.8497 | 6926.5122 | 5376.3831

## Slide 12
Chart: 16 T with 10% margin
| 4.2 | 4.5 | 4.7 | 4.9000000000000004
 | 10413.7451 | 10879.899 | 11682.8436 | 12441.1801
Depending on the cooling scenario the temperature may be 4.7 K (instead of 4.2 K)
Keeping the same margin at 4.7 K would require more conductor than at 4.2 K
Going from 4.2 K to 4.7 K increases the required amount of conductor by ~1300 t (~650 MUSD).
Comparing 1.9 K to 4.7 K makes a difference in the range of 1 GUSD
Conductor amount vs operating temperature

## Slide 13
Total cost of FCC-hh dipoles
FCC with LHC magnet cost without conductor: 630 kEUR/unit x 4578 unit= 3000 MEUR
Conductor for 16 T and baseline margin at 4.2 K or 1.9 K ~10000 t
Conductor for 15 T and baseline margin at 4.2 K or 1.9 K ~7000 t
There is a potential to save around 1 GEUR by replacing “expensive” copper in the SC strand through “cheap” pure-copper strands or a copper jack
Scenario 1 (conductor cost 500 EUR/kg):
FCC-hh 16 T: 8000 MEUR
FCC-hh 15 T: 6500 MEUR
Scenario 2 (conductor cost 800 EUR/kg):
FCC-hh 16 T: 11000 MEUR
FCC-hh 15 T: 8600 MEUR

## Slide 14
Total cost of HE-LHC dipoles
Scenario 1 (conductor cost 500 EUR/kg):
16 T: 2200 MEUR
15 T: 1800 MEUR
Scenario 2 (conductor cost 1000 EUR/kg):
16 T: 3500 MEUR
15 T: 2700 MEUR

## Slide 15: Conclusion
The difference in cost of operating at 1.9 K or 4.7 K is ~1 GEUR
Operating at 15 T instead of 16 T represents a cost reduction of ~1.5 GEUR
Margin is very expensive especially at 4.2 K
  5% (10%->15%) margin at 4.2 K => 40% more conductor cost (~ 3 GEUR)
  5% (15%->20%) margin at 1.9 K => 25% more conductor cost (~ 1.5 GEUR)
Replacing “expensive” copper in the SC strand through “cheap” pure-copper strands or a copper jack may save ~1 GEUR
All above if we can achieve a target cost for the conductor of 500 EUR/kg