## Slide 1: New Cross-section and its rationale
Emelie Nilsson and Susana Izquierdo Bermudez
With acknowledgement to:
C. Loeffler, F. Savary, G. de Rijk, J.C. Perez, L. Bottura, E. Todesco,
B. Bordini, J. Fleiter, M. Karppinen and D. Smekens.

## Slide 2: Need for new design
Performance degradation of PIT conductor during cabling.
[Talk by B. Bordini: CERN Superconductor and cable design and performance]
For LS3: New PIT cable geometry needed to reduce critical current degradation.
Thin edge thickness critical for conductor performance.
Before heat treatment | Bare thickness in (mm) | Bare mid- thickness (mm) | Bare thickness out (mm) | Bare width (mm) | Keystone angle (deg.) | Ic degradation
First Gen. Design | 1.149 | 1.250 | 1.351 | 14.7 | 0.79 | 6-10%
Option 1 | 1.206 | 1.270 | 1.334 | 14.7 | 0.50 | <5%
Option 2 | 1.199 | 1.250 | 1.301 | 14.7 | 0.40 | <5%
Option 3 | 1.186 | 1.250 | 1.314 | 14.7 | 0.50 | ~5%
interpolated value
(to be confirmed)
Notes: Include estimates on cable degradation

## Slide 3: Contents
Need for new design
Coil cross section optimized with ROXIE
  Guidelines for optimization
  Proposed new cross-sections
  Fine tuning capabilities on the cross section
Magnet parameters
Iron saturation
3D effects
Summary

## Slide 4: Guidelines for the optimization
Avoid sharp edges on wedges
Keep position of block 4 (winding condition)
Blocks as radial as possible
Minimize impact coil production and performance
    Assumptions on cable growth during heat treatment:
    1 % growth in width
    3 % growth in mid-thickness
    Keystone angle unchanged
Notes: Our approach: to have a coil cross section as close as possible to the current design

## Slide 5: Persistent current effects in MBHDP101
Geometrically shifted to show the persistent current contribution.
Notes: measurements

## Slide 6: Optimized cross section, Cable Option 2
First gen. design
New design
 | Systematic - Cable Option 2 |  |  |  |  | Max.Persistent at I = 1100 A
Normal | Geometric | Saturation | Persistent | Injection | High Field | 
B1 (T) |  |  |  |  | 11.220 | 
b2 | 0.000 | -14.500 | 0.000 | 0.000 | -14.500 | 0.000
b3 | 7.220 | -0.400 | -8.000 | -0.780 | 6.820 | -20.000
b4 | 0.000 | -0.400 | 0.000 | 0.000 | -0.550 | 0.000
b5 | -0.014 | 0.100 | 2.500 | 2.486 | 0.040 | 3.400
b6 | 0.000 | -0.020 | 0.000 | 0.000 | -0.020 | 0.000
b7 | -0.093 | 0.062 | 0.200 | 0.107 | 0.430 | -0.400
b8 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000
b9 | 0.912 | 0.028 | 0.450 | 1.362 | 1.080 | 0.600
 | Systematic - First Generation |  |  |  |  | Max.Persistent at I = 1100 A
Normal | Geometric | Saturation | Persistent | Injection | High Field | 
B1 (T) |  |  |  |  | 11.221 | 
b2 | 0.000 | -14.500 | 0.000 | 0.000 | -14.500 | 0.000
b3 | 7.459 | -0.400 | -8.000 | -0.541 | 7.010 | -20.000
b4 | 0.000 | -0.400 | 0.000 | 0.000 | -0.550 | 0.000
b5 | -0.014 | 0.100 | 2.500 | 2.486 | 0.100 | 3.400
b6 | 0.000 | -0.020 | 0.000 | 0.000 | -0.020 | 0.000
b7 | -0.093 | 0.062 | 0.200 | 0.107 | 0.100 | -0.400
b8 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000
b9 | 0.912 | 0.028 | 0.450 | 1.362 | 0.960 | 0.600
Keystone angle: 0.4°, Bare inner thickness after HT: 1.236 mm
Notes: around -1 unit at injection, a minimum of -13 at 1.1 kA and around 7 units at nominal
Persistent current from measurements

## Slide 7: Optimized cross section, Cable Option 3
First gen. design
New design
 | Systematic - First Generation |  |  |  |  | Max.Persistent at I = 1100 A
Normal | Geometric | Saturation | Persistent | Injection | High Field | 
B1 (T) |  |  |  |  | 11.221 | 
b2 | 0.000 | -14.500 | 0.000 | 0.000 | -14.500 | 0.000
b3 | 7.459 | -0.400 | -8.000 | -0.541 | 7.010 | -20.000
b4 | 0.000 | -0.400 | 0.000 | 0.000 | -0.550 | 0.000
b5 | -0.014 | 0.100 | 2.500 | 2.486 | 0.100 | 3.400
b6 | 0.000 | -0.020 | 0.000 | 0.000 | -0.020 | 0.000
b7 | -0.093 | 0.062 | 0.200 | 0.107 | 0.100 | -0.400
b8 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000
b9 | 0.912 | 0.028 | 0.450 | 1.362 | 0.960 | 0.600
 | Systematic - Cable Option 3 |  |  |  |  | Max.Persistent at I = 1100 A
Normal | Geometric | Saturation | Persistent | Injection | High Field | 
B1 (T) |  |  |  |  | 11.225 | 
b2 | 0.000 | -14.500 | 0.000 | 0.000 | -14.500 | 0.000
b3 | 7.580 | -0.400 | -8.000 | -0.420 | 7.180 | -20.000
b4 | 0.000 | -0.400 | 0.000 | 0.000 | -0.550 | 0.000
b5 | -0.014 | 0.100 | 2.500 | 2.486 | 0.090 | 3.400
b6 | 0.000 | -0.020 | 0.000 | 0.000 | -0.020 | 0.000
b7 | -0.093 | 0.062 | 0.200 | 0.107 | 0.470 | -0.400
b8 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000
b9 | 0.912 | 0.028 | 0.450 | 1.362 | 1.020 | 0.600
Keystone angle: 0.5°, Bare inner thickness after HT: 1.223 mm

## Slide 8: Fine tuning of field quality
Modify normal multipoles through azimuthal compression
+100 µm mid plane shim
Δb3 = -4.8
Δb5 = -0.9
+100 µm pole shim
Δb3 = +3.5
Δb5 = -0.4

## Slide 9: Fine tuning of field quality
Mid plane shim 1 mm: (Rref = 17 mm)
Pole shim 1 mm:
Dipole | Layer | 𝛿b1 | 𝛿b3 | 𝛿b5 | 𝛿b7 | 𝛿b9 | 𝛿b11
11 T | inner | -30.74 | -34.33 | -8.85 | -2.03 | -0.51 | -0.22
 | outer | -23.07 | -13.30 | -1.41 | -0.14 | -0.02 | 0.00
LHC | inner | -30.30 | -31.80 | -9.10 | -2.42 | -0.65 | -0.20
 | outer | -22.65 | -11.96 | -1.67 | -0.14 | -0.02 | 0.00
Dipole | Layer | 𝛿b1 | 𝛿b3 | 𝛿b5 | 𝛿b7 | 𝛿b9 | 𝛿b11
11 T | inner | 58.80 | 22.51 | -2.44 | 0.56 | -0.43 | 0.14
 | outer | 41.96 | 12.82 | -1.25 | -0.03 | 0.02 | 0.00
LHC | inner | 54.94 | 17.46 | -3.67 | 1.29 | -0.47 | 0.06
 | outer | 41.99 | 12.59 | -0.71 | -0.14 | 0.02 | 0.00
Notes: Fine tuning capabilities similar to lhc main dipole. Strictly negative contribution from MP shim.

## Slide 10: Magnet parameters
Parameters | First gen. | Op. 2 | Op. 3 | Units
Operational temperature | 1.9 |  |  | K
Clear aperture diameter | 60 |  |  | mm
Nominal B-field | 11.22 | 11.22 | 11.23 | T
Nominal current | 11.85 |  |  | kA
Nominal peak field on the coil (including strand field) | 11.75 | 11.76 | 11.76 | T
Stored energy at Inom | 0.97 |  |  | MJ/m
Current sharing temperature | 6.3 |  |  | K
Differential inductance at Inom | 11.97 |  |  | mH/m
Superconductor current density (jsc) | 2560 |  |  | A/mm2
Engineering current density (jeng) | 786 |  |  | A/mm2
Overall current density at (joverall) | 5.23 |  |  | A/mm2
Horizontal EM-force Fx at Inom | 6.23 | 6.22 | 6.22 | MN/m
Vertical EM-force Fy per coil at Inom | 3.15 | 3.16 | 3.16 | MN/m
Notes: Nom peak field in coil? From loadline operational point

## Slide 11: Magnet parameters – load line
Chart: Bp (T)
| 7 | 7.25 | 7.5 | 7.75 | 8 | 8.25 | 8.5 | 8.75 | 9 | 9.25 | 9.5 | 9.75 | 10 | 10.25 | 10.5 | 10.75 | 11 | 11.25 | 11.5 | 11.75 | 12 | 12.25 | 12.5 | 12.75 | 13 | 13.25 | 13.5 | 13.75 | 14 | 14.25 | 14.5 | 14.75 | 15 | 15.25 | 15.5 | 15.75 | 16
Ic (1.9K) REF 2016 (kA) | 57.4812 | 55.0606 | 52.756 | 50.5588 | 48.4617 | 46.4576 | 44.5407 | 42.7053 | 40.9464 | 39.2596 | 37.6407 | 36.0858 | 34.5916 | 33.1548 | 31.7726 | 30.4422 | 29.1612 | 27.9272 | 26.7382 | 25.592 | 24.4869 | 23.4212 | 22.3932 | 21.4014 | 20.4444 | 19.5209 | 18.6297 | 17.7695 | 16.9394 | 16.1381 | 15.3649 | 14.6186 | 13.8986 | 13.2039 | 12.5337 | 11.8874 | 11.2641
Ic (1.9K) REF 2016 - 5% (kA) | 54.6072 | 52.3076 | 50.1182 | 48.0309 | 46.0386 | 44.1348 | 42.3137 | 40.57 | 38.8991 | 37.2966 | 35.7586 | 34.2815 | 32.862 | 31.4971 | 30.184 | 28.9201 | 27.7031 | 26.5309 | 25.4013 | 24.3124 | 23.2626 | 22.2501 | 21.2735 | 20.3313 | 19.4222 | 18.5449 | 17.6982 | 16.8811 | 16.0924 | 15.3312 | 14.5966 | 13.8877 | 13.2037 | 12.5437 | 11.907 | 11.293 | 10.7009
Magnet Load Line | 0.001185 | 1.0084 | 2.0156 | 3.0228 | 4.0299 | 5.0371 | 6.0443 | 7.0515 | 8.0587 | 9.0659 | 10.073 | 11.08 | 12.087 | 13.095 | 14.102 | 15.109 | 16.116 | 17.123 | 18.131 | 19.138 | 20.145
operational point | 11.85
Margin on the load line assuming:
  Design value (-5%): 80.1 %
  -3 % cabling degradation: 79.6 %
  -7 % cabling degradation: 80.6 %
Operational conditions: Iop = 11.85 kA, Bp = 11.76 T (including cryostat and strand self field)

## Slide 12: Iron Saturation – Field Quality
Impact of the iron saturation effect on higher order harmonics < 0.6 units
Chart: I (A)
| 1.1850000000000001 | 712.13 | 1423.1 | 2134 | 2844.9 | 3555.9 | 4266.8 | 4977.8 | 5688.7 | 6399.7 | 7110.6 | 7821.5 | 8532.5 | 9243.4 | 9954.4 | 10665 | 11376 | 12087 | 12798 | 13509 | 14220
b2 new cross section | 0.037375 | 0.037375 | 0.038485 | 0.049911 | 0.063209 | 0.069973 | -0.038404 | -0.51583 | -1.8087 | -3.876 | -5.6315 | -6.706 | -7.372 | -8.1751 | -9.3712 | -11.033 | -13.053 | -15.282 | -17.564 | -19.818 | -22.02
Chart: I (A)
| 1.1850000000000001 | 712.13 | 1423.1 | 2134 | 2844.9 | 3555.9 | 4266.8 | 4977.8 | 5688.7 | 6399.7 | 7110.6 | 7821.5 | 8532.5 | 9243.4 | 9954.4 | 10665 | 11376 | 12087 | 12798 | 13509 | 14220
b3 new cross section | 7.6276 | 7.6276 | 7.6274 | 7.625 | 7.6218 | 7.6206 | 7.6218 | 7.5959 | 7.523 | 7.2619 | 6.8552 | 6.6353 | 6.6095 | 6.6878 | 6.8068 | 6.9394 | 7.0839 | 7.228 | 7.3646 | 7.4961 | 7.6223
Transfer function:
Chart: I (A)
| 1.1850000000000001 | 652.88 | 1304.5999999999999 | 1956.3 | 2607.9 | 3259.6 | 3911.3 | 4563 | 5214.7 | 5866.4 | 6518.1 | 7169.8 | 7821.5 | 8473.2000000000007 | 9124.9 | 9776.5 | 10428 | 11080 | 11732 | 12383 | 13035
TF | 0.99714 | 0.99714 | 0.99713 | 0.99707 | 0.99701 | 0.99702 | 0.99622 | 0.99696 | 0.99595 | 0.99405 | 0.98964 | 0.98488 | 0.97942 | 0.97382 | 0.96847 | 0.96375 | 0.95833 | 0.95356 | 0.94903 | 0.94477 | 0.94078
Notes: Plot b2,b3(current) for old and new designs
TF with cryo

## Slide 13: 3D effects: Mechanical optimization
Preliminary results: Minor changes to current design
Curvature hard-way bend
Inner layer return end
Outer layer return end
Relative change curvature hard bend
from first gen. design:
Chart: arc length along block (mm)
| 765.13 | 787.84 | 806.22 | 814.9 | 823.32 | 831.6 | 839.82 | 848.03 | 856.22 | 864.32 | 872.21 | 879.81 | 887.02 | 893.81 | 900.19 | 906.14 | 911.74 | 916.88 | 921.68 | 926.03 | 929.99 | 933.4
Block 1 (IL) | 0 | -16.0093 | -14.9429 | -10.4463 | -6.2524 | -2.6786 | 0.53423 | 3.4315 | 6.191 | 8.9581 | 11.6586 | 14.1653 | 16.3637 | 18.1762 | 19.6953 | 20.5945 | 21.1646 | 20.4317 | 18.7799 | 15.4694 | 14.0993 | 13.9294
Block 5 (OL) | 0 | -35.7034 | -32.0322 | -27.2239 | -22.5077 | -17.7003 | -12.7477 | -7.6875 | -2.4886 | 2.8752 | 8.2371 | 13.3516 | 17.9124 | 21.5797 | 24.2101 | 25.5762 | 26.0676 | 25.1805 | 24.9787 | 23.6073 | 20.0193 | 19.7106
Notes: (New-ref)/abs(ref)

## Slide 14: Conclusion
Cross section with new PIT cables is feasible.
Field quality and main field comparable to 1st generation design.
Fine tuning capabilities with azimuthal shim demonstrated.
Tests on cable degradation necessary to decide between the two cable geometries.
2D mechanical analysis have shown negligible impact of the coil geometry (option 2 or option 3) on the coil stress.
3D design on-going:
  Small differences from the mechanical optimization point of view.
  No differences are expected for the magnetic optimization.

## Slide 15: Additional slides

## Slide 16: Optimized cross section, Cable Option 2 (2A):
First gen. design
New design
 | Systematic - Cable option 2 |  |  |  |  | Max.Persistent at I = 1100 A
Normal | Geometric | Saturation | Persistent | Injection | High Field | 
B1 (T) |  |  |  |  | 11.191 | 
2 | 0.000 | -14.500 | 0.000 | 0.000 | -14.500 | 0.000
3 | 0.610 | -0.400 | -8.000 | -7.390 | 0.210 | -20.000
4 | 0.000 | -0.400 | 0.000 | 0.000 | -0.540 | 0.000
5 | -0.014 | 0.100 | 2.500 | 2.486 | 0.200 | 3.400
6 | 0.000 | -0.020 | 0.000 | 0.000 | -0.020 | 0.000
7 | -0.093 | 0.062 | 0.200 | 0.107 | 0.840 | -0.400
8 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000
9 | 0.912 | 0.028 | 0.450 | 1.362 | 1.070 | 0.600
 | Systematic - First Generation |  |  |  |  | Max.Persistent at I = 1100 A
Normal | Geometric | Saturation | Persistent | Injection | High Field | 
B1 (T) |  |  |  |  | 11.221 | 
2 | 0.000 | -14.500 | 0.000 | 0.000 | -14.500 | 0.000
3 | 7.459 | -0.400 | -8.000 | -0.541 | 7.010 | -20.000
4 | 0.000 | -0.400 | 0.000 | 0.000 | -0.550 | 0.000
5 | -0.014 | 0.100 | 2.500 | 2.486 | 0.100 | 3.400
6 | 0.000 | -0.020 | 0.000 | 0.000 | -0.020 | 0.000
7 | -0.093 | 0.062 | 0.200 | 0.107 | 0.100 | -0.400
8 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000
9 | 0.912 | 0.028 | 0.450 | 1.362 | 0.960 | 0.600

## Slide 17: Optimized cross section, Cable Option 3 (3A):
First gen. design
New design
 | Systematic - Cable option 3 |  |  |  |  | Max.Persistent at I = 1100 A
Normal | Geometric | Saturation | Persistent | Injection | High Field | 
B1 (T) |  |  |  |  | 11.191 | 
2 | 0.000 | -14.500 | 0.000 | 0.000 | -14.500 | 0.000
3 | 0.750 | -0.400 | -8.000 | -7.250 | 0.350 | -20.000
4 | 0.000 | -0.400 | 0.000 | 0.000 | -0.540 | 0.000
5 | -0.014 | 0.100 | 2.500 | 2.486 | 0.220 | 3.400
6 | 0.000 | -0.020 | 0.000 | 0.000 | -0.020 | 0.000
7 | -0.093 | 0.062 | 0.200 | 0.107 | 0.900 | -0.400
8 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000
9 | 0.912 | 0.028 | 0.450 | 1.362 | 1.010 | 0.600
 | Systematic - First Generation |  |  |  |  | Max.Persistent at I = 1100 A
Normal | Geometric | Saturation | Persistent | Injection | High Field | 
B1 (T) |  |  |  |  | 11.221 | 
2 | 0.000 | -14.500 | 0.000 | 0.000 | -14.500 | 0.000
3 | 7.459 | -0.400 | -8.000 | -0.541 | 7.010 | -20.000
4 | 0.000 | -0.400 | 0.000 | 0.000 | -0.550 | 0.000
5 | -0.014 | 0.100 | 2.500 | 2.486 | 0.100 | 3.400
6 | 0.000 | -0.020 | 0.000 | 0.000 | -0.020 | 0.000
7 | -0.093 | 0.062 | 0.200 | 0.107 | 0.100 | -0.400
8 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000
9 | 0.912 | 0.028 | 0.450 | 1.362 | 0.960 | 0.600

## Slide 18: Cable Option 1, b3 optimized to 0
First gen. design
New design

## Slide 19: Move turn from block 2 1
Option 2
Improved geometry – but b7 is 3 units off (and b5 2 units off for Op 2)
Notes: Change to v8 b and blocks r only

## Slide 20: Move turn from block 2 1 and from 6  5
Option 2
Improved geometry – but b7 is 3 units off
Notes: Change to v8 b and ILOL r only

## Slide 21: Azimuthal stress
Ref. – Azimuthal Stress 12T
OP2 – Azimuthal Stress 12T
-142.7
Average - Azimuthal Stress
-123.1
-7.4
-20.5
-141.2
-122.4
-13.0
-21.1

## Slide 22: Assumptions on cable growth during HT
After heat treatment | Bare thickness in (mm) | Bare mid-thickness (mm) | Bare thickness out (mm) | Bare width (mm)
First Gen. Design | 1.185 | 1.288 | 1.390 | 14.847
Option 1 | 1.243 | 1.308 | 1.373 | 14.847
Option 2 | 1.236 | 1.288 | 1.339 | 14.847
Option 3 | 1.223 | 1.288 | 1.352 | 14.847
Notes: Mid thickness + width
Not after reaction

## Slide 23: Updated cable geometry

## Slide 24: Cable Geometry Before Reaction
Chart: Cable geometry before reaction
| 0 | 14.7 | 14.7
First generation | 1.1487 | 1.3513 | 0
Option 1 | 1.2059 | 1.3341 | 0
Option 2 | 1.1987 | 1.3013 | 0
Option 3 | 1.1859 | 1.3141 | 0

## Slide 25: b3 LHC main dipole
Notes: In the main dipoles we have -2 at injection and about 6 at nominal,

## Slide 26: Iron saturation – field quality
Chart: normal multipoles bn, n>3
| 1.1850000000000001 | 712.13 | 1423.1 | 2134 | 2844.9 | 3555.9 | 4266.8 | 4977.8 | 5688.7 | 6399.7 | 7110.6 | 7821.5 | 8532.5 | 9243.4 | 9954.4 | 10665 | 11376 | 12087 | 12798 | 13509 | 14220
b4 | 0.0030876 | 0.0030876 | 0.0031136 | 0.0034449 | 0.0035654 | 0.003762 | 0.0081326 | 0.010758 | 0.028518 | 0.029651 | -0.03307 | -0.12517 | -0.21605 | -0.29882 | -0.3731 | -0.44401 | -0.5087 | -0.56585 | -0.61772 | -0.6651 | -0.70829
b5 | -0.2459 | -0.2459 | -0.2459 | -0.24591 | -0.24586 | -0.24553 | -0.24311 | -0.23499 | -0.21005 | -0.16399 | -0.11372 | -0.071038 | -0.033841 | -0.0012896 | 0.027674 | 0.052886 | 0.075179 | 0.095212 | 0.11281 | 0.12828 | 0.14192
b6 | -4.7312e-05 | -4.7311e-05 | -4.8081e-05 | -5.1018e-05 | -5.6209e-05 | -5.9204e-05 | 9.9766e-05 | 0.00033284 | 0.0011255 | 0.0023844 | 0.0010122 | -0.0023894 | -0.0060474 | -0.0092454 | -0.011789 | -0.013874 | -0.015454 | -0.016569 | -0.017397 | -0.018035 | -0.01852
b7 | 0.45293 | 0.45293 | 0.45293 | 0.45293 | 0.45294 | 0.45294 | 0.45291 | 0.45286 | 0.45274 | 0.45312 | 0.45423 | 0.45625 | 0.45869 | 0.46121 | 0.46374 | 0.46623 | 0.46864 | 0.47092 | 0.47305 | 0.47504 | 0.47689
b8 | 1.2818e-06 | 1.2708e-06 | 1.2185e-06 | 6.5867e-07 | 6.3801e-08 | -1.3494e-06 | -9.5993e-06 | -3.6269e-05 | -0.0001162 | -0.00021116 | -0.00029871 | -0.0003879 | -0.00046155 | -0.00051099 | -0.00054019 | -0.00055587 | -0.00056035 | -0.00055597 | -0.00054736 | -0.00053712 | -0.00052579
b9 | 0.96538 | 0.96538 | 0.96538 | 0.96538 | 0.96539 | 0.96542 | 0.96559 | 0.96632 | 0.96837 | 0.97219 | 0.97726 | 0.98328 | 0.98949 | 0.99555 | 1.0014 | 1.0072 | 1.0126 | 1.0178 | 1.0227 | 1.0272 | 1.0315
b10 | 4.8214e-08 | 5.5598e-08 | 4.8008e-08 | 3.4433e-08 | 1.5055e-08 | -2.8683e-08 | -2.807e-07 | -1.26e-06 | -3.5448e-06 | -8.1081e-06 | -1.2358e-05 | -1.4964e-05 | -1.5748e-05 | -1.5602e-05 | -1.5161e-05 | -1.4576e-05 | -1.3955e-05 | -1.3371e-05 | -1.2819e-05 | -1.234e-05 | -1.1893e-05
b11 | 0.38181 | 0.38181 | 0.38181 | 0.38181 | 0.38181 | 0.38183 | 0.38189 | 0.38217 | 0.38297 | 0.38446 | 0.38645 | 0.38883 | 0.39128 | 0.39367 | 0.39599 | 0.39825 | 0.40042 | 0.40247 | 0.40439 | 0.40619 | 0.40787

## Slide 27: 3D effects
Lead end