## Slide 1: Coil winding and collaring D. Smekens TE-MSC-LMF
Acknowledgements B. Auchmann
E. Cavanna M. Daly Th. Genestier M. Karppinen Ch. Löffler Ph. Revilak A. Temporal
and all members of the HL-LHC WP11
Review of the 11 T Dipoles at Collimator Section for the HL-LHC – CERN - 6-8 April 2016

## Slide 2: Outline
Objectives for Prototype
Main Parameters of the Coils
  Adopted Features, Changes for the long coils
  Cross-Section, Coil Ends, Wedge Segmentation
Collared Coils
  Main Parameters
  Shimming Approach, New FE Models
Long Coil Production Status
Conclusions

## Slide 3: From Short Model to Prototype Assembly
2-in-1 Prototype 5.5m long is based on 2m long short models developed since 2011
Prototype: 2 collared coils, not tested as single aperture configuration: direct assembly of 4 virgin coils
Prototype: will make use of quench heaters impregnated with the coils on the outer surface (embedded)

## Slide 4: Objectives for the prototype MBH_P001
MBH_C001 September 2016 |  | MBH_C002 November 2016 |  | MBH_C003 January 2017 | 
CR001 | CR002 | CR003 | CR004 | CR005 | CR006
Practice collared coil |  | Prototype magnet MBH_P001 |  |  | 
Low Performance
Nb3Sn Coil CR001
Low Performance
Nb3Sn Coil CR002
Full Performance
Coil CR003
Full Performance
Coil CR004
Full Performance
Coil CR005
Full Performance
Coil CR006
Note: this presentation is using the following simplified naming
CR00x for a coil, full MTF asset identifier: HCMBH_C005_CR00000x
MBH_C00x for a collared coil (HCMBH_C001_CR00000x)
MBH_P001 for the prototype magnet, cold mass only
Notes: Objectives (latest revision): 3 collared coils still this year (if possible), at the latest for January 2017, ready for assembly inside the prototype yokes

## Slide 5: Main Parameters of the Coil
Coil: 56 turns, 2 layers, 6 blocks design, no internal splice |  | 
Coil ID / OD | 59.8 / 121.6 | mm
Coil overall length | 5559 | mm
Straight section length | 5108 | mm
Turns Inner Layer (IL) / Outer Layer (OL) | 22 (IL) / 34 (OL) | 
Impregnation System | Epoxy DGEBA (CTD 101-K) | 
Cable : RRP 0.7 mm dia. , 40 strands, cored, glass-mica insulated |  | 
Cable Length (IL / OL / on spool) | 235 (IL) / 364 (OL) / 680 | m
Cable bare width before / after reaction | 14.7 / 14.85 (+1%) | mm
Cable bare mid-thickness before / after reaction | 1.25 / 1.306 (+4.5%) | mm
Keystone angle before / after reaction | 0.79 / 0.806 | deg.
Number of strands per cable (x strand diameter) | 40 (x 0.7d [mm]) | -
Cable insulation wall thickness (design value) | 0.1 | mm
Insulation Material | Phlogopite + Glass | 
Notes: A brief recall: 56 turn 2 layers coil, no internal splice (680 meters of cable on the winding spools), designed for the collaring using the ”pole loading” concept
The slide mostly to recap the terms used.

## Slide 6: Features for prototype and LS2 magnets
Stays in
Mica-Glass Insulation S-glass sleeve overbraiding Oxide Dispersion Strength. Cu Wedges Laser Sintered 316L flex-spacers Ceramic Binder G-11 Splice Block-Saddle DGEBA (CTD-101K) Epoxy System
Already changed
Sn-Ag splice for Nb3Sn / Nb-Ti interconnect (was Sn-Pb) Copper Stabilization over splice region (was none) Embedded Quench Heaters with new ground insulation scheme (was QH outside coil)
May Change (…currently changing)
Include inter-layer Quench Heaters Coil wedges: minimize gaps and segmentation of the wedges along the coil to allow for coil shrinkage Impregnation: from single point to multi-point resin injection Impregnation: pressurized impregnation during polymerization (3.5bars)

## Slide 7: Coil Cross-Section
Short Model Coils (105 -> 115) all use similar Cross-Section as per original design
Current Cross-Section defined in 2011 insulation wall thickness is larger in reality (0.115 mm) than per design (0.1 mm) Reaction cable growth not re-assessed From short model tests, conductor locus under mechanical strain/compression did not require correction
MBH_P001 Prototype will use the same cross-section (no re-optimization)
Same Cross-Section design, no re-optimization Same wedges and spacers Same coil winding parameters as for short model
Series for LS2 may also use the same cross-section
To be confirmed

## Slide 8: Coil Ends
Short Model Coil Ends
Several Coil Ends iterations required Spacers, saddles and splice block are different on early short model coils until coil 105 As from coil 106->114, spacer design unchanged Quality of winding as improved: coil 106-> coil 108 too long by ~ 8mm each side ; as from 109 length of coil ends is constant and as per design
MBH_P001 Prototype will use identical design
Same Coil Ends as short coils Winding operations OK for long coils: generate coil ends as per design
Series for LS2
Requirements To be confirmed
Remaining Issue
Filling Quality of the Inter-Layer Cavities
Legacy versions

## Slide 9: Wedge Segmenting
Short Model Coils are progressively decreasing the gaps and segmentation of the wedges
Wedge segmentation not in 3D CAD models Gaps are (were) required for coil shrinkage (winding and reaction) Short Coil Winding & Reaction: no shrinkage
MBH_P001 Prototype has more wedge segments
Long extruded Cu-ODS wedges were unavailable until recently (now up to 3.2 meters) Long Coil Winding: important spring back (~ 5mm) Long Coil Reaction: unknown shrinkage
Series for LS2
TBC: 2 segments and one gap in straight section Gap size to be defined
Issues
Wedge Extremities not well insulated Gaps Induce Resin Rich Areas (inner layer not accessible)

## Slide 10: Collared Coils – Main Parameters
Collar Packs and Loading Poles | 
Collar Thickness | 3mm
Material | Austenitic Steel Nippon Steel YUS 130S
Standard Riveted Pack Length | 65 mm (20 collars)
# of Collars per long collared coils | 3418
Loading Pole Material | Titanium Ti6Al4V
Loading Pole Unit Length | 240 mm
Coil Pre-Stress by Pole Loading, current collar design | 
Estimated Pre-StressTunability | +/- 15 MPa
Minimum Shim Increment Used | 0.05 mm
Maximum coil azim. pre-stress (averaged at pole turn @ RT) * | ~200 MPa
* permanent deformation of collar nose and collaring pressing surfaces

## Slide 11
Strain-stress curves from 10-stacks RRP108/127 (coil 105)
Shimming Approach
Short Model Collared Coils (SP102, SP103, DP101)
Shimming empirically increased for SP102 Low hysteretical modulus measured on 10-stacks SP103 shimmed according to non-linear properties FE Model reworked and refined since mid 2015
Prototype: MBH_C001, C002, C003 collared coils
Will use identical FE Model identical shimming procedure More studies on coil properties required
Notes: Shimming empirically increased for SP102 (based on known shimming of SP101 and quench behaviour)

## Slide 12: New FE Models
18.8GPa Linear 10-18.8 GPa Non Linear
~ 50% extra shimming elastic
Initial Shimming (theoretical) | Shimming used in SP103 and DP101
Recent developments on 11T F.E. models have been presented during the
“Collaboration meeting on DS 11T Dipole grounds held at Fermilab”, September 2015:
http://indico.cern.ch/event/434223/
and during TE/MSC Technical Meetings:
“Mechanical aspects of the 11T magnet”, December 2015 https://indico.cern.ch/event/461705/
“Mechanical measurements in superconducting magnets” , January 2016:
https://indico.cern.ch/event/487129/
“Mechanical aspects of Nb3Sn magnets for HL-LHC - Session on measurement results” , February 2016:https://indico.cern.ch/event/496158/
Notes: Pre-requisite: known material properties, known geometry
Approach: quasi bi-linear stress-strain curve based on samples (10-stacks) measurments. No direct mechanical measurments on the coil itself

## Slide 13: Coil Supplies & Coil Production: as of April 2016
 | Coil Parts | Winding/Curing | Reaction | Splicing | Quench Heater | Impreg. | Collaring Schedule
Copper dummy | OK | OK 1 | OK 2 | OK 3 | missing | ongoing… | 
CR001 practice | OK | OK 1 | OK | on hold | missing |  | Sept 2016
CR002 practice | OK | OK 1 | on hold |  |  |  | Sept 2016
CR003 proto_1 | OK | OK 1 | on hold |  |  |  | Nov 2016
CR004 proto_2 | OK | OK 1 |  |  |  |  | Nov 2016
CR005 proto_3 | OK |  |  |  |  |  | Jan 2017
CR006 proto_4 | parts missing 4 |  |  |  |  |  | Jan 2017
CR007 (spare) | parts missing 4 |  |  |  |  |  | 
1 Minor insulation damage during winding process. Coil usable.
2 Important damage to insulation (dummy coil)
3 Splice not according to latest design (dummy coil)
4 delivery expected in May 2016

## Slide 14: Conclusions
A brief overview of what is currently used to build the prototype collared coils
Prototype coils are almost identical to short model, ”just longer”.
No re-optimization, no change of cross-section
An important difference is the embedded (impregnated) quench heater system that will be discussed in talks later during this review
New FE models and better understanding of the coil properties
Good progress both in the long coil design and construction

## Slide 15
Hereafter, back up slides…

## Slide 16: 11T Dipole Coils: Naming conventions
6
4
3
2
5
1
7
Nb3Sn Cable, mica insulation, Glass Sleeved
Mid-Plane
Filler Wedge
Loading Plate
Key
SLS Spacer w/Flex Legs
Saddle with integrated splice block
Nb3Sn / Nb-Ti Splice
a
b
c
d
e
f
Insulated cable
Filler Wedge
Loading plate
Inter-layer
Inner ground wrap
Outer ground wrap (prototype variant: including quench heaters)
Notes: A brief recall: 56 turn 2 layers coil, no internal splice (680 meters of cable on the winding spools), designed for the collaring using the ”pole loading” concept
The slide mostly to recap the terms used.

## Slide 17
Ongoing work for FE Material Input Data and Model Validation
1
2
3
1
Experimental Test | Results | Temp
Compression | E-modulus (E), Poisson’s ratio (ν), σ, ε | RT 77 K 4.2 K
Tension | Longitudinal E-modulus (E11T) | RT 77 K 4.2 K
Sample Type |  |  |  |  | Results | Temp
Material Characterisation | Epoxy | Fiber Glass |  |  | Eij, νij, σij, εij | RT 77 K 4.2 K
 | Epoxy | Fiber Glass | Mica |  |  | 
 | Reacted Cable | Epoxy |  |  |  | 
 | Reacted Cable | Fiber Glass | Epoxy |  |  | 
 | Reacted Cable | Fiber Glass | Mica | Epoxy |  | 
Height Effects |  | 4-stack | 18-stack |  |  | 
3-Point Bend Test |  |  | ASTM 198 D | Long Stack | Gij | 
  Additional Experiments to determine the following:
    Thermal Expansion Coefficients (ij)
    MIIT’s (Tests at ≈400K)
    Dielectric property degradation during compression
Source: M. Daly

## Slide 18
Characterisation procedure
Fiber Glass Composite (% Vf)
2D Model
10-stack Measurements
3D Model
Coil Model 2D & 3D
Validate:
E-Modulus Press using strain Gauges
(Digital Imaging Correlation)
E, ε
3-Point Bend Tests
Validate with Measurements
Sample Fabrication and Experimental Work
Modelling and Calibration of Models
σ, ν
Finite Element Properties
Material Characterisation
Source: M. Daly