## Slide 1: Model magnet test results and analysis - Quench performance, mechanics and operation requirements
G. Willering and C. Löffler
J. Feuvrier, O. Ditsch, J-C. Perez, F. Savary, Philippe Grosclaude and all that were involved in all production and design steps.
Review of the 11T dipoles at Collimator Section for the HL-LHC,
6 April 2016, CERN

## Slide 2: Outline
Setting the scene
  MB magnet in the RB circuits
Quench behavior of 11T models at CERN
  Quench overview
  Virgin training
  Erratic/detraining quenches
  Thermal cycles
  Test at 4.3 K
  Plateau currents
Mechanics
  Improvements in modeling since the last review
  Single vs double aperture structure

## Slide 3: Setting the scene: RB circuit operation
MBH magnets will replace MB magnets in the LHC RB circuits and need to be fully compatible.
Current operation: 10.98 kA, 6.5 TeV equivalent
Design operation: 11.85 kA, 7 TeV equivalent.
Example of LHC RB circuit powering in October 2015
  Total time at nominal current: 304 hours (40 %)
  Number of ramps to nominal: 80
  Maximum time at nominal current: 25 hours

## Slide 4: Setting the scene: MB quenches
HWC 2015: in total 179 quenches up to 11.1 kA in MB magnets
  Average of 0.14 quenches per magnet.
Operation 2015: 5 ‘flattop’ quenches were registered.
No fixed targets set for virgin training quenches for MBH magnets in SM18, but as low as possible after thermal cycle is required.
Stable operation up to nominal current is very important.
Quenches of LHC main dipoles per sector
See LMC meeting, 8 April 2015, by G. Willering

## Slide 5: Outline
Setting the scene
  MB magnet in the RB circuits
Quench behavior of 11T models at CERN
  Quench overview
  Virgin training
  Erratic/detraining quenches
  Thermal cycles
  Test at 4.3 K
  Plateau currents
Mechanics
  Improvements in modeling since the last review
  Single vs double aperture structure

## Slide 6: Model overview
In this presentation the mirror configuration is not taken into account.
Scheme: courtesy S. Izquierdo Bermudez

## Slide 7: Quench overview at 1.9 K
Total number of quenches at 1.9 K: 86
Very limited detraining after thermal cycles, apart from coil 107
94 % of short sample reached.
 | coil | Quenches to nominal field | Quenches to ultimate field | Quenches to nominal field after thermal cycle
SP101 | 106 | 4 | - | 0
 | 107 | 12 | - | 8
SP102 | 106 | 3 | 17 | 1
 | 108 | 2 | 4 | 0
SP103 | 109 | 5 | 5 | -
 | 111 | 8 | 11 | -
DP101 | 106 | 0 | 2 | 0
 | 108 | 0 | 0 | 0
 | 109 | 0 | 0 | 0
 | 111 | 0 | 0 | 0
 | Maximum current reached (kA) | % Iss
SP101 | 11.9 | 82
SP102 | 12.8 | 88
SP103 | 12.8 | 90
DP101 | 13.2 | 94

## Slide 8: Virgin training
Including all quenches reached higher current than coil has reached before.
DP101 cannot really been seen as ‘virgin’ coil.
DP101 started with 3 ‘massive’ quenches in the midplane of coil 106. After this settling no more quenches recorded there.
Except for coil 107, the interlayer jump has a very limited number of quenches.
Head
Transition Region
 |  | Pole turn |  |  |  |  | Other | 
 | Coil # | Interlayer jump | Transition | Straigth- section | Head | unknown poleturn | Mid-plane | Other blocks
SP101 | 106 |  | 1 | 1 |  |  |  | 
 | 107 | 7 | 4 | 2 |  |  |  | 
SP102 | 106 | 1 | 1 | 3 | 3 |  | 1 | 
 | 108 |  | 1 |  |  |  |  | 
SP103 | 109 |  | 2 | 2 | 2 |  |  | 
 | 111 |  |  | 4 |  | 3 |  | 
DP101 | 106 | 3 |  |  |  |  | 3 | 
 | 108 |  |  |  | 1 |  |  | 
 | 109 |  |  |  |  |  |  | 
 | 111 |  |  |  |  |  |  | 
 | Total | 11 | 9 | 12 | 6 | 3 | 4 | 0

## Slide 9: Erratic and/or detraining quenches
Every quench more than 100 A lower than magnet reached before. (100 A is the margin used for training in the LHC)
Most detraining quenches in the pole turns.
No specific ‘weak spot’, except in coil 107.
Head
Transition Region
 |  | Pole turn |  |  |  |  | Other | 
 | Coil # | Interlayer jump | Transition | Straigth- section | Head | unknown poleturn | Mid-plane | Other blocks
SP101 | 106 |  |  |  |  |  |  | 
 | 107 | 1 | 3 |  | 13 |  |  | 
SP102 | 106 | 2 | 1 | 4 | 4 |  | 1 | 
 | 108 |  | 1 |  |  |  |  | 
SP103 | 109 |  |  |  |  |  |  | 
 | 111 |  |  | 4 |  | 1 |  | 
DP101 | 106 | 1 |  |  | 2 |  |  | 
 | 108 |  |  |  | 1 |  |  | 
 | 109 |  |  |  |  |  |  | 
 | 111 |  |  |  |  |  |  | 
 | Total | 4 | 5 | 8 | 20 | 1 | 1 | 0

## Slide 10: Going beyond design current
Only DP101 was tested beyond ultimate current
3 quenches at highest currents all in the same location at 13.2 kA in the midplane with exactly the same quench pattern.
The inner layer midplane turns of coil 109 and 111 quenched simultaneously.
Midplane turn inner layer has high field and high stress.
Possibly limited by Iss if we take into account strain dependence.
High Field
High Stress
Roxy model by S. Izquierdo Bermudez

## Slide 11: Quench performance at 4.3 K
Virgin training always at 1.9 K. Quench at 4.3 K gives large stress on the test station with up to 1.3 MJ deposited energy.
SP101 limited by coil 107 at 85 % of Iss in pole turn, transition region.
SP102 limited by coil 106 at 90 % in layer jump
SP103 limited by coil 111 at 92 % in straight segment close to layer jump
Some correlation between quench locations during virgin training at 1.9 K and quenches at 4.3 K.

## Slide 12: Stable behavior at high currents
In all models holding current tests were performed, up to 10 hours at nominal current and 2.5 hours at ultimate current.
Not a single quench was recorded during flattop or ramp down for all models!

## Slide 13: First CERN double aperture performance
Remarkable performance after re-assembly and thermal cycle.
0 training quenches to nominal
2 quenches to ultimate

## Slide 14: Outline
Setting the scene
  MB magnet in the RB circuits
Quench behavior of 11T models at CERN
  Quench overview
  Virgin training
  Erratic/detraining quenches
  Thermal cycles
  Test at 4.3 K
  Plateau currents
Mechanics
  Improvements in modeling since the last review
  Tuning of stresses
  Single vs double aperture structure

## Slide 15: Model progress
Since last review (december 2014)
Major step in understanding: using non-linear modeling and changed modulus describes 3 different types of observed data very well:
  10 samples of 10-stacks
  Geometric changes in coil 107 after cold powering
  Stress state in single apertures after cold powering
More research ongoing to continu the learning process and further support the assumptions.
  (more info about the test plan see the presentation by Michael Daly (CERN), Claudio Fichera (CERN) https://indico.cern.ch/event/496158/ )
E-modulus press in development, see presentation of J-C. Perez

## Slide 16: 10-stacks: Compressive Strength/Cracking
Increasing Stress
Sample S2-1: 50 MPa
Sample S5-2: 200 MPa
Sample S5-1: 150 MPa
Test data: https://edms.cern.ch/document/1534894/1
Test performed by Oscar Sacristan de Frutos / EN-MME
Coil material data defined by uniaxial 10-stack compression test (10 samples)
FEA based comparison with non-linear material properties
Material behavior assumed isotropic due to lack of data (more tests are being prepared)
Tangent modulus 10.8GPa; lin. Modulus 18.8GPa (no temperature dependency could be measured)
Cracks initiate as from 150MPa, and are generalized at 200 MPa.
Defects not necessarily observed in Coil 107 after test to 11T. Examination was done on multiple cross-section. Absence of cracks suggests mismatch between FE, based on linear material properties, and reality.

## Slide 17: Model validation: Permanent deformation of coils after testing
11T coils can only be measured after the glued trace is removed
Only coil 107 could be measured after testing to 11T
Deformation is presented in midplane reduction
After cold test:
CERN 11T coil 107
  500mm central 60µm
  Towards heads 40µm
  Coil metrology:
    https://edms.cern.ch/project/CERN-0000152984
Coil 107 after manufacturing – virgin state
-0.204mm
-0.061mm
Coil 107 after testing in MBHP101
0.013mm
-0.109mm

## Slide 18
Chart: Stress collar nose / MPa
| after collaring | after welding | 1.9K before testing | 12T | 200K Quench | 1.9K after testing | after testing
2in1 102 | -125.6531 | -121.5971 | -108.7502 | -21 | -133 | -79 | -109.5344
2in1 103 | -110.4919 | -116.7806 | -98.1561 | -23 | -110 | -72 | -118.8896
FE 102 lin | -166.7406 | -166.7406 | -167.135 | -93.2381 | -216.4526 | -164.8477 | -179.4516
FE 103 lin | -200.5929 | -200.5929 | -206.5148 | -132.36 | -256.0086 | -204.1515 | -210.306
FE 102 non-lin | -133.3766 | -133.3766 | -113.2364 | -18.4259 | -130.5539 | -77.4862 | -88.5321
FE 103 non-lin | -141.6931 | -141.6931 | -117.6766 | -35.9778 | -155.6977 | -103.6817 | -126.7295
Non lin. Material properties / modulus 10.8 / 18.8GPa coil
Measured result
Half bridge - strain gauge
Lin. Material properties module 18.8GPa coil
Model validation: Stress state after cold powering tests
Chart: Stress collar nose / MPa
| after collaring | after welding | after testing
SP101 | -153.3333 | -145.1471 | -117.1677
SP102 | -164.5386 | -162.6666 | -115.7812
SP103 | -133.3313 | -139.1813 | -116.3297
All 3 collared coils end up at the same stress after
testing
Mechanical instrumentation and measurements by Ph.Grosclaude and M. Guinchard

## Slide 19: Tuning pre-stress: Parameters which determine the coil pre-stress
Shimming plan:
Calculate given “arc length” by coils
Adapt lateral shims to “arc length” to create the required azimuthal excess
For fine tuning vary “pole-collar” shim
Based on FEA adapt “collar-yoke” shim
Goal: keep the azimuthal coil stress between -5 to -150MPa
Lateral shim
Arc length
Coil size up
Pole-collar shim
Coil size bottom
Collar-Yoke shim
Nominal values: Pole lateral=0.2mm Pole collar=0.2mm Collar yoke=0.4mm
Coil size=0.06mm Midplane=0mm

## Slide 20: Tuning pre-stress: Summary of build models
MBHSP101 (az-excess 376+250=626µm)
  Goal was to stay under the designed pre-load (azimuthal excess of 520µm)
  Flaw during assembly, unforeseen midplane shim of 0.25mm
MBHSP102 (657µm)
  Reproduce the shimming from SP101, without the midplane shim
  The loading pole in the transition region was made from one piece, stiffer transition
  Arc excess was 25% more than “as designed” state
MBHSP103 (857µm)
  Arc excess was increased to 60% more than “as designed” state
MBHDP101
  Combination of CC102 & CC103
  Increase of “collar-yoke” shim on CC102 by 50µm (CC102 never went stable to 12T)
Transition region

## Slide 21: Tuning pre-stress: History of build 1in1 models
(midplane shim 0.25mm)
Design based on lin. Coil modulus 30GPa
Peak azimuthal stresses occurring during excitation to 12T, not during assembly. Highest stress during assembly in coil block 4 during collaring (10% lower then stresses on midplane during excitation)
Values represent the average azimuthal stresses in one cable. Min always in coil block 4, max always in coil block 1

## Slide 22: Difference between single and double aperture structure
Chart: average azimuthal stress per outer cable of coil block at 12T (min-max over coil)
| CB4 | CB6 | CB1 | CB5
SP102 | 1.8716 | 3.3241 | -94.2809 | -97.7398
DP101-102 | -16.7297 | -2.8069 | -97.0568 | -104.7851
SP103 | 1.621 | 1.4883 | -103.8287 | -100.26
DP101-103 | -26.6876 | -10.6077 | -108.5685 | -114.2555
CB 1
CB 5
CB 4
CB 6
Delta 102 Coil Block 4 = -18.8MPa
Delta 103 Coil Block4 = -28.3MPa
Delta 102 Coil Block 6 = -6.1MPa
Delta 103 Coil Block6 = -12.1MPa
Mechanical instrumentation and measurements by Ph.Grosclaude and M. Guinchard

## Slide 23: Conclusions
Considerable number of training quenches up to nominal current in virgin condition, about 5 per coil (excluding coil 107)
Very few training quenches after thermal cycle
Remarkable performance with magnets in double aperture structure after reassembly: 0 quenches to nominal current, 2 quenches to ultimate.
Not a single quench at flattop.
Major steps in understanding of modeling made.
Double aperture predicted to have higher pole loading: Strong improvement of erratic/detraining quench levels.

## Slide 24: Thank you

## Slide 25: References and further reading
For mechanical measurements and comparison with FEA see:
  https://indico.cern.ch/event/496158/contribution/1/attachments/1226921/1796665/1602_11Tmech-inst_MSCTech_LOEF.pptx
For coil reference data and plans for mechanical characterization see:
  https://indico.cern.ch/event/496158/contribution/2/attachments/1226917/1796659/Material_Presentation_MDaly_CFichera_Final_43_v3.pptx
For more details about the FE-work on 11T (response analysis, stress analysis) see:
  https://indico.cern.ch/event/461705/contribution/0/attachments/1198897/1743732/151203_11Tmech_MSCtech_ToUpload_3.pptx
For sensitivity analysis see:
  https://indico.cern.ch/event/434223/session/1/contribution/16/attachments/1157669/1665137/1509_CERN_Model_assembly_and_sensitivity_CL.pptx
For mechanical measurements on superconducting magnets
  https://indico.cern.ch/event/487129/contribution/0/attachments/1214972/1774270/TE_MSC_Technical_meeting_21thJanuary.pptx
EDMS documents with cold powering results:
  MBHSP101: 1578771
  MBHSP102: 1578772
  MBHSP103: 1578773
  MBHDP101: 1578493

## Slide 26
History of new FE Models
18.8GPa Linear 10-18.8 GPa Non Linear
~ 50% extra shimming elastic
Initial Shimming (theoretical) | Shimming used in SP103 and DP101
Recent developments on 11T F.E. models have been presented during the
“Collaboration meeting on DS 11T Dipole grounds held at Fermilab”, September 2015:
http://indico.cern.ch/event/434223/
and during TE/MSC Technical Meetings:
“Mechanical aspects of the 11T magnet”, December 2015 https://indico.cern.ch/event/461705/
“Mechanical measurements in superconducting magnets” , January 2016:
https://indico.cern.ch/event/487129/
“Mechanical aspects of Nb3Sn magnets for HL-LHC - Session on measurement results” , February 2016:https://indico.cern.ch/event/496158/

## Slide 27: Virgin quench curves split out per coil

## Slide 28: Short sample limit as function of strain
Uncertainties in calculations of strain state of conductor in the midplane.
Stress and strain data strongly depends on directiOn.
Not a lof of measurement data available, data measured on PIT cables suggest 70 % reduction of Iq at 12.6 T may be possible with 150 Mpa of pressure on the broad face of the cable.
Critical Current Measurements of High-Jc Nb3Sn Rutherford Cables under Transverse Compression
B. Bordini, P. Alknes, A. Ballarino, L. Bottura, L. Oberli
cern cds 1662553

## Slide 29: Reason for diff. in stress in block 4 – Yoke deforms differently
Chart: Pressure in the yoke midplane
2in1 12T | -72.049 | -65.144 | -61.743 | -59.896 | -58.682 | -57.821 | -57.06 | -56.33 | -55.552 | -54.77 | -53.852 | -52.934 | -51.931 | -50.842 | -49.753 | -48.602 | -47.353 | -46.104 | -44.855 | -43.735 | -42.674 | -41.613 | -40.978 | -42.665 | -38.058 | -34.436 | -32.464 | -31.602 | -31.029 | -30.663 | -30.388 | -30.161 | -30.02 | -29.89 | -29.798 | -29.727 | -29.655 | -29.6 | -29.548 | -29.496 | -29.408 | -29.283 | -29.158 | -28.979 | -28.672 | -28.365 | -27.918 | -27.361 | -26.712 | -25.877 | -24.924 | -23.842
2in1 1.9K | -135.7 | -120.61 | -112.25 | -107.06 | -103.31 | -100.54 | -98.297 | -96.271 | -94.646 | -93.031 | -91.71 | -90.389 | -89.214 | -88.188 | -87.162 | -86.335 | -85.818 | -85.302 | -84.785 | -85.355 | -86.424 | -87.492 | -89.626 | -97.533 | -63.673 | -56.11 | -51.412 | -48.66 | -46.465 | -44.701 | -43.17 | -41.76 | -40.6 | -39.474 | -38.486 | -37.576 | -36.665 | -35.873 | -35.101 | -34.329 | -33.555 | -32.779 | -32.003 | -31.179 | -30.24 | -29.3 | -28.219 | -27.025 | -25.733 | -24.243 | -22.623 | -20.858
1in1
2in1
midplane
2in1 yoke “bends” during excitation around the collared coils.
Inward movement of the insert
2in1 deforms more

## Slide 30: Reason for difference in block 4 – Collar to Yoke interface at 12T
Chart: Collar to Yoke Pressure
midplane
45 degrees
midplane
45 degrees
2in1 stronger support at 45 degrees
2in1 yoke

## Slide 31: Extremities DS11T at 12T
Max. measured force is on the 2in1
The max. EM-force per aperture is 400kN
A force of 250kN in the 2in1 is a coil movement of 0.65mm
60% 2in1 & 45% 1in1 of total force seen in the end-plate (expected was 25%)
Chart: max. EM-force on end-plate at 12T
| DP102 | DP103 | SP101 | SP102 | SP103
CS | 212.82 | 210.4 | 123.2231 | 172.19 | 164.18
NCS | 224.39 | 242.7397 | 122.276 | 150.94 | 150.67
11T
Mechanical instrumentation and measurements where carried out by our colleagues from EN-MME Michael Guinchard <michael.guinchard@cern.ch> Philippe Grosclaude <philippe.grosclaude@cern.ch

## Slide 32: Summary of model shimming
Chart: 11T-model shimming summary
| as designed (coil#) | MBHSP101 (106/107) | MBHSP102 (106/108) | MBHSP103 (109/111) | MBHSP104 (112/113)
top collar-diameter | 0 | -50 | 0 | 0 | 0
bottom collar-diameter | 0 | -50 | 0 | 0 | 0
top collar-yoke | 400 | 360 | 410 | 410 | 410
bottom collar-yoke | 400 | 360 | 410 | 410 | 410
top pole-coil | 200 | 100 | 250 | 250 | 250
bottom pole-coil | 200 | 100 | 200 | 250 | 250
top coil size | 60 | 150 | 100 | 250 | 140
bottom coil size | 60 | 150 | 40 | 40 | 250
midplane shim | 0 | 250 | 0 | 0 | 0
total azimuthal excess | 520 | 626.2537 | 656.6667 | 856.6667 | 890

## Slide 33: FE - 2in1 - Shell to Coil - stress relation (warm)
As soon as the yoke gap is closed most force are transmitted in the yoke
Manageable risk to not over stress the coil during the welding operation
Main goal of the welding is to close the yoke gap at room temperature
Chart: Shell Displacement (nom: 0.65) / mm
| 0 | 0.2 | 0.4 | 0.6 | 0.8 | 1 | 1.2 | 1.6 | 1.8 | 2 | 2.2000000000000002 | 2.4 | 2.6 | 2.8 | 3 | 3.2 | 3.4 | 3.6
Traction-SG Shell | 52.241 | 100.9225 | 161.5 | 235.35 | 310.915 | 390.01 | 470.6 | 631.725 | 712.245 | 792.69 | 873.045 | 953.41 | 1033.72 | 1113.975 | 1194.235 | 1274.42 | 1354.575 | 1434.71
Stress Intensity - coil (Max) | 91.037 | 104.83 | 115.7 | 119.53 | 122.61 | 124.8 | 126.67 | 130.43 | 132.31 | 134.33 | 136.46 | 138.63 | 140.81 | 142.99 | 145.21 | 147.47 | 149.73 | 152.05