## Slide 1: Transfer function

## Slide 2: TRANSFER FUNCTION (TF)
Possible sources of error
  Iron properties
  Packing factor of the yoke laminations
  Geometric
Chart: I (A)
measured | 1985.7464 | 53.0736 | -43.0304 | -34.7658 | -42.5924 | -40.7692 | -28.8462 | -17.6129 | -10.197 | -6.1776 | 0 | -0.38536 | -17.1292 | -59.6204 | -122.2446 | -196.0211 | -274.1616 | -353.0663 | -373.3222
Discrepancy ~ 50 units between measured and expected values.

## Slide 3: Comparison to MB dipole
Chart: DS-Dipole
measured | 1985.7464 | 53.0736 | -43.0304 | -34.7658 | -42.5924 | -40.7692 | -28.8462 | -17.6129 | -10.197 | -6.1776 | 0 | -0.38536 | -17.1292 | -59.6204 | -122.2446 | -196.0211 | -274.1616 | -353.0663 | -373.3222
At the same level of saturation we have similar agreement in the case of the MB dipole
[P. Hagen]

## Slide 4: Saturation @ Imm = 11.25 kA

## Slide 5: Data from production
Chart: H [A/m]
Chart: H [A/m]
Review of data available from LHC production on going trace back what are the most relevant samples to look at.
Sample 950155
REF: Production of Low-Carbon Magnetic Steel for the LHC Superconducting Dipole and Quadrupole Magnets. LHC Project Report 898

## Slide 6: Further investigation on the iron MP
Analysis made based on BH data from the LHC MB production show the same saturation as the one obtained using “BH IRON LHC”
BH DATA | diff in the TF (units)
bh iron LHC | REF
bhiron2 (ROXIE standard) | -26
bh fit as in Stephan's book | -9
bh sample 955310 | -2
bh sample 954231 | 0
bh sample 950155 | 0
bh tentem (opera) | -49
No impact!
Critical!!

## Slide 7: Importance of iron characterization at higher field levels
A shift of + 0.1 T at H>2.0E+4 A/m with respect to the “LHC production data” is enough to fit MBHSP101 and MBHSP102 measurements

## Slide 8: TF:Packing factor of the yoke laminations
Chart: I (A)
| 1000 | 2000 | 3000 | 4000 | 5000 | 6000 | 7000 | 8000 | 9000 | 10000 | 11000 | 12000
 | 0 | 0 | 0 | 0.25085 | 1.0034 | 4.0135 | 7.8838 | 10.7864 | 12.1521 | 13.6461 | 14.5947 | 15.887
The difference can be partly explained by the 100 % packing factor of the iron laminations observed during magnet assembly
[C. Loffler]
Difference in computed transfer function for 98.5% and 100% packing factor
With the packing factor we can potentially explain ~ 15 units (out of 50)

## Slide 9: TF: Geometric
If the coil is shifted outwards radially, the iron saturation increases (goes in the bad direction). In addition to that, only ~13 units for 350 µm radial shift, so big radial displacement (inwards) is needed to explain 50 units of discrepancy.
Chart: Radial shift (mm)
| 0 | 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35
 | -464.8566 | -466.6989 | -468.6398 | -470.5835 | -472.5299 | -474.4791 | -476.33 | -478.2798
Yoke shrinkage (coil shrinkage = 0 mm/m) |  |  | 
Yoke shrink. | TF 20A | TF 11.25 kA | units of sat
0 mm/m | 9.941E-04 | 9.479E-04 | -465
2 mm/m | 9.949E-04 | 9.481E-04 | -470
Coil shrinkage (yoke shrinkage = 0 mm/m) |  |  | 
Coil shrink. | TF 20A | TF 11.25 kA | units of sat
0 mm/m | 9.941E-04 | 9.479E-04 | -465
3 mm/m | 9.960E-04 | 9.502E-04 | -460
Design assumptions on coil/yoke warm2cold dimensions
  Yoke shrinkage = 2 mm/m
  Coil shrinkage = 3 mm/m
REMARK: Analysis performed using standard ROXIE bh data (bhrion2)
5 units less of saturation if yoke shrink. = 0 mm/m (goes in the good direction), but 5 units more of saturation if coil shrink. = 0 mm/m (goes in the bad direction)

## Slide 10: TF: Summary
Measured saturation is lower than the one predicted by the model. Sources of error:
  BH data: the discrepancy can be reduced from 70 units to 50 units, if bh data from LHC production is used instead of the standard roxie bh2 data. A shift of + 0.1 T at H>2.0E+4 A/m with respect to the “LHC production data” is enough to fit MBHSP101/MBHSP102/MBHSP103 measurements
  Packing factor of the iron laminations: discrepancy can be reduced from 50 units to 35 units if a packing factor of 100 % instead of 98.5 % is considered.
  To explain 35 units of discrepancy by shifting radially the coil, the coil should be moved inwards by almost 1 mm, which is unrealistic

## Slide 11: Decay and snapback

## Slide 12: Decay and snapback
decay
snapback
Definition of decay and snapback. Behaviour in the LHC MB dipoles
N. Aquilina

## Slide 13: MBHDP101
Different state of magnetization in the 1st ramp up
Increase of magnetization at the injection plateau!!
Decay?
Snapback?
1st ramp up
2nd & 3rd ramp up

## Slide 14: LHC MB vs. 11 T
Sign inversion on the harmonics! It seems that in the 11 T the strand magnetization is increasing instead of decreasing.
Bottura

## Slide 15: Main field
Main field noisy, but an increase on magnetization is also visible!
Injection Plateau

## Slide 16: LHC MB vs. 11 T
Make plots for the 11 T
Sammut (magnets on the test bench, not under LHC standard operation cycle)

## Slide 17: SB Exponential fitting
SB + PC
SB only

## Slide 18: SB Exponential fitting
 | b3-decay | ΔI (A)
MBHSP102 | -1.2 | 2
MBHSP103 | -0.7 | 1
MBHDP101-Ap1 | -0.89 | 1.5
MBHDP101-Ap2 | -0.89 | 1.5
Remark: in the LHC dipoles
Analysis done with the data on the central segments.

## Slide 19: LHC MB vs. 11 T
The ‘shape” of the field harmonics due to strand magnetization is similar for the LHC-MB dipoles and for the 11 T.
    What can be the origin of this different behaviour in terms of decay and snapback?
The only difference is that in the 11 T dipole inner and outer layer are wound together, and in the LHC-MB there is a splice in between the layers

## Slide 20: Injection level study
Remember, for B lower than ~ 2 T, flux jumps are visible in the strand magnetization data. In the three current levels, the field in the coil is < 2T.
760 A
1100 A
1700 A
Fiscarelli

## Slide 21: Injection level study

## Slide 22: Consistency checks
From: L. Bottura. Decay and Snap-back in LHC Main Magnets; Prepared for the Mini-Workshop on Decay and Snapback in Superconducting Magnets. Fermilab, November 8th, 2002.
Consistency checks:
current distribution depends on powering history 
  Flattop current study and flattop duration study, same trend than LHC-MB dipoles

## Slide 23: Flat top current study
LHC: scaling for long magnets similar to short models
11 T
Decay increase (in absolute value) at increasing the flat-top current, both in LHC dipoles and 11 T.
LHC MB
Bottura
Fiscarelli

## Slide 24: Flat top current duration
Decay decrease at increasing flat-top duration, both in LHC dipoles and 11 T.
Saturation of decay & SB
LHC MB
11 T
Bottura
Fiscarelli

## Slide 25: Consistency checks
From: L. Bottura. Decay and Snap-back in LHC Main Magnets; Prepared for the Mini-Workshop on Decay and Snapback in Superconducting Magnets. Fermilab, November 8th, 2002.
Consistency checks:
current distribution depends on powering history 
larger decay & SB observed close to the ends of long magnets, where current imbalance is larger X
  We don’t see this, but maybe we don’t have enough statistics, and this is only clearly seen in long magnets.

## Slide 26: Consistency checks
From: L. Bottura. Decay and Snap-back in LHC Main Magnets; Prepared for the Mini-Workshop on Decay and Snapback in Superconducting Magnets. Fermilab, November 8th, 2002.
Consistency checks:
current distribution depends on powering history 
larger decay & SB observed close to the ends of long magnets, where current imbalance is larger X
current distribution saturates for times comparable (or longer) than the characteristic time 
  Longer characteristic time in the 11 T magnet when compared to the LHC MB.

## Slide 27: Injection time
Longer time constant for the 11 T.
The smaller amplitude of the decay in the 11 T is due to this longer time constant.
  They saturate to more or less the same value (I would expect Δb3 to be larger in the 11 T as strand magnetization is 10 times larger)
Sammut

## Slide 28: Consistency checks
From: L. Bottura. Decay and Snap-back in LHC Main Magnets; Prepared for the Mini-Workshop on Decay and Snapback in Superconducting Magnets. Fermilab, November 8th, 2002.
Consistency checks:
current distribution depends on powering history 
larger decay & SB observed close to the ends of long magnets, where current imbalance is larger X
current distribution saturates for times comparable (or longer) than the characteristic time 
current distribution change does not depend on temperature changes 
  If the magnet is tested again, can we do a machine cycle at 4.2 K?
the SB does not depend on the acceleration ramp, quasi-DC process 

## Slide 29: Temperature
LHC MB
Bottura

## Slide 30: Consistency checks
From: Decay and Snap-back in LHC Main Magnets; Prepared for the Mini-Workshop on Decay and Snapback in Superconducting Magnets. Fermilab, November 8th, 2002.
Consistency checks:
current distribution depends on powering history 
larger decay & SB observed close to the ends of long magnets, where current imbalance is larger X
current distribution saturates for times comparable (or longer) than the characteristic time 
current distribution change does not depend on temperature changes 
the SB does not depend on the acceleration ramp, quasi-DC process 

## Slide 31: Ramp Rate Dependence
-10A/s
40A/s
20A/s
80A/s
40 A/s not usable, there is a small drift on the current at 760 A (1A)
It is compared to the three standard machine cycle (RR=10 A/s)

## Slide 32: Ramp rate
LHC MB
LHC MB
Bottura
Bottura
There is no dependence on the ramp rate in MBHDP101.
The frequency of the acquisition is not enough to capture the decay at RR=20A/s and RR=80 A/s

## Slide 33: Consistency checks
From: Decay and Snap-back in LHC Main Magnets; Prepared for the Mini-Workshop on Decay and Snapback in Superconducting Magnets. Fermilab, November 8th, 2002.
Consistency checks:
current distribution depends on powering history 
larger decay & SB observed close to the ends of long magnets, where current imbalance is larger X
current distribution saturates for times comparable (or longer) than the characteristic time 
current distribution change does not depend on temperature changes ?
  We need more data to check this
the SB does not depend on the acceleration ramp, quasi-DC process 