## Slide 1
Advances in thin film lead photocathodes
R.Nietubyć, J. Lorkiewicz, J. Sekutowicz

## Slide 2
Milestones
Deliverables

## Slide 3
Eucard2 obligations
D. 12.8.
Optimised procedure for microdroplets flattening with an UV laser
Optimised procedure for preparation of flat, clean and adherent Pb/Nb films
Change the Deliverable
Reason
We found that plasma pulsed irradiation is more effective that the laser one. Basically we learned how thick layer must be deposited to undergo a right change caused by energy deposition.
Delay

## Slide 8
… towards D12.9 Pb/Nb plug photocathodes measurements and characterization at HZDR
The maximum program for the experiment would be: 1. assembling the Pb-coated plug in the vacuum chamber, 2. laser- cleaning accordingly to John's recipe, 3. measure QE at ca. 260 nm , 4. irradiate the cathode for several weeks in total (can be done
in many shorter periods) with your laser: 0,5 W, 500 kHz, 10 ps , 260 nm 5. measure QE again.
Further steps…

## Slide 9
1 plasma pulse of 1.8 J/cm2
15 µm Pb underway…
Too thin and thus perforated
8 µm Pb
UHV arc deposition
X 500
X 1000
12 µm Pb
1 plasma pulse of 1.5 J/cm2
2 pulses of 1.5 J/cm2
3 pulses of 1.5 J/cm2
X 1000
X 1000
X 2000
Distinct areas of perforations size of which did not exceed 10 µm
non-coated area amounting to 3-5% of the total layer surface.
20 µm
20 µm
20 µm
Eucard2 - 2nd Annual Meeting, 22.04.2015, Barcelona
Pb/Nb until April 2015

## Slide 10
20 µm
20 µm, 5 × 1.5 J/cm2
12 µm, 2 × 1.5 J/cm2
Further flattening

## Slide 11
50 m
10 µm, 25  1 J/cm2 without shielding
10 µm, 25  1 J/cm2 through a hole in mask
3 mm
We found that surface morphology depends on that whether it was irradiated with a mask or without it. Mask impedes an energy transfer from pulse to layer. It leaves crater and droplets remnants
Further flattening

## Slide 12
20 m
Laser cleaning
Plasma irradiation leaves surface smooth Laser treatment increases the QE a lot. This is accompanied with the roughenieng the surface
20 m
17 µm, 5  1.5 J/cm2 through a hole in mask
20 m

## Slide 13
In depth propagation of melting and evaporation fronts. 1. – bulk melting, 1.5 J/cm2; 2. – droplets melting 1.5 J/cm2; 3. – bulk melting, 1 J/cm2; 4. – droplets melting 1 J/cm2; 5. – bulk evaporation, 1.5 J/cm2; 6. – droplets evaporation, 1.5 J/cm2; 7. – bulk evaporation, 1 J/cm2; 8. – droplets evaporation, 1 J/cm2
Calculations for 1 J/cm2
We managed to decrease the plasma pulse energy to get the fluency of 1 J/cm2 . This reduces the samples thickness needed to survive. Corresponding heat transfer calculations have been performed

## Slide 14
X-ray diffraction
10 µm, 25  1 J/cm2
no shielding
no filtering
5 µm, 10  1 J/cm2
no shielding
filtering
Measured with Cu K1,2 with a laboratory diffractometer in -2 geometry
50 m
[111] texture occurs for both layers, for thicker layer however no other orientation can be seen.
Does it come from thickness or from irradiation?
Photoemission dependence on surface orientation will be studied by calculations
Intensity [a.u]
2  [deg]
2  [deg]
Intensity [a.u]

## Slide 15
Fine scan of 333 reflections. Lattice constants and crystallites in-depth dimension [111] evaluated with Scherrer formula:
5 μm filtered D111=115nm a= 4.9519 Å
10 μm unfiltered D111=141nm a=4.9529 Å
X-ray diffraction
Rocking curve around reflex 333. It gives the distribution of [111] crystalline plane orientations relative to sample surface
Spread of crystallite orientation in thocer layer is smaller
Intensity [a.u]
Intensity [a.u]
2  [deg]

## Slide 16
Nd:YAG laser, 2nd harmonic: 25 mJ/pulse, 20 Hz, 10 ns
Xe lamp 150 W  0.5 W in 200 – 210 nm
Czerny-Terner monochromator,
Optical fiber
picoamperometer, measures above 10 pA
Turbo- and scroll- pumps give 10-7 mbar
QE measurement setup

## Slide 17
QE measurement setup
Optical fiber
Faraday cup for breakdown
Anode holder with an optical fiber and mirror
sample
Sample holder rotates to enable laser cleaning
For breakdown measuremes, the distance between sample and anode can be adjusted with accuracy of 0.25 mm
HV pulse is 12.5 kV during 1ms
 50 MV/m

## Slide 18
Cleaning
YAG harmonic 532 nm 5 mJ/ (mm2 pulse) , 10 Hz  0.05 W
Excimer Kr 190 nm 10 J/ (mm2 pulse) , 300 Hz  0.003 W 2010
240 nm, 60 J/(mm2 pulse), 105 pulses 2015 (DESY& BNL)
Mesurements
We need
50 pA at 200 nm while QE-10 -5  30 W of light on the sample
50 pA at 250 nm while QE-10 -6  250 W of light on the sample
We measured 20 pA (10 pA above the noise) while using white light and dirty sample
Next Steps:
clean the sample with laser
or with glow discharge
improve the transmission, mostly mirror reflection
QE measurements

## Slide 19
Optimised procedure for preparation of flat, clean and adherent Pb/Nb films
Delay
We are going to produce a number of Pb/Nb samples
flattened down to roughness < 1 m
with QE measured higher than 1.510-4 at 260 nm
For that we need to prepare cleaning with excimer laser. Unfortunately it will not be possible this year, so we will try to substitute it with Nd:YAG 2nd harmonics and look for other cleaning methodes
We expect to be ready about November 2016
Delivery D12.8

## Slide 20
Summary
We reached the satisfactory flatness
XRD studies
QE measurements will be launched
 cleaning capabilities
QE measurements vs laser irradiation time (DESY, HZDR)