## Slide 1: Microwave SQUID multiplexer for the readout of large MMC arrays
Mathias Wegner
01.06.2016

## Slide 2
Contents
Metallic magnetic calorimeters
From single detectors to very large arrays
Microwave SQUID multiplexer
Multiplexer chip design
Experimental results
Summary and outlook

## Slide 3
Metallic magnetic calorimeters
Absorber
Pickup-coil
Weak thermal link
Thermal bath @ T ~ 30 mK
To SQUID
Paramagnetic
sensor
Magnetic
field
Signal rise
t0 < 100 ns
Signal decay
t1 > 1 ms
Detector principle
Fundamental energy resolution
Micro calorimeter operated at
low temperatures T < 50 mK

## Slide 4
Single channel detector performance
Semiconductor
detector
55Mn, Ka
5.9 % @ 60 keV
Fast signal rise time
Very good energy resolution
Excellent linearity
DEFWHM = 1.6 eV @ 6 keV
t0 < 100 ns
Three world records related to microcalorimeters
Metallic magnetic calorimeters

## Slide 5
Metallic magnetic calorimeters
Absorber
Stems
Paramagnetic sensor
Meander-shaped
pickup coil
dc-SQUID
SQUID input coil
Detector geometry

## Slide 6
Why dc-SQUID readout?
Single channel dc-SQUID readout
dc-SQUID operation principle
dc-SQUID = periodic flux to voltage converter
Operation at very low temperatures
Quantum limited noise level
Very large bandwidth
Ic
Ic

## Slide 7
Signal linearization (flux locked loop)
Single channel dc-SQUID readout
Linear range of dc-SQUID response very small (F < F0/4)
Negative flux feedback for compensation of initial flux change

## Slide 8
Double-stage SQUID configuration
Single channel dc-SQUID readout
Semiconductor amplifiers have much higher noise level than SQUIDs
Making use of a 2nd dc-SQUID for signal amplification
Large bandwidth
Very low noise
Low power dissipation
T = 300 K
T < 100 mK
100 mK … 4 K

## Slide 9
Application: The ECHo experiment
Electron capture of 163Ho
t1/2 = 4570 y
QEC = 2833(30)stat(15)sys eV
Calorimetric measurement of decay spectrum
Embedded holmium in absorber:
Quantum efficiency > 99.99%
Measure independent of BR
Absorber top
Absorber bottom
AuEr sensor
Detector bias
Implanted 163Ho

## Slide 10
Application: The ECHo experiment
Calorimetric spectrum of 163Ho
Sub-eV sensitivity for ne mass requirements
Statistics: Nev > 1014 Activity: A ~ 10 Bq / pixel Large arrays: Ndet > 105
Non-vanishing electron neutrino mass distorts spectrum around endpoint

## Slide 11
Towards large MMC detector arrays
Single detector channel requires:
- 2 SQUIDs
- 10 wires
- Room temperature electronics
Duplication of single-channel readout not scalable
Number of wires
Parasitic heat load
System complexity
Costs
How to read out such large number of detector channels?
Multiplexing necessary
~ N of channels - time domain
- freqency domain
- …
Why is multiplexing mandatory?

## Slide 12
Example: Radio frequencies in Stuttgart
Towards large MMC detector arrays
Frequency domain multiplexing
System bandwidth divided into non-overlapping frequency bands
Modulation of carrier frequency by low frequency signal (amplitude, frequency,…)
Advantage: Simultaneous signal transmission of all channels
amplitude
frequency
89.5 MHz
BigFM
92.3 MHz
SWR3
96.2 MHz
SWR2
103.9 MHz
Klassik Radio

## Slide 13
Towards large MMC detector arrays
Components for cryogenic frequency domain multiplexing
Josephson junction
Tank circuit
Carrier frequency selection
Non-linear element

## Slide 14
The microwave SQUID multiplexer
Superconducting coplanar waveguide l/4 resonators
transmission
frequency
fr
Operation at cryogenic temperatures T < 100 mK
Quality factors Qi > 100.000 possible extremely low power consumption
Resonance frequencies to GHz possible large bandwidth per channel

## Slide 15
The Josephson junction
The microwave SQUID multiplexer
1. Josephson equation:
2. Josephson equation:
Non-linear inductance
Phase difference:
Supercurrent: Is
Voltage: V

## Slide 16
The microwave SQUID multiplexer
Phase difference f given by magnetic flux F through the SQUID loop
rf-SQUID = flux dependent inductance
Dissipationless compared to dc-SQUIDs
F
Tank
circuit
LJ
LS
LT
k
rf-SQUID operation
Tank
circuit
Ltot
CT

## Slide 17
Principle single multiplexer channel
Feedline
Single detector
rf-SQUID
Superconducting
quarter-wave
resonator
Energy deposition in absorber
Magnetic flux change in
related temperature sensor
Magnetic flux change
In rf-SQUID
Shift of resonance frequency of corresponding resonator
Monitoring resonance
frequency shift
The microwave SQUID multiplexer

## Slide 18
transmission
frequency
signal
time
fr
The microwave SQUID multiplexer

## Slide 19
fexc
time
temperature
transmission
frequency
time
amplitude
multiplexer
in
out
f1
f1
The microwave SQUID multiplexer

## Slide 20
Injection of
frequency comb
Extraction of
amplitude
Energy input in channel 3
The microwave SQUID multiplexer
Principle N multiplexer channels
Two cables and one amplifier for the readout of hundreds of channels
f1
f2
f3
fN

## Slide 21
amp
[MHz]
[GHz]
amp
[MHz]
[GHz]
The microwave SQUID multiplexer
Software defined radio (in development)
FPGA
DAC
ADC
µMUX
FPGA
DAC
ADC
µMUX
amp
[MHz]
[GHz]
amp
[MHz]
[GHz]
Signal
modulation

## Slide 22
The microwave SQUID multiplexer
Flux ramp modulation (in development)
rf-SQUID output strongly non-linear (periodic as dc-SQUID)
Linearization with FLL impossible for multiplexer (2 wires per channel)

## Slide 23
The microwave SQUID multiplexer
Flux ramp modulation (in development)
Linearization by transducing SQUID output signal into a phase shift
Simultaneous linearization of hundreds of channels using only 2 wires

## Slide 24
The microwave SQUID multiplexer
Flux ramp modulation (in development)
Linearization by transducing SQUID output signal into a phase shift
Simultaneous linearization of hundreds of channels using only 2 wires

## Slide 25
The microwave SQUID multiplexer
Multiplexer Chip
Simultaneous readout of N detector channels
First prototypes available and operationable
Software Defined Radio
FPGA based readout of multiplexer
in development
Flux Ramp Modulation
rf-SQUID linearization
in development
Microwave SQUID multiplexing components
Very large bandwidth
Very low noise level
Linear response

## Slide 26
Multiplexer Chip Prototype
On-chip heat bath
HF input
Detector array
HF output
64 MMC pixels with on-chip multiplexer
rf-SQUIDs
Detector bias
9.1 mm
Superconducting
microwave resonators
19 microfabricated layers: sputtering, wet & dry etching, electroplating…
Meander-shaped
pickup coil
Weak thermal link
Au absorber on stems
on AgEr300ppm sensor
To SQUID
input coil
Thermal bath

## Slide 27
Multiplexer Chip Prototype
On-chip heat bath
HF input
Detector array
HF output
64 MMC pixels with on-chip multiplexer
Detector bias
9.1 mm
Superconducting
microwave resonators
19 microfabricated layers: sputtering, wet & dry etching, electroplating…
rf-SQUIDs
To resonator
To detector
Washer coil
Modulation coil
Input
coil
Josephson
Junction
-
-
+
+

## Slide 28
Multiplexer Chip Prototype
On-chip heat bath
HF input
Detector array
HF output
64 MMC pixels with on-chip multiplexer
Detector bias
9.1 mm
Superconducting
microwave resonators
19 microfabricated layers: sputtering, wet & dry etching, electroplating…
rf-SQUIDs
Coplanar
waveguide
Elbow coupler
Common
feedline
HF range 4 … 8 GHz
Bandwidth ~ 1 MHz

## Slide 29
Multiplexer Characteristics
Characterization by means of a vector network analyzer
Resonance frequency shift by rf-SQUID close to design value
Imod = -14 … +12 uA
fixed SQUID flux
Dfmax ~ 1 MHz
fr (F)

## Slide 30
Multiplexer Performance
First demonstration of multiplexed readout 2016
Fully analog setup with 2 HF signal generators
Simultaneous acquisition of signals from two independent MMC detectors

## Slide 31
Multiplexer Performance
Signal size & noise performance
  Low pulse height due to high chip temperature and too less persistent current
  Increased flux noise level due to low read-out power of multiplexer
  t0 ~ 640 ns
  t1 ~ 340 µs
  TChip > 50 mK
  1.6µF0/√Hz

## Slide 32
Multiplexer Performance
  Energy resolution degraded due to small signal size and too high noise level
  Different performance due to different signal-to-noise ratios
DEFWHM = 64 eV @ 6 keV
DEFWHM = 87 eV @ 6 keV
Channel 1
Channel 2
  55Mn
  55Mn

## Slide 33
How to improve?
200 µm
Simulations for optimizing multiplexer parameters in progress
Problem: Heat bath very large (1.5 cm)
Solution: Heatsink pixels to chip backside
Chip temperature > 50 mK
Rather large noise level
Pixel 1
Pixel 2
Wafer
Hole with Au
  Energy resolution DEFHWM < 10 eV possible in near future
Thermal bath on chip backside

## Slide 34: Summary & Outlook
Excellent performance of metallic magnetic calorimeters
Single channel readout not possible for large arrays
Microwave SQUID multiplexer suited for readout of large arrays
First simultanous readout of two detector channels demonstrated
Detector performance degraded due to:
  High chip temperature
  Non-optimal sensor magnetization
  Rather high noise level
New detector thermalization and multiplexer simulations in progress
DEFWHM < 10 eV possible in near future

## Slide 35: Thank you for your attention