## Slide 1
The nanoUCx and the new ISOLDE n-converter: status and future developments
P. Bricault, A. Gottberg, W. Hwang, R. Luis, T.M. Mendonca, L. Popescu, T. Stora and others
João Pedro RAMOS (CERN)
EN-STI-RBS

## Slide 2: Outline
  New n-converter
Motivation
Design and simulations
Concept prototype
Future: design of the optimized n-converter
nanoUCx
Motivation
Material development
Prototype testing
Future: production upscaling
    Release fundamentals
(The new UO2 batch)

## Slide 3: Motivation
Neutron-rich fission fragments are very important for physics research
  However they come with huge neutron deficient isobaric contaminations
Use neutron converter
  Suppression of isobaric contaminants (n-rich)
Geometry could be further optimized
  Important for all ISOL facilities
Pictures courtesy of Raul Luís
p beam

## Slide 4: Design and optimizations
Thicker UCx target
to increase the 238U mass
old radius = 0.7 cm
new radius = 1.5 cm
Diagonal cut in the
UCx Target
to avoid the highest proton fluences
Shorter UCx target
to remove the region with
higher proton fluences
old length = 20 cm
new length = 10 cm
Thicker spallation target
to better “contain” the proton fluences
old radius = 0.6 cm
new radius = 1.4 cm
Slide courtesy of Raul Luís

## Slide 5: Design and optimizations
UCx target concentric to the converter:
Improve interaction probability with neutrons
Make target thinner (better for release efficiency)
Pictures courtesy of Raul Luís
2nd optimized design
yield gains in neutron-rich isotopes
yield reductions in neutron-deficient isotopes

## Slide 6: Concept prototype testing at ISOLDE
Case of 80Zn/80Rb ratio – 220
Simulations predicted ~ 20
A. Gottberg, T.M. Mendonca, R. Luis, J.P. Ramos, C. Seiffert, S. Cimmino, et al.,NIMB 336 (2014) 143–148.
Simplified version of the optimized of the n-converter:
Power supply limit 1000A
Limited target operation temperature to 1750oC
  Standard operation 1950-2100oC
Conventional
New
Zn
Rb

## Slide 7: Future
Build the optimized converter for ISOLDE
  Engineering challenges that will have to be overcome
    ANSYS – thermal simulations
      Beam power deposition
      Oven - heating by Joule effect
    FLUKA
      Neutron and proton fluences
      Beam power deposition
      Isotope production
  Reproduction of converter in other ISOL facilities (TRIUMF and SCK-CEN):
  Cope with higher beam powers
  Different target and ion source systems
Pictures courtesy of S. Cimmino
?

## Slide 8
4. Ionization
3. Effusion
2. Diffusion
1. Production
(Nuclear Reactions)
+/- 8V
500 A
+/- 9 V
1000 A
Ion Source
Pulsed
Protons
Proton
– Proton flux
– Cross section for reaction
– Number of exposed atoms
nanoUCx
Status update
UCx takes >70% of beam time

## Slide 9: Production Procedure
Wet Planetary milling
UO2
(18 μm to 160 nm)
Isopropanol - IPA
𝑈𝑂2+6𝐶→𝑈𝐶2+2𝐶+2𝐶𝑂
Vacuum
Ultrasonication, mixing with MWCNT and drying
+
+
Pressing porous compacts
Final material (UCx + MWCNT)
22 m2/g and 75% porous pellets
Target – 11.4 g/cm2 (0.6 g/cm3)
  Conventional is ~28 g/cm2 (1.4 g/cm3) 2x more (actinide waste)
Powders Dry Mixing
UO2 (18 μm) + Graphite (30 μm)
Pressing porous compacts
𝑈𝑂2+6𝐶→𝑈𝐶2+2𝐶+2𝐶𝑂
Vacuum
 | Conventional UC |  | nanoUCx |  | Factor
 | Before | After | Before | After | 
Surface A. (m2/g) | 5.2 | 0.1 | 30 | 22.1 | +220x
Porosity | 47% | 56% | 67% | 76% | +35%
Density (g/cm3) | 4.5 | 3.67 | 1.89 | 1.95 | -47%
Conventional UCx
nanoUCx
400 nm
87x smaller scale
A. Gottberg, et al.

## Slide 10: Nano Uranium Carbide Online at ISOLDE
Chart: yield [µC-1]
| 8Li (#466 UC-Re) | 9Li (SC) | 25Na | 26Na (SC) | 30Na | 46K (SC) | 50K | 50Ca | 68Cu (highest DB entry) | 68mCu (highest DB entry) | 76Ga (highest DB entry) | 81Ga (highest DB entry) | 81Rb | 88Rb (#493 UC-Ta) | 93Rb (SC) | 96Rb (SC) | 132In | 142Cs (#477 UC-W) | 139Cs (#477 UC-W) | 207Fr (SC)
ISOLDE Conventional UCx | 4100000 | 3900000 | 290000000 | 600000000 | 51000 | 8900000 | 50000 | 24000 | 80000000 | 300000000 | 10000000 | 200000 | 170000 | 400000000 | 130000000 | 14000000 | 8000 | 400000000 | 1500000000 | 2300000
ActILab nano UCx | 28000000 | 19000000 | 2800000000 | 920000000 | 140000 | 390000000 | 86000 | 68000 | 960000000 | 340000000 | 29000000 | 1100000 | 22000000 | 8000000000 | 260000000 | 15000000 | 17000 | 1100000000 | 2100000000 | 85000000
A. Gottberg, et al.
ActILab
T1/2=59.6 s
840 ms
178 ms
59.6 s
1.07 s
48 ms
115 s
472 ms
13.9 s
30 s
3.8 m
32.6 s
1.22 s
4.58 h
17.8 m
5.84 s
1 s
0.20 s
1.7 s
9.3 m
14.8 s
T1/2=48 ms

## Slide 11: The New UO2 batch
Chart: Manganese Yields(μC-1)
| 63 | 64 | 65 | 66 | 68
IDS | 6000 | 1000 | 500 | 13 | 7
Data Base | 150000000 | 1700000 | 200000 | 7000 | 1000 | 170 | 4
Yield checks | 180000000 | 6000000 | 560000
Target at 1990oC
Ta source at 1780oC
(quartz cold line reduces intensity down to 1/2)
Chart: Cadmium Yields (μC-1)
| 132 | 132 | 131 | 130
IDS | 1 | 0.4 | 16.8 | 901
Database | 10 | 1000 | 10000
Target at 2050oC
Ta source at 2000oC
Protons on converter
Towards the end
Chart: Al and Mg Yields (μC-1)
| 1
Yield Checks Al | 180
Yield Checks 2 Al | 410
IDS Al | 150
ISOLTRAP Al | 280
Database Al | 86
Yield Checks Mg | 140
Yield Checks 2 Mg | 450
IDS Mg | 400
Database Mg | 140
Yield Checks
IDS/ISOLTRAP
Database
 | μC-1 | DB
30Mg | 2.3E6 | 6.0E5
30Al | 3.2E6 | 5.7E6
33Mg | 3.0E3 | 3.0E3
Small difference in impurities to old batch
To be done: Material characterization and comparison to old batch
Physics yields courtesy of IDS and ISOLTRAP
Target at 1900-2000oC
Ta source at 2000-2050oC
Protons on target
No quartz
#550
#547 & #548
#543
162 ms
68 ms
97 ms
4.6 s
0.71 s
0.25 s
89 ms
92 ms
64 ms
28 ms
20 ms
56 ms
ISOLTRAP | μC-1 | DB
46Ar (7.8 s) | 1.3E4 – 1.3E5 | -
47Ar (1.23 s) | 7.2E2 – 1.4E3 | 9.6E3
Target at 1900oC
Ion Souce at 1950oC
#541
Ar Yields
Kr2+ impurities – 4 to 70x
Good Physics
Material generally operated at conservative temperatures!!
Margin for improvement!

## Slide 12: For the future
nanoUCx
New UO2 batch
Old UO2 batch
?
upscaling
+
CNT
+
+
nanoUCx production:
2 persons, 1 month  1 target
WANT: 1 person, 1 week  1 target
FACTOR 8
Current issues:
Milling results not exactly reproducible
Too much liquid involved to produce 1 target (7 L)
  CNT are the problem (5g need 1.4 L of IPA)
nanoUCx v2.0
Fundamental studies on the release of isotopes from UCx
  Diffusion and effusion from nanomaterials
    A lot of data from UCx and now nanoUCx
  Target material physical-chemical and morphological properties influence on the yields and release time structure

## Slide 13: End
Thank You!
Questions or comments?

## Slide 14
D = constant
Reduction of 100x grain size
from μ2 to μ1
time after proton impact
Theoretically 5x more yield!
ν1= ν2 = 5 s-1 (200 ms)
μ1 = 2 s-1 (500 ms)
μ2 = 0.02 s-1 (50 s)
Diffusion limited vs. Effusion limited
ν1 = 0.8 s-1 (1.25 s)
μ1 = 10 s-1 (100 ms)
ν2 = 20 s-1 (50 ms)
μ2 = 0.03 s-1 (33 s)
Release time structure similar to many nanomaterial targets
time after proton impact
Effusion and Diffusion
μ Diffusion
ν Diffusion

## Slide 15
Effusion and Diffusion
Diffusion and Effusion
Grain size reduction
x100
Diffusion
Effusion
(1 diffusion, 1 effusion time constants)

## Slide 16: Possible problems (examples) – spare slide
Ca A | (s-1)
52 | 1.0E+03
53 | 2.5E+01
54 | >3.0E-01
Broken units during online period:
#524-UC-Ta (used)
#507-UC-W (used)
#511-Pb-VD7 (used)
All used targets
2x, 3x
UCx + xO2 →UO2 + xCO2
UO2 + 4C →UC2 + 2CO
Spontaneous oxidation!
Temperature
However not fully reversible
Irreversible changes to the microstructure!
Two used VADIS units failed this year
Anode photo after thermal cycle
Metal surface is initially smooth
Anode bends and touches other parts
Short circuit
Heat shields touching transfer line
COLLAPS run
Should be at least x10
Chart: Decrease of 32Ar Yield on CaO#123 (ISOLTRAP)
| 0 | 2.6583333332673647 | 6.0583333333488554 | 10.141666666546371 | 15.116666666697711
 | 1 | 0.72656 | 0.52503 | 0.55286 | 0.30301
Too high temperature!
400 nm
SSA = 38 m2/g
48h at 800oC
SSA = 4 m2/g
48h at 1200oC
3 μm
In the frontend, heating
#545