## Slide 1
Cable production at KIT
A. Kario, S. Otten, A. Kling, A. Jung, R. Nast, W. Goldacker
Institute for Technical Physics, Karlsruhe Institute of Technology, Karlsruhe

## Slide 2
Outline:
Tape material delivered from CERN
Cables/punch material deliveries
Punching tool upgrade
Mechanical test with CEA Saclay
Discussion

## Slide 3
Fujikura – Cu – KIT:
REBCO 3-6 µm
Cu 20 µm
electroplating
Cu 20 µm
Hastelloy 75 µm
Sample provided by Fujikura.

## Slide 4
SuNAM- CERN:
Delivered from CERN
to KIT for punching test 40 m
Change in punching tool
needed (tape width)

## Slide 5
SuperOx- CERN:
28 µm
29 µm
26 µm
*cross-section of one of the previous samples

## Slide 6
Punching possibilities:
Wl
Wc
Tp
Transposition lenght (mm) | Strand width (Wl)/ Bridge width (Wc) (mm) | Tape width (mm)
226 (old) | 5.5 | 12.1(SP, SOx) 12.4 (Bruker)
300 (new - multipunching) | 5.85 | 12.1(SP, SOx, Bruker Ag) 12.2 (SuNAM)
300 (future - in one step) | 5.85 | Ag or Cu tapes? 0.05 or 0.1 mm thick?

## Slide 7
Roebel cable for transverse stress at U. Twente:
Roebel cable: 226 TL, 15 strands:
1. SuperPower CC + KIT impregnation
2. SuperPower CC + CERN impregnation
3. Bruker CC + CERN impregnation
CERN: delivers resin and glass fibre to UT
KIT: Bruker (ready) and 2 SuperPower cables (in preparation)
UT: experiments planned 2016
Old experiment:
Roebel cable: 126 TL, 10 strands
SuperPower tape, 20 µm Cu (per site)
KIT impregnation

## Slide 8
Horizontal spacing error in standard cable (5.5 mm wide strands) and the burr
870 µm
421 µm
Error reduced by widening strands to 5.9 mm (laser-cut cable)
279 µm
151 µm
Roebel cable with old and new design:
0.1 mm
0.1 mm

## Slide 9
New geometry now possible in punching tool
  5.85 mm strand width
  300 mm transposition length
Baseline for next EuCARD-2 cables
174 µm
240 µm
Cross-section of first punched cable with new geometry (15 strands)
New punching tool and cable geometry:
10.2 µm

## Slide 10
Mechanical test of the cos-theta coil end geometry
(CEA Saclay + KIT):
Measurement at KIT with
CEA Saclay (77 K, s.f.)
CERN-3D form print
Courtesy of M. Durante

## Slide 11
Designed at CEA Saclay
Printed at CERN in Bluestone resin (suitable for low T)
Experiment order: mold 3, 2, 1
Mold 3:
  Twist: 74° over 110 mm (Tp = 535 mm)
  No bend
Mold 2:
  Twist 74° over 80 mm (Tp = 389 mm)
  No bend
Mold 1 (coil shape):
  Twist: 74° over 80 mm (Tp = 389 mm)
  Bend: R = 22 mm
Experiment: 3D-printed Molds
170 mm
Images by C. Lorin

## Slide 12
No degradation observed
Small Ic increase (reversible in cable 2)
Chart: Roebel cables in CEA torsion mold (T = 77 K, self-field)
| Cable 1 (left-hand wound) | Cable 2 (right-hand wound)
straight | 1457.1 | 1442.2133
mold no. 3 | 1460.1214 | 1458.6133
mold no. 2 | 1460.0067 | 1461.2267
mold no. 1 | 1470.2143 | 1457.9533
mold removed | 1444.2867
 | Twist pitch [mm] | Bending radius [mm]
Mold 3 | 535 | -
Mold 2 | 389 | -
Mold 1 | 389 | 22
No degradation of Ic with all used molds:

## Slide 13
Progress and plans:
Bruker substrate tape (200 m) -> new geometry dummy Roebel cable - delivered
Punching test (short lenght) – in progress
- SuNAM, SuperOx (delivered by CERN)
Two Roebel cables for U. Twente test from SuperPower – in progress
Roebel cable for contact test -> CEA Saclay - finished
Roebel with filaments (U. Southampton) - to be done
CEA Saclay and CERN dummies requirements?
Cables from delivered tape (SuNAM, SuperOx)
Fresca test (Bruker punch and coat cable)?
Feather0 test?
Tapes - new procurement (Ag cap?)