## Slide 1
Production of novel and advanced materials: Molybdenum-graphite
J.Guardia on behalf of Stefano Bizzaro
Presentation of our manufacturing facilities and capabilities
WP11 topical meeting
University of Malta, Valletta, Malta
27-28th April 2016
Notes: Malta 29 April 2016

## Slide 2: Outline
Overview of the company
Collaborations ongoing with CERN
Material production
Machining and testing capabilities

## Slide 3
Founded in year 2000 in the industrial area in San Bonifacio (Verona) in Italy, with an area of 1600 square meters, it represents a factory think up for design, research, development and production in technical/applied mechanical industry.
consultancy, design, research and development
special machining (ceramic and graphitic materials)
composite materials for high temperatures
High temperature thermal treatment in high vacuum
We collaborate with important suppliers, customers, laboratories, universities and research centers and we are involved in a continuous research for innovative solutions.
COMPANY PRESENTATION

## Slide 4: Collaborations with CERN

## Slide 5
Absorber material for HL-LHC collimators
R&D on novel materials, on-demand processes and high-precision machining.
Cathode pictures from Pascal Simon (CERN EN-MME)
MG-6303Ga sintered plate.
Dimensions 100 x 150 x 30mm
Tapering and blocks HRMT23 experiment
Cathode for CERN electron guns (HL-LHC hollow e-lens)
R&D on materials, density, doping elements and shape.
Collaborations with CERN

## Slide 6
Thermal treatment (firing) of ferrite plates for LHC collimators
1000ºC 48h in air + 1000ºC 48h in vacuum
Total duration ≈10days
Collaborations with CERN
Ferrite
Supports
TCTP Collimator RF system

## Slide 7: Material production

## Slide 8
MATERIAL MG6530 Aa
MATERIAL MG - 6403 Ga
MATERIAL ALUMINIUM GRAPHITE
MATERIAL ALUMINUM DIAMOND

## Slide 9
Molybdenum-graphite:
Liquid Phase Sintering at ~2800°C and 35 MPa.
Reducing H2-N2 atmosphere at 10-6 mbar.
Liquid metal-carbon phase allowed to spill out of the moulds to enhance compaction and reduce final density.
Composition (Grade MG-6403-Aa)
  95.3%vol. Natural Graphite (~45µm)
  4.5%vol. Molybdenum powder (~5µm)
  0.2%vol. Titanium powder (~5µm)
Powders pre-cleaning under H2-N2 atmosphere
MG-6303-Ga dimensions 100 x 150 x 30mm
Metal/Ceramic Matrix Composites

## Slide 10
►
MIXER
POWDER PREPARATION
MIXED POWDER
MOLD FOR GREEN POWDER
500 TON PRESS FOR GREEN BODY
GREEN BODY
MOLD GRAPHITE
PRODUCTION PHASES OF THE COMPOSITES
PLATE WITH DIE AFTER VACUUM HOT PRESSING 2800 ° C 35 MPa 25 minutes.
VACUUM HOT PRESSING 150 TON
Notes: VACUUM HOT PRESSING 150 TON

## Slide 11: VACUUM HOT- PRESSING 150 TON
VACUUM
VACUUM HOT-PRESSING C°1200
VACUUM HOT-PRESSING C°2800
COMPOSITE FINISHED
Notes: VACUUM HOT-PRESSING C° 2400 EL

## Slide 12
INDUCTIVE VACUUM HOT- PRESSING 150 TON 1500 C°
INDUCTION SPIRAL
INDUCTIVE VACUUM HOT PRESSING 900 C°
INDUCTIVE VACUUM HOT PRESSING 1500 C°
FURNACE CHAMBER
MATERIAL
Notes: MATERIAL

## Slide 13
MACHINES FOR PREPARING POWDER COMPOSITES
SIEVES CALIBRATED
ASPIRATED BENCH
MACHINE FOR POWDER COATING PAUDAL
MIXER IN VACUUM AND HEAT

## Slide 14: Material testing and machining

## Slide 15
DENSITY
DUROMETER
ELETRICAL CONDUCIVITY
ROUGHNESS
Notes: ELETRICAL CONDUCIVIT

## Slide 16
PROCESSING WITH CNC GRAPHITE
MOLD GRAPHITE
PROGRAM FOR MACHINE 3D CNC
TAPERINGS - BLOCK HRMT23
Notes: TAPERINGS - BLOCK HRMT23

## Slide 17
PROCESSING WITH CNC GRAPHITE
MOLD GRAPHITE

## Slide 18
PROCESSING WITH CNC GRAPHITE
SAMPLE
SAMPLE
Notes: SAMPLE

## Slide 19
BREVETTI BIZZ SRL via dell’Industria 37047 San Bonifacio (VR) ITALY Tel.-Fax. +39 0456102718 www.brevettibizz.com – info@brevettibizz.com
Notes: C