## Slide 1: Q4 Protection
Q4 Protection
Preliminary analysis

## Slide 2: Introduction
This presentation talks about the protection of the Q4 quadrupole.
A first study of the quench protection for the current design of the quadrupole is proposed. Results are shown for one aperture
The study is realised thanks to the software Qtransit based on the M.N.Wilson quench code and which have been developed by CEA for performing quench simulation

## Slide 3: INPUTS
Q4 Cable |  | 
h | 8.8 mm | 
wi | 0.77 mm | 
wo | 0.91 mm | 
Strand diameter (d) | 0.475 mm | 
N strand | 36 | 
Radial insulation (e) | 0.08 mm | 
Azimuthal inslation (e) | 0.08 mm | 
Insulated cable crosss section | 8.960 mm2 | 
Detection threshold | 0,1 V | These values have been confirmed by CERN (Mail from E.Todesco 08/03/2016)
Validation time | 10 ms | 
Maximum Hotspot temperature allowed | < 250K | These values are conservatives (Mail from B. Auchmann 09/03/2016)
Maximum voltage to ground allowed | 800 V | 

## Slide 4: HYPOthesis
To simulate the quench propagation for the Q4 magnets we used a model of two coils where the first coils represent the inner layer of the 4 coils and the second coils represent the outer layers.
The two layers are separated by a G10 shim of 0,5 mm which delays the thermal conduction between the two layers.
The total volume of the 4 coils and the total energy are accounted for. QH are fired on all coils.
=
M12
L1
L2

## Slide 5: HYPOthesis
The critical surface of the Q4 wire in NbTi is given in the following graph:

## Slide 6: Definitions of the various time delays
Inner layer
Outer layer
T=0s
VALIDATION &
POWER SUPPLY OFF
QUENCH HEATERS FIRED
QUENCH HEATERS PROVOKED THE QUENCH OF THE OUTER LAYER
QUENCH
TQuenchcoil1
DETECTION
QUENCH HEATERS PROVOKED THE QUENCH OF THE INNER LAYER
Time delay
Tblind
Tvalidation
TQHdelay
TQH
Case 1:The outer layer quenches before the quench heaters provok a quench
Time delay
TQuenchcoil2
TQuenchbackcoil2
TQuenchbackcoil1

## Slide 7: Definitions of the various time delays
Inner layer
Outer layer
T=0s
VALIDATION &
POWER SUPPLY OFF
QUENCH HEATERS EFECTIVE
QUENCH HEATERS PROVOKED THE QUENCH OF THE OUTER LAYER
QUENCH
DETECTION
QUENCH HEATERS PROVOKED THE QUENCH OF THE INNER LAYER
Time delay
Tblind
Tvalidation
TQHdelay
TQH
Case 2: The outer layer quenches when the quench heaters provok a quench
TQuenchcoil1
TQuenchbackcoil2
TQuenchbackcoil1

## Slide 8: Simulation tools: qtransit
Qtransit is a CEA software based on the M.N.Wilson quench code.
The Qtransit program calculate the thermodynamics of a coil when a quench occurs.
The temperature rise at the initial quench point define in the inputs. After calculation the code gives the final temperatures inside the winding and the voltage induced
The geometry and the materials of the cable are given in the inputs

## Slide 9: HYPOthesis
Hypothesis | 
L1 | 9,21E-3 H
L2 | 12,34E-3 H
M12 | 8,55E-3 H
LEQ1 | 37,55E-3 H
I | 4590 A
Quench Heater | Placed on the outer layer
Tquenchcoil1 | 0 s
Tblind | 6 ms
Tvalidation | 10 ms
Tquenchcoil2 | 6+10+40=56 ms
Tquenchbackcoil2 | 56 ms
Tquenchbackcoil1 | 75+56=131ms
Tdelay | ≈ 75ms
TQH+TQHdelay | 40 ms (to be verified)
The mutual inductances have been found by using the ROXIE code
The layer-to-layer time delay of 75ms has been estimated thanks to a 1D transient finite elements method. The simulations have been made for a time delay of 50ms, 75ms and 100ms
The simulations have been made with and without quench heaters.

## Slide 10: SImulation
Hypothesis | 
Without quench heater | 
Time delay | 50 ms
Maximum Hotspot temperature in coil 1 | 279,9 K
Maximum Hotspot temperature in coil 2 | 152,4 K
Maximum voltage to ground | 547,8 V
Hypothesis | 
With quench heater | 
Time delay | 50 ms
Maximum Hotspot temperature in coil 1 | 167,9 K
Maximum Hotspot temperature in coil 2 | 85,8 K
Maximum voltage to ground | 340,2 V
Voltage accross each layer
Voltage accross each layer

## Slide 11: SImulation
Hypothesis | 
Without quench heater | 
Time delay | 75 ms
Maximum Hotspot temperature in coil 1 | 293 K
Maximum Hotspot temperature in coil 2 | 118,3 K
Maximum voltage to ground | 594,6 V
Hypothesis | 
With quench heater | 
Time delay | 75 ms
Maximum Hotspot temperature in coil 1 | 177,6 K
Maximum Hotspot temperature in coil 2 | 84,3 K
Maximum voltage to ground | 340,2 V
Voltage accross each layer
Voltage accross each layer

## Slide 12: SImulation
Hypothesis | 
Without quench heater | 
Time delay | 100 ms
Maximum Hotspot temperature in coil 1 | 300,1 K
Maximum Hotspot temperature in coil 2 | 89,4 K
Maximum voltage to ground | 634 V
Hypothesis | 
With quench heater | 
Time delay | 100 ms
Maximum Hotspot temperature in coil 1 | 178,9 K
Maximum Hotspot temperature in coil 2 | 84,9 K
Maximum voltage to ground | 340,2 V
Voltage accross each layer
Voltage accross each layer

## Slide 13: RESULTS
Results |  |  |  |  |  | 
 | Without quench heater |  |  | With quench heater |  | 
Time delay | 50 ms | 75 ms | 100 ms | 50 ms | 75 ms | 100 ms
Maximum Hotspot temperature in coil 1 | 279,9 K | 293 K | 300,1 K | 167,9 K | 177,6 K | 178,9 K
Maximum Hotspot temperature in coil 2 | 152,4 K | 118,3 K | 89,4 K | 85,8 K | 84,3 K | 84,9 K
Maximum voltage to ground | 547,8 V | 594,6 V | 634 V | 340,2 V | 340,2 V | 340,2 V

## Slide 14: Conclusion
The QTRANSIT code has been used on the updated version of Q4.
Simulations with and without QH have been carried out
The highest hot spot temperature (300 K) is reached in absence of QH and with a layer-to-layer time delay of 100 ms.
With QH:
  the hotspot is limited to ~180 K.
  The max V to ground is ~340 V
Next steps:
  Simulation with ROXIE
  Detailed design of the QH: high/low field, strip design and number of circuits

## Slide 15: Open questions
Powering scheme of the Q4?
Number of heaters PS

## Slide 16: Annex
Hypothesis | 
Without quench heater | 
Time delay | infinite
Maximum Hotspot temperature in coil 1 | 305,6 K
Maximum Hotspot temperature in coil 2 | 1,9 K
Maximum voltage to ground | 687,4 V
Hypothesis | 
With quench heater | 
Time delay | 100 ms
TQHdelay+TQH | 60 ms
Maximum Hotspot temperature in coil 1 | 210,7 K
Maximum Hotspot temperature in coil 2 | 78,7 K
Maximum voltage to ground | 634 V