## Slide 1: Magnet Design
Paolo Ferracin
International Review of the Inner Triplet Quadrupoles (MQXF) for HL-LHC
7-10 June, 2016
CERN

## Slide 2: Outline
Overview of MQXF design
Strand and insulated cable
Coil design, magnetic analysis, magnet parameters
Support structure and mechanical analysis
Quench protection

## Slide 3: Overview of MQXF design
Target: 132.6 T/m
  150 mm coil aperture, 11.4 T Bpeak
Q1/Q3 (by US-AUP Project)
  2 magnets MQXFA with 4.2 m
Q2a/Q2b (by CERN)
  1 magnet MQXFB with 7.15 m
Different lengths, same design
Al shell pre-loaded with bladders
  First time for an accelerator magnet

## Slide 4: Overview of MQXF design
OD: 630 m
Stainless steel shell
  8 mm for LHe containment
Aluminum shell
  29 mm thick
Iron yoke
  Gaps open
  4-fold symmetry
Iron master plates
  Bladder and keys
Iron pad
SS axial rods
Aluminum collars
G10 pole key
Ti alloy poles

## Slide 5: Overview of MQXF design

## Slide 6: Overview of MQXF design LARP
LHC Accelerator Research Program (since 2003)
  R&D on Nb3Sn quadrupoles for LHC luminosity upgrade
From TQ/LQ series to MQXF
  From 90 to 150 mm
MQXF scale-up of HQ
  Similar coil lay-out
  Same structure concept
  Successfully tested

## Slide 7: Overview of MQXF design From HQ to MQXF
Aperture from 120 mm to 150 mm
  Strand increased from 0.778 mm to 0.85 mm
  Cable from 15 to 18 mm width (similar stress with +30% forces)
Same coil lay-out
Same structure concept
  Pre-load capabilities of HQ design qualified and successfully tested
Larger OD: from 570 to 630 mm
Additional accelerator features
HQ
MQXF

## Slide 8: Overview of MQXF design LHC low- quadrupole support structures
Cold mass OD from 490/420 to 630 mm
More than double the aperture: from 70 to 150 mm
~4 times the e.m. forces in straight section
~6 times the e.m. forces in the ends
MQXB
MQXA
MQXF
In scale

## Slide 9: Overview of MQXF design Comparison with LHC MB and 11T
  Fx = 340 t/m
  _e.m.= 50-60 MPa
  Fz_aperture = 24 t
  Fx = 620 t/m
  _e.m.= 90-110 MPa
  Fz_aperture = 48 t
  Fx = 680 t/m
  _e.m.= 100-110 MPa
  Fz_aperture = 120 t

## Slide 10: Outline
Overview of MQXF design
Strand and insulated cable
Coil design, magnetic analysis, magnet parameters
Support structure and mechanical analysis
Quench protection

## Slide 11: Superconducting Strand
0.85 mm strand, 1.2 Cu/SC
Short model program
  OST RRP 108/127, 132/169
  EAS Bruker PIT 192
Prototype program
  RRP 108/127
  PIT 192 (with barrier)
Specifications
  RRP
    632 A (2450 A/mm2)at 12 T
    331 A (1280 A/mm2) at 15 T
  PIT
    590 A (2290 A/mm2) at 12 T
    331 A (1280 A/mm2) at 15 T
Filament   55 µm
See B. Bordini, L. Cooley

## Slide 12: Superconducting Strand
The MQXF1 case: all coils within specs.

## Slide 13: Superconducting cable (2nd generation)
40-strand cable
Mid – thickness after cabling
  1.525 +/- 0.010 mm
Width after cabling
  18.150 +/- 0.050 mm
Keystone angle
  0.40 +/- 0.10 deg.
Pitch length
  109 mm
SS core 12 mm x 25 μm thick
Assumed expansion during reaction
  4.5% in thickness: ~70 μm
    same keystone angle
  1.2 % in width: ~210 μm
Mid–thickness after reaction
  1.594 mm
Width after reaction
  18.363 mm
70 μm
210 μm
See B. Bordini, L. Cooley

## Slide 14: Superconducting strand and cable Dimensional variation during reaction
Cable/coil size after reaction is critical
  Issue in HQ01
Single cable, stacks, coil cross-section
  Image analysis of cable contours
Consistent data from different set-ups, labs, and coils
See J. C. Perez

## Slide 15: Superconducting strand and cable Dimensional variation during reaction
Overall volume expansion: +3.0 to 3.5%
Single strand
  +3.5% in volume
    +3.4% in area
    +0.1 in length
Bare cable (or loose insulation)
  +3.5% in volume
    +3.0% in thickness
    +1.0% in width
    -0.5% in length
Braided cable
  +3.0 to +3.5% in volume
    +3.0% in thickness
    +0.0 to +0.5% in width
    -0.2 to 0.0% in length
Dependence on tooling and braiding
See J. C. Perez

## Slide 16: Cable insulation
AGY S2-glass fibers 66 tex with 933 silane sizing
32 (CERN, CGP) or 48 (LARP, NEW) coils (bobbins)
  Variables: # of yarn per coil and of picks/inch
Target: 145 5 μm at 5 MPa, average 3 cycles

## Slide 17: From 1st to 2nd generation Insulated cable design
Keystone angle reduced from 0.55 to 0.40
  Critical current degradation due to cabling reduced to <5% both for RRP and PIT
Assumed width expansion
  From 2% to 1.2 %  increased coil compaction
Thickness of insulation
  From 0.150 to 145 µm  increased coil compaction

## Slide 18: Outline
Overview of MQXF design
Strand and insulated cable
Coil design, magnetic analysis, magnet parameters
Support structure and mechanical analysis
Quench protection

## Slide 19: Coil design
Two-layer, four-blocks design
22+28 = 50 turns
Pole impregnated with the coil
Splice extension 140 mm long
2 end spacers for peak field reduction (1%) and field quality

## Slide 20: Coil design
Coated parts with cuts
Image analysis of cable contours
  Good fit of end-spacers
  But, up to 0.5 mm azimuthal and radial shift in straight section
Space for expansion reduced for 2nd generation coils
  From 2 to 1% on width
  Assumed ins. thickness in Roxie from 150 to 145 m

## Slide 21: Magnetic analysis
Allowed harmonics below 1 units
  Confirmed by measurements
6 blocks in the ends
  Minimized integrated harmonics
  1% lower peak field in the ends wrt straight section
    Iron pad removed from the ends
See S. Izquierdo Bermudez

## Slide 22: Magnetic analysis

## Slide 23: Magnetic analysis Corrective strategies
Allowed harmonics
  Pole/mid-plane shims
Un-allowed harmonics
  Magnetic shims
See S. Izquierdo Bermudez

## Slide 24: From 1st to 2nd generation Coil design
Account for the new cable geometry
  New keystone angle and dimensions after reactions
Corrected the impact of coil mechanical deformation
Optimized harmonics at 123 T/m
  Operational current will be between 90% and 100% of nominal, depending on the LHC final energy
Added S2-glass shims on mid-plane and pole
Compensated end effects on the integrated harmonics

## Slide 25: Magnet parameters
Self field corr. (ITER barrel)
5% cabling degradation
Gop= 132.6 T/m
  Iop: 16.47 kA
  Bpeak_op: 11.4 T
RRP: 78%of Iss at 1.9 K
PIT: 79% of Iss at 1.9 K
Stored energy: 1.2 MJ/m
Inductance: 8.2 mH/m

## Slide 26: From 1st to 2nd generation Operational margin
From 1st to 2nd generation design
  We started with magnet Iop at 81% of Iss
  Length: 4.0 to 4.2 m for Q1/Q3, 6.8 to 7.15 m for Q2
    Reduction of gradient from 140 to 132.6 T/m
    Magnet Iop from 81% to 76% of Iss
  RRP spec. reduced from 361 to 331 A (1400 to 1280 A/mm2) at 15 T
    Magnet Iop from 76% to 78% of Iss
  PIT spec. reduced from 631 to 590 A (2450 to 2290 A/mm2) at 12 T, but same at 15 T
    Magnet Iop at 79%

## Slide 27: Outline
Overview of MQXF project and design
Strand and insulated cable
Coil design, magnetic analysis, magnet parameters
Support structure and mechanical analysis
Quench protection

## Slide 28: Magnet design MQXFB
Superconducting coil
See J. C. Perez

## Slide 29: Magnet design MQXFB
Pole key for alignment
See J. C. Perez

## Slide 30: Magnet design MQXFB
Aluminium collar
  No coil pre-load
See J. C. Perez

## Slide 31: Magnet design MQXFB
Bolted iron pad
  No coil pre-load
See J. C. Perez

## Slide 32: Magnet design MQXFB
Iron master
  Half-length plates for bladders and keys
See J. C. Perez

## Slide 33: Magnet design MQXFB
Loading and alignment keys
See J. C. Perez

## Slide 34: Magnet design MQXFB
Second iron master
  Coil-pack sub-assembly
See J. C. Perez

## Slide 35: Magnet design MQXFB
Iron yoke laminations
See J. C. Perez

## Slide 36: Magnet design MQXFB
Segmented aluminium shell
See J. C. Perez

## Slide 37: Magnet design MQXFB
Tack-welding blocks
  Aligned to the yoke
See J. C. Perez

## Slide 38: Magnet design MQXFB
Backing strip
  For Lhe vessel welding
See J. C. Perez

## Slide 39: Magnet design MQXFB
Welded LHe vessel
  Minimum welding tension
See J. C. Perez

## Slide 40: Magnet design MQXFB
Axial support system
  SS rods and end-plates
See J. C. Perez

## Slide 41: Magnet assembly and pre-loading
Shell-yoke modules combined
Insertion of coil-pack sub-assembly
Then bladder operation
-110 MPa
-100 MPa
-140 MPa
-140 MPa
Deformed shape and coil peak azimuth. stress from ANSYS
See G. Vallone

## Slide 42: Mechanical analysis
Shell force shared by collars and key at room T
25% intercepted at 1.9 K
Coil compressed at Gop
  Alignment maintained
-110 MPa
-100 MPa
-140 MPa
-140 MPa
Coil peak azimuth. stress
See G. Vallone

## Slide 43: Axial loading
SS rods free to contract
Possible to
  apply coil pre-load equal to e.m. force
  maintain coil – end-parts contact pressure
See G. Vallone

## Slide 44: LHe vessel
Shell cut-outs to align magnet during module assembly and tack welding process
Stainless steel shell welded with 50-100 MPa tension
  Still in contact after cool-down
See J.C. Perez
See H. Prin

## Slide 45: Rigidity of the structure
Radial
   strain: ~70 
  Shell radius r: 307 mm
  r ~20 m
Axial
  z strain: ~70 
  Rod/coil length l: 1500 mm
  l ~100 m
See G. Vallone
Very small changes under e.m. forces

## Slide 46: Alignment
Pole key
Collar-pad
Pad-master
Master-master key
Master-yoke
Tack-welding blocks
Modules aligned via
  Yoke slots
  Pins
  Tack-welding blocks
See J. C. Perez

## Slide 47: Laminations
With respect to previous review
  2 short model structures with thin laminations fabricated and under test
See J. C. Perez
Structure 1 and 2
Structure 3 and 4

## Slide 48: Cooling
Requirements
  1.5 mm clearance tube - coil
  Perforated inner layer trace (40%)
  Pole: 8 mm holes every 50 mm
    Same in the pole key
  Clear path around axial rods
  77 mm heat exchanger holes
    Top for bus-bars, bottom for cooling
  Cross-talk channels in the yoke
    8 mm diameter, every ~700 mm
  Free helium section of 150 cm2

## Slide 49: Outline
Overview of MQXF project and design
Strand and insulated cable
Coil design, magnetic analysis, magnet parameters
Support structure and mechanical analysis
Quench protection

## Slide 50: Quench protection
Challenge: 50% more stored E in the coil than LHC MB
No dump (only 5% of energy, due to high inductance)
Outer layer QH: 350-360 K reached (failure scenarios)
For additional redundancy and peak T reduction
  Inner layer QH: Cooling and detachment issues
  CLIQ (Coupling-Loss-Induce-Quench) system
    Tested on HQ and MB, aspects related to the circuit being analyzed
See G. Ambrosio

## Slide 51: Appendix

## Slide 52: Superconducting strand RRP
Jc(4.22 K, 12 T)≈2450 A/mm2
Jc(4.22 K, 15 T)≈1280 A/mm2
Spec at 15 T reduced from 360 to 330 from last review

## Slide 53: Superconducting strand PIT
Jc(4.22 K, 12 T)≈2290 A/mm2
Jc(4.22 K, 15 T)≈1280 A/mm2

## Slide 54: Strands, cables and coils
References: |  | 
Strands: | [1] | D. Bocian et al., Measurements of Nb3Sn Conductor Dimension Changes During Heat Treatment, Proc. AIP Conf., 2012.
 | [2] | N. Andreev et al., Volume Expansion of Nb-Sn Strands and Cables During Heat Treatment, Adv. in Cryogenic Eng., 2007.
Cables: | [3] | I. Pong et al., Dimensional Changes of Nb3Sn Cables during Heat Treatment, Int. Cryogenic Materials Conf., 2015.
 | [4] | M. Durante et al., Geometrical behavior of Nb3Sn Rutherford cables during heat treatment, IEEE Trans. Appl. Supercond., 2016.
Coils: | [5] | T. Holik et al., Cross-section analysis of MQXF coils, IEEE Trans. Appl. Supercond., 2016.
 | [6] | E. Rochepault et al., Dimensional Changes of Nb3Sn Rutherford Cables During Heat Treatment, IEEE Trans. Appl. Supercond., 2016.
Conductor | Insulation | Thickness [%] |  | Width [%] |  | Length [%] |  | Area | Volume
 |  | Range | Avg. | Range | Avg. | Range | Avg. | Avg. [%] | Avg. [%]
Strand | Bare | 1.6:1.9 | 1.7 | 1.6-1.9 | 1.7 | 0.08 | 0.08 | 3.4 | 3.5
MQXF Cables | Bare | 2.9:3.1 | 3.0 | - | - | - | - | - | -
 | Sleeve | 2.6:3.0 | 2.8 | 1.1:1.3 | 1.1 | -0.55:-0.30 | -0.4 | 3.9 | 3.5
 | Braid | 2.9:3.6 | 3.2 | -0.20:0.15 | 0.0 | -0.05:-0.20 | -0.1 | 3.2 | 3.1
LARP coil 1 | Braid | 1.7:4.5 | 3.1 | 0.3:0.6 | 0.5 | -0.23:-0.14 | -0.18 | 3.6 | 3.4
CERN coil 101 | Braid | 1.7:4.3 | 3.0 | -0.0:0.3 | 0.1 | -0.08:-0.00 | -0.03 | 3.1 | 3.0
During the heat treatment, assuming braided insulation:
Cables expand by +3% in thickness and <+0.5% in width
Cables contract by -0.1 % in length
Overall volume expansion is around +3%

## Slide 55: Impact of insulation
Chart: Length [%]
| -0.5 | -0.5 | -0.3 | -0.45 | -0.4 | -0.4 | -0.55000000000000004
MQXF - unc. - sleeve | 4.2 | 4.1 | 3.9 | 3.55 | 4.1 | 3.75 | 3.85
MQXF - unc. - braided | 3.3 | 3.55 | 3.5 | 2.95 | 2.95 | 3.15
HQ - conf. - sleeve | 2 | 2.45
Linear trend | 4.08 | 1.92
LARP coil 1 | 3.57
CERN coil 101 | 3.1457
Chart: After winding+curing [%]
| -0.15 | -0.12000000000000002 | -0.13900000000000001 | -0.16 | -0.14000000000000001 | -0.05 | -0.15 | -9.5000000000000015E-2 | -0.10499999999999998 | -0.15000000000000002
MQXF CERN | -0.04 | -0.043 | -0.047 | 0 | -0.01 | 0.01 | -0.025 | -0.08 | -0.03
MQXF LARP | -0.167 | -0.2315 | -0.139 | -0.188 | -0.168 | -0.171 | -0.22394
HQ02 | -0.205 | -0.2075 | -0.165 | -0.155 | -0.17
HQ03 | 0.04375 | -0.125 | -0.025 | 0.03125 | -0.015 | -0.05625 | -0.06
000 (Cu) | -0.23
 | 0.13 | -0.22
 | -0.07 | -0.42
 | 0.1 | -0.25
 | -0.04 | -0.39
QXFP | -0.10575 | -0.09375 | -0.09375 | -0.083675 | -0.1052
-0.17
-0.20
-0.34
-0.37
Cables: area and length
Coils: length during fabrication steps
Cables confined in a tight braid expand less in area and contract less in length
Braid is less tight for LARP coils than for CERN coils
Behavior similar to HQ02 sleeves
 more contraction in length

## Slide 56: Radial tolerance sensitivity of each part
Tolerance closer to the coil has relatively bigger impact on the stress of the coil in the tolerance quadrant.
The master attach to the pad is slightly more sensitive to the tolerance; the yoke and shell are all less sensitive.

## Slide 57: Impact of azimuthal tolerance
Assume each azimuthal tolerance is 25 μm, the resultant coil twist angle is (Sensitivity check):
Coil twist angle (mrad) | Collar/Pole key | Pad | Master | Yoke
0.21 | 25 | 0 | 0 | 0
0.19 | 0 | 25 | 0 | 0
0.12 | 0 | 0 | 25 | 0
0.09 | 0 | 0 | 0 | 25
0.61 | 25 | 25 | 25 | 25
 | Collar/Pole key | Pad | Master | Yoke
Max allowable azimuthal tolerance (μm) | 119 | 132 | 212 | 278
If the twist angle of coil is 1 mrad, the each corresponsing azimuthal tolerance is: (Sensitivity check):

## Slide 58: Conclusion
The yoke and shell have the least sensitivity on radial tolerance. Tolerance on the other parts have similar influence to the coil stress.
The typical tolerance build-up in manufacturing only impact coil stress within about +/- 10 MPa.
The typical azimuthal tolerances in manufacturing meet the physical envelop requirement of MAXF.

## Slide 59: Shell segmentation and LHe vessel (I)
In case of full length aluminum shell
  High z and z due to friction and high thermal contraction
    Risk of ratcheting
  Variation of shell axial z due to friction
    Large coil stress  variation
Aluminum shell in 0.755 m segments
  LQ/HQ shell axial stress levels
  Coil azimuthal stress variation 10 MPa
Optimization of shell segments for long model in progress
See talk from M. Juchno