## Slide 1: Magnetic Measurements and Analysis
S. Izquierdo Bermudez, J. DiMarco, X. Wang
G. Ambrosio, G. Chlachidze, P. Ferracin, T. Holik,
G. Sabbi, S. Stoynev, T. Strauss, E. Todesco, G. Valone, G. Velev et al.
MQXF International Review, CERN, June 2016

## Slide 2: Outline
MQXFS1 parameters and features
Magnetic measurements system
Magnetic measurement overview
Geometric field errors
Machine cycle analysis
Summary and next steps

## Slide 3: Outline
MQXFS1 parameters and features
Magnetic measurements system
Magnetic measurement overview
Geometric Field Errors
Machine Cycle Analysis
Summary and next steps

## Slide 4: MQXFS1 parameters and features
MQXFS1 was assembled using 2 coils from CERN (coil 103 and 104) and 2 coils from LARP (coil 3 and 5).
CERN coils:
  Use RRP 132/169 layout
  Are systematically smaller than nominal
LARP coils:
  Use RRP 108/127 layout
  Are systematically bigger than nominal
Magnetic length is ≈ 1.2 m and the uniform straight section ≈ 0.5 m
Magnet and coil positioning
G. Ambrosio et al., MQXFS1 Design Report, http://larpdocs.fnal.gov//LARP-public/DocDB/ShowDocument?docid=1074
X. Wang et al., Coordinate system for magnetic measurements of MQXF magnet, http://larpdocs.fnal.gov//LARP/DocDB/0010/001079/003/MQXF-MagMeasCoordinateSystem-v1.docx
References
 | Units | MQXFS
Magnetic length | mm | 1192
Overall coil length (including splice extension) | mm | 1510
Magnetic yoke extension | mm | 1550
Magnetic pad extension | mm | 975

## Slide 5: MQXFS1 parameters and features
As a general rule CERN MQXF short coils are smaller in size than LARP coils:
  LARP coils: Azimuthally oversized by 50 – 100 µm
  CERN coils: Azimuthally undersized by 50 – 200 µm
Reference
G. Ambrosio et al., MQXFS1 Fabrication Report, http://larpdocs.fnal.gov//LARP/DocDB/0011/001117/001/MQXFS1_Fabrication_Report_V1_050916.pdf
amount that a best fit circle to the coil OD deviates from the nominal outer diameter
total deviation from nominal of the left and right midplanes

## Slide 6: MQXFS1 parameters and features
104
103
5
3
Reference
G. Ambrosio et al., MQXFS1 Fabrication Report, http://larpdocs.fnal.gov//LARP/DocDB/0011/001117/001/MQXFS1_Fabrication_Report_V1_050916.pdf
Goal: bring all the coils on the same collar arc length
Coil 103
Mid-plane on target
Undersized OR by 0.025 mm or in target
Coil 104
Mid-plane undersized by 0.05 – 0.1 mm
Undersized OR by 0.050 mm or in target
Coil 5
Mid-plane oversized by 0.05 mm
OR in target
Coil 3
Mid-plane oversized by 0.05 mm
Oversized OR by 0.025 mm
0.050 mm to match LARP coils OR location
+0.050 mm to compensate for coil undersized
0.050 mm to match LARP coils OR location
Remark: Assembly rotated by 90 degrees to be consistent with the magnetic axis definition

## Slide 7: Outline
MQXFS1 parameters and features
Magnetic measurements system
Magnetic measurement overview
Geometric Field Errors
Machine Cycle Analysis
Summary and next steps

## Slide 8: Magnetic Measurements System
General approach:
Short rotating probes scanning the magnet bore
FNAL-developed PCB probe technology (already validated in HQ models)
All measurements reported at 50 mm ref. radius
Warm measurements during assembly at LBNL:
Probe supported by temporary bore tube
MQXF probe (provided by FNAL) has a radius of 59.5 mm, and length of 110 mm (& 220 mm)
No automatic system for longitudinal positioning
Cold/warm measurements at Fermilab VMTF:
Probe shaft centered in (new) anti-cryostat
MQXF probes have a 50.5 mm radius (taking into account clear bore and anti-cryostat requirements)
Vertical test sled positions and rotates probe
Different PCB probes in the two Thermal Cycles
  TC1: 30 layer, 110 & 220 mm, with attenuator
  TC2: 2 layer, 55 and 110 mm, no attenuator
2-layer PCB
55 & 110 mm
30-layer PCB
110 & 220 mm
TC2:
TC1:
Warm measurements during assembly (LBNL)
Vertical test sled
(FNAL VMTF)
Probe shaft & spring-loaded bearing blocks

## Slide 9: Outline
MQXFS1 parameters and features
Magnetic measurements system
Magnetic measurement overview
Geometric Field Errors
  Warm magnetic measurements
  Cold magnetic measurements
  Cold-warm correlation
  Possible source of field errors and correcting actions
Machine Cycle Analysis
  Iron saturation effect
  Persistent currents effects
Summary and next steps

## Slide 10: Magnetic Measurements Overview (I)
Warm measurements during assembly (July-August 2015):
  Performed after insertion of the collared coil (before and after pre-loading)
  The plan is in the future to perform also measurements on the collared coil (before insertion on the yoke-shell structure)
First thermal cycle (TC1, March 2016)
    Warm measurements before cool-down in VMTF in good agreement with those performed during assembly
    Signal from 30-layer PCB probe saturates amplifiers, requiring the use of an attenuator  difficult to correct (data not usable)
Reference: MQXFS1 Test Plan,
http://larpdocs.fnal.gov//LARP-public/DocDB/ShowDocument?docid=1079

## Slide 11: Magnetic Measurements Overview (II)
Second thermal cycle (TC2, April 2016)
  Replaced 30-layer probe with 2-layer probe and no attenuator
  Field quality characterization up to nominal current
    Longitudinal scans at selected currents
    Accelerator cycle to nominal current
    Ramp rate dependence
    Stair step measurement
    Effect of reset current
  Additional studies up to ultimate current
    Accelerator cycle to ultimate current (including a cycle with longer injection plateau)
    Z-scan at ultimate current
  Measurements during and after warm-up
    Magnetic measurements at intermediate temperatures
    Final z scan after warm up
Reference: MQXFS1 Test Plan,
http://larpdocs.fnal.gov//LARP-public/DocDB/ShowDocument?docid=1079
Focus for this presentation

## Slide 12: Outline
MQXFS1 parameters and features
Magnetic measurements system
Magnetic measurement overview
Geometric Field Errors
  Warm magnetic measurements
  Warm-Cold-Warm correlation
  Possible source of field errors and correcting actions
Machine Cycle Analysis
Summary and next steps

## Slide 13: Warm magnetic measurements – Main Field
20-30 units discrepancy on the transfer function with respect to ROXIE model using the nominal coil geometry.
In the straight part (z=[-300,200] mm), the longitudinal variation of the main field is within 8 units.
Reference: S. Izquierdo Bermudez, Analysis of MQXFS1 warm magnetic measurements, https://indico.fnal.gov/getFile.py/access?contribId=2&resId=0&materialId=slides&confId=11130

## Slide 14: Warm measurements – Field Harmonics After Assembly
Field harmonics are evaluated at 2/3 of the aperture radius (Rref=50 mm).
The standard deviation of the harmonics on the straight section (z=[-300,200] mm) corresponds to a random displacement of the coil blocks of 50 µm.
 | Normal Components (bn) |  |  |  | Skew Components (an) |  |  | 
n | Average | Max | Min | Std. Dev. | Average | Max | Min | Std. Dev.
3 | -3.24 | -1.17 | -4.56 | 1.20 | 3.46 | 4.84 | 2.38 | 0.91
4 | 0.30 | 1.59 | -0.70 | 0.79 | -4.18 | -2.91 | -5.58 | 0.83
5 | 2.47 | 2.84 | 2.27 | 0.18 | -0.55 | 0.36 | -1.05 | 0.47
6 | 3.57 | 6.78 | 2.60 | 1.21 | 0.65 | 2.27 | -0.30 | 0.73
7 | 0.13 | 0.40 | -0.18 | 0.20 | 0.27 | 0.70 | 0.02 | 0.20
8 | 0.23 | 0.31 | 0.05 | 0.08 | -0.25 | -0.03 | -0.45 | 0.13
9 | 0.15 | 0.29 | 0.00 | 0.10 | 0.31 | 0.43 | 0.18 | 0.07
10 | -0.49 | -0.33 | -1.25 | 0.26 | 0.12 | 0.25 | 0.00 | 0.07

## Slide 15: Warm measurements - Before vs. After Pre-Loading
Chart: Average warm measurements, 10 A
| -3.0205907684210098 | 0.55800485842326297 | 2.6820352168456498 | 2.09873928771249
bn | -3.2437 | 0.29781 | 2.4666 | 3.5695
 | 3.4613 | -4.183 | -0.54595 | 0.6481
 | -10 | 10
A measurable effect is observed, however, the overall strength and longitudinal structure of the harmonics is not fundamentally altered
Pre-load effect is relatively small compared to coil fabrication or initial assembly (collared coil)
b6
a3
b5
b4
a6
a4
a5
b3

## Slide 16: Cold Magnetic Measurements - Cold vs. Warm
Chart: Average measurements on the straight part
| -3.2436896959506898 | 0.297811904057738 | 2.4665772609401602 | 3.5695336527556001
 | -4.2053 | 0.32098 | 2.7586 | 0.94726
 | 3.2937 | -6.4909 | -0.86709 | 0.52424
 | -10 | 10
b6
a3
b5
b4
a6
a4
a5
b3
Good cold warm correlation, except:
  b3, which increases by 1 unit
  a4, which increases by 2 units
Allowed harmonics in very good agreement with the model.
 | MEASURED (average at Inom) | ROXIE
b6 | 0.95 | 0.68
b10 | -0.51 | -0.39
b14 | -0.70 | -0.66

## Slide 17: Warm Magnetic Measurements Before vs. After Cold Test
Chart: Average warm measurements on the straight part, 10 A
| -3.2436896959506898 | 0.297811904057738 | 2.4665772609401602 | 3.5695336527556001
 | -3.8914 | 0.29982 | 2.5673 | 4.1802
 | 3.2622 | -4.7159 | -0.55372 | 0.49996
 | -10 | 10
  Very good correlation on the field harmonics before and after cold powering test  there is not a permanent deformation on the coil visible in terms of field quality.
  The overall strength and longitudinal structure of the harmonics is not fundamentally altered
b6
a3
b5
b4
a6
a4
a5
b3

## Slide 18: Contribution of the Coil Ends
The contribution of the coil ends is very well captured by the 3D ROXIE model
Measurements at 10 A after cold test, using 50 mm probe

## Slide 19: Un-Allowed Harmonics Coil Cross Sections Characterization
Efforts on going to link the measured un-allowed harmonics to the possible errors on the coil turns positioning based on cross section analysis.
What we observe:
  Mid plane and pole turns are well in place.
  Large azimuthal/radial deviation on the intermediate coil turns (∽ 0.5 mm)
[E. Holik]
[E. Rochepault]

## Slide 20: b3 and a3
Measured normal and skew sextupole can be corrected inserting magnetic shims in the bladders slot
  Magnetic shims installed in MQXFS1b to prove the correction capabilities
Correction capabilities using 9x58 mm shim in the bladder slots |  | 
Order | bn | an
3 | 4.24 | -4.24
4 | 0.00 | 0.00
5 | 0.40 | 0.40
6 | 0.00 | 0.00
MQXFS1 Meas. | b3 |  | a3 | 
 | Warm | Cold | Warm | Cold
Average | -3.24 | -4.21 | 3.46 | 3.29
Max. | -1.17 | -1.83 | 4.84 | 5.06
Min. | -4.56 | -5.34 | 2.38 | 1.14
Std. Dev. | 1.20 | 1.14 | 0.91 | 1.37

## Slide 21: b4 and a4
104
5
3
103
Large a4 is expected due to the differences in between CERN and LARP coils
  Should improve when assembling coils produced in the same manufacturing line.
 |  | b4 |  | a4 | 
 |  | Warm | Cold | Warm | Cold
Computed |  | 0.00 |  | -4.82 | 
Measured | Average | 0.30 | 0.32 | -4.18 | -6.49
 | Max. | 1.59 | 2.06 | -2.91 | -5.11
 | Min. | -0.70 | -0.96 | -5.58 | -8.14
 | Std. Dev. | 0.79 | 1.10 | 0.83 | 0.96

## Slide 22: b5
Max effect
~No change
With the level of displacements measured in coil cross sections, large high order harmonics can be generated.
If all other coils were nominal:
      10 turns within box are shifted 700 µm
      Max effect region has ~ 0.002 units per strand
-> 40/2 strands * 10 turns * 0.002 * 700/100 = 2.8 Units from one coil
(measured b5 = 2.5)
Actions taken: Reduction of the room left for conductor expansion during heat treatment for the second generation design:
  From 2% to 1.2% in width
  (0.150 mm less per turn)
  From 4.5 % to 3.8% in thickness
  (0.010 mm less per turn)
[E. Holik]

## Slide 23: Outline
MQXFS1 parameters and features
Magnetic measurements system
Magnetic measurement overview
Geometric Field Errors
Machine Cycle Analysis
  Iron saturation effect
  Persistent currents effects
Summary and next steps

## Slide 24: Transfer function
Saturation well captured by ROXIE model
Good agreement calculation/measurements on geometric transfer function:
  Measured field is 30 units stronger assuming a coil radial contraction during cool down of 3 mm/m
  Measured field is 10 units stronger introducing the coil deformation as computed in ANSYS.

## Slide 25: Allowed harmonics
The effect of the iron saturation effect on b6 is close to ROXIE prediction.
The impact of saturation on the rest of the harmonics is negligible (as expected).
The impact of the coil deformation during powering due to the electromagnetic forces is small (as expected).

## Slide 26: Persistent current effects (I)
Excellent agreement between measurements and model for the allowed harmonics
Estimates using magnetization measurements and the model developed based on HQ experience. [X. Wang]
Magnetization measured by M. Sumption and X. Xu at OSU
Strands provided by A. Ghosh and B. Bordini
(measurements performed in reference strands, not on extracted strands from MQXFS1)

## Slide 27: Persistent currents effects (II)
b3
a3
[X. Wang]
MQXFS1 used different strands layout:
  132/169 strands: CERN coils 103 and 104
  108/127 strands: LARP coils 3 and 5
As a result, additional non-allowed that are over-estimated in the model

## Slide 28: Outline
MQXFS1 parameters and features
Magnetic measurements system
Magnetic measurement overview
Geometric Field Errors
Machine Cycle Analysis
Summary and next steps

## Slide 29: Summary
Good agreement in terms of saturation, coil end effects and persistent currents.
Geometric field errors:
  b3 and a3 can be corrected through magnetic shims
  a4 can be explained due to the differences in between CERN/LARP coils.
  Higher order harmonics (as the measured b5) can be generated considering the measured azimuthal displacements on coil cross sections.
  The overall strength and longitudinal structure of the harmonics is not fundamentally altered from the initial assembly (collared coil) to powering  The dominant source of field errors is the coil geometry and its initial assembly in the collared coil.

## Slide 30: Plans
Based on MQXFS1a experience: field errors are very similar before and after magnet loading.
Based on HQ experience: coil pack assembly is enough to identify the non-allowed harmonic content simplify the process as there is no need to introduce the coil pack in the yoke-shell assembly.
Plans for MQXFS3: Perform two coil pack assemblies at CERN with different shimming configuration.
HQ02
HQ03
HQ02
HQ03

## Slide 31: Thank you

## Slide 32: Magnetic Measurements Plan
Current [kA] | Symbol | Gradient [T/m] | Remarks
0.01 | I.warm | 0.09 | Warm measurements
0.1 | I.res | 0.9 | Reset level for pre-cycle
0.96 | I.inj | 8.5 | Injection level
6.0 | I.lim | 48.8 | Current limit (pre-training)
16.48 | I.nom | 132.6 | Nominal level
17.76 | I.ult | 143.2 | Ultimate level
21.5 | I.ssl | 171.0 | 1.9K Short Sample Limit
Pre-cycle (applied to all measurements):
From 0 to I.nom at 14 A/s,
Hold for 300 s at I.nom,
Ramp down to I.res at 14 A/s
Hold for 0s at I.res
Ramp to I.inj at 14 A/s
[Hold at I.inj included in meas. cycle]
Studies performed:
Axial scans at I.warm, I.inj, I.lim, I.nom, I.ult
Accelerator cycles to I.nom, I.ult
Effect of reset current: [100], 300, 500 A
Long injection plateau: 6000 s
Stair-step loop (21 current steps)
Ramp rate dependence: [14], 20, 40, 80 A/s
Reference: MQXFS1 Test Plan, http://larpdocs.fnal.gov//LARP-public/DocDB/ShowDocument?docid=1079
Main Current Levels

## Slide 33: Harmonics at nominal current
 | Normal Components |  |  |  | Skew Components |  |  | 
n | Ave | Max | Min | Std. Dev. | Ave | Max | Min | Std. Dev.
3 | -4.21 | -1.83 | -5.34 | 1.14 | 3.29 | 5.06 | 1.14 | 1.37
4 | 0.32 | 2.06 | -0.96 | 1.10 | -6.49 | -5.11 | -8.14 | 0.96
5 | 2.76 | 3.16 | 2.58 | 0.19 | -0.87 | 0.09 | -1.42 | 0.50
6 | 0.95 | 3.53 | 0.27 | 0.95 | 0.52 | 1.76 | -0.45 | 0.68
7 | 0.18 | 0.43 | -0.19 | 0.19 | 0.32 | 0.77 | 0.07 | 0.20
8 | 0.25 | 0.34 | 0.12 | 0.07 | -0.65 | -0.44 | -0.88 | 0.15
9 | 0.22 | 0.40 | 0.07 | 0.12 | 0.33 | 0.48 | 0.15 | 0.09
10 | -0.51 | -0.36 | -1.07 | 0.19 | 0.16 | 0.26 | 0.04 | 0.07

## Slide 35
Roxie non-insulated conductors

## Slide 36: Transfer Function

## Slide 37: Probe Resolution (TC2)
Text

## Slide 38: Straight section b3, a3, b4, a4
Axial variations (measured with short probe) need to be considered when analyzing/evaluating results

## Slide 39: Before vs. After Pre-Loading
A measurable effect is observed, however, the overall strength and longitudinal structure of the harmonics is not fundamentally altered
Pre-load effect is relatively small compared to coil fabrication or initial assembly (collared coil)