## Slide 1: Coil strain
Paolo Ferracin and Giorgio Ambrosio
International Review of the Inner Triplet Quadrupoles (MQXF) for HL-LHC
7-10 June, 2016
CERN

## Slide 2: TQS01 – shell, keys, rods
No collars – islands attached to coil
Bladders for coil azimuthal pre-stress.
Piston for coil axial pre-stress.
Low RT assembly pre-stress.
High Cold assembly pre-stress.

## Slide 3: TQ coils

## Slide 4: TQS01/01b: Quench-Origin Comparison
1,4,5
Ramp
1
TQS01
Plateau
Ramp
TQS01b
Plateau
1

## Slide 5
TQC01 post test Island

## Slide 6: Coil fabrication process
Nb3Sn coils are wound around segmented bronze poles (heat treat.)
Because of bronze high thermal contraction, gaps open after cool-down and increase during ramp-up
In TQ test, quenches occurred around gaps: peak tension in pole turn
Displacement scaling: 100

## Slide 7: Coil fabrication process
Displacement scaling: 100
Nb3Sn coils are wound around segmented bronze poles (heat treat.)
Because of bronze high thermal contraction, gaps open after cool-down and increase during ramp-up
In TQ test, quenches occurred around gaps: peak tension in pole turn

## Slide 8: Coil fabrication process
Displacement scaling: 100
Nb3Sn coils are wound around segmented bronze poles (heat treat.)
Because of bronze high thermal contraction, gaps open after cool-down and increase during ramp-up
In TQ test, quenches occurred around gaps: peak tension in pole turn

## Slide 9: Coil fabrication process
Displacement scaling: 100
Nb3Sn coils are wound around segmented bronze poles (heat treat.)
Because of bronze high thermal contraction, gaps open after cool-down and increase during ramp-up
In TQ test, quenches occurred around gaps: peak tension in pole turn

## Slide 10: Coil fabrication process
Displacement scaling: 100
Nb3Sn coils are wound around segmented bronze poles (heat treat.)
Because of bronze high thermal contraction, gaps open after cool-down and increase during ramp-up
In TQ test, quenches occurred around gaps: peak tension in pole turn

## Slide 11: Coil fabrication process
Displacement scaling: 100
Nb3Sn coils are wound around segmented bronze poles (heat treat.)
Because of bronze high thermal contraction, gaps open after cool-down and increase during ramp-up
In TQ test, quenches occurred around gaps: peak tension in pole turn

## Slide 12: Coil fabrication process
Displacement scaling: 100
Nb3Sn coils are wound around segmented bronze poles (heat treat.)
Because of bronze high thermal contraction, gaps open after cool-down and increase during ramp-up
In TQ test, quenches occurred around gaps: peak tension in pole turn

## Slide 13: Coil fabrication process
Pole material changed to titanium alloy (low contraction)
  Pole in compression
Gap closed during operations
No peak tension in pole turn

## Slide 14: MQXFS1 – FE Strains (From G. Vallone)
Provided values are computed by means of the 3D FE model at the magnetic centre
Longitudinal strains:
  Negligible at room temperature
  Constant along the radial direction
  Almost equal on the pole turn and on mid-plane
  Not affected by the Lorentz Forces
PIn
PMid
POut
MIn
MMid
MOut
Pole Turn Strains |  |  |  |  |  | 
 |  |  |  | Longitudinal |  | 
Step |  |  |  | PIn | PMid | POut
Loading |  |  |  | 42 | 40 | 39
Cool-down |  |  |  | 1554 | 1549 | 1546
130 T/m |  |  |  | 1578 | 1574 | 1571
140 T/m |  |  |  | 1578 | 1574 | 1571
 |  |  |  | Longitudinal |  | 
Step |  |  |  | PIn | PMid | POut
Loading |  |  |  | 42 | 40 | 39
Cool-down |  |  |  | 1554 | 1549 | 1546
130 T/m |  |  |  | 1578 | 1574 | 1571
140 T/m |  |  |  | 1578 | 1574 | 1571
 | Mid Plane Strains |  |  |  |  | 
 |  |  |  | Longitudinal |  | 
Step |  |  |  | MIn | MMId | MOut
Loading |  |  |  | 45 | 42 | 41
Cool-down |  |  |  | 1601 | 1603 | 1614
130 T/m |  |  |  | 1631 | 1631 | 1644
140 T/m |  |  |  | 1634 | 1633 | 1648
 |  |  |  | Longitudinal |  | 
Step |  |  |  | MIn | MMId | MOut
Loading |  |  |  | 45 | 42 | 41
Cool-down |  |  |  | 1601 | 1603 | 1614
130 T/m |  |  |  | 1631 | 1631 | 1644
140 T/m |  |  |  | 1634 | 1633 | 1648

## Slide 15
100 %
95 %
90 %
From H. Bajas