## Slide 1: Cos-θ magnet status at CEA Saclay Maria DURANTE, Clément LORIN
WP10 General Meeting
CERN, Vidyo, 03/05/2016

## Slide 2: Cos-θ design
Design A - Cable A – « thick » cable : 12 x 1.2 mm² bare, 13 tapes Bruker 140-µm thick
Design B - Cable B – « thin » cable : 12 x 1.0 mm² bare, 15 tapes ép. 100 µm-thick
Cos-θ A : 1.2 mm + 2x100µm insulation, 14 turns
Cos-θ B : 1.0 mm + 2x125µm insulation, 17 turns
Layout | Unit | Cosϑ A | Cosϑ B
Iop | kA | 11.68 | 10.06
Bop | T | 5 | 5
Bpeak | T | 5.7 | 5.8
Ic | kA | 14.4 | 15.2
LL margin | (%) | 20 | 34
T margin | K | 20 | 30
Sd. inductance | mH/m | 0.49 | 0.73
coil inner radius | mm | 22 | 24
yoke inner raidus | mm | 50 | 50
yoke outer raidus | mm | 112 | 110
Nb. of turns | - | 14 | 17
Unit len. of cond. | m | 20 | 24

## Slide 3: Cos-θ : Insert Mode
Insert Mode
Layout | Unit | Cosϑ A | Cosϑ B
Iop | kA | 6.4 | 7.1
Bop | T | 2.1 + 13 | 2.6 + 13
Ic | kA | 7.1 | 7.9
LL margin | (%) | 10 | 10
T margin | K | 8 | 8
S. inductance | mH/m | 0.37 | 0.55
M. inductance | mH/m | 1.37 | 1.77
coil inner radius | mm | 22 | 24
inner tube th. | mm | 6 | 8
outer shell th. | mm | 12 | 10
Fx per ½ coil | kN/m | 1226 | 1669
Fy per ½ coil | kN/m | -60 | -95
Fz | kN | 61 | 90
σT | MPa | 140 | 155
σR | MPa | 75 (~50) | 110 (~70)
azi. deflection | µm | 125 | 140
von Mises inner | MPa | 600 | 760
von Mises outer | MPa | 240 | 250
Layout | unit | Cosϑ A & B
bore radius | mm | 16
external radius | mm | 49
pad (collar) th. | mm | 2.5

## Slide 4: Cos-θ : Quench protection
Quench analysis by Erkki Härö and Antti Stenvall (TUT)
    DESIGN A, done
      Standalone: very challenging
      Insert mode: ok
    DESIGN B, to be done ?
Standalone
Insert Mode

## Slide 5: Cos-θ : Magnet ends
Two end designs
  One spacer per cable turn
  (ew: 7.6 mm, hw: 2 m)
  Conventional design, 2/3 cable blocks (ew: 7.3 mm, hw: 22 cm)
Winding test with SS dummy Roebel cable
  Similar behavior for both ends
   Keep the conventional way as baseline

## Slide 6: Cos-θ : Coil 3D design
Design A coil
  Straight section = 200 mm
  Total length = 670 mm
  Cable unit length : 17 + 3 m
Design B coil
  Straight section = 200 mm
  Total length = 700 mm
  Cable unit length = 21 + 3 m

## Slide 7: Cos-θ : Magnet ends
Innermost turn path outwards the magnets
  Winding tests  improved support for the final coil
  
  Tests in collaboration with KIT on Desing B OK !
Mold 3 : twist 75° x 110 mm
Mold 2 : twist 75° x 80 mm
Mold 1 : S1 + twist + S2

## Slide 8: Cos-θ : Internal connexions
Superconductor side
Superconductor side
SC side
SC side
SC side

## Slide 9: Cos-θ : Instrumentation
Voltages taps
  Central wire co-wound to cancel inductive effects ?
Temperature sensors
  Strips inside the cable going out from the winding on the outer surface
  Long strips on the outer surface of each coil block
Trace development started

## Slide 10: Cos-θ : End spacers
Prospecting for 3D printing of end spacers started
  Visit of 3T RPD, UK (Thanks, Glyn !)
    Tolerance: +/-0.2 mm (possibility to go down to +/- 0.1 mm)
    Roughness: Ra = 5 µm on surfaces in contact with cable, 50 µm elsewhere
    Spacer slit in the z-direction
    Two options : Solid or Hollow pieces (2-mm-wall thickness)
  An offer from 3DSystems, FR
  PRODWAY, FR to be contacted
z direction

## Slide 11: Cos-θ : Tools 1/2
Coil winding tools

## Slide 12: Cos-θ : Tools 2/2
Coil Impregnation tools
Call for tender launched for design A tools
Detailed studies for Design B tools is ongoing

## Slide 13: Cos-θ : Schedule
Procurements : mid-end of June 2016
Dummy cable: 2 x 20 m – mid of June 2016
Dummy coils (winding-impregnation): July-August 2016
Dummy magnet assembling: September-October 2016
Superconducting cable: 3 x 20 m – End of September 2016
Start working of SC magnet: October-November 2016