## Slide 1: Pulsed Laser Deposition

## Slide 2: Pressure tests
Name | Substrate | Pressure N2 (Pa) | Average δmax
PLD_aC_09_1 | Cu | Vacuum (<5.00E-7) | 1.24
PLD_aC_06_1 | St St | 2 | 1.04
PLD_aC_07_1 |  |  | 1.17
PLD_aC_08_1 |  |  | 1.17
PLD_aC_09_2 | Cu |  | 1.2
PLD_aC_10_2 | Cu | 4 | 0.971
PLD_aC_11_2 |  |  | 0.97
PLD_aC_12_1 |  |  | 0.964
PLD_aC_14_2 |  |  | 0.98
PLD_aC_10_1 | Cu | 8 | 0.912
PLD_aC_11_1 |  |  | 0.953
PLD_aC_12_2 |  |  | 0.954
PLD_aC_14_1 |  |  | 0.969
PLD_aC_13_2 | Cu | 15 | 0.956
PLD_aC_13_1 | Cu | 20 | 0.986
Chart: δmax VS Pressure
| 4.9999999999999998E-7 | 2 | 2 | 2 | 2 | 4 | 4 | 4 | 4 | 8 | 8 | 8 | 8 | 15 | 20
 | 1.24 | 1.04 | 1.17 | 1.17 | 1.2 | 0.971 | 0.97 | 0.964 | 0.98 | 0.912 | 0.953 | 0.954 | 0.969 | 0.956 | 0.986
Laser fluence Φ = 2.2 to 2.5 J/cm²
Substrate : rolled St. St. or Cu foil
Deposition duration : 15 min
1
2
3

## Slide 3: Pressure tests
Chart: PLD_aC_10_2 4 Pa of N2
| -1.4224730000000001E-15 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 160 | 220 | 280 | 340 | 400 | 460 | 520 | 580 | 640 | 700 | 760 | 800 | 900 | 1000 | 1100 | 1200 | 1300 | 1400 | 1500 | 1600 | 1700 | 1800
PLD_aC_10_2_p1 | 1.0003 | 0.32413 | 0.43011 | 0.48795 | 0.51485 | 0.56968 | 0.61659 | 0.65793 | 0.71127 | 0.7507 | 0.78666 | 0.91133 | 0.94612 | 0.94564 | 0.91935 | 0.88588 | 0.8456 | 0.80598 | 0.76986 | 0.73333 | 0.69986 | 0.66699 | 0.64875 | 0.60458 | 0.56743 | 0.53645 | 0.50726 | 0.48038 | 0.45756 | 0.43694 | 0.41904 | 0.40045 | 0.38767
PLD_aC_10_2_p2 | 1.0002 | 0.34941 | 0.45155 | 0.51426 | 0.54761 | 0.59894 | 0.65298 | 0.69884 | 0.74617 | 0.78626 | 0.82356 | 0.94897 | 0.9824 | 0.97892 | 0.94757 | 0.91039 | 0.86517 | 0.82342 | 0.78232 | 0.74306 | 0.70894 | 0.67876 | 0.65813 | 0.61291 | 0.57696 | 0.54298 | 0.51187 | 0.48395 | 0.4645 | 0.4432 | 0.42368 | 0.40829 | 0.39532
PLD_aC_10_2_p3 | 1.0014 | 0.35408 | 0.45984 | 0.51733 | 0.54861 | 0.60392 | 0.65521 | 0.69482 | 0.74585 | 0.79073 | 0.82536 | 0.95134 | 0.98462 | 0.9811 | 0.95047 | 0.90824 | 0.86566 | 0.82289 | 0.78203 | 0.74501 | 0.71079 | 0.67815 | 0.65624 | 0.61355 | 0.57436 | 0.54101 | 0.51292 | 0.48721 | 0.46589 | 0.44375 | 0.42738 | 0.40821 | 0.39263
45°
Laser 248 nm
+ Optics
3
2
1
Chart: PLD_aC_13_1 20 Pa of N2
| 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 160 | 220 | 280 | 340 | 400 | 460 | 520 | 580 | 640 | 700 | 760 | 800 | 900 | 1000 | 1100 | 1200 | 1300 | 1400 | 1500 | 1600 | 1700 | 1800
PLD_aC_13_1_p1 | 1.0004 | 0.30162 | 0.42042 | 0.48621 | 0.50817 | 0.57025 | 0.61717 | 0.65922 | 0.70318 | 0.74663 | 0.78897 | 0.9161 | 0.95748 | 0.95994 | 0.947 | 0.9079 | 0.87069 | 0.82708 | 0.79288 | 0.76141 | 0.72187 | 0.68795 | 0.66424 | 0.64029 | 0.5953 | 0.56086 | 0.54032 | 0.51098 | 0.47979 | 0.46039 | 0.44372 | 0.4195 | 0.40105
PLD_aC_13_1_p2 | 0.99995 | 0.2808 | 0.38886 | 0.44509 | 0.47622 | 0.55121 | 0.57721 | 0.62876 | 0.6805 | 0.71766 | 0.74104 | 0.86663 | 0.91628 | 0.95009 | 0.89939 | 0.8798 | 0.85454 | 0.81806 | 0.78239 | 0.75867 | 0.73314 | 0.68577 | 0.69113 | 0.63623 | 0.59261 | 0.55448 | 0.53205 | 0.50699 | 0.47581 | 0.45976 | 0.44886 | 0.42863 | 0.41203
PLD_aC_13_1_p3 | 0.99815 | 0.31591 | 0.44576 | 0.51311 | 0.55674 | 0.62854 | 0.68994 | 0.72516 | 0.76894 | 0.81613 | 0.8539 | 0.98359 | 1.0358 | 1.0256 | 1.0238 | 0.99102 | 0.94277 | 0.92845 | 0.89549 | 0.8643 | 0.83767 | 0.80279 | 0.77542 | 0.7302 | 0.67542 | 0.64906 | 0.61054 | 0.57821 | 0.55079 | 0.52545 | 0.49693 | 0.47203 | 0.45998
Chart: PLD_aC_13_1
| O 1s | N 1s | Cu 2p
PLD_aC_13_1_p1 | 9.127 | 6.042 | 1.465
PLD_aC_13_1_p2 | 8.154 | 5.909
PLD_aC_13_1_p3 | 7.885 | 4.608
Point 1 : 1.5 % of Cu : carbon layer non homogeneous
Different δmax in 1 sample
Copper content at higher pressures

## Slide 4: Influence of the base pressure
Name | Subs. | Base pres. (mbar) | Pres. N2 (Pa) | Average δmax
PLD_aC_10_2 | Cu | < 5.00*10-9 | 4 | 0.971
PLD_aC_11_2 |  |  |  | 0.97
PLD_aC_12_1 |  |  |  | 0.964
PLD_aC_14_2 |  | 6.7*10-7 |  | 0.98
PLD_aC_10_1 | Cu | < 5.00*10-9 | 8 | 0.912
PLD_aC_11_1 |  |  |  | 0.953
PLD_aC_12_2 |  |  |  | 0.954
PLD_aC_14_1 |  | 6.7*10-7 |  | 0.969
Chart: 8 Pa of N2
| 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 160 | 220 | 280 | 340 | 400 | 460 | 520 | 580 | 640 | 700 | 760 | 800 | 900 | 1000 | 1100 | 1200 | 1300 | 1400 | 1500 | 1600 | 1700 | 1800
5.10-9_10_1_p3 | 1.002 | 0.3233 | 0.42019 | 0.46752 | 0.5017 | 0.55306 | 0.59483 | 0.64191 | 0.68452 | 0.71826 | 0.7505 | 0.87007 | 0.91459 | 0.92373 | 0.90986 | 0.88676 | 0.85338 | 0.81532 | 0.78114 | 0.74665 | 0.71393 | 0.68695 | 0.67006 | 0.62969 | 0.59582 | 0.5621 | 0.53252 | 0.50573 | 0.47884 | 0.45916 | 0.44091 | 0.42206 | 0.41129
5.10-9_11_1_p3 | 1.0005 | 0.33456 | 0.44735 | 0.50337 | 0.53369 | 0.58757 | 0.62983 | 0.68056 | 0.7336 | 0.77249 | 0.81566 | 0.94776 | 0.97636 | 0.97691 | 0.96373 | 0.90815 | 0.86895 | 0.82495 | 0.78571 | 0.75066 | 0.71778 | 0.68923 | 0.66655 | 0.61909 | 0.58138 | 0.54111 | 0.51076 | 0.48868 | 0.46254 | 0.44395 | 0.4308 | 0.4128 | 0.39445
5.10-9_12_2_p1 | 0.99976 | 0.32089 | 0.43976 | 0.48299 | 0.51019 | 0.57514 | 0.61518 | 0.65015 | 0.70785 | 0.75099 | 0.78398 | 0.90792 | 0.9492 | 0.96283 | 0.9318 | 0.89773 | 0.86162 | 0.82405 | 0.78541 | 0.75335 | 0.72279 | 0.69032 | 0.67193 | 0.63122 | 0.58921 | 0.55213 | 0.52722 | 0.49815 | 0.46867 | 0.45279 | 0.43595 | 0.41435 | 0.40302
7.10-7_14_1_p1 | 0.9982 | 0.31311 | 0.42422 | 0.48566 | 0.53358 | 0.58006 | 0.63036 | 0.68003 | 0.72613 | 0.76651 | 0.80219 | 0.91668 | 0.96445 | 0.98238 | 0.97321 | 0.95223 | 0.92349 | 0.8615 | 0.80069 | 0.74364 | 0.69278 | 0.64759 | 0.60708 | 0.57336 | 0.54194 | 0.4919 | 0.45255 | 0.41712
Chart: 4 Pa of N2
| 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 160 | 220 | 280 | 340 | 400 | 460 | 520 | 580 | 640 | 700 | 760 | 800 | 900 | 1000 | 1100 | 1200 | 1300 | 1400 | 1500 | 1600 | 1700 | 1800
5.10-9_10_2_p3 | 1.0014 | 0.35408 | 0.45984 | 0.51733 | 0.54861 | 0.60392 | 0.65521 | 0.69482 | 0.74585 | 0.79073 | 0.82536 | 0.95134 | 0.98462 | 0.9811 | 0.95047 | 0.90824 | 0.86566 | 0.82289 | 0.78203 | 0.74501 | 0.71079 | 0.67815 | 0.65624 | 0.61355 | 0.57436 | 0.54101 | 0.51292 | 0.48721 | 0.46589 | 0.44375 | 0.42738 | 0.40821 | 0.39263
5.10-9_11_2_p3 | 1.0005 | 0.33456 | 0.44735 | 0.50337 | 0.53369 | 0.58757 | 0.62983 | 0.68056 | 0.7336 | 0.77249 | 0.81566 | 0.94776 | 0.97636 | 0.97691 | 0.96373 | 0.90815 | 0.86895 | 0.82495 | 0.78571 | 0.75066 | 0.71778 | 0.68923 | 0.66655 | 0.61909 | 0.58138 | 0.54111 | 0.51076 | 0.48868 | 0.46254 | 0.44395 | 0.4308 | 0.4128 | 0.39445
5.10-9_12_1_p3 | 0.99863 | 0.34148 | 0.45553 | 0.50759 | 0.54141 | 0.6039 | 0.64886 | 0.69123 | 0.74362 | 0.78443 | 0.81869 | 0.94831 | 0.98886 | 0.99079 | 0.97092 | 0.93008 | 0.8894 | 0.84909 | 0.80792 | 0.77031 | 0.73684 | 0.70343 | 0.68274 | 0.63982 | 0.59848 | 0.56387 | 0.53758 | 0.50835 | 0.48202 | 0.46475 | 0.4447 | 0.42283 | 0.41138
7.10-7_14_2_p3 | 1.0011 | 0.32066 | 0.43515 | 0.49954 | 0.54761 | 0.59409 | 0.6447 | 0.6911 | 0.74062 | 0.78096 | 0.81536 | 0.92867 | 0.97238 | 0.98604 | 0.97226 | 0.94495 | 0.91227 | 0.84164 | 0.77511 | 0.71554 | 0.66466 | 0.61969 | 0.58013 | 0.54853 | 0.51722 | 0.46743 | 0.42893 | 0.39581
δmax not sensitive to the base pressure up to 7*10-7 mbar

## Slide 5: Air exposure
Name | Subs. | Base pres. (mbar) | Pres. N2 (Pa)
PLD_aC_10_1 | Cu | < 5.00*10-9 | 8
Chart: Ageing
| 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 160 | 220 | 280 | 340 | 400 | 460 | 520 | 580 | 640 | 700 | 760 | 800 | 900 | 1000 | 1100 | 1200 | 1300 | 1400 | 1500 | 1600 | 1700 | 1800
J+0_10_1_p2 | 1.0007 | 0.3115 | 0.4167 | 0.4598 | 0.4835 | 0.53154 | 0.54342 | 0.60368 | 0.68101 | 0.74389 | 0.75347 | 0.89636 | 0.90412 | 0.90976 | 0.88981 | 0.84205 | 0.83556 | 0.80727 | 0.78627 | 0.75792 | 0.7367 | 0.70108 | 0.66542 | 0.61699 | 0.58039 | 0.55349 | 0.52758 | 0.50585 | 0.48146 | 0.46366 | 0.44286 | 0.41832 | 0.4008
J+17_10_1_p2 | 1.0005 | 0.34859 | 0.43762 | 0.51539 | 0.56459 | 0.61605 | 0.64698 | 0.68772 | 0.73598 | 0.77658 | 0.81798 | 0.93792 | 0.97729 | 0.9976 | 0.99202 | 0.97304 | 0.9216 | 0.88517 | 0.83378 | 0.77786 | 0.7445 | 0.6788 | 0.63512 | 0.59733 | 0.57172 | 0.5247 | 0.48025 | 0.44723
Conditions | δmax
1h air exposed + 4 days in vacuum | 0.910
17 days air exposed in Al foil | 0.998
+10%

## Slide 6: Electron energy loss spectroscopy
δmax decreases = intensity at 290 eV (C1s peak) increases
+ losses intensity increases
Chart: SEY
| -1.4224730000000001E-15 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 150 | 200 | 250 | 300 | 350 | 400 | 500 | 600 | 700 | 800 | 900 | 1000 | 1100 | 1200 | 1400 | 1600 | 1800
PLD_aC_10_1_air | 1.0005 | 0.34859 | 0.43762 | 0.51539 | 0.56459 | 0.61605 | 0.64698 | 0.68772 | 0.73598 | 0.77658 | 0.81798 | 0.93792 | 0.97729 | 0.9976 | 0.99202 | 0.97304 | 0.9216 | 0.88517 | 0.83378 | 0.77786 | 0.7445 | 0.6788 | 0.63512 | 0.59733 | 0.57172 | 0.5247 | 0.48025 | 0.44723
PLD_aC_05_flat | 0.96672 | 0.56909 | 0.73991 | 0.86712 | 0.95672 | 1.0651 | 1.1112 | 1.1882 | 1.2533 | 1.3413 | 1.3839 | 1.5215 | 1.5698 | 1.5513 | 1.5168 | 1.4568 | 1.3941 | 1.2977 | 1.1662 | 1.0744 | 0.9958 | 0.9325 | 0.87103 | 0.82141 | 0.78132 | 0.70109 | 0.64291 | 0.59296
PLD_aC_04_2_ext | 0 | 0.38736 | 0.64711 | 0.86683 | 0.99787 | 1.1102 | 1.2052 | 1.2887 | 1.3929 | 1.4648 | 1.5282 | 1.5843 | 1.7295 | 1.7566 | 1.7178 | 1.6452 | 1.5544 | 1.4707 | 1.3169 | 1.1837 | 1.0772 | 0.99107 | 0.92109 | 0.85781 | 0.80695 | 0.7639 | 0.68901 | 0.62884 | 0.58262
Chart: EELS

## Slide 7: Adhesion test
Name | Substrate | Pressure N2 (Pa) | Average δmax
PLD_aC_09_1 | Cu | Vacuum (<5.00E-7) | 1.24
PLD_aC_12_1 | Cu | 4 | 0.964
PLD_aC_12_2 | Cu | 8 | 0.954
PLD_aC_13_1 | Cu | 20 | 0.986
For all the samples : very low adhesion (dollies removed without pulling them off)
-> try adhesion tests on samples with stainless steel substrate
Evaluate the adhesion of the layers
Effect of the pressure

## Slide 8: Deposition in a full tube
Experimental setup :
Rolled Cu foil
Target manually rotated
Deposition duration : 30 min
8 Pa of N2
Inhomogeneity of the width : geometrical effect
Plasma plume disappears during the deposition : ablation rate non constant ?
Chart: PLD_aC_15_1
| -1.4224730000000001E-15 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 150 | 200 | 250 | 300 | 350 | 400 | 500 | 600 | 700 | 800 | 900 | 1000 | 1100 | 1200 | 1400 | 1600 | 1800
PLD_aC_15_1_p1 | 1.0004 | 0.37741 | 0.47496 | 0.52594 | 0.56635 | 0.59697 | 0.63305 | 0.66709 | 0.72518 | 0.78725 | 0.86115 | 0.95782 | 0.97349 | 0.98745 | 0.97876 | 0.9679 | 0.93083 | 0.87184 | 0.80798 | 0.75058 | 0.6997 | 0.65338 | 0.61108 | 0.57635 | 0.54907 | 0.4981 | 0.46286 | 0.43973
PLD_aC_15_1_p2 | 1.0006 | 0.36663 | 0.46651 | 0.5223 | 0.56854 | 0.6066 | 0.65299 | 0.69898 | 0.74233 | 0.78151 | 0.81468 | 0.91726 | 0.96796 | 0.97787 | 0.97066 | 0.95239 | 0.92379 | 0.86528 | 0.80724 | 0.7533 | 0.70459 | 0.66157 | 0.6213 | 0.5878 | 0.55895 | 0.50817 | 0.46821 | 0.43794
PLD_aC_15_1_p3 | 1.0004 | 0.37903 | 0.47605 | 0.53388 | 0.58332 | 0.62336 | 0.66802 | 0.71361 | 0.75956 | 0.79691 | 0.83221 | 0.94011 | 0.98092 | 0.99771 | 0.98887 | 0.96728 | 0.94054 | 0.87304 | 0.81257 | 0.75566 | 0.70395 | 0.66008 | 0.6217 | 0.58703 | 0.55483 | 0.50422 | 0.46593 | 0.43617

15_1
15_2
Chart: PLD_aC_15_1
| O 1s | N 1s | Cu 2p
PLD_aC_15_1_p1 | 8.642 | 3.852 | 0.151
PLD_aC_15_1_p2 | 7.879 | 3.065
PLD_aC_15_1_p3 | 7.571 | 2.295