## Slide 1: Superconducting Magnets
Gijs de Rijk
CERN
CAS
Budapest, Hungary, 7th October 2016

## Slide 2: High Field Accelerator Magnets
Introduction: magnetic field and superconducting magnets
How to get high fields in accelerator dipole and quadrupole magnets ?
Superconductors for magnets
Practical accelerator magnet design
High field superconducting magnets for future accelerators
Literature on High Field Magnets
2

## Slide 3: Maxwell equations
Integral form Differential form
With:
Ampere’s law
Faraday’s equation
Gauss’s law for magnetism
Gauss’s law

## Slide 4: Magnetic field quality: multipole description
In a ring shaped accelerator, where the beam does multiple passes, one typically demands :

## Slide 5: Magnetic Length
In 3D, the longitudinal dimension of the magnet is described by a magnetic length
A circular yoke around the coil can give a 10-15% field increase
The magnetic length Lmag for SC magnets is adjustable by varying the length of the yoke: often the coils stick outside the end of the yoke: no easy rule of thumb for Lmag
Courtesy A. Milanese, CERN
Notes: Looking along the longitudinal (z) direction, the field B is maximum at the centre (z = 0) of the magnet, it is more or less constant till reaching the ends, where it rolls off to reach a 0 value outside. The magnetic length lm is defined as that length which – multiplied by the central field value B0 – returns the same integrated field.
The same holds substituting the field B with the gradient G, or with any multipoles Bn, An. In this case, the integrals have to be performed on the not-normalized (upper case) coefficients, and the normalized terms (lower case) are then obtained by dividing by the integral of the fundamental harmonic.
For long magnets – where the longitudinal dimension is much larger than the gap – the behavior is dominated by the (long) central part, so taking the values of 2D simulations and multiplying by a length yields good results. For short magnets, the behavior is intrinsically 3D.

## Slide 6: Magnetic fields
From Ampere’s law with no time dependencies
We can derive the law of Biot and Savart
(Integral form)
If you wanted to make a B = 8 T magnet with just two infinitely thin wires placed at 50 mm distance one needs : I = 5105 A
LHC dipole coil 80 turns of 11850 A at 8.3 T = 9.48105 A )
To get high fields one needs very large currents in small volumes
For LHC dipole@8.3 T ~1 MA in 3300 mm2 : ~300 A/mm2
(overall current density in the coil area)
Courtesy E. Todesco

## Slide 7: Coils for generating the Perfect Dipole Field
Conductors 2 solid Intercepting ellipses (or circles)
  A uniform, opposite polarity, current density in the area of two intersecting ellipses produces a pure dipolar field, but:
    The aperture is not circular
    Not easy to simulate with a flat cable
Thick conductor shell with a cos current distribution J = J0 cosQ
  Pure dipolar field
  Easier to reproduce with a flat rectangular cable
q

## Slide 8: Magnet types and higher orders
a “pure” multipolar field can be generated by a specific coil geometry
dipole n=1
quadrupole n=2
sextupole n=3
skew
normal
Courtesy P. Ferracin, CERN

## Slide 9: What is specific about accelerator magnets ?
Cylindrical volume with perpendicular field
Dipoles, quadrupoles, etc
Field quality:
Field quality formulated and measured in a multipole expansion,
Long magnets: dipoles from 6 m (Tevatron) to 15 m (LHC)
Often magnets are bend (9.14 mm sagitta for the LHC dipoles)
Artist view of a dipole, from M. N. Wilson « Superconducting Magnets »
CosQ coil : J = J0 cosQ

## Slide 10: The state of the art: Comparison between dipoles and solenoids
We can see roughly a factor 2 due to Coil «efficiency» and to force-stress management
Courtesy L. Rossi

## Slide 11: Superconducting accelerators magnets; the state of the art
Maximum attainable field slowly approaches 16 T
  20% margin needed (80% on the load line):
  for a 16 T nominal field we need to design for 20 T

## Slide 12: Forces
Scaling of force on coil quadrant vs. Field
Plot for recent production and R&D dipoles
The electromagnetic loads in a 20 T dipole would be a factor 5 to 8 larger than in the LHC dipoles

## Slide 13: Stored Energy
Scaling of the energy per unit length of magnet vs. Field
Plot for recent production and R&D dipoles
Scaling of the energy per unit length of magnet in recent production vs. R&D dipoles
x10

## Slide 14: Existing Superconducting Accelerator dipole magnets (1)
.
HERA
75 mm bore
B = 5.0 T
T = 4.5 K
first beam 1991
Tevatron
76 mm bore
B = 4.4 T
T = 4.2 K
first beam 1983
RHIC
80 mm bore
B = 3.5 T
T = 4.3-4.6 K
first beam 2000
LHC
56 mm bore
B = 8.34 T
T = 1.9 K
first beam 2008
Courtesy P. Ferracin, CERN
Notes: All these machines are cooled with He. LHC is the only one to work with superfluid helium. These extra 2 K mean a lot – the cryogenic system becomes at once more complex and less thermodynamically efficient – though the heat transfer between the bath and the coil is much improved. From a magnetic viewpoint, working at 1.9 K instead of 4.2 K shifts the critical current curve of Nb-Ti enough to make operation at 8.3 T (or almost, we are at 7.7 T now in the machine) possible with margin.
LHC is the only twin bore layout of these four.
The Tevatron is the only one with a warm iron yoke, that is, the iron is not in the cold (liquid He) mass.

## Slide 15: Existing Superconducting Accelerator dipole magnets (2)
RHIC: 3.5 T
2000
Tevatron: 4.4 T
1983
HERA: 5 T
1992
LHC: 8.34 T
2008
Courtesy R. Gupta

## Slide 16: Existing Superconducting Accelerator dipole magnets (3)
20 years were needed to go from 4 T to 8 T !
Machine | place | Type | Energy (GeV) | Peak Dipole field (T) | ♯ dipoles | Dipole Length (m) | Ring circ. (km) | Year
Tevatron | FNAL (USA) | p-pbar FT/coll. | 1000 x 1000 | 4.4 | 774 | 6.12 | 6.28 | 1983/ 1987
HERA | DESY (D) | e-/+ - p collider | 40x920 | 5 | 416 | 8.82 | 6.34 | 1992
RHIC | BNL (USA) | p-p, Au-Au, Cu-Cu, d-Au | 100/n | 3.5 | 2x192+12 | 9.45 | 3.83 | 2000
LHC | CERN (Eu) | p-p, Pb-Pb | 7000 x 7000 | 8.34 | 1232 | 14.3 | 26.66 | 2008

## Slide 17: Type II Superconductors
Below a the critical surface the material is “superconducting”. Above the surface it is “normal conducting”
Qc Critical Temperature (at zero field and current density)
Bc2 Critical Field (at zero temperature and current density)
Jc Critical Current Density ( at zero temperature and field)
The Critical surface depends on the material type Nb-Ti, Nb3Sn, etc) and the processing
Superconducting
means: R = 0
J: few x 103 A/mm2 inside the superconductor
Critical surface
for Nb-Ti
Courtesy M. Wilson
Courtesy L. Bottura
Quantized fluxoids in a superconductor

## Slide 18: Superconductivity
Typical operational conditions (0.85 mm diameter strand)
Cu
Nb3Sn
Nb-Ti
J ~ 5 A/mm2
I ~ 3 A
B = 2 T
J ~ 1500-2000 A/mm2
I ~ 400 A
B = 8-9 T
J ~ 1500-2000 A/mm2
I ~ 400 A
B = 12-13-16 T
Courtesy P. Ferracin, CERN

## Slide 19: Superconducting materials: Nb-Ti
Niobium and titanium combine in a ductile alloy
  It is easy to process by extrusion and drawing techniques.
When cooled down to about 9 K it becomes a type II superconductor.
  Tc is ~9.2 K at 0 T.
  BC2 is ~14.5 T at 0 K.
The cost is approximately 100-150 US$ per kg of wire.
Courtesy: M.N. Wilson

## Slide 20: Superconducting materials: Nb3Sn
Niobium and tin form Nb3Sn
  Brittle and strain sensitive
When cooled down to about 18 K it becomes a type II superconductor.
  TC0m is ~18 K at 0 T and 0 strain.
  BC20m is ~28 T at 0 K and 0 strain.
The cost is approximately 700-1500 US$ per kg of wire.
Courtesy: A. Godeke

## Slide 21: Available Superconductors
Nb-Ti: the workhorse for 4 to 10 T
  Up to ~2500 A/mm2 at 6 T and 4.2K or at 9 T and 1.9 K
  Well known industrial process, good mechanical properties
  Thousands of accelerator magnets have been built
  10 T field in the coil is the practical limit at 1.9 K
Nb3Sn: towards 20 T
  Up to ~3000 A/mm2 at 12 T and 4.2 K
  Complex industrial process, higher cost, brittle and strain sensitive
  25+ short models for accelerator magnets have been built
  ~20 T field in the coil is the practical limit at 1.9 K, but above 16 T coils will get very large
HTS materials: dreaming 40 T (Bi-2212, YBCO)
Current density is low, but very little dependence on the magnetic field
Used in solenoids (20T range), used in power lines – no accelerator magnets have been
built (only 1 model) – small racetracks have been built

## Slide 22: High temperature superconductor zoo

## Slide 23: Superconducting strands: Nb-Ti
B(T)
J(A/mm2)
T(K)
Nb-Ti is the workhorse for present accelerators, medical magnets, cyclotrons, etc

## Slide 24: Multifilament wires Fabrication of Nb-Ti multifilament wires
Monofilament rods are stacked to form a multifilament billet, which is then extruded and drawn down.
When the number of filaments is very large, multifilament rods can be re-stacked (double stacking process).
A. Devred
Courtesy A. Devred, ITER; P. Ferracin, CERN

## Slide 25: Multifilament wires Fabrication of Nb3Sn multifilament wires
Since Nb3Sn is brittle, it cannot be extruded and drawn like Nb-Ti.
The process requires several steps:
  Assembly multifilament billets from Nb3Sn precursor
  Fabrication of the wire through extrusion-drawing
  Fabrication of the cable
  Fabrication of the coil
  “reaction”: the Cu, Sn and Nb are heated to 600-700 C and the Sn diffuses in Nb and reacts to form Nb3Sn
Powder in tube (PIT) process
Courtesy P. Ferracin, CERN

## Slide 26: Nb3Sn strand types

## Slide 27: Superconducting strands and tapes: BSCO
BSCO: Bismuth strontium calcium copper oxide
Available in strands (OST)
Can reach 400 A/mm2 (overall)
Is fragile under stress and strain
Powder in a silver tube
Has to be reacted at 850°C with a temperature precision of 1°C in an oxygen atmosphere
Can be cabled in high current Rutherford cables
Difficult technology but could be promising for high field magnets in >20 T region

## Slide 28: Superconducting tapes: YBCO
YBCO: Yttrium barium copper oxide
Available in tapes : YBCO deposited on a substrate to impose the texture (1-2 mm)
Can reach > 600 A/mm2 (overall)
Is strong under axial stress and strain
Limited cabling possibilities:
Difficult technology but could be promising for high field magnets in >20 T region.
A

## Slide 29: Superconducting cables for magnets
We need multi-strand cables
  Superconducting accelerators are ramped up in time spans 100 s to 1000 s
  Coils are designed for voltages to ground of around 1000 V
  With the number of turns and the current the inductance is to be limited to keep the voltage below 1000 V
  Dipoles and Current:
    Tevatron B = 4.4 T ; I ~ 4000 A
    Hera B = 5 T ; I ~ 6000 A
    LHC B = 8.3 T ; I ~ 12000 A
  For magnets 10 T < B < 15 T the current has to be 10kA < I < 15 kA
  For stability reasons strands are 0.6 mm < strand diameter < 1 mm
  With a Cu-nonCu ratio (stability) around 1 and a Jc ~ 1000 A/mm2
   a 1 mm diameter strand can carry ~400 A
   so we need a 30 strand cable to get up to 12 kA

## Slide 30: Cable types
.
Courtesy A. Balarino

## Slide 31: Rutherford cables
Compact cables giving high overall current density
Easy rectangular geometry for convenient winding

## Slide 32: How to get high fields in accelerator dipole and quadrupole magnets ?
From Ampere’s law one can derive the field resulting from the current in a line conductor and integrate this over the surface of a coil
Dipole 60º sector coil [see ref 10, 14]
  The field is proportional to the current density j
  The field is proportional to coil width
  The field is independent of aperture
with: r : inner radius coil
w : coil width
r : radial coordinate
J : current density
Quadrupole 30º sector coil [see ref 11, 14]
  The gradient is proportional to the current density j
  The gradient depends on w/r
 by having very high current density close to the beam pipe
Cross-section of a
dipole
based on 60º sector coils
Cross-section of a quadrupole
based on 30º sector coils
See: E. Todesco et al. ref[10] and indirectly : N. Wilson ref[1], K-H Mess et al. ref[2]
For a in depth study of magnetic field calculations: S. Russenschuck ref[4]

## Slide 33: The forces with high field dipole and quadrupole magnets
One can derive the maximum stress in the mid-plane for a sector dipole coil
Dipole 60º sector coil [see ref 1, 12]
(Typically: for 8T : 40 MPa , for 13 T 130 MPa )
with: r : inner radius coil
r : radial coordinate
w : coil width
J : current density
Quadrupole 30º sector coil [see ref 1, 13 ]
Cross-section of a
dipole
based on 60º sector coils
Cross-section of a quadrupole
based on 30º sector coils
Courtesy M. Wilson

## Slide 34: Electro-magnetic forces
The e.m. forces in a dipole magnet tend to push the coil
  Towards the mid plane in the vertical-azimuthal direction (Fy, F < 0)
  Outwards in the radial-horizontal direction (Fx, Fr > 0)
Tevatron dipole
HD2
TQ
HQ
The e.m. forces in a quadrupole magnet tend to push the coil
  Towards the mid plane in the vertical-azimuthal direction (Fy, F < 0)
  Outwards in the radial-horizontal direction (Fx, Fr > 0)
Courtesy P. Ferracin, CERN

## Slide 35: Conductor stability and AC behaviour
Pure massive superconductor is not stable as they (Nb-Ti, Nb3Sn) are poor normal conductors
To ‘cryogenically stabilize’ the conductor one surrounds it in Cu:
  good electrical conductivity
  good heat transfer to the He
During current ramping the filaments will magnetize  make them thinner
Filaments will have magnetic coupling  twist the strand
Practical low temperature superconductors are made as thin (5 mm – 100 mm) superconducting filaments in a Cu matrix , which is twisted
Courtesy M. Wilson

## Slide 36: Quench: a thermal runaway effect
Due to perturbations locally the conductor can get T > Tc (Jl,Bl)
A thermal runaway can then occur, called a Quench
With stored energies > MJ the coils can overheat if nothing is done (T = 3000K is possible ! )
What to do ?
Detect the quench : SC: R=0  V=0, quench V>0 (typically 100mV threshold)
Switch power convertor off
Heat up the whole coil with quench heaters
Dump energy of the circuit into a dump resistor

## Slide 37: Practical accelerator magnet design: Dipoles
Two types of coils are in use for high field magnets:
Cos(Q) coil and Block coil
Cos(Q) coil (the traditional solution)
  Allows a very good field quality (bn < 1.10-4) in thin coils
    all (but one) existing accelerators use this type of coil
  Is very efficient wrt the quantity of superconductor used
  The EM forces cause a stress buildup at the midplane where also high fields are located
  Wedges are needed in the straight part (‘Keystoned’ cable)
  The ends are short, special geometry for which there is a large experience but not it is easy
D20
Courtesy LBNL
Courtesy M. Wilson

## Slide 38: Practical accelerator magnet design: Dipoles
Block coil (used on development magnets)
  Used with thick coils the field quality is good
    Not yet used in accelerators
  Is less efficient (~10%) wrt to cos(Q) for quantity of superconductor used
  The EM forces cause a stress buildup at the outside edge of the coil where the fields are lower
  The straight part is very easy : rectangular cable and wedges (field quality)
  ‘flared ends’ look easy but there is little experience exists to make them
HD2
Courtesy LBNL

## Slide 39: Quadrupole coil geometries
Cos(Q) coil
  Allows a very good field quality (bn < 1.10-4)
    all (but one) existing accelerators use this type of coil
  Is very efficient wrt the quantity of superconductor used
  The EM forces cause a stress buildup at the midplane where also high fields are located, (but are limited)
  Wedges are needed in the straight part (‘Keystoned’ cable)
  The ends are short, special geometry for which there is a large experience but not it is easy
Courtesy M. Wilson

## Slide 40: Prestress
Why prestress ?
  Field quality is determined by the cable positioning (be precise to ~0.02 mm)
  Under the MN forces the coils will move
    Apply prestress to fix the positioning
  Very small amounts of heat can quench the coil: limit the movement (avoid stick-slip effects on ~10 mm movements)
    Apply prestress to fix the positioning
How to put prestress ?
  Three methods:
  Compress at room temperature: collar system
  Use room temperature prestress plus differential shrinkage at cooldown: Al or stainless steel shrinking cylinder and/or a (shrinking) key
  Compress a bit at room temperature and use differential shrinkage at cooldown: Al shrinking cylinder + bladder and key system
Order of magnitudes: LHC @ 8.34 T: 70 MPa warm, 30 MPa cold
Fresca2 @ 13 T: 60 MPa warm, 130 MPa cold

## Slide 41: Prestress: collars
“The classical solution”
Thin collars put around the coil
The coil is well contained in a fixed cavity
Pressed together and locked with pins or keys
At 300K apply a prestress 2‐3 times of what is needed as part of the stress is lost during cooldown: for very high field tends to be too high (LHC:70 MPa at 300 K and 40 MPa at cold)
Field quality is in good part determined by collar shape
If the coils size is not so well controlled, the stress can be too high or too low
Nb3Sn is stress sensitive and this could be a problem
Hera dipole
DESY
TQC quadrupole
LARP-FNAL
LHC dipole
CERN

## Slide 42: Prestress: shrinking cylinder and/or prestress key
The differential shrinking and room temperature prestress between a (thick) shell or key and the Fe (split) yoke provides prestress
Pre-stress completely depends on dimensioning of the components and the materials
HFDA
FNAL
Courtesy A. Zlobin

## Slide 43: Prestress: Al shrinking cylinder + bladder and keys
Developed at LBNL, example: TQS a LARP model quadrupole
300 K: Bladders pressurized with water (<600 bar) , then insert keys  load between 10 MPa and 80 MPa
Cooldown: differential shrinkage between AL shell and Fe yoke load another ~100 MPa
Needs careful mechanical FE modeling before and strain measurements during bladder operations and cooldown
2 layers
Filler
Keys
4 pads
Bladder
Yoke
Aluminum shell
Courtesy S. Caspi

## Slide 44: Looking in the kitchen of future magnet development
What is happening after the 8T magnets for LHC ?
At CERN
Upgrade the LHC luminosity: HL-LHC (HILUMI)
  use large aperture Nb3Sn triplet quadrupoles (12T class)
  improve collimation: use a few 11T dipoles to make space
Go to higher energies
  16 T Nb3Sn dipoles in the LHC ring for Ecom=26 TeV : HE-LHC
  16 T Nb3Sn dipoles in a 100 km new ring for Ecom=100 TeV : FCC (Future Circular Collider)
  But even !
  20 T HTS hybrid dipoles in the LHC ring: for Ecom=33 TeV : HE-LHC
  20 T HTS hybrid dipoles in a 80 km new ring for Ecom=100 TeV : FCC
In China
A similar completely new project is being studied in China: SPPC (C=54 km, B=20 T, Ecom=71 TeV)
For these, basic High Field Magnet development programs are since many years running in the US and Europe and recently in China

## Slide 45: Superconducting accelerators magnets; the state of the art
Maximum attainable field slowly approaches 16 T
  20% margin needed (80% on the load line):
  for a 16 T nominal field we need to design for 20 T

## Slide 46: CERN-European development evolution
RMC (Racetrack Model Coil)
Laminated Yoke
Vertical Pad
Aluminium Shell
Longitudinal Rods
Horizontal Pad
Nb3Sn Coil
Electrical connexion box
SMC (Short Model Coil)
Short Model Coil
FReSCa2 13T
Nb3Sn Dipole
Race-track
Model Coil
FReSCa2
11 T dipole
(CERN)

## Slide 47: Basic magnet technology development for HILUMI and beyond (2004-2013) ; US development evolution
By courtesy of D. Dietderich, LBNL

## Slide 48: Basic HFM development : Some achievements at LBNL (1995-2004)
Since 20 years LBNL is running a high field dipole development program
Some achievements:
D20, 50 mm aperture, cosQ 4 layer dipole, reached 13.5 T@1.9K
HD1, flat block coil, 8 mm aperture, reached 16 T
HD2, flared end block coil, 36 mm aperture, reached 13.8 T
These pose a clear breakthrough above 10 T with a new coil layout (block coil) and a mechanical structure aimed (shell-bladder and keys) at high fields
A.D. McInturff, et al., Proc. of PAC 1997, 3212

## Slide 49: Basic HFM development : EuCARD high field dipole (Fresca2):
Diameter Aperture = 100 mm
L coils = 1.5 m
L straight section = 700 mm
L yoke = 1.6 m
Diameter magnet = 1.03 m
156 turns per pole
Iron post
Bcenter = 13.0 T
I13T = 10.7 kA
Bpeak = 13.2 T
Emag = 3.6 MJ/m
L = 47mH/m
Courtesy Attilio Milanese, Pierre Manil
42
42
36
36
Fresca2 : CERN, CEA construction phase
First tests 2014

## Slide 50: Fabrication of Fresca2 coils
Straightforward technology to wind block coils with flared ends:
This is a lesson for FCC magnets !

## Slide 51: HILUMI IT magnet zoo
Courtesy E. Todesco

## Slide 52: HL-LHC: MQXF low beta Nb3Sn quadrupole
A CERN LARP collaboration.
Nominal Gradient 132.6 T/m
Aperture diameter 150 mm
Peak Field 12.1 T
Current 17.5 A
Loadline Margin 20% @ 1.9 K
Stored Energy 1.32 MJ/m
Spring 2016 the first model achieved the nominal and ultimate field at FNAL !
By courtesy of G. Ambrosio (FNAL), P. Ferracin (CERN et al)

## Slide 53: HL-LHC: 11 T Dispersion suppressor magnet
First Nb3Sn magnet to go into an accelerator (2019) !
Present model program (CERN and FNAL)
  demonstrated the required performance (11.25 T at 11850 A) and Achieved accelerator field quality
Nominal Field 11 T
Aperture diameter 60 mm
Peak Field 11.35 T
Current 11.85 kA
Loadline Margin 19.7% @ 1.9 K
Stored Energy 0.96 MJ/m

## Slide 54: FCC development (2014 - ... )
LHC
27 km, 8.33 T
14 TeV (c.o.m.)
FCC-hh
80 km, 20 T
100 TeV (c.o.m.)
FCC-hh
100 km, 16 T
100 TeV (c.o.m.)i
HE-LHC
27 km, 20 T
33 TeV (c.o.m.)
Geneva
PS
SPS
LHC

## Slide 55: Magnets for FCC and HE-LHC
For a 17 + 17 TeV collider
  Need 20 T dipoles
2010 first ideas on HE-LHC magnets
Graded HTS ⎻ Nb3Sn ⎻ Nb-Ti
Courtesy: E. Todesco

## Slide 56: FCC: Magnet design for 16 T dipoles, LTS Nb3Sn
P. McIntyre, 2005
E. Todesco, 2013
GL. Sabbi, 2014
Blocks
E. Todesco 2013
D. Schoerling 2015
Cos-q
S. Caspi, 2014
Canted Cos-q
R. Gupta, 1997
J.M. Van Oort, R. Scanlan, 1994
Common coils

## Slide 57: US program lines
5T Nb-Ti
2014-2015
10T Nb3Sn
2015-2016
2016
canted-cos-q
cos-q
2017
common coils
2018

## Slide 58: FCC: 16T dipole options
Common coils
F. Toral (CIEMAT)
Cos-theta coil
S. Farinon, P. Fabbricatore (INFN)
Block coil
C. Lorin, M. Durante (CEA)
Canted Cos-theta
B. Auchmann (CERN/PSI)

## Slide 59: FCC Nb3Sn performance targets
Ultimate Nb3Sn ? Pursue the idea of improved high field pinning
(D. Dietrich and R. Scanlan, A. Godeke)
All single parameters are in reach, their combination is the challenge !
Dstrand: 0.5…1 mm
JC (16 T, 4.2 K) > 1500 A/mm2
m0DM (1 T,4.2 K) <150 mT (Dfil < 20 m)
RRR > 150
UL > 5 km
Cost(16 T, 4.2 K) < 5 USD/kAm
Large cables, cabling !
Field quality
Stability, protection
ITER material cost per kg

## Slide 60: HTS: First attempt towards 20 T
J.M. Rey, F. Borgnolutti, CEA-Saclay
6 T HTS (YBCO) insert for test in FReSCa2
To get to 19 T
But without bore
CEA + CRNS Grenoble
19 T

## Slide 61: EuCARD2 5T accelerator quality ReBCO magnet
5 Tesla stand alone, (18 T in 13 T background), @ 4.5K, 40 mm aperture, 10 kA class cable, Accelerator Field quality
http://eucard2.web.cern.ch/

## Slide 62: EuCARD2 5T : Feather0 - Feather-M2.0
Feather0: First coil in the test station
Feather2: winding of first coil with dummy cable in progress

## Slide 63: CERN HTS program plan (planning phase)
Twisted stack
CORC
Roebel
“DOCO”
?
?

## Slide 64: Final remark
Superconducting accelerator magnets in the 4 T – 8 T range are “state of the art” using Nb-Ti conductor
Magnets in the 12 T range using Nb3Sn are in the prototyping phase for HILUMI
Development models have been shown to work up to 16 T
For future colliders 16 T magnets are being designed
Development for HTS magnets for the 20 T range has started
Lots of fun ahead !

## Slide 65: Literature on High Field Magnets
Books
M. Wilson, Superconducting magnets / Oxford : Clarendon Press, 1983 (Repr. 2002). - 335 p
K-H. Mess, P. Schmüser, S. Wolff, Superconducting Accelerator Magnets, Singapore, World Scientific, 1996. - 218 p.
Y. Iwasa, Case studies in superconducting magnets : design and operational issues . - 2nd ed. Berlin : Springer, 2009. - 682 p.
S. Russenschuck, Field computation for accelerator magnets : analytical and numerical methods for electromagnetic design and optimization / Weinheim : Wiley, 2010. - 757 p.
CERN Accelerator school, Magnets, Bruges, Belgium 16 – 25 June 2009, Editor: D. Brandt, CERN–2010–004
Conference proceedings and reports
21st International Conference on Magnet Technology, Hefei, China, 18 - 23 Oct 2009, IEEE Trans. Appl. Supercond. 20 (2010)
The 2010 Applied Superconductivity Conference, Washington DC, US, 1-6 Aug 2010, , IEEE Trans. Appl. Supercond. 21 (2011)

## Slide 66: Literature on High Field Magnets (2)
Papers and reports
S. Caspi, P. Ferracin, “Limits of Nb3Sn accelerator magnets“, Particle Accelerator Conference (2005) 107-11.
S. Caspi, P. Ferracin, S. Gourlay, “Graded high field Nb3Sn dipole magnets“, 19th Magnet Technology Conference, IEEE Trans. Appl. Supercond., (2006) in press.
E. Todesco, L. Rossi, “Electromagnetic Design of Superconducting Dipoles Based on Sector Coils”, Phys. Rev. Spec. Top. Accel. Beams 10 (2007) 112401
E. Todesco, L. Rossi, AN ESTIMATE OF THE MAXIMUM GRADIENTS IN SUPERCONDUCTING QUADRUPOLES, CERN/AT 2007-11(MCS),
P. Fessia, et al., Parametric analysis of forces and stresses in superconducting dipoles, IEEE, trans. Appl, Supercond. Vol 19, no3, June 2009.
P. Fessia, et al., Parametric analysis of forces and stresses in superconducting quadrupole sector windings, sLHC Project Report 0003
Websites
http://www.magnet.fsu.edu/magnettechnology/research/asc/plots.html

## Slide 67: Acknowledgements
For this lecture I used material from lectures, seminars, reports, etc. from the many colleagues. Special thanks goes to:
Giorgio Ambrosio (FNAL), Luca Bottura (CERN), Shlomo Caspi (LBNL), Arnaud Devred (ITER), Paolo Ferracin (LBNL), Attilio Milanese (CERN), Jeroen van Nugteren, Juan-Carlos Perez (CERN), Lucio Rossi (CERN), Stephan Russenschuck (CERN), Ezio Todesco (CERN), Davide Tommasini (CERN), Martin Wilson