## Slide 1
18th May 2016
Operational process (Rb filling, installing & recycling) – v0r3

## Slide 2
Rb source – Double valve system
Proposal is to utilise a double valve system with no intermediate purge port
Simplest configuration that allows Rb source and plasma cell modules to be independently isolated
Following slides show pictorial procedures for:
Filling flask with Rb
Attaching to plasma cell
Recycling & removing Rb collection flask
Rb flask
Valve 1 (manual)
flask isolation
Valve 2 (controlled)
experimental operation
1
2
The following convention is used:
GREEN = rubidium
LIGHT GREY = UHV
DARK BLUE = argon
WHITE = air

## Slide 3
Rb source – First time filling
Fume hood (Argon environment)
Closed
1
Rb
20°C
Rb
50°C
50°C
Closed & capped
1
20°C
Closed
1
Closed
1
Transport to TT41
1
2
3
4
First time Rb filling procedure (all completed in Ar filled fume hood):
Empty flask, manual valve and Rb loaded into Ar hood
Rb is heated to 50C and poured into empty flask using a funnel
Rb cooled to 20C and closed & capped valve added to flask
Flask assembly transported to TT41 for installation on vapour source
Pour in warm liquid Rb

## Slide 4
Rb source – Future filling
Fume hood (Argon environment)
Closed
1
50°C
Closed & capped
1
20°C
Closed
1
Closed
1
Transport to TT41
1
2
3
4
Pour in warm liquid Rb
20°C
Recycle flask
50°C

## Slide 5
Rb source – Installing Rb flask 1
1
20°C
Closed
1
20°C
Closed
Open
Fill with Ar
2
20°C
Closed
1
20°C
Closed
2
20°C
20°C
Closed
1
20°C
Closed
2
20°C
Closed
1
20°C
Closed
2
20°C
1
2
3
4
5
TT41
Gas bag

## Slide 6
Rb source – Installing Rb flask 2
TT41
Closed
1
20°C
Closed
2
20°C
Open
1
20°C
Open
2
20°C
Open
1
20°C
Closed
2
20°C
6
7
8
Ready for experiment
Pull UHV
Pull UHV
Pull UHV

## Slide 7
First time Rb installation procedure (all completed in TT41, upstream & downstream ends follow same process):
Place filled Rb flask and valve assembly into gas bag
Fill plasma cell and vapour source with argon (open Rb flow path valve to ensure intra-valve space is filled with argon)
Attach gas bag to Rb flow path on vapour source and fill with argon
Remove caps from Rb flask and plasma cell system and join flask to Rb flow path
Remove gas bag from system and retain for disconnection
Pull vacuum on full sytem
Open Rb flow path valves to ensure vacuum above Rb in flask
Close controlled Rb flow path valve
Disconnecting is very similar to the above process but temperatures in the flow path need to be controlled to minimise chance of Rb liquid in valves and intra-valve space
Rb source – Installing

## Slide 8
Rb source – Removing recycling flask 1
Fill with Ar
20°C
20°C
40°C
20°C
Ready for disconnect
1
2
3
4

## Slide 9
20°C
20°C
20°C
20°C
5
6
7
Rb source – Removing recycling flask 2

## Slide 10
20°C
20°C
8
9
Rb source – Removing recycling flask 3

## Slide 11
Removal of Rb recycling flask procedure (all completed in TT41, upstream & downstream ends follow same process):
Fill plasma cell and vapour source with argon
Warm expansion chamber to 40°C to liquefy Rb and allow it to flow into recycling flask
Cool system to 20°C to ensure all Rb is solid
Fit recycling chamber around Rb flask and seal
Fill recycling chamber with argon
Disconnect recycling flask from chamber and cap
Fit empty recycling flask to expansion chamber
Empty recycling chamber of argon & remove Rb recycling flask (full and capped) from the recycling chamber
Pull vacuum on full system
System is back in original configuration with Rb removed from expansion chamber
Rb source – Removing recycling flask

## Slide 12
Rb source – Volume between valves
Volume between valve seals:
Approx. 318257mm³
This volume filled with ‘dirty’ argon gas between Rb flask changes

## Slide 13
Rb source – Volume between valves
Using the following assumptions:
Volume between valve seals = 320000 mm3
‘Dirty’ argon gas is 95% argon; 5% air
Air is 20% oxygen
Principle reaction with rubidium forms Rb2O (Rubidium oxide)
Amount of oxygen present in intra-valve ‘dirty’ argon = 0.00014 moles
Amount of rubidium consumed = 0.00056 moles = 0.05g
Amount of rubidium oxide formed = 0.00028 moles = 0.05g = 50mg
50mg in 500g = 0.01% contamination with oxide with each new flask added