## Slide 1: The 11T Dipole Magnet for HL-LHC Holland @ CERN
CERN Council Chamber – 2 June 2016
F. Savary

## Slide 2: OUTLOOK
Introduction
Main parameters of the 11T Dipole
The 11T Dipole Plan in the Timeline of HL-LHC
From technology demonstration to “final” design
Quench performance of MBHDP101
Challenges
Summary

## Slide 3: Introduction
Create space in the dispersion suppressor regions of LHC, i.e. a RT beam vacuum sector, to install additional collimators needed to cope with beam intensities larger than nominal
Collimators are needed in IP7 to absorb off-momentum particles/beam losses (proton operation)
Replace a standard Main Dipole by a pair of 11T Dipoles producing the same integrated field of 119 T·m at 11.85 kA
Interconnect
Space for Collimator
11 T dipole cold mass
By-pass cryostat
15660 mm
LS2
LS3

## Slide 4: Definition of the cryo-assembly
LBH_A
LBH_B
By-pass cryostat
LMBHA
LMBHB

## Slide 5: OUTLOOK
Introduction
Main parameters of the 11T Dipole
The 11T Dipole Plan in the Timeline of HL-LHC
From technology demonstration to “final” design
Quench performance of MBHDP101
Challenges
Summary

## Slide 6: Main parameters of the 11T Dipole
Characteristic | Value | Unit
Aperture | 60 | mm
Distance between apertures at RT / 1.9 K | 194.52 / 194.00 | mm
Magnetic length | 5.307 | m
Coil length | 5.415 | m
Magnet length, between end plates | 5.799 | m
Cold mass assembly length | 6.252 | m
Operating temperature | 1.9 | K
Nominal operation current | 11.85 | kA
Bore field @ nominal current | 11.23 | T
Peak field @ nominal current | 11.59 | T
Stored energy/m at Inom | 0.9663 | MJ/m
Cable bare width before reaction | mm | 14.7
Cable bare mid-thickness before reaction | mm | 1.25
Keystone angle | Degree | 0.79
Strand diameter | 0.700  0.003 | mm
Number of strands per cable | 40 | -
Cable insulation thickness, before/after reaction | 0.150/0.110 | mm
  Mica tape, COGEBI FIROX®, 80 μm
  S2-glass braided on cable
  Epoxy resin CTD-101K

## Slide 7: OUTLOOK
Introduction
Main parameters of the 11T Dipole
The 11T Dipole Plan in the Timeline of HL-LHC
From technology demonstration to “final” design
Quench performance of MBHDP101
Challenges
Summary

## Slide 8: Timeline of HL-LHC
2 will be installed during LS2 + 1 spare
2 will be installed during LS3 + 1 spare
TODAY

## Slide 9: OUTLOOK
Introduction
Main parameters of the 11T Dipole
The 11T Dipole Plan in the Timeline of HL-LHC
From technology demonstration to “final” design
Quench performance of MBHDP101
Challenges
Summary

## Slide 10: From technology demonstration to “final” design
MBHSP01
MBHSP02
MBHDP01
MBHSP03
MBHSP10X [RRP]
MBHSP20X [PIT]
MBHDP101
MBHDP102 [RRP] - 201 [PIT]
LBH_P001 [RRP] - 2 [PIT]
6 blocks – 56 turns
Same coil design @ FNAL and CERN as starting point
Integrated pole concept @ FNAL
Removable pole concept @ CERN

## Slide 11
First 5.5 m long coils
made @ CERN
MBHDP101
MBHDP01

## Slide 12: The 11T Dipole Plan in the Timeline of HL-LHC
2015 |  |  |  |  |  |  |  |  |  |  |  | 2016 |  |  |  |  |  |  |  |  |  |  |  | 2017 |  |  |  |  |  |  |  |  |  |  |  | 2018 |  |  |  |  |  |  |  |  |  |  |  | 2019 |  |  |  |  |  |  |  |  |  |  |  | 2020 |  |  |  |  |  |  |  |  |  |  |  | 2021 |  |  |  |  |  |  |  |  |  |  |  | 2022 |  |  |  |  |  |  |  |  |  |  |  | 2023 |  |  |  |  |  |  |  |  |  |  |  | 2024 |  |  |  |  |  |  |  |  |  |  | 
J | F | M | A | M | J | J | A | S | O | N | D | J | F | M | A | M | J | J | A | S | O | N | D | J | F | M | A | M | J | J | A | S | O | N | D | J | F | M | A | M | J | J | A | S | O | N | D | J | F | M | A | M | J | J | A | S | O | N | D | J | F | M | A | M | J | J | A | S | O | N | D | J | F | M | A | M | J | J | A | S | O | N | D | J | F | M | A | M | J | J | A | S | O | N | D | J | F | M | A | M | J | J | A | S | O | N | D | J | F | M | A | M | J | J | A | S | O | N | D
 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | LS2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | LS3 |  |  |  |  |  |  |  |  |  |  | 
For LS2, Models, X-Section 1, RRP |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
For LS2, Prototype P1, X-Section 1, RRP |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Series Production for LS2, X-Section 1, RRP |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | For LS3, Models, X-Section 2, PIT & RRP |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Series Production for LS2-Spare and LS3, X-Section 2, PIT & RRP |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Cold tests of LBH_P1 + Cryo-by-pass + LBH__001
For LS3, Prototype LBH_P2,
X-Section 2, PIT
* 2 cryo-assemblies for IP7
B8L7 & B8R7
* 1 spare cryo-assembly
* 2 cryo-assemblies for IP7 B10L7 & B10R7
* 1 spare cryo-assembly
available
in end 2021
Beginning of winding
Beginning of winding
Beginning of winding
Spare

## Slide 13: OUTLOOK
Introduction
Main parameters of the 11T Dipole
The 11T Dipole Plan in the Timeline of HL-LHC
From technology demonstration to “final” design
Quench performance of MBHDP101
Challenges
Summary

## Slide 14: Quench performance of MBHDP101
MBHSP102
MBHSP103
MBHDP101
Holding current tests were performed, up to 10 hours at nominal current and 2.5 hours at ultimate current
Not a single quench was recorded during flattop or ramp down for all models!
 | Maximum current reached (kA) | % Iss
SP101 | 11.9 | 82
SP102 | 12.8 | 88
SP103 | 12.8 | 90
DP101 | 13.2 | 94

## Slide 15: OUTLOOK
Introduction
Main parameters of the 11T Dipole
The 11T Dipole Plan in the Timeline of HL-LHC
From technology demonstration to “final” design
Quench performance of MBHDP101
Challenges
Summary

## Slide 16: How can Holland contribute to the 11T?
HiLumi Goes to Industry
25-26 June 2015 - CERN
Legend:
We are covered
We need more suppliers
We desperately need suppliers
Dutch Precision Fair
November 2015
Veldhoven
Item # | Description | Raw material | 2018 | Later | What is challenging
1 | Coil keys | AISI 316 L – DIN 1.4435 |  |  | Machining (accuracy & elasticity)
2 | End spacers | SLS – AISI 316 L – DIN 1.4435 |  |  | Metrology, electrical insulation?
3 | Saddles | Impregnated glass fiber as per IEC/EN 61212-3-1 EP-GC22 |  |  | 5-axes machining, GC22, accuracy
4 | Removable pole | TA6V annealed (Ti6Al4V; 3.7165) |  |  | Accuracy & material
5 | Wedges – precision profiles | Aluminum oxide dispersion strengthened copper (ODS) |  |  | Accuracy, material ODS
6 | Quench heaters | Polyimide – St.Steel – Copper |  |  | Flexible Printed Circuits
7 | Collars | YUS-130S (High Mn Steel) |  |  | Fine blanking, accuracy
8 | Collaring keys | AISI 316 L – DIN 1.4435 |  |  | Accuracy
9 | Yoke laminations & inserts | Low carbon steel |  |  | Fine blanking, accuracy
10 | Heat exchanger tube | Oxygen Free Cu – UNS C10200 |  |  | Cu quality
11 | Bus bars – hollow bars | Oxygen Free Cu – UNS C10200 |  |  | Length, Cu quality
12 | Lyras | Oxygen Free Cu – UNS C10200 |  |  | Cu quality
13 | Shells | AISI 316 LN – DIN 1.4429 |  |  | Raw material, thickness, accuracy
14 | End covers | AISI 316 LN – DIN 1.4429 |  |  | Raw material, accuracy

## Slide 17: NEW challenges w.r.t. to Nb-Ti magnets, 1
Reaction treatment (48 h @ 210°C – 48 h @ 400°C – 50 h @ 640°C)
To form Nb3Sn compound

## Slide 18: NEW challenges w.r.t. to Nb-Ti magnets, 2
Impregnation
Insulation system:
Mica C-shaped tape
Braided fiber glass impregnated with epoxy resin

## Slide 19: Coil keys – end spacers – saddles
Can be produced from STP files
Item 4: Coil key, AISI 316 L
Item 5: Selective Laser Sintering (SLS) end spacer, AISI 316 L, with flex. legs
Item 6: Saddle, EP-GC22, base material woven glass cloth, matrix epoxy resin
After curing
After reaction
After impregnation

## Slide 20: Loading pole – ODS wedge
Insulated cable
Filler Wedge
Loading plate
Inter-layer
Inner ground wrap
Outer ground wrap
Wedges, to be made of aluminum Oxide Dispersion Strengthened copper, cold drawn in length of 2.6 m
a
b
c
d
e
f
Loading pole, to be made of titanium, 240 mm long

## Slide 21: Quench heaters
A strip of stainless steel of 20 m running along the coil outer surface
A thin copper layer of 5 m (electrolytic deposition) to reduce the resistance of the strip in between 2 heating areas
The substrate is a 50 m polyimide film
+
+
-
-
Heating areas
(stainless steel)
Non-heating areas
(copper plated stainless steel)
Polyimide film
(substrate)
Overall length: 5600 mm
Width: 160 to 300 mm

## Slide 22: Collars – collaring keys – yoke laminations
    3 mm thick high Mn steel
    0.2 > 400 MPa
Yoke laminations: 5.8 mm thick low carbon steel
Collars
Butraco
Jeijen metaaltechniek B.V.
Kusters & Bosch

## Slide 23: Shells – End covers, main parts of the He vessel
Material: AISI 316 LN, hot rolled plates formed in folding press, thickness: 15 mm
Tight fit with yoke laminations, i.e. need to be precise
Weldability and Leak tightness
Material: AISI 316 LN
Powder metallurgy for the dished cover, or welded construction for the flat cover
Weldability and Leak tightness

## Slide 24: Summary
The HiLumi HL-LHC Project is in the construction phase
Most components are not standard, specifications are demanding
  Materials (remember … will work between -271°C and +640°C for the coil components)
  (Very) tight tolerances
Limited quantities, but high quality requirements
Technology developments are needed, e.g. magnets, quench heaters
Finding the Higgs boson, and more, requires exploring the unexplored, going beyond its own limits
Challenging, however rewarding

## Slide 25: Thank you for your attention For any question, email Frederic.Savary@cern.ch