## Slide 1: Halbach magnets and correctors for the C and eRHIC projects
N. Tsoupas, S. Brooks, A. Jain, G. Mahler, F. Meot, V. Ptitsyn, D. Trbojevic
FFAG’16

## Slide 2: Conclusion
This study and the measurements show that the Halbach type permanent magnets with wedges have many advantages over the Iron dominated magnets, and can be used as magnets in an FFAG cell.
2/20
FFAG’16

## Slide 3: The C project is a prototype electron accelerator for the eRHIC project
FFAG’16
Injection: 5 MeV e- 100 mA rep-rate 325 MHz
1.3 GHz 16 MV/m ~80 MeV
5 MeV Beam dump
Splitter
Merger
Two concepts: Energy Recovery Linac (ERL)
Fixed Field Alternating Gradient (FFAG)
Energies [GeV]
76
146
216
286

## Slide 4: 76 – 286 MeV NS-FFAG Cornell Lattice 100 cells : Orbits and magnets in the 10.5 m diameter
BD
QF/2
13.598
x (mm)
-13.364
32.99 cm
10.99 cm
3 cm
-8.98 mm
GD = -27.493 T/m ByD = 0.5044 T
GF = 42.54 T/m ByF =-0.104 T
11.9 mm
4.0 cm
11 cm
286 MeV
216MeV
76 MeV
146 MeV
LINAC ENERGY 70 MeV
Injector 6 MeV
4.0 cm
QF/2
ECEN=225 MeV
-2.44
16.04
10.924
4/20
FFAG’16
-18.331 mm
Quads are displaced by ~16 mm and are 3 cm apart
QFC
QDC
16 mm

## Slide 5: Conventional Quad
Displaced transversely: LARGE APERTURE
Small Distance apart: INTERFERENCE
FFAG’16
16 mm diplacement
3 cm separation

## Slide 6: One of the versions of the proposed eRHIC projects
FFAG’16
3 Trajectories
9 Trajectories

## Slide 7
θD= 3.3757mrad
BD =0.0465 T,
GD = -8.631 T/m
xDoffset=+5.3 mm
x(mm)
θF/2=3.9115/2 mrad
1.685 GeV
5.015 GeV
3.350 GeV
0.40 m
0.40 m
0.9194 m
-5.3
-5.6
5.3 mm
-6.8
ECEN=3.8 GeV
8.8
1.065/2 m
1.065/2 m
-12.1
θF/2=3.9115/2 mrad
16.0
Quad center
Quad center
D
F/2
F/2
10.7
-10.9
2.7846 m
3.5
Low Energy (Scott Berg) NS-FFAG Cell 1.685-5.015 GeV
BF= 0.0465 T,
GF= 8.631T/m
xFoffset= -5.3 mm
FFAG’16
Magnet Interference and
Transverse displacement
Not a problem
Consumption of energy may be problem

## Slide 8
8/20
Isometric view of Magnetized Wedges
Cross section of Magnetized Wedges of NdFeB or SmCo

Direction of the easy axis =(n+1) +/2
Dipole n=1
Quad n=2
Sext n=3

FFAG’16
Electron bunches

## Slide 9
2D Design establishes the direction of the easy axis for 12pole multipole=0 at R=1 cm
9/20
Perm. Magnet Material NdFeB
FFAG’16
This error can be minimized to < 1%

## Slide 10: Superposition of multipoles
FFAG’16
Btot=Bquad+Bdip
No Displacement
of the Quad is needed
Advantages of using
Halbach type of magnets
Btot=Bupstream+Bdownstrm
Insignificant field distortion
10/20

## Slide 11: A Halbach magnet can accept corrector magnets
Due to the high saturation of the PM material (1.0)
Any external field will not alter the field generated by the PM.
Btot= BPM + Bext superposition of fields.
Material is isotropic.
11/20
FFAG’16
This field superposition was tested experimentally.

## Slide 12: Test of Field superposition with permanent magnets
PMQ #1
PMQ #2
Spacer
Window frame dipole
Quad assembly inside dipole
(Approximately centered)
12/20
FFAG’16

## Slide 13: 3D Magnetic field calculations for the FFAG cells
3Dimensional Field map is
obtained over the volume of
a single cell where beam exists.
By component at the median plane
between the two magnets
13/20
FFAG’16

## Slide 14: Closed orbits in the range 1.3 GeV to 6.6 GeV
QF
QD
x-along beam [m]
Y transverse [m]
14/20
FFAG’16

## Slide 15: Tunes Qx,Qy and chromaticities x, y; Range: 1.3 GeV to 6.6 GeV
15/20
FFAG’16

## Slide 16: Calculations of the maximum beam emittance x transported in all six arcs for each of the five orbits.
3.96 GeV
1.32 GeV
6.60 GeV
2.64 GeV
5.28 GeV
Max_N-rms=0.02 m.rad
Required_N-rms to be transported=30x10-6 m.rad
16/20
FFAG’16

## Slide 17
Calculations of the maximum beam emittance y transported in all six arcs for each of the five orbits.
Max_N-rms=0.02 m.rad
Required _N-rms to be transported=30x10-6 m.rad
17/20
FFAG’16

## Slide 18
1.3 GeV
2.6 GeV
6.6 GeV
QF
QD
Beta functions of 3 different energies
x
y
18/20
FFAG’16

## Slide 19
0.4 mm Iron
1 mm Inconel
0.1 mm Al
B=0.83 T
B=0.03 Gauss
5 mm
5 mm
19/20
FFAG’16
A 5 mm septum Permanent Magnet

## Slide 20: Conclusions
The Halbach type permanent magnets with wedges is a good alternative to replace the Iron Dominated permanent magnets.
20/20
FFAG’16
Issues with Halbach type PM
Temperature compensation may be needed for (NdFeB) material. But there are ways to solve temperature compensation issues.
Tolerances of easy axis direction and Br

## Slide 21
The End
Thank you for your attention
FFAG’16