## Slide 1: PH-DT-DD: SSD-Solid State Detectors
EP-DT-DD Meeting – 8.7.2016
The team today (CERN & visitors):
R&D: Development of radiation tolerant silicon detectors in the framework of RD50 and CMS
Service: Characterization of semiconductor detectors
PhD students:
Sofia OTERO UGOBONO
Esteban Curras Rivera
Hannes Neugebauer
Laura Franconi
Summer students:
Ayushi, Bhavita, Shivika, Urban
Visiting Scientist:
Marcos Fernandez Garcia
Trainee/FTEC:
Joaquin Gonzalez (0.5 FTE)
Isidro Mateu Suau (0.5 FTE)
CERN Staff
Michael Moll (0.6 FTE)
Urban
Bhavita
Shivika
Michael
Sofia
Laura
Marcos
Joaquin
Esteban
Isidro
Hannes
Julien
Left SSD since Nov.15:
Christian Gallrapp (Fellow)
Celso (Trainee)
EP-
….no dedicated technician!
..soon visiting: Rogelio (Seville)

## Slide 2: Present Projects and Services
SSD activities at CERN
RD50 Collaboration
  Steering and Management of the RD50 collaboration (50 Institutes, 300 members)
    Michael: Co-Spokesperson, budget holder, CERN Contact, Glimos; Veronique: secretary
  Characterization and simulation of radiation effects in silicon devices
    Development of characterization tools (TSC, edge-TCT, Two-Photon TCT, …)
    Measure damage parameter (CV,IV, CCE, TCT) and defect properties (TSC, I-DLTS)
    Simulate detector performance (TCAD, TRACS)
    Defect/Material engineering: p/n-type, different resistivity, impurities,…
  LGAD (Low Gain Avalanche Detectors) and APDs (Avalanche Particle Detectors)
    Fast timing applications
    Charge amplification in highly damaged detectors
  3D detectors, CMOS sensors, …
CMS Collaboration & RD50
  Sensor development for the High Granularity Calorimeter (HGC)
Service
  Measurement of sensors for/with external groups
….its all about silicon sensors and their application as HEP detector.
No major changes since November 2015

## Slide 3: Damage & defect parameterization
Lab infrastructure improvements
  Cryocooler
    Optimization of cryocooler for more accurate temperature reading during temperature scan (20K to 240K in 20min)
    Design and simulation of new PCB using a ceramic substrate (collaboration with MPT Workshop: Antonio, Rui)
    Re-design of the mechanical support and connections to reduce thermal loads
  Addition of functionalities in the controlled temperature chamber (Susi)
    Automatic I-V measurements at different temperature steps, I-T measurements, C-V measurements
Study on leakage current temperature dependence
  Evaluation of activation energy for silicon (work with IRRAD team)
    Wide range of temperature scaling values published in literature
    A value of Ea = 1.20 eV was obtained by our work in agreement of theoretical predictions with midgap defect level
(Proof of concept for the new Cryocooler design (Ceramic PCB + Temperature sensor pressed near the DUT + reduced thermal load due to cables)
10K/min
Details: RD50 workshop 6/2016: Isidre for T-scaling of leakage current [link]

## Slide 4: CMS: High Granularity Calorimeter
HGC
  600 m2 of silicon sensors (6M channels) exposed up to 1.5x1016 neq/cm2; Structure of sensors: Hexagonal pads
  Radiation tests of sensor structures performed by SSD [Esteban thesis] with Uni HH
  CCE (beta, laser), CV, IV, test beam (with CMS team) on irradiated sensors: (p, n, FZ, EPI, 50 to 300 mm)
Details: RD50 workshop 6/2016: Esteban for HGC sensor radhard testing [link]
-30C
Sensors: p- vs. n-type ; FZ vs. EPI
  Proof of concept: Sensors operational up to highest fluence
  300mm sensors: unclear why n-type is better !?
  120mm sensors: unclear why EPI better than DD-FZ !?
    Very welcome effect: For HPK 8” production no DD-FZ wafers available, will have to use epitaxial wafers!
Timing (test beam data)
    Reaching 20ps time resolution for S/N > 30
dd-FZ 320um
dd-FZ 200um
dd-FZ 120um
Epi 100um
20ps

## Slide 5: Sensors with intrinsic gain
LGAD (Low Gain Avalanche Detectors) [Ultrafast Silicon Detectors – UFSD]
  RD50 collaboration (several institutions); producer CNM and FBK, soon: HPK
  Experiments considering LGAD as option: ATLAS HGT, CMS fast (hermetic) timing, CTPPS
  SSD: Study of gain homogeneity and gain loss after proton irradiation
Details: RD50 workshop 6/2016: Sofia for LGAD [link], Michael for DD-APD [link]
~ 1 MIP
~ 15ps
DD-APD (Deep Diffused Avalanche Particle Detectors) [Hyperfast Detectors]
  Collaboration with some US CMS groups and producer RMD in the US
  Time resolution obtained on un-irradiated devices: 15ps
  Test beam in collaboration with RD51 (….analysing data)
gain approx. 5 before irradiation

## Slide 6: 3D sensors
Project of Laura Franconi (visiting PhD student, Talent) ….writing thesis now
p+ column
n+ column
Sketch of 3D sensor
IV curves before and after proton irradiation at different fluences
Same colour = same 3D diode, before and after irradiation
3.3E13 neq/cm2
1.0E14 neq/cm2
2.5E14 neq/cm2
4.5E14 neq/cm2
2.2E15 neq/cm2
5.0E15 neq/cm2
n+ column
p+ column
Punch through
column
Laser mapping in SSD lab
... good example of collaborative use of the SSD equipment (service)
Red front light gets reflected on the metal lines connecting the n+ and the p+ columns and on the columns themselves: reduced charge collection in these areas.

## Slide 7: TPA – Two Photon Absorption
Two Photon absorption:

## Slide 8: TPA – Two Photon Absorption
Investigation on a new technique for sensor characterization (TPA – TCT)
  Deposition of charge at specific position in detector
  Laser: l  1300 nm; P  50-100 pJ; DT  240 fs
  Proof of principle presented last LHCC
  Example of application:
    HVCMOS sensors (AMS 180nm), 10 ohmcm
    100mm x 100 mm passive pixel, measured at 80V, 20C
Two Photon absorption:
[M.Fernandez-Garcia et al, VCI 2016, Feb.2016]
    Sketch of HVCMOS sensor
    Map of charge collected within 10ns
    Map of collection time needed to get 98% of charge

## Slide 9: TPA-TCT after irradiation
Technique can also applied to heavily irradiated sensors!
[M.Fernandez-Garcia, RD50 Workshop, 6/2016]
YES !!!!

## Slide 10: 1year outlook – SSD activities
Laboratory and equipment
    Continue working on sample holder fitting on “all characterization stations”
    Continue building up a TSC system for defect characterization (evaluate possibility to get DLTS)
    Prepare TCT+ to measure time resolution with laser beams
    Evaluate possibility for “low-cost” TPA system at CERN
Upcoming projects in framework of RD50 with SSD participation
  Nitrogen enriched silicon (RD50-2016-01)
    Status: Material produced in collaboration with TOPSIL, Mask design finalized [CERN SSD  TCT, CCE(Alibava), proton irradiation]
  Gallium doped LGAD sensors (RD50-2016-02)
    Status: First tuning of implantation and diffusion hardware at CNM against TCAD tools finished; First set of detectors with different implant/diffusion ready for distribution to project partners [CERN SSD  TCT, CCE, proton irradiation]
  HVCMOS sensors
    Preparation of RD50 submission ongoing [CERN SSD  e-TCT, TPA-TCT]
  Acceptor removal and defect characterization
    Dedicated production run at CIS, Erfurt for CERN SSD finished, sensors arrived at CERN, next step: testing of sensors and irradiation
    Continue development of TSC at CERN to participate in defect characterization
  Timing with LGAD and APD
    Study of time resolution as function of fluence (Ga-LGAD and DD-APD)
CMS HGC
    Finalize CCE study on highly irradiated sensors and test beam studies [Esteban]
    Start evaluating epitaxial silicon [….HPK has no deep diffused 8” possibility!]

## Slide 11: Infrastructure & Equipment
Bldgs.28/186 (4 labs, 1 sensor storage area, 4 offices, ..)
  IV/CV [2x], Alibava (CCE) [2x], Beta (CCE), e-TCT, TCT+; I-DLTS, TSC
I-DLTS (Current Deep Level Transient Spectroscopy)
TCT+: TCT (Transient Current Technique)
Cooling to 10K
TSC (Thermally Stimulated Currents)
-70C to 180C
CCE (Charge Collection Efficiency)
Wafer/Sample storage