## Slide 1: Electron and fog background ~ next approach~
Tatsuhiro Naka
Nagoya University

## Slide 2: Intrinsic radioactive background
U-238 | Th-232 | K-40 | Ag-110m | C-14
27 | 6 | 69020 | (~400) preliminary | 24000
~27 | ~6 | 35 | (~400) | 24000
1-10 | ~ 1 | < 35 | (~400) | < 100
Radioactivity [mBq/kg]
・normal gelatin
・AgBr production from KBr
・de-ionized gelatin
・AgBr production from NaBr
・gelatin → synthetic polymer
Ra-226 ~ 1/10
Ra-228 < 1/30
Present device
T1/2~ 250 days
⇒ should we use old Ag?
~1/2000

## Slide 3: Electron rejection power

## Slide 4: Sensitivity control toward low-background device
Q.E. control of AgBr crystal due to structure inside of crystal
Formation efficiency control of latent image specks on the surface of crystal
e.g., Tz compound
Development sensitivity control
⇒ output the difference of activation energy for latent image specks
Temperature
⇒output the energy-loss mechanism, especially low velocity atom and β-ray

## Slide 5
90% C.L.
C
Kr
Preliminary
Temperature dependence on the sensitivity for current NIT device
M. Kimura et al., NIMA (VCI2016) 2016
S/N (NR /electrons) is increase in lower temperature.
⇒ Dependence of energy loss mechanism
Nuclear recoil : thermal spike in the AgBr crystal due to nuclear stopping power and high electron stopping power
Electrons: only ionization and low dE/dx
Cryogenic condition is critical for electron background rejection .
In addition, stability for emulsion device should be improved.

## Slide 6: Background rejection expectation
Chart: total event intensity
| 1.0000000000000002 | 1.0647770971833779 | 0.92146413946300332 | 0.66204860720438374 | 0.62050380404116445
NIT-40 | 0.11154 | 0.15189 | 0.074409 | 0.050325 | 0.039074
expected | 0.11154 | 0.071384 | 0.040153 | 0.017846 | 0.010038 | 0.0044615 | 0.0011154 | 0.00071384 | 0.00017846 | 4.4615e-05 | 1.1154e-05
expected (-20℃) | 0.01 | 0.0064 | 0.0036 | 0.0016 | 0.0009 | 0.0004 | 0.0001 | 6.4e-05 | 1.6e-05 | 4e-06 | 1e-06
expected (-50℃) | 0.001 | 0.00064 | 0.00036 | 0.00016 | 9e-05 | 4e-05 | 1e-05 | 6.4e-06 | 1.6e-06 | 4e-07 | 1e-07
expected(-100℃) | 1e-05 | 6.4e-06 | 3.6e-06 | 1.6e-06 | 9e-07 | 4e-07 | 1e-07 | 6.4e-08 | 1.6e-08 | 4e-09 | 1e-09
expected (-150℃) | 1e-07 | 6.4e-08 | 3.6e-08 | 1.6e-08 | 9e-09 | 4e-09 | 1e-09 | 6.4e-10 | 1.6e-10 | 4e-11 | 1e-11 | 6.4e-12 | 3.6e-12 | 4e-13 | 1e-13
Usual temp.
-20 ℃
-50 ℃
-100℃
Crystal sensitivity control (e.g., chemical, doping )
Temperature control
Standard sensitized treatment
Electron background rejection power using only elliptical analysis
≒
-150 ℃
Leakage rate
∝(crystal sensitivity )2
100 g・month

## Slide 7: Summary of Sensitivity relationship between ion and γ-rays (Am-241)
Chart: gamma-rays (Am-241)sensitivity
| 3.2000000000000045E-3 | 8.4000000000000061E-2 | 0.44000000000000006
C 30 keV | 0.57 | 1.02 | 0.99
Kr 150 keV | 0.98 | 1.1 | 1.01
Tz concentration
(5-8 mmol/Agmol)
Very preliminary result for NIT sensitivity using Tz compound
Chart: total event intensity
| 1.0000000000000002 | 1.0647770971833779 | 0.92146413946300332 | 0.66204860720438374 | 0.62050380404116445
NIT-40 | 0.11154 | 0.15189 | 0.074409 | 0.050325 | 0.039074
expected | 0.11154 | 0.071384 | 0.040153 | 0.017846 | 0.010038 | 0.0044615 | 0.0011154 | 0.00071384 | 0.00017846 | 4.4615e-05 | 1.1154e-05
expected (-20℃) | 0.01 | 0.0064 | 0.0036 | 0.0016 | 0.0009 | 0.0004 | 0.0001 | 6.4e-05 | 1.6e-05 | 4e-06 | 1e-06
expected (-50℃) | 0.001 | 0.00064 | 0.00036 | 0.00016 | 9e-05 | 4e-05 | 1e-05 | 6.4e-06 | 1.6e-06 | 4e-07 | 1e-07
expected(-100℃) | 1e-05 | 6.4e-06 | 3.6e-06 | 1.6e-06 | 9e-07 | 4e-07 | 1e-07 | 6.4e-08 | 1.6e-08 | 4e-09 | 1e-09
expected (-150℃) | 1e-07 | 6.4e-08 | 3.6e-08 | 1.6e-08 | 9e-09 | 4e-09 | 1e-09 | 6.4e-10 | 1.6e-10 | 4e-11 | 1e-11 | 6.4e-12 | 3.6e-12 | 4e-13 | 1e-13
-150 ℃
-100 ℃
-50 ℃
-20 ℃
Relationship between ion and γ-ray sensitivity

## Slide 8: Obtain the information of nano-structure
1 μm
C 60 keV
Generation of filament
⇒ unique information of latent image specks (i.e., by particle, not dust)
Filament structure
⇒ nuclear recoil is very complicated structure, but electron should be very simple.
These information should be reflected in the localized surface plasmon resonance, especially reflection spectrum and reaction due to polarization of light.
not have image yet

## Slide 9: How do we check that?
current achievement is around -15 ℃
⇒ Can we keep lower temperature?
How do we check the sensitivity of low-temperature device?
⇒ high intensity radiation if expose from
outside of system
⇒ natural radiation source if set inside the system
Ex.) K-40 (N.A. 0.0117 %)
β-decay : Q-value 1.311 MeV (89 % D.P.)
γ-decay ：1.461 MeV (10.7 % D.P.)
KBr powder of 10 g ⇒ ~ 107 decay/day
γ-ray effect should be small from decay rate and cross section, but β-ray may be useful to check that
KBr powder
NIT
By very rough estimation, β-day will be accumulated about 1-10 /(10µm)3 for 10 days exposure.
⇒ Simulation is needed taking into account β-spectrum
Refrigerant
Refrigerant
N2 gas
N2 gas
Thermo-sensor

## Slide 10: Fog

## Slide 11: Development sensitivity tuning
Fog
Signal
Activation energy (ORP)
Developer
Current (usual) development treatment
Kinetical process
Fog
Signal
Developer
Reduction process
Activation energy (ORP)
oxidation
Reduction
Ideal situation
Equilibrium process
Time
Fog
Signal
Developed intensity
Ag+ + e- (decomposition)
e-
Ag+
Signal
Fog

## Slide 12: Current study (task within November)
We need to know redox potential of latent image specks using Redox
buffer ⇒ now on going
Tuning of redox potential for developer ⇒ it’s easy
Easy method (idea from Prof. Tani)
Diluted developer
Usual developer
Size difference of specks between fog and signal should be enhanced.
Ratio of Signal size and contrast to fog will be enhanced.

## Slide 13: Conclusions
Lower temperature should be critical to achieve high electron rejection power
Combination both low-temperature and chemical sensitivity control is very promising because those processes reveal essentially difference process.
Development treatment is not optimized yet, and there are room for improvement.
Redox potential control is under studying, and go to study for improvement of developer to reduce the background