## Slide 1
STATUS OF THE WOUND CONDUCTOR TASK
D. Pulikowski, P. Ebermann, F. Wolf, J. Fleiter, S. Luzieux, S. Triquet, F. Meuter,
D. Tommasini, C. Scheuerlein, D. Schoerling, T. Koettig, F. Lackner
TE-department - MSC-LMF, MSC-MNC, MSC-SCD, MSC-MDT, CRG-CI
FCC Week 2017, Berlin
31th, May 2017

## Slide 2
What can we measure directly in the Nb3Sn coils or a magnet assembly
Winding tension during the winding process
Coil geometry after impregnation (no ext. stress)
Stress condition on shell assembly, axial stress reaction on end support plates, rods
Strain conditions on supporting structures (collar nose in case of 11T)
Pressure sensitive foils can provide information on pole and midplane stress and the related distribution
What we currently can not measure
Conductor stress-strain state during coil fabrication, magnet assembly, cooling & operation
What do we currently estimate from simulations
Stress-distribution in the coil cross-section (mainly in 2D) to develop knowledge on required pre-stress at ambient temperature, achieved precision is strongly depending on input parameters
Shimming of coils to achieve and keep pre-stress during different operation conditions (cooling – operation) is presently based on the measured coil geometry and stress estimation from FEA simulations using the stiffness measurements from 10-stack sample (stacked cables comparable to coil cross-section)
Mechanical coil characterization by measurement and simulation
Characterization of Nb3Sn wound conductor

## Slide 3
Characterization of Nb3Sn wound conductor
Windability
Material characterization
Development of winding test setup to define a “windability factor” allowing comparison between different Rutherford cables
Irreversible degradation
Quantify irreversible degradation of the conductor during the magnet assembly at RT
Develop knowledge about stress distribution on Rutherford cable stack under the transversal load
Improving knowledge of magnet material parameters for refinement of FE modelling
Improved FE meshing using tomographic coil characterization
Development of adequate scanning method to quantify strand displacements during the winding process
Lateral shim
Coil size top
Collar nose shim
Coil size bottom
Collar-Yoke shim
Arc length

## Slide 4
The dominating load case in accelerator magnets is transverse compressive
Coils are loaded during the assembly, cooling, powering, quenching & thermal cycles
Experimental results about the room temperature (RT) stress limits of Nb3Sn wires, cables and coils at which irreversible conductor degradation occurs are lacking
The ongoing experiment aims to determine the critical RT transverse compressive stress limits of cured, reacted and impregnated Nb3Sn coil components
The degradation is quantified in terms of critical current and n-value
Ic degradation after transversal pressure at RT

## Slide 5
TESTING SEQUENCE
  The Ic of a reacted and impregnated two stack cable sample is measured in FRESCA
  Sample is taken out from FRESCA and compressed in a controlled manner at ambient temperature
  The sample is re-measured in FRESCA to check if, and by how much the compression has modified the IC
Improved knowledge on stress-distribution
The test setup has been optimized in order ensure a known pressure distribution during the load step
Cable compression on hydraulic press
FRESCA sample, RRP – Nb3Sn 11T cable stack

## Slide 6: The Press
OPTIMIZATION OF THE LOADING STEP
Pressure measurement films from FujiFilm are used to measure the pressure distribution during the loading cycle
We optimized the pressing tool to provide a reasonable uniform pressure on the sample
Courtesy of P. Ebermann & F. Wolf
Notes: Superconductive coil characterization for next dipoles and quadrupoles generation
Malathe Khalil
05/08/2016 CERN

## Slide 7
RESULTS
Comparison of fitted voltage-current-curves at Bapp = 9.6 T at T = 4.2 K
No degradation observed up to 150 MPa
*
* Measurements are ongoing on 31st of May.
First results at 4.2 K show relative degradation Ɛ in the order of 2 – 3 %

## Slide 8
WINDABILITY
Measure and model the geometrical evolution of cables during winding.
Identification of the parameters dominating this process to possibly provide feedback for cabling & winding.
Set-up a standard to quantify a “windability factor” or similar.
Courtesy of D. Pulikowski
CERN-LMF, 11T dipole winding machine
CERN-LMF, 11T dipole pole end
Notes: New slide from Davide.
Showing that conductor development is launched at international level, Russia, Japan, (Korea and Europe in preparation)
Underline importance of that development as main cost driver for the hadron collider machine.

## Slide 9
Typical findings during the winding of Nb3Sn coils
Protrusion from the mandrel surface
Strand pop-out
WINDABILITY
Quantify geometrical displacements due to observed instabilities
Proposal and definition of a “windability factor” allowing to compare results of different cable geometries

## Slide 10
Allows to wind specimens with the Rutherford type cables in 1 DOF
Provides repeatable conditions;
Allows to adjust several winding parameters:
  Winding tension, Bending radius, Cable guide position and angle & winding direction.
1DOF
Winding tension (mass)
Cable guide
Path
Envelope
Protrusion
Pop-out
1 DOF WINDING MOCKUP
Sample holder for winding tests

## Slide 11
0
45
90
135
180
1 DOF WINDING MOCKUP

## Slide 12
Z
Y
A
1 DOF WINDING SCANNER

## Slide 13
Stability of the winding is the average standard deviation () of three specimens for each winding tension and direction.
It describes the performance spread for one parameter set.
Nb-Ti shows the worse envelope instability.
11T RRP shows multiple times larger winding instability of pop-out and protrusion.
WINDING STABILITY OF Cu, Nb-Ti AND RRP Nb3Sn CABLES

## Slide 14
Envelope
Protrusion
Pop-out
Envelope trends are declining, the smallest deformation is achieved by 11T Cu cable.
Pop-out: Nb-Ti shows least dependence on the winding tension.
Larger protrusion deformation in favourable direction for 11T RRP and Nb-Ti.
WINDING STABILITY OF Cu, Nb-Ti AND RRP Nb3Sn CABLES
Preliminary results on first samples:

## Slide 15
Impact of insulation and impregnation conditions on the coil stiffness
Variables:
  The insulation (e.g. impact of Mica foil)
  The impregnation (variation of compaction level of the cable stack)
  The sample length (15 mm, 30 mm, 100 mm)
Measurements:
  Force measurement by calibrated load cells in the force line of a hydraulic test setup
  Displacement measurement direct at the sample with an extensometer
  Displacement measurement of the press tools by capacitive gauges
MECHANICAL PROPERTIES OF A CABLE STACKS
Courtesy of F. Wolf

## Slide 16
FURTHER ACTIVITIES
Thermomechanical properties of a Nb3Sn coil (11 T) and tooling constituents in collaboration with Federal Laboratory for Materials Research and Testing (BAM), Berlin.
Young’s moduli, shear moduli, Poisson ratio and thermal expansion coefficients vs temp (-150°C to 700 °C).
To be completed by September 2017.
Friction coefficients between 11 T dipole materials pairs in collaboration with Federal Laboratory for Materials Research and Testing (BAM), Berlin. Friction measurements are performed at RT and in LHe. Materials pairs are TiAlV on 316L shim, TiAlV on Polyimide, steel on Polyimide, and the effect of MoS2 coatings on friction is studied (at RT and in LHe). To be completed by September 2017.
Nb3Sn strain state distribution in a 11 T dipole coil, in collaboration with ID15A beamline of European Synchrotron (ESRF) and StressSpec beamline at Heinz Maier-Leibnitz Zentrum (MLZ), Munich.
Nb3Sn strain state distribution at RT and at 10 K without externally applied stress
Nb3Sn strain state distribution at RT with external stress applied through steel collars
Tomographic studies of the Nb3Sn conductor in 11 T dipole coils in collaboration with Federal Laboratory for Materials Research and Testing (BAM), Berlin, ANTARES beamline at Heinz Maier-Leibnitz Zentrum (MLZ), Munich, and Fraunhofer Institute for Industrial Mathematics (ITWM), Kaiserslautern. Determination of the 3D shape of Rutherford cables in coils. To be completed by September 2017.

## Slide 17
CONCLUSIONS
The results coming from the characterization of the irreversible cable degradation at RT, though very preliminary seem encouraging and support the choices performed within the EuroCirCol study
The winding setup may allow to define a windability factor useful for future cable development and winding process (robust and repeatable quality, production time)
The study of the stiffness of cable stacks depending on their manufacturing procedure has been started
A number of studies are under way to refine input parameters and meshes for FE analysis, and to characterize the internal stress distribution in Nb3Sn coils