## Slide 1: Copper Laser-Engineered Surface Structures (LESS)
FOLLOW-UP MEETING
Elisa García-Tabarés Valdivieso
TE-VSC-SCC
19th July 2016

## Slide 2: LESS Copper: University of Dundee
SEY at RT

## Slide 3: LESS Copper: University of Dundee
SEY goes down during SEY measurement.
It goes up immediately after the measurement.
SEY dispersion is reduced as we increase the temperature.
Conditioning of the sample?
SEY at cold
300K

## Slide 4: LESS Copper: University of Dundee
Conditioning?
27.06.2016
SEY goes down during the measurement.
During conditioning, instead of going down, SEY increases.
Is the sample charging due to the presence of copper oxide?

## Slide 5: LESS Copper: University of Dundee
Oxide removal (SPECS system)
C1s
O1s

## Slide 6: LESS Copper: University of Dundee
Oxide removal (SPECS system)
http://xpssimplified.com/elements/copper.php

## Slide 7: LESS Copper
Oxide removal (SPECS system)
CuLMM
http://xpssimplified.com/elements/copper.php

## Slide 8: LESS Copper: University of Dundee
Oxide removal (SPECS system)

## Slide 9: LESS Copper: University of Dundee
SEY at cold after oxide removal
SEY goes down during SEY measurement.
It goes up immediately after the measurement.
SEY dispersion is reduced as we increase the temperature.
Same behavior as before oxide “removal” but, dispersion has been reduced.

## Slide 10: LESS Copper: University of Dundee
SEY after solvent MC20
“Type c” LESS Cu

## Slide 11: LESS Copper: University of Dundee
LESS Copper_2
LESS Copper_1