## Slide 1: Work Function measurements and low energy SEY
Sample | PLD_1 | PLD_2 | PLD_3 | DC_sp.
ΦKel (eV) | 5.29 | 5.4 | 5.53 | 5.87
Max SEY | 1.8 | 1.6 | 1.0 | 0.95
Work Function measurements
Work function increases → maximum SEY decreases
  Low energy electron not able to escape
SEY drop shift ↔ Differences between work functions
  More energy needed to overcome the barrier
Low Energy SEY
Comparison : SEY drop shift / ∆Φ