## Slide 2: COLLABORATION AGREEMENT CERN-LNL-STFC (KE2722/BE/FCC)
Fabrication seamless cavities 2x 400 MHz & 800 MHz (4x mono-cell 2x two-cell) @ LNL
6 GHz cavities coating and RF test @ LNL
Development of coating system (1.3 GHz) @ STFC
Sample (up to 40) characterization (SEM, XPS, XRF, TEM, XRD, AFM) @ STFC

## Slide 3: 6 GHz status from Enzo
Modification of the spinning procedure in order to have a scratch-free internal surface without the need to apply a mechanical treatment by vibrotumbler
Design and construction of a new magneton sputtering system in order to sputter simoultaneosly all the cavity in one run (Before we had to move the cavity all over a shorter magnetron).
Implementation of the kapton flange system for sealing the cavity at liquid helium temperature in order to avoid leaks at the superfluid temperature.
Improvement of UH Vacuum in the Cryogenic inserts where the cavities are plugged (not yet completed)
Maintenance and service of the RF bench (expected to be completed for December 2016)
About cavities we have done the following:
  we have used 9 cavities,
  on them we have done 11 different depostions
  of these 11 depositions, 5 caviies were not measured because of film peling or other problems
  the remaining 6 cavities were measured at 4.2 K. and at 1,8 K.
The rf performances we got on these last cavities were always improving
We plan to measure more cavities in the next months

## Slide 4: FCC RF R&D WP4
COLLABORATION AGREEMENT CERN-LNL-STFC (KE2722/BE/FCC)
  Framework for scientific collaboration in Superconducting RF cavities technology (S.C.)
  Study and optimization of the surface treatment facility at CERN (Leonel Ferreira)
  Nb coating of 400 MHz and 800 MHz cavities at CERN (Guillaume Rosaz)
  Prepare for 800 MHz Nb/Cu cavities RF warm and cold measurements at CERN (Mathieu Therasse)

## Slide 5: FCC 400 MHz cavities = LHC
Seamless cavities
OFE copper
February 2017?
Surface preparation tbd
Coating ready

## Slide 6: FCC 800 MHz cavities
Seamless cavities
OFE copper
Mid-end 2017?
Surface preparation tbd
Coating tbd

## Slide 7: Surface preparation
EP compulsory
  Seamless cavities
  Need to remove at least 120 µm from the surface – cannot be done with SUBU
  Vertical: possible solution
  Horizontal: best option – issue: SPACE
SUBU as a backup:
  LHC bench  new flanges to be designed
Manpower, resources tbd

## Slide 8: Coating technique
DCMS
  Power supplies, cathode (400 MHz) available
  Known technique
  Quick to set-up
  Not promising from a performance point of view
HiPIMS
  At least as good as DCMS
  Possibly better than DCMS (bias)
  Two new power supplies needed
  Possible new cathode design
OTHER TECHNIQUE? (ECR etc…)  long setup time, no experience at CERN.

## Slide 9: RF test
LHC bench available for 400 MHz
Insert, tooling, hardware etc. needed for 800 MHz
tbd