## Slide 1: Nb-coated copper crab cavity alternative for FCC
Alexej Grudiev
17.05.2017

## Slide 2: Outline
Crab cavity system for FCC-hh
Motivation for Nb-coated crab cavity
Cavity design and parameters
Budget and time line

## Slide 3: Crab cavity system for FCC-hh (april 2017)
Schematic layout:
E. Cruz-Alaniz,
Nov. 2016, Barcelona
Information for FCC-hh provided by FCC-hh general design WG: D. Schulte, E. Cruz-Alaniz, A. Seryi, R. Martin, R. T. Garcia
 | FCC-hh |  | HL-LHC (R. Calaga, Chamonix 2012)
RF frequency [MHz] | 400 |  | 400
Total voltage V [MV] | 18 (uncertainty ±20%) |  | 6 ÷ 10
Available length [m] | 20 |  | 
Beam separation [mm] | 250 (maybe 204 soon) |  | 194
Average beta in the ring [m] | (339+67)/2 = 203 |  | 200
Beta* [m] | 0.3 | 0.1 | 15 ÷ 25
Crossing angle [urad] | 89 | 154 | 235 ÷ 290
Beta at CC location [m] | 10100 ÷ 10900 | 30300 ÷ 32700 | 4000

## Slide 4: Comparing CC pars for FCC-hh to the HL-LHC
MORE CCs: Total voltage is 3 (2) times higher => 6 cavities per beam/side/IP
Available length: 20m/(6x2) = 1.7 m per cavity is sufficient even for longer alternatives (WOWCC)
Larger beam separation 250 vs 194 may give some advantages in case of redesign
EFFECTIVE TRANSVERSE IMPEDANCE IS MUCH (up to 3x8=24 times) HIGHER than for HL-LHC:
  Beta function at the CC location is 2.5 -> 8 times higher for the same <beta>
  Number of cavities per beam 2-3 times higher
Low impedance CC are desirable
In Conclusion: larger number of cavities, larger beam coupling impedance and different beam separation justifies looking into new alternatives for FCC-hh CC system

## Slide 5: Motivation
S. Aull, SRF2015

## Slide 6: Motivation
S. Aull, SRF2015
Can we apply the state of the art coating technique to 400 MHz crab cavity?

## Slide 7: Introduction
This work package covers design, construction and testing of 2 prototypes of a compact superconducting crab-cavity for LHC using Nb-on-Cu-coating technique.
The cavity shape is based on the ridged waveguide resonator with wide open apertures to provide access to the inner surface of the cavity for coating.
It also provides natural damping for HOMs and rather low longitudinal and transverse impedances.
The final goal is to validate the fabrication and coating of the cavity prototypes and to characterize its high gradient performance in a vertical test at 4K

## Slide 8: Main Parameter
Frequency [MHz] | 400.000
G [] | 109
Vx [MV] | 3.0
Total Energy [J] | 10.4
Rx/Q [] | 343.5
Epeak [MV] | 50
Bpeak [mT] | 78
Bpeak = 70 … 80 mT
w [mm] | 251.70
h [mm] | 251.70
r [mm] | 42.00
L [mm] | 1400.00
d [mm] | 192.00
L/2
h
w
r
d
d
Notes: Make clear here why we are interested in the rfq. It has several advantages over the octupoles in a machine like LHC or HL-LHC.

## Slide 9: Non-linear behaviour of surface resistance (S. Calatroni, S. Aull)
LHC: Rs(Brf)[nOhm] = 54.7 + 19.0*exp(0.054*Brf[mT])
ECR: Rs(Brf)[nOhm] = 46.9 + 17.1*exp(0.023* Brf[mT])
There is a big potential in the new coatings but let’s be conservative and take LHC cavity data.

## Slide 10: Power loss distribution on the surface for 30 degree taper at 3 MV
Psurf [W/m^2]
Rs [nOhm] LHC fit
Brf [T]
Total power loss: 67W
Q0_Nb_3MV = 3.9e8

## Slide 11: Q0 calculation
Nominal kick voltage 3 MV  Bpeak up to 80 mT
Results above 40mT for LHC uncertain due to lack of measurement data
Q based on extrapolation of Rs from the LHC data
Q0 (Rs=const.) = 4.45e8
Q0 (Rs=Rs(B)) = 4.05e8
Homogeneous Rs
Inhomogeneous Rs(B)
S. Bauer, W. Diete, B. Griep, M. Peiniger, et al., in Proc. 1999 Workshop on Superconductivity (1999) pp. 437–439.
Notes: Make clear here why we are interested in the rfq. It has several advantages over the octupoles in a machine like LHC or HL-LHC.

## Slide 12: Wake Field and Impedance Calculation
Loss factor [V/pC] | 0.012
(ZL/N)eff [m] | 0.974
Kick factor x [V/pC/m] | 1.673
Kick factor y [V/pC/m] | 0.460
(ZT)eff x [/m] | 1562.8
(ZT)eff y [/m] | 437.6
Kick factor x [V/pC/m] | 0.733
Kick factor y [V/pC/m] | 0.769
(ZT)eff x [/m] | 631.9
(ZT)eff y [/m] | 791.9
Monopole
Dipole
Quadrupole
Notes: Make clear here why we are interested in the rfq. It has several advantages over the octupoles in a machine like LHC or HL-LHC.

## Slide 13: Assembly concept of the WOWCC copper substrate
brazing
welding
welding
Total weight: 290 kg

## Slide 14: Integration of WOWCC into LHC-coating setup
Aim of the integration study:
Get overall dimensions and weight of the setup
Formulate requirements for the infrastructure in the B252
Communicate the requirements to the responsible for the infrastructure in B252
Pave the way to the future work on the design of the coating setup
Total hight:
5.5 m
Total weight:
820 kg
WOWCC + frame weight:
517 kg

## Slide 15: Work package structure:
Task 1: RF design (Alexej Grudiev (RF))
Task 2: Mech. Design of the prototype and tooling (Ofelia Capatina (MME))
Task 3: Fabrication of the “substrates” (Pierre Naisson (MME))
Task 4: Surface treatment (Leonel Ferreira (VSC))
Task 5: Coating system and coating (Alban Sublet (VSC))
Task 6: Rinsing and clean room assembly of the prototypes for testing (Mikko Karppinen (RF))
Task 7: Cold Testing in cryostat (Mikko Karppinen (RF))

## Slide 16: Schedule
 | 2016 |  |  |  | 2017 |  |  |  | 2018 |  |  |  | 2019 |  |  |  | 2020 | 
 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2
Material procurement |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Fabrication 1st proto |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Fabrication 2nd proto |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Coating R&D |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Coating system design |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Coating system construction |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
(Re-)Coating 1st proto |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Cold testing 1st proto |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
(Re-)Coating 2nd proto |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Cold testing 2nd proto |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 

## Slide 17: Budget and manpower profile (end of 2016)
 |  | 2016 | 2017 | 2018 | Total
Budget [kCHF] | Design Material Fabrication Chemistry Coating RF infrastructure | 20 80 0 0 0 ? | 20 ~0 150 100 150 ? | ? ? 50 50 50 ? | 
 | Total | 100 | 420 | 150 | 670
Manpower [FTE] |  |  |  |  | 
 | Engineer (ENG) | 0.33 | 0.85 | 0.5 | 1.7
 | Technician (TEC) | 0 | 1.5 | 1.5 | 3.0
 | Fell/PJAS (FEL) | 0.45 | 0.25 | 0.25 | 1.0
The resources for SRF infrastructure modification in order to accommodate the WOWCC prototypes are not included
20% less cost for coating system
Reduction of manpower for coating
2PM-ENG
3PM-FEL
3PM-TEC

## Slide 18: Summary why would we do coated crab
No thermal run-away (operation, machine protection)
Potential to reach 5 MV per cavity if coating is (2-3 times) better than for LHC 400 MHz main RF cavities (cost, impedance)
Lower impedance (x2, Z/n; x3 Z_x,y)
No magnetic shielding (cost)
Material (cost)