## Slide 1: Heater quench study
Michinaka Sugano
D1 magnet review, KEK, 30 June – 1 July 2016

## Slide 2: Outline
Spot heater test
  Current dependence of detection time
  Quench propagation speed
QPH test
  Current and power (energy) density dependence of delay time
  Comparison between four QPHs
All tests were carried out under energy extraction with 73 mW dump resistor. Current decay was not included in the test items.

## Slide 3: Spot heater test
Two spot heaters for each coil (high field, low field regions)
At each magnet current, amplitude and duration of pulsed current to a SPH were adjusted until quench occurred.
Maximum current to the magnet was limited to 9.5 kA.
Detection time was evaluated from balanced voltage rise.
Quench propagation speed was estimated from voltage signals using voltage taps .
Return end
Spot heater at high field region
Lead end
Spot heater at low field region

## Slide 4: Evaluation of detection time
Spot heater (20 V, 40W)
Current: 2 - 9.5 kA
Voltage threshold: 0.1 V
Validation time: 10 msec
Vbal=0.1 V
Balanced
voltage
Heater
voltage
Heater
Current
Time to
DVbal=0.1 V
Validation time
Detection time
Detection time =
Time to DVbal=0.1 V + Validation time

## Slide 5: Current dependence of balanced voltage rise
Faster voltage rise at higher current and field
Change of slope due to transversal propagation
Vbal=0.1V
Vbal=0.1V
High field
Low field

## Slide 6: Current dependence of detection time
Longer measured detection time than calculation under adiabatic condition is reasonable.
Data of I2 integral over detection time can be obtained, which will be used to discuss quench protection.

## Slide 7: Quench propagation velocity
High field
Low field
SPH1
SPH3

## Slide 8: QPH test
Energy deposition test at different charged energy of a PS
PSs from CERN with C=7.05 mF and maximum charged voltage of 800 V were utilized to fire QPHs.
Only one QPH was connected with a 3 W dummy resistor in series for each test to evaluate delay time.
Maximum current to the magnet was limited to 9.5 kA.
A SUS strip in a QPH with t25 mm x w15 mm x l2 m without Cu ilands covers 9 turns in CB1 (low field)
Heater
strip

## Slide 9: Evaluation of delay time
Delay time
Balanced
voltage
QPH
voltage
Current: 688 A (Injection) - 9.5 kA
QPH was fired at 100%, 50%, 25% (37.5%) of stored energy of a PS
Delay time: Time difference between QPH firing and the onset of balanced voltage
t0
teff
Delay time was evaluated as a function of
Ppeak: Peak power density (=VQPH,max2/RQPH/S, S=Area of QPH)
Eeff: Effective energy density ()
3 W
dummy
resistor
VQPH
QPH1
QPH2
QPH3
QPH4
V
7.05 mF

## Slide 10: Comparison of QPH1-4
Test at 9.5 kA
Very good agreement of delay time among all QPHs
Subsequent tests were performed for QPH1.
 | Position of QPH | Ppeak (W/mm2) | Eeff (J/mm2) | Delay time (msec)
QPH1 | Top, ramp side | 0.73 | 0.017 | 31
QPH2 | Top, non-ramp side | 0.71 | 0.016 | 31
QPH3 | Bottom, ramp side | 0.70 | 0.016 | 32
QPH4 | Bottom, non-ramp side | 0.71 | 0.016 | 31
I = 9.5 kA
1
2
3
4
View from LE

## Slide 11: Power and energy dependence of delay time

## Slide 12: Current dependence of delay time
At injection current, quench did not occur at Ppeak=0.25 W/mm2.
Required power density to induce quench above injection current > 0.35 W/mm2
Injection
Nominal

## Slide 13: Summary
Spot heater and QPH tests were carried out up to 9.5 kA.
Detection time for quench starting at low and high field regions could be experimentally determined.
Homogeneous performance was confirmed for four QPHs.
From the current dependence of delay time, minimum required power density to induce quench could be evaluated.
In MBXFS02, the design of the QPH will be changed so that heater strips cover high field region as well as low field one.
We need to perform evaluation of current decay as well as the same spot heater and QPH test at higher current .