## Slide 1: Measurement during the assembly and ELQA
Michinaka Sugano
D1 magnet review, KEK, 30 June – 1 July 2016

## Slide 2: Outline
QA test results in the following fabrication steps
  Coil winding
  Curing
  Coil size measurement
  Instrumentation
  QPH, Insulations
  Collaring
  Yoking
  Shell, end ring welding and splice work

## Slide 3
Coil winding
Curing
Coil size measurement
Instrumentation
QPH, Insulations
Collaring
Yoking
Shell, end ring welding and splice work

## Slide 4: Coil winding
Visual inspection of cable surface
Following items were checked every after winding a half turn.
  Measurement of cable position and angle at the coil ends
  Check of ground fault btw the cable and the winding mandrel with a tester
Check of fitting between the cable and end spacers with Fuji paper
Meas. of cable angle
with a micro-protractor
Meas. of cable position
with a caliper
Check of fitting between
the cable and an end spacer
Fuji paper
Top, LE2
Top, LE6

## Slide 5
Coil winding
Curing
Coil size measurement
Instrumentation
QPH, Insulations
Collaring
Yoking
Shell, end ring welding and splice work

## Slide 6: Curing
Change of coil length and position of end spacers before and after curing  Shrinkage of total coil length < 1mm
During curing
Check of ground fault with a tester
Measurement of coil resistance
Temperatures at the mandrel and forming block
After curing
Electrical tests
  Measurement of Coil resistance  No change before and after curing
  Inductance measurement Same inductance between two coils
  Surge test  Normal waveform up to 3 kV
 | Coil resistance at 20oC (W) |  | Coil inductance at 100 Hz (mH)
 | Before curing | After curing | After curing
Top coil | 0.234 | 0.232 | 2.17
Bottom coil | 0.234 | 0.233 | 2.15
Surge test (Top coil)
Time (msec)
Voltage (V)

## Slide 7
Coil winding
Curing
Coil size measurement
Instrumentation
QPH, Insulations
Collaring
Yoking
Shell, end ring welding and splice work

## Slide 8: Coil size measurement
50 ton hydraulic press
Two pushing bars with strain gauges
 Pressure applied to the coil MPs every 20 mm can be measured.
Four linear gauges
 Coil deformation
5.4 m-long-bench
 Longitudinal distribution
Hydraulic cylinder
Load cell
Upper block
Lower block
Dummy
mandrel
Pushing bars
Linear gauges
Measure the pressure to compress a coil to the final size and compare it with the target value of pre-stress
Thanks to Glyn Kirby
R5
R4
R3
R2
R1
L5
L4
L3
L2
L1
Pushing bars
20 mm

## Slide 9: Results on coil size measurement
Good homogeneity at the straight section
Measured values: 95 – 97 MPa
Average MP stress after yoking by ANSYS: 104 MPa (including 10 MP margin)  Measured value is 7 – 9 MPa lower
Pmax at coil end: 15 MPa at max (Measured at 6 mm from the coil end)
Improvement of the setup to enable a measurement of the pole stress
is necessary.
Straight section
 | Ramp side | Non-ramp side
Top coil | 95.2±2.4 | 96.7±2.1
Bottom coil | 96.6±3.1 | 97.2±2.7
Pmax in SS after correction of machine deformation (MPa)
Non-ramp
side
Ramp side

## Slide 10
Coil winding
Curing
Coil size measurement
Instrumentation
QPH, Insulations
Collaring
Yoking
Shell, end ring welding and splice work

## Slide 11: Instrumentation
Soldering the voltage taps
Attachment of spot heaters
After instrumentation work
Coil resistance  No change
Coil inductance  No change
Surge test  Normal waveform up to 3 kV
Check of insulation between a coil and spot heaters with a tester
 OK
Voltage taps
Spot heater

## Slide 12
Coil winding
Curing
Coil size measurement
Instrumentation
QPH, Insulations
Collaring
Yoking
Shell, end ring welding and splice work

## Slide 13: QPH test
Before starting cold mass assembly, energy deposition test was performed for the two of four QPH strips.
A SUS strip was clamped with Al bars to avoid excessive heating-up.
Almost same energy corresponding to full charging voltage of the PS (800 V) was deposited to one heater strip and a 3 W dummy resistor.
Reasonable decay constant of QPH voltage expected from CPS = 7.05 mF and the circuit resistance was confirmed.
Wrinkles were observed after test, but we confirmed no change of the strip resistance. We decided to use them for the 2m model.
Additional QPH test was carried out after yoking as well.

## Slide 14
Coil winding
Curing
Coil size measurement
Instrumentation
QPH, Insulations
Collaring
Yoking
Shell, end ring welding and splice work

## Slide 15: Collar strain gauges
4 strain gauges at each position (full bridge), 3 longitudinal positions in the straight section
Relationship between applied load and strain was calibrated using a tensile testing machine and the dedicated jigs at RT and 77 K.
Apparent strain was also measured between RT and 77 K.
Michinaka Sugano, D1 magnet review, 30 June 2016
Collar gauge
Calibration jigs

## Slide 16: Collaring
During collaring (for each collar sub-stack assembly)
Coil resistance  No change
Check of ground fault with a tester
  Coil-to-coil, coil-to-ground, coil-to-spot heater, coil-to-QPH
   No ground fault
After collaring
Position of each collar sub-stack
Diameter of collared coil
Monitoring of collar pole strain  No additional strain
Coil resistance  No change
Cable resistance between voltage taps  No change
QPH and spot heater resistance  No change
Coil inductance at 100 Hz
Top (2.67 mH), Bottom (2.67 mH)
Surge test  Normal waveform
Hi-pot test to 5 kV for 1 min for coils, QPHs
 Insulation resistance > 100 GW
SPH1(LF)
SPH2(LF)
SPH3(HF)
SPH4(HF)
Top coil
Bottom coil
Collar
QPH2
QPH1
QPH3
QPH4

## Slide 17
Coil winding
Curing
Coil size measurement
Instrumentation
QPH, Insulations
Collaring
Yoking
Shell, end ring welding and splice work

## Slide 18: Yoke gauge
Strain gauges were attached at the tip of the tapers at the yoke MP to monitor contact between upper and lower yokes.
Apparent strain was measured between RT and 77 K.

## Slide 19: Yoking
Before yoking
All yoke plates were weighted and categorized to 6 groups.
Yoke plates were picked up evenly from each group so that total length of each yoke sub-stack can be homogenized.
Yoking trial
Check of pre-stress to the ramp boxes at the GFRP collars with Fuji paper
 ~ 30 MPa (Target value: 40 MPa)
Polyimide shims were inserted
instead of Fuji papers.
(Total thickness of 0.4 mm
comparable to Fuji papers)
During yoking
Coil resistance  No change
Check of ground fault with a tester
 No ground fault
Monitoring of collar pole
and yoke strain
 Next slide
Fuji paper
MP
Ramp box

## Slide 20: Strain and stress measurement during yoking
A
C
D
A
B
A
C
D
B
Collar pole
Yoke
A: Before yoking
B: Contact between upper and lower yoke
C: Key insertion
D: After releasing load to yoke shoulder
(After yoking)
CG-T-Ra
CG-T-Rb
CG-B-Ra
CG-B-Rb
View from LE
YG-B-Rb
YG-B-Ra

## Slide 21: Pre-stress after yoking
Measured in three longitudinal positions in SS
Average pre-stress: 64.6±9.6 MPa
Measured pre-stress is lower than the target value of 80 MPa.
L
M
R
T-a
T-b
B-a
B-b
View from LE
L: LE side
M: Middle
R: RE side
in the straight section

## Slide 22: After yoking
Outer diameter of yoked magnet  Next slide
Coil resistance  No change
Cable resistance between voltage taps  No change
QPH and spot heater resistance  No change
Coil inductance at 100 Hz
Top (2.80 mH), Bottom (2.80 mH)
Surge test  Normal waveform
QPH test at a half energy  Similar voltage waveform for all QPHs
Hi-pot test  Insulation resistance > 100 GW for coils and QPHs

## Slide 23: Outer diameter of yoked magnet
Oval deformation of yoked magnet is observed.
OD in the vertical direction is 0.19 mm larger than OD in the horizontal direction, which is comparable to ANSYS calculation.
OD1
OD2
OD3
OD4
Long. position from LE | OD1 | OD2 | OD3 | OD4
50 | 550.079 | 550.070 | 549.909 | 549.905
700 | 550.030 | 550.040 | 549.882 | 549.860
1000 | 550.075 | 550.070 | 549.853 | 549.851
1300 | 550.030 | 550.043 | 549.858 | 549.860
1968 | 550.039 | 550.053 | 549.840 | 549.829
Ave. | 550.051 | 550.053 | 549.868 | 549.861
A
B
55mm
12mm
33mm
Yoke deformation
calc. with ANSYS

## Slide 24
Coil winding
Curing
Coil size measurement
Instrumentation
QPH, Insulations
Collaring
Yoking
Shell, end ring welding and splice work

## Slide 25: Shell welding
Temperature (Shell surface at strain gauges and a coil end)
  Strain of collar pole, yoke and shell
After each welding pass
Measurement of Shell deformation
  Gap between upper and lower shell
  Gap between shell and yoke
Gap btw two halves of shells
with a caliper
Gap btw shell and yoke with
thickness gauges
640 mm
RE
LE
Shell strain gauges
(azimuthal and axial)
Active
Dummy
Dummy
Active

## Slide 26: Shell deformation
Deformation in the azimuthal direction
1-2 pass: Bending deformation is dominant
3-9 pass: Tensile strain developed
10-11 pass: No additional strain
Shell strain: 0.09 - 0.1% (azimuthal)
-0.05% (longitudinal)
Pass
number
1
2
3
4
5
6
7
8
9
10
11
Azimuthal
Axial
A
B
C
D
E
F
G
H

## Slide 27: After shell welding, end ring welding, ramp lead slice work
Coil resistance  No change
Cable resistance between voltage taps  No change
QPH and spot heater resistance  No change
Coil inductance at 100 Hz
Top (2.79 mH), Bottom (2.79 mH), 2 coils (8.10 mH)
Surge test  Normal waveform
Hi-pot test: 100 GW between 2 coils and ground (OK)

## Slide 28: Variation of pre-stress during fabrication
Pre-stress after yoking was 15 MPa lower than the target value.
Absolute value of strain could not be measured at cold. This should be solved by the next cold test.
Upper and lower limit of
the error bars correspond
to the max. and min. values
among 12 collar gauges.
Target value after yoking
RT

## Slide 29: Summary
Cable angle at coil end is more inclined than the designed values even after optimization. Design of the end spacers should be modified.
In coil size measurement, we confirmed that stress to the final size in the straight section was homogeneous, but the average value was 7 – 9 MPa lower than ANSYS calculation.
Electrical soundness of the magnet and heaters was confirmed throughout the fabrication processes.
Pre-stress of the coils at pole after yoking was 15 MPa lower than the target value.

## Slide 30: Buckups

## Slide 31: Coil size measurement procedure
Measure the iron dummy coil to estimate machine
deformation as a function of applied load
Compress a coil to the machine limit (Disp.=0 mm)
Correct the value of Pmax considering machine deformation
  Ambiguity on machine deformation can influence on the result. We assumed the simplest case in which stress distribution in an iron dummy coil is neglected.
  (This assumption maximizes the Pmax. )
Loading
Unloading
Pressure – displacement curve
Machine
displacement
Pmax
Iron dummy coil

## Slide 32: Summary of electrical test for coils
 | Coil resistance at 20oC (W) |  | Coil inductance 100 Hz (mH) |  | Surge test to 3 kV |  | Hi-pot test to 5 kV, 1 min Insulation resistance | 
 | Top | Bottom | Top | Bottom | Top | Bottom | Top | Bottom
Curing | 0.234 | 0.234 | 2.17 | 2.15 | OK | OK | > 100 GW | > 100 GW
Instrumentations | 0.234 | 0.233 | 2.15 | 2.15 | OK | OK | > 100 GW | > 100 GW
Collaring | 0.233 | 0.233 | 2.67 | 2.67 | OK | OK | > 100 GW | > 100 GW
Yoking | 0.233 | 0.233 | 2.80 | 2.80 | OK | OK | > 100 GW | > 100 GW
Shell, end ring welding, ramp splice work | 0.233 | 0.234 | 2.79 | 2.79 | OK | OK | 100 GW | 
Coils were electrically sound throughout the fabrication processes.