## Slide 1: Utilization of radioisotope trackers to determine the local environment of Hg(II) in dithiocarbamate functionalized nanoparticles
C. O. Amorim1, J. N. Gonçalves1, D. S. Tavares2, C. B. Lopes2, A. S. Fenta1,3,
N. M. Fortunato1, J. Schell4,5, T. Trindade2, E. Pereira2, J. G. Correia6, V. S. Amaral1
1. Physics Department and CICECO, University of Aveiro, 3810-193 Aveiro, Portugal
2. Department of Chemistry, CICECO and CESAM, Aveiro Institute of Nanotechnology, University of Aveiro, 3810-193 Aveiro, Portugal
3. KU Leuven, Instituut voor Kernen Stralingsfysica, 3001 Leuven, Belgium
4. CERN, Geneva, Switzerland
5.Institut für Materialwissenschaft, Fakultät für Ingenieurwissenschaften, Universität Duisburg-Essen, Germany
6. Centro de Ciências e Tecnologias Nucleares, Instituto Superior Técnico, Universidade de Lisboa, 2686-953, Sacavém, Portugal
IS 515:Radioactive probe studies of coordination modes of heavy metal ions from natural waters to functionalized magnetic nanoparticles
Spokesman: V. S. Amaral Contact person: J.G. Correia
T. Trindade1, A. L. Daniel-da-Silva1, C. Lopes1, E. Pereira1, V. S. Amaral1, J. N. Gonçalves1, J. P. Araújo2, C. T. Sousa2, A. M. L. Lopes3, J. G. Correia4, J. Roeder4, M. Stachura5 and L. Hemmingsen5
Aveiro1, Copenhagen5, Lisboa3, Porto2, Sacavém4, and ISOLDE/CERN

## Slide 2: Outline
Introduction
  Motivation
  Functionalized Magnetic Nanoparticles
Radioactive Trackers (How much Hg sorption?)
  Quantitative sorption analysis
Hyperfine/Local properties (Hg coordination?)
  DFT modeling
  PAC Spectroscopy
Conclusions
Utilization of PAC radioisotope trackers and DFT calculations to determine local environment of Hg(II) in dithiocarbamate functionalized particles for magnetic removal of Hg2+ from water
  DFT and PAC crossover

## Slide 3: Motivation
Water pollution by heavy metal ions is a serious environmental problem
Growing interest in sorbents for water decontamination
Magnetic Nanoparticles
  Easy separation using a magnetic field
  High effective surface area
  Easy and cheap to produce

## Slide 4: Functionalized Magnetic Nanoparticles
SiO2
Magnetite Nanoparticles (NP) functionalized with dithiocarbamate (DTC)
Two different geometries were used:
“A” type nanoparticles
  Cubic geometry with ≈ 100 nm side
  Diferent types of functionalizations
“B” type nanoparticles
  Spheric geometry with ≈ 50nm diameter
  Diferent types of functionalizations

## Slide 5: Functionalized Magnetic Nanoparticles
SiO2
Fe3O4
A1
Fe3O4
SiO2
A2
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
Fe3O4
SiO2
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
A3
NHn
DTC-Na
NHn
DTC-Na
NHn
DTC-Na
NHn
DTC-Na
NHn
DTC-Na
NHn
DTC-Na
NHn
Na-DTC
NHn
Na-DTC
Fe3O4
SiO2
NHn
DTC-Na
NHn
DTC-Na
NHn
DTC-Na
NHn
DTC-Na
NHn
DTC-Na
NHn
Na-DTC
NHn
Na-DTC
NHn
Na-DTC
NHn
Na-DTC
NHn
DTC-Na
NHn
DTC-Na
NHn
DTC-Na
A4
DTC-Hg
DTC-Hg
DTC-Hg
DTC-Hg
DTC-Hg
DTC-Hg
Hg-DTC
DTC
DTC
DTC-Hg
DTC
DTC
DTC-Hg
Hg-DTC
DTC
Hg-DTC
DTC
DTC
DTC
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
Fe3O4
SiO2
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
DTC-Hg
A5

## Slide 6: Functionalized Magnetic Nanoparticles
Fe3O4
Fe3O4
B1
Fe3O4
SiO2
B2
NHn
Fe3O4
SiO2
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
B3
NHn
Fe3O4
SiO2
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
DTC-Na
DTC-Na
DTC-Na
DTC-Na
DTC-Na
DTC-Na
DTC-Na
DTC-Na
DTC-Na
Na-DTC
Na-DTC
Na-DTC
Na-DTC
Na-DTC
Na-DTC
Na-DTC
B4
NHn
Fe3O4
SiO2
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
NHn
DTC-Hg
DTC-Hg
DTC
DTC-Hg
DTC-Hg
DTC
DTC-Hg
DTC-Hg
DTC-Hg
DTC
Hg-DTC
DTC
Hg-DTC
DTC
Hg-DTC
DTC
B5

## Slide 7: Radioactive Trackers
1. Implantation of 199mHg on ice
2. We melted the radioactive ice and added it to the NP suspension (Ultra-sonication during 20 minutes)
3. We measure the activity of the radioactive water + NP (which are in a test tube) in a HPGe detector gamma spectrometer.
4. NP separation from the solution using a strong magnet
5. We measure the remaining activity of the dry NP

## Slide 8: Radioactive Trackers
13/2+
5/2-
1/2-
532.48KeV
158.38KeV
0KeV
199mHg
42.6m
2.47ns
stable
ϒ1
374.10KeV
ϒ2 (Iγ=52.3%)
158.38KeV
199mHg
199Hg
199Hg
6. We integrate the measured activities to determine the absolute activity measured in the spectrometer.
7. We calculate the loss due to radioactive decay to compensate the loss measured and then we obtain the sorption percentage.
8. We repeat several times to add statistics to the sorption measurements .

## Slide 9: Radioactive Trackers
NP | Sorption (S) | ∆S
A2 | 14% | 5%
A4 | 73% | 5%
B2 | 25% | 6%
B4 | 50% | 1%
Hg sorption percentage for different types of NP measured with the gamma spectrometer for 20 minutes sonication
Concentrations of ≈ 1ng/dm3
  Legal limit concentration for Hg in drinking water = 2 µg/dm3
  Rain water concentration: 5-100 ng/dm3
Non-functionalized
Functionalized with DTC
Cubic larger
Spherical smaller

## Slide 10: Radioactive Trackers
Physical non intrusive measurement
  Chemical analysis usually needs processing which can alter the desired conditions of Hg environment
Direct measurement of Hg
  Recycling sorbent NP (difficult to infer with traditional methods)
  Study of external factors in the NP (such as temperature)
  Tracking of Hg
  Hg mapping would be possible
    Plants/animals Hg retention mapping
Very high sensitivity ( C < 1 pg/dm3, in comparison with ng/dm3 with fluorescence spectroscopy)
Advantages of Radioactive Trackers

## Slide 11: PAC Spectroscopy
13/2+
5/2-
1/2-
532.48KeV
158.38KeV
0KeV
199mHg
42.6m
2.47ns
stable
ϒ1
374.10KeV
ϒ2
158.38KeV
199mHg
199Hg
199Hg
To infer the coordination/local environment of Hg2+ PAC Spectroscopy was made
199mHg Isotope used
Cascade of 2 γ photons
Intermediate state perturbed by local environment
Perturbation affects angular correlation of γ photons

## Slide 12: PAC Spectroscopy
Local and/or external fields induce Hyperfine splitting
Information given by Hyperfine splitting:
Hyperfine Magnetic Field (HMF)
Electric Field Gradient (EFG)
Asymmetry parameter (ƞ)

## Slide 13: PAC Results
Experimental Ratio Plot + Fitted curve
Fourier Transform

## Slide 14: DFT Modeling
Density Functional Theory calculations were performed using the software VASP©.
Method
  Projector Augmented Wave (PAW)
Functional
  Generalized Gradient Approximation – PBE (GGA-PBE)
  Local Density Approximation (LDA)
Input
  Structural parameters
  Atoms
  PAW Atomic Potentials
Output
  Electric Field Gradient (EFG)
  Total Energy
  Relaxed Structure coordinates
  (∆EFG < 7%)

## Slide 15: DFT Modeling
DTC1
Calculated Local Environment:
Fe3O4
SiO2
distance
distance

## Slide 16: DFT Results
DTC1

## Slide 17: DFT Modeling
DTC2
Calculated Local Environment:
distance
Fe3O4
SiO2

## Slide 18: DFT Results
DTC2

## Slide 19: DFT Modeling
DTC3
Calculated Local Environment:

## Slide 20: DFT Results
DTC3

## Slide 21: DFT Modeling
SiO3Hg
Calculated Local Environment:
+D

## Slide 22: DFT Results
SiO3Hg

## Slide 23: DFT Modeling
SiO2Hg
Calculated Local Environment:
+D

## Slide 24: DFT Results
SiO2Hg

## Slide 25: PAC Results

## Slide 26: PAC Results

## Slide 27: PAC Results
D=+5 pm
D=0 pm
D=-15 pm
DFT

## Slide 28: PAC Results
D=+5 pm
D=0 pm
D=-15 pm
DTC1
D=+5 pm
D=-15 pm
DTC2
D=0 pm

## Slide 29: PAC Results
D=-5 pm
D=0 pm
D=-15 pm
DTC2

## Slide 30: PAC Results
D=-25 pm
D=0 pm
DFT

## Slide 31: PAC Results
DFT
D=50 pm
D=0 pm

## Slide 32: PAC Results
D=50 pm
D=0 pm
DFT
D=0 pm
D=10 pm

## Slide 33: PAC Results

## Slide 34: Conclusions
Radioactive Trackers allowed us to study different kinetics of sorption.
Fe3O4/SiO2/DTC functionalized NP (A4 and B4) have much higher sorption efficiency than Fe3O4/SiO2 NP (A2 and B2)

## Slide 35: Conclusions
The local environment/coordination of Hg2+ was determined by PAC-DFT crossover
In A2 and B2 NP, Hg mostly coordinates in SiO2Hg local environment.
In A4 and B4 NP (as well as in the Reference powders), Hg mostly coordinates in DTC2 local environment.
In A5 and B5 NP, Hg coordinates in SiO2Hg, SiO3Hg and DTC2 local environments.
Fe3O4
SiO2
B2
Fe3O4
SiO2
A2

## Slide 36: Acknowledgements
This work was developed within the scope of the project CICECO-Aveiro Institute of Materials, POCI-01-0145-FEDER-007679 (FCT Ref. UID /CTM /50011/2013), financed by national funds through the FCT/MEC and when appropriate co-financed by FEDER under the PT2020 Partnership Agreement. We would like to acknowledge the SFRH/BD/93336/2013 and SFRH/BD/84743/2012 FCT grants, and BMBF through grants 05K13TSA, 05K13MG1, and funding by ENSAR.