## Slide 1: Protecting High Field Magnets with the Coupling Loss Induced Quench System, CLIQ
E. Ravaioli (LBNL)
4 November 2016
E. Ravaioli, “CLIQ”, PhD thesis, 2015
http://doc.utwente.nl/96069/

## Slide 2
High Magnetic Field
B = 5-20 T
High Energy Density
e = B2/(2 µ0) ≈ 10-40 MJ/m3
Quench
If of a point of conductor suddenly becomes non-superconducting, it starts heating up
High Current Density
J ≈ kA/cm2
The energy stored in the magnet is usually sufficient to melt kilos of copper and damage the magnet!
Homogeneous distribution of the quench energy
Quick propagation
of the resistive zone is needed
Discharge of the magnet current with coil resistance
Quench in a superconducting magnet
Today’s focus:
Active protection systems quenching quickly and homogeneously the entire coil

## Slide 3
CLIQ – Coupling-Loss Induced Quench
Current change
Magnetic field change
Coupling losses (Heat)
QUENCH
Temperature rise
Patent EP13174323.9

## Slide 4
CLIQ on a full-size 14 m LHC main dipole
LHC main dipole magnet
Twin aperture magnet
Magnetic Length 14.3 m
Self-inductance 100 mH
Nominal current 11.8 kA
Peak magnetic field 8.3 T
Superconductor Nb-Ti
2 CLIQ Units
U0=500 V C=80 mF
Fast and effective heating mechanism
Technology proven on full-scale magnets
Validated simulations

## Slide 5
CLIQ on a full-size 14 m LHC main dipole
LHC main dipole magnet
Twin aperture magnet
Magnetic Length 14.3 m
Self-inductance 100 mH
Nominal current 11.8 kA
Peak magnetic field 8.3 T
Superconductor Nb-Ti
2 CLIQ Units
U0=500 V C=80 mF
Very robust and reliable components

## Slide 6
Comparison with traditional technology
Faster current discharge

## Slide 7
Comparison with traditional technology
Lower hot-spot temperature

## Slide 8
Simulated temperature profiles
Traditional technology
CLIQ
More homogeneous temperature

## Slide 9
Some examples of CLIQ applications…
HL-LHC
12 T quadrupole
FCC
16 T dipole
FCC
20 T dipole

## Slide 10
Outlook
CLIQ: Faster and more effective energy deposition mechanism
CLIQ: More robust electrical design
Tested on a full-size accelerator dipole & quadrupole magnets
In the baseline for the protection of HL-LHC Nb3Sn inner triplets
Protection of future magnets
(Future Circular Collider, HTS)
Will CLIQ technology influence
the design of future accelerator magnets? (less Cu, more compact)

## Slide 11
QUESTIONS?
E. Ravaioli, “CLIQ”, PhD thesis, 2015
http://doc.utwente.nl/96069/
ERavaioli@lbl.gov
2012
Idea
2013
Patent
2015
PhD, “CLIQ”
HL-LHC baseline
2016

## Slide 12
Annex

## Slide 13
Previous work
Quench using a capacitive discharge
“Temperature and Pressure Rise in Supercritical Helium during the Quench of Indirectly Cooled SC Coils”, R. M. Schotter and H. W. Lorenzen, Technische Universität München
“…a short pulse with high amplitude is obtained which makes the coil normalconducting nearly instantly by superconductor losses, field distortion and current amplification.
“Quench Protection for a 2-MJ Magnet”, Taylor et al., Lawrence Berkley National Laboratory
“…turning the entire magnet normal by dumping a short pulse of current from a capacitor bank through the windings.”
1978
1996
Glyn Kirby was looking for a way to quench/protect the magnets with AC induced heating inside the cable.
Vladimir Datskov suggested capacitive idea from the two old paper.
Emmanuele Ravaioli added the improvement with the reverse diode to keep the capacitive current oscillating.
February 2013: CLIQ tests on a solenoid in B165. June 2013: EU Patent filed.
2012-13

## Slide 14
Traditional approach: Quench heaters
Quench heaters are μm-thin strips glued to the coil, which heat the turns by thermal diffusion
Example:
HL-LHC 12 T Nb3Sn quadrupole model magnet (MQXFS1, 1.2 m)

## Slide 15
CLIQ magnetic-field change
The oscillating current introduced by CLIQ rapidly change the local magnetic field
Quasi-static field during operation
Oscillating field at CLIQ discharge
B
.
B

## Slide 16
Inter-filament coupling loss
Cu
SC
“Fast” loss:
Characteristic time constant in the order of ms or tens of ms
Filament twist-pitch
Matrix effective transverse resistivity
More effective heat deposition with respect to conventional technology based on thermal diffusion
Faster and more homogeneous quench initiation
Lower hot-spot temperature
Deposited power density roughly proportional to B2
B
.
.

## Slide 17
CLIQ main advantages & disadvantages
More effective energy deposition
Faster and more homogeneous quench initiation
More robust electrical design
Easier to implement and repair
Lower expected failure rate
Integration in the magnet circuit to be studied
Internal voltage distribution to be carefully analyzed
Redundancy of the system

## Slide 18
Scaling CLIQ performance
  CLIQ effectiveness
  → Coil geometry
  → Position of CLIQ connections
  → Electrical order of the poles
  → etc…
At high current
Low energy needed to start the quench
High energy density, needs to be quick!
 POWER density is the key parameter
At low current
High energy needed to start the quench
Low energy density, velocity not critical
 ENERGY density is the key parameter
(Number of CLIQ units)^2
(Charging voltage)^2
(magnetic length)^-2 (fixed by design)
Number of CLIQ units
(Charging voltage)^2
Capacitance of each unit
(magnetic length)^-1
Magnetic length
# of CLIQ units
Capacitance

## Slide 19
CLIQ effectiveness, Ѱ1
How much dB/dt for given voltage and magnet length?
Quadrupole
Cos-θ
dipole
Block-coil
dipole
Solenoid

## Slide 20
CLIQ on a 1 m Nb3Sn model magnet
Fast and effective heating mechanism
Technology proven on Nb3Sn magnets

## Slide 21
CLIQ on full-scale Nb3Sn low-β quad
HL-LHC inner triplet quad
Magnetic Length 7.15 m
Self-inductance 68 mH
Nominal current 16.5 kA
Peak magnetic field 8.3 T
Superconductor Nb3Sn
1 CLIQ Unit
U0=1 kV C=40 mF
All simulations performed with the software LEDET
CLIQ in the baseline: first application in an accelerator

## Slide 22
Simulated temperature distribution
Due to CLIQ’s faster quench initiation,
lower hot-spot temperature and more homogeneous temperature distribution
With outer quench heaters
With CLIQ

## Slide 23
Simulated protection performance
CLIQ performance similar to QH’s covering most coil turns

## Slide 24
CLIQ on full-scale LHC quadrupole
LHC matching quadrupole
(1 aperture)
Magnetic Length 3.4 m
Self-inductance 72 mH
Nominal current 3.6 kA
Superconductor Nb-Ti
1 CLIQ unit
U0=650 V C=8.8 mF

## Slide 25
Comparison with conventional QH’s
EE
EE

## Slide 26
Electro-Thermal and Coupling modeling
How to implement this coupling mechanism?

## Slide 27
LEDET model
All simulations presented today are performed with the LEDET 2D model
(Lumped-Element Dynamic Electro-Thermal)
The interaction between the superconducting magnet and the local coupling currents is modeled with an array of RL dissipative loops mutually coupled with the magnet self-inductance
Inter-filament coupling currents
Inter-strand coupling currents
Example: HL-LHC 12 T Nb3Sn quadrupole magnet (MQXF)
2x 16000 IFCL loops
400 ISCL loops
[1] E. Ravaioli, “CLIQ”, PhD thesis, 2015
[2] E. Ravaioli et al., Cryogenics 2016
Runs in 3 minutes!

## Slide 28
Influence of effective transverse resistivity
Good protection performance in a wide range of feff
Significant influence of feff
on the introduced current IC

## Slide 29
First HL-LHC Nb3Sn model quadrupole
FNAL vertical magnet test facility

## Slide 30
CLIQ units and terminals
CLIQ terminals added at LBNL
Main leads
CLIQ leads
CLIQ units designed and manufactured at CERN

## Slide 31
CLIQ integrated in the MQXF circuit

## Slide 32
CLIQ on 11 T dipole magnet
11 T dipole magnet
Twin aperture magnet
Magnetic Length 6 m
Self-inductance 69 mH
Nominal current 11.8 kA
Peak magnetic field 11.2 T
Superconductor Nb3Sn
2 CLIQ Units
U0=1 kV C=40 mF
J. Blomber Ghini, “Protecting the superconducting
11T Hi–Lumi LHC dipole with the new Coupling-Loss Induced Quench protection system”, CERN Report, 2015
CLIQ is not considered for the quench protection of the 11 T dipole magnets in the HL-LHC

## Slide 33
CLIQ integration in the MB/11T circuit
MB
Magnetic Length 14.3 m
Self-inductance 100 mH
Nominal current 11.8 kA
Peak magnetic field 8.3 T
Superconductor Nb-Ti
2 CLIQ Units
U0=500 V C=80 mF
J. Blomber Ghini thesis
Not considered for implementation
CLIQ is not considered for the quench protection of the 11 T dipole magnets in the HL-LHC

## Slide 34
CLIQ on 11 T dipole magnet
MB
Magnetic Length 14.3 m
Self-inductance 100 mH
Nominal current 11.8 kA
Peak magnetic field 8.3 T
Superconductor Nb-Ti
2 CLIQ Units
U0=500 V C=80 mF
J. Blomber Ghini thesis
Not considered for implementation
J. Blomber Ghini, “Protecting the superconducting
11T Hi–Lumi LHC dipole with the new Coupling-Loss Induced Quench protection system”, CERN Report, 2015
CLIQ is not considered for the quench protection of the 11 T dipole magnets in the HL-LHC

## Slide 35
CLIQ on 16 T block-coil magnet
Pole-Pole
Crossed-Layer
Layer-Layer
Requiring 2 intra-layer CLIQ terminals
Requiring 1 intra-pole CLIQ terminal
J. Blomber Ghini, thesis, 2015

## Slide 36
CLIQ on 16 T block-coil magnet
Pole-Pole
Crossed-Layer
Layer-Layer

## Slide 37
CLIQ on 16 T block-coil magnet
Baseline 2014
CLIQ allows a safe increase of the non-copper fraction
Compact, cost-effective magnets

## Slide 38
CLIQ on 20 T LTS/HTS block-coil magnet
Nb3Sn 15 T Outsert
in series to
Bi-2212 5 T Insert
1 CLIQ Unit
U0=1 kV C=150 mF
Optimum CLIQ configuration

## Slide 39
CLIQ on 20 T LTS/HTS block-coil magnet
Thot Nb3Sn <350 K
Thot Bi-2212 <300 K
LTS+HTS protection with CLIQ: HTS insert is safely discharged by the resistance developed in the LTS outsert connected in series

## Slide 40
CLIQ on 20 T LTS/HTS block-coil magnet
Performance at 20 T | Outsert | Insert
Operating current | 13.5 kA | 
Peak field in the conductor | 15.4 T | 20.4 T
Current density in the sc | 970 A/mm2 | 1980 A/mm2
Operating temperature | 4.2 K | 
Self-inductance at 20 T | 33.8 mH/m | 
Self-inductance at 1 T | 68.5 mH/m | 
Magnet length | 14 m | 
Conductor | Outsert | Insert
Superconductor | Nb3Sn | Bi-2212
Stabilizer | Cu | Ag / AgMg
Number of strands | 51 | 48
Strand diameter | 0.80 mm | 0.85 mm
Fraction of non-stabilizer | 54% | 25%
Cable width | 22 mm | 22 mm
Cable thickness | 1.40 mm | 1.49 mm