## Slide 1: Q4 update
M. Segreti, H. Felice, J.M. Rifflet, E. Todesco
Q4 update
WP3 - Q4 update - 25 November 2015

## Slide 2
| P 2
Magnetic design using MQM cable
Magnetic design optimized at the nominal current in the two apertures
Harmonics are calculated at the reference radius (2/3 of the aperture radius)
Magnet integrated strength = 440 T
Margin on the load line = at least 20 %
Cable used= MQM insulated with its classical insulation (0.08 mm thick after curing & collaring). Main characteristics of MQM cable are listed below
WP3 - Q4 update - 25 November 2015

## Slide 3
| P 3
2 layers of MQM cable
Inner blocks: 17 + 8 turns
Outer blocks: 16 +10 turns
Aperture = 90 mm (as before)
Integrated gradient = 440 T
Magnetic length = 3.67 m
Nominal gradient = 120 T/m
Loadline margin = 20 %
Temperature = 1.9 K
Nominal current = 4590 A
Stored energy = 0.81 MJ
Differential inductance = 2 × 37.5 mH
Magnetic design using MQM cable
WP3 - Q4 update - 25 November 2015

## Slide 4
| P 4
Calculation with collars (assuming a relative permeability of 1.0025)
Re-optimized cross-section to minimize impact of collars on b6
Magnetic design using MQM cable
WP3 - Q4 update - 25 November 2015

## Slide 5
| P 5
Peak field = 6.4 T
Calculation with collars (assuming a relative permeability of 1.0025)
At 4590 A, collars increase the peak field on conductor by about 0.12 T
Magnetic design using MQM cable
WP3 - Q4 update - 25 November 2015

## Slide 6
| P 6
Field quality
WP3 - Q4 update - 25 November 2015

## Slide 7
| P 7
I nom
Evolution of normal relative multipoles with the current (cable eddy currents taken into account)
Field quality
Transient from 250 A to 6 kA
WP3 - Q4 update - 25 November 2015

## Slide 8
| P 8
I nom
Evolution of b6 with the current (cable eddy currents taken into account)
Field quality
Transient from 50 A to 6 kA
WP3 - Q4 update - 25 November 2015

## Slide 9
| P 9
Unbalanced regime
Field quality
WP3 - Q4 update - 25 November 2015

## Slide 10
| P 10
Simulation :
Collaring (key)
Insulation creep (20 %)
Cooling
Energisation at 110 % of Inom  Magnetic forces are computed at each coil node
Mechanical model
CAST3M
Mechanical study
WP3 - Q4 update - 25 November 2015

## Slide 11
| P 11
Thermomechanical properties of materials
20 % loss of pre-stress is assumed after collaring due to insulation creep
Thanks to Julio for his data on MQM magnet!
Mechanical study
WP3 - Q4 update - 25 November 2015

## Slide 12
| P 12
min = 10 MPa
Azimuthal stress distribution in coil at each main step
After collaring
After creep
After cooling
At 110 % of nominal current
Mechanical study
WP3 - Q4 update - 25 November 2015

## Slide 13
| P 13
Azimuthal displacement
Radial displacement
Displacement in coil due to magnetic forces
Mechanical study
WP3 - Q4 update - 25 November 2015

## Slide 14
| P 14
The self-standing collar solution as mechanical structure is validated
Mechanical study
WP3 - Q4 update - 25 November 2015

## Slide 15
| P 15
View of a 600 mm long model
Coil ends
Lead end
Return end
WP3 - Q4 update - 25 November 2015

## Slide 16
| P 16
Coil ends
WP3 - Q4 update - 25 November 2015
Localization of the peak field (6.5 T i.e. only 1 % higher than in the straight part)

## Slide 17
| P 17
Integrated b6 has been minimized
Coil ends
WP3 - Q4 update - 25 November 2015

## Slide 18
Ongoing effort with Jean-Marc Gheller and Denis Bouziat to establish a cost estimate of the test of the single aperture short model at CEA-Saclay
Mechanical
Cost estimate based on the recovery/modification of existing components
  Top plate
  6 kA current leads
  Current leads insert
Ongoing CAD modeling to assess the required effort to perform:
  The modification of the top plate
  The integration of the current leads
  The addition of a safety valve
  The addition of a central port for magnetic measurements (performed by CERN)
    A flange ISO K DN100 is presently considered => to be discussed with CERN
Limited space on the top plate requires some optimization
DAQ and Magnet Protection
  Assessment of available equipment is ongoing
| P 18
Cost estimate for the short model test aT CEA
WP3 - Q4 update - 25 November 2015

## Slide 19
| P 19
4.2 K cold box for the current leads
Cryostat at 1.9 K (23 mbar)
Pre-cooling obtained by LN2 heat exchanger
Magnet in cryostat
WP3 - Q4 update - 25 November 2015

## Slide 20
N° | Description | Steering committee 04/09/2015 | As of 25/11/2015 Starts in/ Completed in
2.1 | Complete design of the single aperture magnet short model | July 2016 | Aug 2015 /July 2016
2.2 | Winding and polymerization of short coil 0 | December 2016 | Sept/Dec 2016
2.3 | Completion of all coils (1 set + 2 spares in total?) | July 2017 | Jan / April 2017 (~12 weeks)
2.4 | Single aperture magnet short model assembly (instrumentation + collaring + yoking) | September 2017 | March/June* 2017
2.5? | Assembly procedure end of cold mass (quad + correctors) Test of short model | December 2017 | July / Oct 2017
Proposal for new Milestones and deliverables FOR short model
WP3 - Q4 update - 25 November 2015
*preliminary assumption

## Slide 21
Thanks for your attention
Q4 update
WP3 - Q4 update - 25 November 2015