## Slide 1: 16T Cosq Dipole Mechanical Analysis
BARBARA CAIFFI
on behalf of INFN team:
G. Bellomo, P. Fabbricatore, S.Farinon, V. Marinozzi, M. Sorbi and G. Volpini

## Slide 2: Overview
Principal stresses and failure criteria
2D calculation: plain strain vs plain stress
2D mechanical optimization
Cosq 2D models
Conclusions

## Slide 3: Principal Stresses
The principal stress s1, s2 and s3, defined for each single element, are those in which the stress-strain tensor is diagonal
(s3< s2< s1).
s3 ~ sx in block coil geometry
s3 ~ sq in cosq geometry
Von Mises stress is defined as:
Stress-strain tensor
In cartesian coordinate system
PRINCIPAL coordinate system: system in which the SS tensor is DIAGONAL

## Slide 4: Principal Stresses
sq
sr
s3
s1
sVM
Principal stresses s1, s3 are shown together with sr, sq sVM for comparison.
In cosq design, the symmetry is almost azimuthal: s3 ≈ sq. sq can be compared with sy of block coil configuration.
sr is negligible.
sVM is a sort of average between s1 and s3.

## Slide 5
Cables undergo degradation if:
stress on conductors >150 MPa @room temperature;
stress on conductors > 200 MPa @cold;
stress on conductors > 150 MPa @cold after energization in the high field region → attention must be given in particular to first layers.
Tensile stress on the iron yoke at 4 K < 200 MPa.
Contact pressure Ti pole-conductors > 2 MPa after energization at 16T.
2D Mechanical Optimization
F[N]
 | No turns | sq –layer (MPa) | sq –winding (MPa)
layer 1 | 13 | 86 | 121
layer 2 | 20 | 123 | 
layer 3 | 29 | 126 | 
layer 4 | 39 | 148 | 

## Slide 6
 | E modulus [GPa] (T=4K) | E modulus [GPa] (T=300K) | a (K-1) | νxy
Conductor | Ex=33 Ey=27.5 | Ex=30 Ey=25 | ax=3.08E-3/296 ay=3.36E-3/296 | 0.3
Steel | 210 | 191 | 2.8e-3/296 | 0.28
Iron | 224 | 204 | 2.0e-3/296 | 0.28
Aluminum | 79 | 72 | 4.2e-3/296 | 0.3
Copper | 110 | 100 | 3.4e-3/296 | 0.3
Resin | 27.5 | 25 | 2.5e-3/296 | 0.2
Titanium | 126.5 | 115 | 1.7e-3/296 | 0.3
+10%
Material Properties

## Slide 7
2D Mechanical Model
Configurations studied:
There is not a best mechanical solution, each E.M. design must be optimized with ad hoc configurations!
Vertical cut in iron yoke and steel pad
Bladder&key
C-clamp
Vertical cut in the steel pad
Horizontal cut in the iron yoke
Bladder&key
Horizontal cut in iron yoke and steel pad
Bladder&key

## Slide 8
2D Mechanical Model
New E.M. design and new material properties (EM modulus for conductors, etc.) requires new mechanical solutions and optimizations.
Aluminum alloy shell;
Iron yoke cut at 45o;
Rectangular steel pad cut vertically;
Bladder&key, used to give pre-stress, 4 keys place horizontally and 4 keys placed vertically

## Slide 9
Al alloy
Iron
SS
Key2
Intf=0.5 mm
Vertical cut
Bladder & key configuration
Keys length= 20 mm, xkey1=10 mm, ykey1=10 mm,
interference key1= 0.1 mm, interference key2= 0.5 mm.
Rectangular steel pad, cut vertically, 20-60 mm thick.
Circular iron yoke, cut at 45o, 133-175 mm thick.
Rectangular shaped steel pad and horizontal and vertical keys allow to decouple x and y component of pre-stress.
55 mm
133 mm
20 mm
2D Ansys Model
ANSYS model
20 mm
60 mm
175 mm
Key1
Intf=0.1 mm
45o cut

## Slide 10
s θ peak=-176 MPa
s θ peak= -179 MPa
sθ peak= -100 MPa
Contact Pressure [Pa]
Contact Pressure [Pa]
Contact Pressure [Pa]
Cool Down
Assembly
Energization
Azimuthal Stress s θ [Pa]
Azimuthal Stress s θ[Pa]
Azimuthal Stress s θ [Pa]
Contact Pressure and Azimuthal Stress
Contact Pressure [Pa]
Energization @ 105%I
Azimuthal Stress s θ [Pa]
s θ peak= -177 MPa

## Slide 11
Von Mises Stress in Mechanical Structures
(color scale fixed at yield limit in Pa)
Assembly
Al alloy
Iron Yoke
sVM peak=225 MPa
Steel Pad
sVM peak=410 MPa
sVM peak=272 MPa
YIELD LIMIT
YIELD
LIMIT
YIELD LIMIT
sVM av=52 MPa
sVM av= 24 MPa
sVM av= 54 MPa

## Slide 12
sVM peak=410 MPa
Von Mises Stress in Mechanical Structures
(color scale fixed at yield limit in Pa)
Assembly
Al alloy
Iron Yoke
Steel Pad
YIELD LIMIT
YIELD
LIMIT
YIELD LIMIT
sVM peak=225 MPa
sVM peak=272 MPa
sVM av=52 MPa
sVM av= 24 MPa
sVM av= 54 MPa

## Slide 13
sVM peak=225 MPa
sVM peak=410 MPa
sVM peak=272 MPa
sVM av= 54 MPa
Von Mises Stress in Mechanical Structures
(color scale fixed at yield limit in Pa)
Assembly
Al alloy
Iron Yoke
Steel Pad
sVM peak=272 MPa
YIELD LIMIT
YIELD
LIMIT
YIELD LIMIT
sVM av=52 MPa
sVM av= 24 MPa

## Slide 14
Cool Down
Al alloy
sVM peak=277 MPa
sVM peak=640 MPa
Steel Pad
sVM peak=1200 MPa
Von Mises Stress in Mechanical Structures
(color scale fixed at yield limit in Pa)
Iron Yoke
YIELD LIMIT
YIELD LIMIT
YIELD
LIMIT
sVM av=131 MPa
sVM av=56 MPa
sVM av=170 MPa

## Slide 15
sVM peak=1200 MPa
Cool Down
Al alloy
sVM peak=277 MPa
sVM peak=640 MPa
Steel Pad
Von Mises Stress in Mechanical Structures
(color scale fixed at yield limit in Pa)
Iron Yoke
YIELD LIMIT
YIELD LIMIT
YIELD
LIMIT
sVM av=131 MPa
sVM av=56 MPa
sVM av=170 MPa

## Slide 16
Energization
Al alloy
sVM peak=521 MPa
sVM peak=589 MPa
Steel Pad
sVM peak=819 MPa
Von Mises Stress in Mechanical Structures
(color scale fixed at yield limit in Pa)
YIELD LIMIT
YIELD LIMIT
YIELD
LIMIT
sVM av=122 MPa
sVM av=70 MPa
sVM av=175 MPa

## Slide 17
Assembly
Cool Down
Energization
sVM peak=850 MPa
sVM peak=1120 MPa
sVM peak=255 MPa
Von Mises Stress in Titanium Poles
(color scale fixed at yield limit in Pa)
YIELD LIMIT
YIELD
LIMIT
YIELD
LIMIT
sVM av=84 MPa
sVM av= 124 MPa
sVM av=50 MPa

## Slide 18
Assembly
Cool Down
Energization
sVM peak=850 MPa
sVM peak=1120 MPa
sVM peak=255 MPa
Von Mises Stress in Titanium Poles
(color scale fixed at yield limit in Pa)
YIELD LIMIT
YIELD
LIMIT
YIELD
LIMIT
sVM av=84 MPa
sVM av= 124 MPa
sVM av=50 MPa

## Slide 19
The mechanics of the 16T cosq dipole has been investigated, giving particular importance to the fulfillment of the following requirements: stress on conductors ( <150 MPa @room temperature, < 200 MPa @cold, <150 MPa after energization in the high field zone), contact pressure Ti pole-conductors > 2 MPa after energization.
Taking into account that:
- recommended material properties list was finalized during last EuroCircol
collaboration meeting;
- a new E.M. for cos-theta model was considered after US-EuroCirCol meeting;
a completely new mechanical model was developed, in order to fulfil these new conditions.
The new configuration has:
- rectangular steel collar, cut vertically;
- circular your yoke, cut at 45°;
- 4 key placed horizontally and 4 key placed vertically, in order to give x and y pre-stress
separately
ANSYS calculations show that the new configuration:
- fulfills stress limits on the conductor;
- has good contact pressure at the pole for all the layers;
- almost fulfills stress limit on stress on structure materials .
Conclusions

## Slide 21
Back-up slides

## Slide 22
Plain stress approximation is less conservative but more compatible with 3D simulation results.
Plane strain
Plane stress
Plane strain is a stress state that varies only in the X and Y directions. The strain in the Z direction is always zero, as are the XZ and YZ shear strains, since the boundaries are fixed.
Plane stress is a stress state that varies only in the X and Y directions. The stress in the Z direction is always zero, as are the XZ and YZ shear stresses.
Plane stress is generally used on flat, thin structures, where the deformation is assumed to be solely in the plane of the structure.
Plain Strain vs Plain Stress