## Slide 1
Discussion
D. Schoerling
8th of November 2016, Annual EuroCirCol meeting

## Slide 2: Discussion
Comparison of different design options in terms of performance to be able to take a decision on the reference option or options for the CDR
Distribution of the work for the reference option(s)
Structural FEA analysis, possible options and optimization criteria
Material properties of materials used in the magnet (focus on wedges)
Required loadline margin in the ends
Yield strength in the iron/steel
Cost model considerations

## Slide 3: Magnet design for 16 T (EuroCirCol – 18%)
Design |  | Cos- | Block | Common-C
Operating current | (kA) | 10.275 | 8.47 | 9.0
Field in the aperture | (T) | 16.0 | 16.0 | 16.0
Margin at 4.2 K | % | 10.0 | 9.3 | 10.0
Intrabeam spacing | (mm) | 250 | 250 | 280
Stored magnetic energy per unit length/ap | (MJ/m) | 1.5 | 1.7 | 2.4
Inductance/aperture | (mH/m) | 25 | 44 | 58
LI/aperture | (H.A/m) | 257 | 374 | 522
Diameter IL | (mm) | 1.1 | 1.1 | 1.1
Strands/cable IL | - | 28 | 24 | 24
Cu/Non-Cu IL | - | 1.0 | 1.0 | 1.0
Diameter OL | (mm) | 0.7 | 0.7 | 1.05-1.1
Strands/cable OL | - | 38 | 37 | 14-12
Cu/Non-Cu OL | - | 2.0 | 1.0 | 1.8-2.2
Total area of Cu/aperture | (mm2) | 5004 | 4751 | 5400
Total area of Non-Cu/aperture | (mm2) | 3403 | 4751 | 3470
Total mass of Non-Cu for FCC-hh | (t) | 3876 | 5412 | 3954
Total mass of conductor for FCC-hh | (t) | 9576 | 10824 | 10104
Jeng IL | (A/mm2) | 386 | 371 | 394
Jeng OL | (A/mm2) | 703 | 595 | 789
Joveral IL | (A/mm2) | 270 | 260 | 265
Joveral OL | (A/mm2) | 459 | 386 | 480
Hot spot temperature | (K) | 328 | 308 | 350
Voltage to ground | (V) | 1400 | 1200 | TBA
Voltage turn-to-turn | (V) | 103 | 82 | TBA
V layer-to-layer | (V) | 1800 | 1100 | TBA
Cos-
Block
Common-Coil

## Slide 4: Magnet design for 16 T (EuroCirCol – 14%)
Design |  | Cos- | Block | Common-C
Operating current | (kA) | 11.18 | 10.93 | 9.17
Field in the aperture | (T) | 16.0 | 16.0 | 16.0
Margin at 1.9 K | % | 14.0 | 14.0 | 14.0
Intrabeam spacing | (mm) | 250 | 250 | 320
Stored magnetic energy per unit length/ap | (MJ/m) | 1.3 | 1.5 | 2.1
Inductance/aperture | (mH/m) | 19.9 | 24 | 49
LI/aperture | (H.A/m) | 222 | 262 | 452
Diameter IL | (mm) | 1.1 | 1.1 | 1.2
Strands/cable IL | - | 22 | 24 | 18
Cu/Non-Cu IL | - | 0.85 | 0.8 | 1
Diameter OL | (mm) | 0.712 | 0.7 | 1.2-1.15
Strands/cable OL | - | 36 | 39 | 10
Cu/Non-Cu OL | - | 2.15 | 1.6 | 2.2-3.5
Total area of Cu/aperture | (mm2) | 3920 | 4300 | 4971
Total area of Non-Cu/aperture | (mm2) | 2730 | 3295 | 2572
Total mass of Non-Cu for FCC-hh | (t) | 3110 | 3750 | 2930
Total mass of conductor for FCC-hh | (t) | 7590 | 8650 | 8590
Jeng IL | (A/mm2) | 540 | 480 | 450
Jeng OL | (A/mm2) | 780 | 730 | 760
Joveral IL | (A/mm2) | 360 | 330 | 320
Joveral OL | (A/mm2) | 510 | 480 | 490
Hot spot temperature | (K) | 344 | 350 | 384
Voltage to ground | (V) | 770 | 1200 | 3200
Voltage turn-to-turn | (V) | 86 | 105 | 100
V layer-to-layer | (V) | 910 | - | 4300
Block
Auxiliary coils not shown
Common-Coil
Cos-

## Slide 5: EuroCirCol-Design options
The reference parameter space has been finalized considering recommendations from the 1st WP5 EuroCirCol Review (11-13 May 2016, http://indico.cern.ch/event/516049)
2LPo1D-03
C.Lorin; M.Durante; M.Segreti
2LPo1D-02
M.Sorbi; G.Bellomo; P.Fabbricatore;
S.Farinon; V.Marinozzi; G.Volpini
2LPo1D-08
F.Toral; J.Munilla; T.Martinez;
L. Garcia-Tabares
scale / 2
A specific feature of this program is that different design options are being considered with the same specification and analysis tools so that they can be compared relatively to each other.

## Slide 6: Distribution of the work

## Slide 7: Structural FEA analysis, possible options and optimization criteria (1/12)
Von Mises, Third Principal Stress, Azimuthal stress -> Barbara/Stefania
Plane stress vs strain -> Barbara/Stefania
Stress pattern within the cos-theta coil -> Barbara/Stefania

## Slide 8: Plane stress vs plane strain (2/12)
Jaakko Murtomäki
Plane stress:
All stress components that are associated with magnet longitudinal dimension are zero (shear and normal stress)
Plane strain:
All strain components that are associated with magnet longitudinal dimension are zero (shear and normal strain)

## Slide 9: 2D and 3D model (3/12)
Jaakko Murtomäki
2D model boundary conditions, Fx = 68 N
3D model boundary conditions, Fx = 68 N
E = 200 GPa,  = 0.3

## Slide 10: Plane strain vs stress (4/12)
Jaakko Murtomäki & Felix Wolf
Plane stress allows z-displacement and plane strain does not
Plane-strain assumption e_33:
Plane stress: Fz =  Fx (friction less boundary)
Von Mieses:
Plane stress:
Plain strain:

## Slide 11: RMM: Geometry (5/12)
1
3
2D
3D
Contacts:
Pole – pole: sliding (contacts 1 and 3 only)
Middle coil – external coil: sliding
Inside coil (pole, layer, inter-layer): bonded
Coil properties:
44 GPa isotropic cold and warm
3.36/3.08 mm/m orthotropic
Slide of E. Rochpault

## Slide 12: RMM: Contacts (6/12)
3D
v5d
2D
Pl Stress
v18
-18.1
47.5
38.6
174
3.95
164
146
20.1
177
74.0
82.9
5.1
30.7
86.7
48.3
226
0.1
191
2D
Pl Strain
v18
Slide of E. Rochpault

## Slide 13: RMM: Coil Seqv (7/12)
22.5
161
175
51.8
130
172
22.6
3D
v5d
34.3
114
185
88.0
163
76.0
2D
Pl Stress
v18
16.7
159
273
182
125
245
180
265
2D
Pl Strain
v18
Slide of E. Rochpault

## Slide 14: RMM: Summary (8/12)
 | Contact [MPa] |  |  | Seqv [MPa] |  | 
 | Loading | 4.2 K | 18 T | Loading | 4.2 K | 18 T
3D | 20.1..146 | 74.0..177 | 5.1..82.9 | 34.3..114 | 88.0..185 | 76.0..163
2D P. stress | 4.0..164 | 38.6..174 | -18.11..47.5 | 22.5..1302 | 51.8..175 | 22.6..172
2D P. strain | 0.1..191 | 48.3..226 | 30.7..86.7 | 16.7..1252 | 182..2652 | 180..245
+/-10%
+/-20%
No match in value or location
1Sharp peak effect
2discarding corner effects
Slide of E. Rochpault

## Slide 15: Fresca2: Geometry (9/12)
2D
3D
Contacts:
Pole – pole: sliding
Middle coil – external coil: sliding
Inside coil (pole, layer, inter-layer): bonded
Coil properties:
44/52 GPa orthotropic cold and warm
3.36/3.08 mm/m orthotropic
Slide of E. Rochpault

## Slide 16: Fresca2: Contacts (10/12)
-42.9
62.9
24.0
120
2.8
52.2
51.8
6.8
116
44.3
50.1
-22.5
3D
V3,13T
0.6 mm
2D
Pl. stress
13T
0.6 mm
31.5
169
2.3
58.1
2D
Pl. strain
13T
0.6 mm
103
8.7
Slide of E. Rochpault

## Slide 17: Fresca2: Coil Sx (11/12)
3D
V3,13T
0.6 mm
-51.3
-4.8
-35.9
-130
-53.8
-2.7
-23.5
-137
-50
111
-147
14.6
-138
2D
Pl. stress
13T
0.6 mm
-60.0
-2.1
-30.6
-198
-60
-14.7
-181
2D
Pl. strain
13T
0.6 mm
Slide of E. Rochpault

## Slide 18: Fresca2: Summary (12/12)
 | Contact [MPa] |  |  | Sx [MPa] |  | 
 | Loading | 4.2 K | 18 T | Loading | 4.2 K | 18 T
3D | 6.8..51.8 | 44.3..116 | -22.5..50.1 | -51.3..-4.8 | -130..-35.9 | -138..14.6
2D P. stress | 2.8..52.2 | 24.0..120 | -42.9..62.9 | -502..-2.7 | -137..-23.5 | -147..111
2D P. strain | 2.3..58.1 | 31.5..169 | -8.7..103 | -602..-2.1 | -198..-30.6 | -181..-14.7
+/-10%
+/-20%
No match in value or location
1Sharp peak effect
2discarding corner effects
Slide of E. Rochpault

## Slide 19: Mechanical properties of Cu wedges (1/4)
The stress-strain behaviour of annealed Cu is non linear. Plastic behaviour is already observed when the stress exceeds about 20 MPa. The 0.2% proof stress (Rp0.2) is less than 50 MPa.
Young‘s modulus cannot be derived from the initial loading curve. Instead it is estimated from the unloading curve (Ea).
Even at 4.2 K annealed Cu cannot cary substantial loads.
Slide of C. Scheuerlein
 | Ea (GPa) | Rp0.2 (MPa) | Rm (MPa)
Cold-worked Cu wire | 1270.8 | 39715 | 4275.9
Annealed Cu wire | 1082.1 | 46.22.6 | 2041.6
Tensile properties of cold drawn Cu wire before and after annealing at 695 °C (measured at RT).
From: C. Scheuerlein, F. Lackner, F. Savary, B. Rehmer, M. Finn, P. Uhlemann, “Mechanical properties of the HL-LHC 11 Tesla Nb3Sn magnet constituent materials”, IEEE Trans. Appl. Supercond., submitted

## Slide 20: Mechanical properties of Glidcop wedges (2/4)
Slide of C. Scheuerlein
RT properties
Al oxide dispersion strengthened Cu (tradename Glidcop) RT mechanical properties measured after prior 650°C coil reaction heat treatment. Stres-strain curves of Ti-6Al-4V and 316LN stainless steel are shown for comparison.
Comparison of Glidcop stress strain curvers under longitudinal tensile and transverse compressive loading.

## Slide 21: Glidcop Young’s modulus temperature dependence (3/4)
Slide of C. Scheuerlein
Chart: Temperature (K)
| 297.14999999999998 | 373.15 | 473.15 | 573.15 | 673.15 | 773.15 | 873.15 | 923.15
 | 93 | 89.8 | 84.9 | 79.3 | 73.8 | 69.6 | 63.5 | 61.9
 | 108.52 | 108.3088 | 104.7967 | 93.3951 | 89.5267 | 84.4367 | 79.3467 | 74.2567 | 69.1667 | 64.0767 | 61.5317 | 57.62
Temperature dependent Young’s and shear moduli are measured by the resonance method in the temperature range 20-650 °C.
A 4.2 K Glidcop Young’s modulus of 109 GPa is obtained by fitting and extrapolating the 20-650°C data.

## Slide 22: Glidcop, some add. information (4/4)
The raw material is patented (http://www.cep-freiberg.de/en/), owned by a professor of Technical University Bergakademie Freiberg.
The production process of the wedges is such that CEP Freiberg produces the granulate and does a first extrusion, with a die produced by Luvata. Then this raw material is transported to Luvata, which are then probably performing some annealing to reduce internal stress, do acid cleaning to clean the surface and bring the wedges to final shape. Their extrusion is limited to 5 kg (currently). We at CERN have 6 m long wedges received from Luvata. The price is around 200 EUR/kg.
The material was selected because it does not transform its state during the heat treatment (no grain growth), it has a high specific heat and thermal conductivity. Another suitable material would be Ni-super-alloy, but it is very expensive and maybe magnetic (to be checked).
Should we start a study if the extrusion amount can be increased and the cost reduced?
D. Smekens

## Slide 23: Required loadline margin in the ends
A reduction of the field of around 1 T (loadline margin around 20%) in the ends seems appropriate?

## Slide 24: Yield strength in the iron/steel (1/6)
Slide of E. Rochpault
Material | Production | Thickness [mm]
Magnetil | Hot-rolled Laminations | 2.5-8
ST430 | Laminations | 
Armco | Hot-rolled Laminations | 1.5-30
HSLA | Hot-rolled pole sheets | 2-12
Silicon steels | Cold-rolled | <1.5

## Slide 25: Mechanical properties (2/6)
Material | Modulus [GPa] |  | Rp0.2 [MPa] |  | Contraction [μm/m/K]
 | RT | 4.2 K | RT | 4.2 K | To 4.2 K
SS 316LN | 203 [1], 193* | 210* | 324 [1], 286* | 930* | 10.3 [2], 9.83*
Magnetil | 213* [1], 200 [4] | 211 [4], 224* | 117/124 [1], 115/123 [4] (rolling/perp.); 180* [4] | 821 (77K) [4], 723* | 7.5 (11.5K) [4], 6.28*
ST430 | 200* [3], 200 [5,6] | 210* [3] | 205 [5], 310* [3],[6] | 830* | 6.03*
Armco | 200 [6], 213* | 224* | 305 [6], 170 [3], 233 [8], 180* | 723* | 6.28*
HSLA | ~200 [7] |  | 250-900 [7] |  | 
Silicon steels |  |  | 295 (2.5% Si) [3], 450? |  | 
*RMM baseline, best reference
[1] Scheuerlein et al., Mechanical properties of the HL-LHC 11 Tesla Nb3Sn magnet constituent materials, ASC 2016
[2] Collings, Applied Superconductivity, Metallurgy, and Physics of Titanium Alloys. International Cryogenics Monograph Series, 1986.
[3] Sgobba, Private Communication + ASM Handbook, 9th ed., vol. 3.
[4] Bertinelli, Production of Low-Carbon Magnetic Steel for the LHC Superconducting Dipole and Quadrupole Magnets, 2006
[5] http://www.pennstainless.com/ [6] http://www.azom.com/
[7] Keppert, Pole sheets Data sheet, voestalpine Steel Division
[8] EDMS#1382378 + Izquierdo, Private communication
Slide of E. Rochpault

## Slide 26: HSLA steels (3/6)
HSLA = High-strength low-alloy
Classified by yield strength:
    Norm EN 10265 (EU): 700-TG-179 = 700 MPa
    Norm SAE (Society of Automotive Engineers): 980X = 80 ksi = 552 MPa
Low carbon content: 0.05-0.25 %
Other elements up to 2%: mainly Mn, also Cu, Ni, Nb…
Magnetic polarization inversely proportional to the yield strength
Mainly obtained in sheets and strips (already annealed), but also in plates, shapes and bars
Sheets from 2 to 12 mm thick
Big press for punching required?
Open questions: properties at cold?, cycling test?
Slide of E. Rochpault

## Slide 27: Steel: Magnetic properties (4/6)
Slide of E. Rochpault
Material | Coercivity [A/m] | Max. μr | Saturation [T]*
Low-carbon [3] | 60-140 | 2200-5500 | 2.15
Magnetil [4] | 80 | ~7000 | 2.19
Armco [8] | ~200 | 3000-6000 | ~2.15
ST430 [3] | 240-320 | 1100-1600 | 1.47
1010 [3] | 80-160 | ~3800 | 2.10
HSLA [7] | ~400 | ~3000 | <2.0?
Silicon steels [3] 1% 2.5% 3% | 140-260 60-150 100-160 | 1700-6000 1800-11000 7500-15000 | 2.06 2.00 ~1.80
*lim(B-μ0H) H∞

## Slide 28: Steel: Conclusion (5/6)
Slide of E. Rochpault
Low-carbon steel usually used in SC magnets: Magnetil, Armco
  Very high saturation fields: 2.0-2.1 T
  But, limited yield strength: <200 MPa at RT
Si steels:
  Very high saturation fields: up to 2.0 T
  Higher yield strength ~300 Mpa
  But, cold rolled, then laminations < 1.5 mm
ST430:
  Higher yield strength ~300 Mpa
  Low saturation field: ~1.5 T
  Should we explore this option in more detail?
  HSLA:
  Very high saturation fields: up to 2.0 T
  Very high (and large choice of) yield strength: 250-900 MPa
  Small impact of strength on saturation field
  Should we explore this option in more detail? Which one?

## Slide 29: Steel: Test specification (6/6)
Slide of S.I. Bermudez
Traction tests at room temperature and 4.2 K to determine the yield limit.
Fracture tests at 4.2 K to determine the fracture toughness (KIc). The best reference we have now is 30 MPa*m1/2, that translates in a maximum tensile stress in the yoke of 280 MPa at cold assuming that we can have cracks of 1 mm in the material
Fatigue tests at 4 K
  Cycling to 200 MPa to determine the number of cycles before rupture (it should be larger than 20.000 for HiLumi magnets)
  Cycling to 300 MPa to determine the number of cycles before rupture (useful for 16 T magnets). If someone thinks that it would be very useful for the design to have S1(4K)>300 MPa, we can ask to perform this test at slightly larger load.

## Slide 30: Cost model considerations (1/1)
Detection equipment and circuit protection is not part the EuroCirCol cost model
Tolerances are very important for the cost of the parts. At the time for LHC performed Monte-Carlo simulations in 2D. What is your opinon to include this in the study?
End spacers could be done from a material, which is easily machinable and does not have (excessive) grain growth during the heat treatment, is non-magnet and fulfils the mechanical/structural specifications (if it exists or can be created). Should we write a specification and start a study?
Wedges, study of different materials to be started?

## Slide 31: Tensile stress (1/3)
The CCT design has seen some tensile stress, which influence does it have on the performance?

## Slide 32: Axial tensile stress-strain relation of Nb3Sn/Cu PIT wire at 4.2 K (2/3)
Slide of C. Scheuerlein
Lattice strain in the different constituents of a Nb3Sn PIT wire measured simultaneously by X-ray diffraction as a function of wire stress at 4.2 K.
From C Scheuerlein et al, Supercond. Sci. Technol. 27 (2014) 044021
At 4.2 K 100 MPa axial tensile stress on the PIT type Nb3Sn wire causes an axial strain of about 0.25%.
The reversible axial strain influence on Ic increases with increasing applied field. At 16 T more than 30% Ic reduction are possible, depending on the Nb3Sn strain state in the unloaded conductor.
The axial tensile strain irreversibity limit reported for RRP and PIT type Nb3Sn wires is typically below 0.25% strain (at 4.2 K).

## Slide 33: 4.2 K uniaxial tensile stress-strain behaviour of PIT, RRP and Bronze Route wires (3/3)
Slide of C. Scheuerlein
Stress in the BR, RRP and PIT wire as a function of Nb3Sn axial strain at 4.2 K. Stress is tensile force normalised to the wire cross section.
Comparison of the stress-strain in the Nb3Sn PIT wire at RT and at 4.2 K. Stress is normalised to the non-Cu wire cross section, assuming that the Cu does not carry substantial loads.
Similar stress-strain behaviour in RRP and PIT type wires.
Strong Nb3Sn lattice softening during cooling to 4.2 K.

## Slide 34: Conclusion