## Slide 1: EP-DT-DD: SSD-Solid State Detectors
PhD students:
Sofia OTERO UGOBONO
Esteban Curras Rivera
Hannes Neugebauer
Laura Franconi
Short term visitors (in period 7-10.2016):
Rogelio Palomo (1m) (ES, University Seville)
Geetika Jain (2m) Delhi University
EP-DT-DD Meeting – 13.10.2016
The team (CERN & visitors):
R&D: Development of radiation tolerant silicon detectors in the framework of RD50 and CMS
Service: Characterization of semiconductor detectors
Visiting Scientist:
Marcos Fernandez [1 FTE]
Sebastian White [0.25 FTE]
Fellows
Julio Calvo Pinto (1FTE)
Trainees:
Joaquin Gonzalez (0.5 FTE)
Isidro Mateu Suau (0.5 FTE)
Pedro Almeira (1 FTE)
CERN Staff
Michael Moll (0.6 FTE)
Urban
Bhavita
Shivika
Michael
Sofia
Laura
Marcos
Joaquin
Esteban
Isidro
Hannes
Julien
Left SSD since July 2016:
4 Summer Students Ayushi Jain, Bhavita Modi, Shivika Chhabra, Urban Senica
….no dedicated technician!
Julio
Pedro
Sebastian
thesis writing

## Slide 2: Present Projects and Services
SSD activities at CERN
RD50 Collaboration
  Steering and Management of the RD50 collaboration (50 Institutes, 300 members)
    Michael: Co-Spokesperson, budget holder, CERN Contact, Glimos; Veronique: secretary
  Characterization and simulation of radiation effects in silicon devices
    Development of characterization tools (TSC, edge-TCT, Two-Photon TCT, …)
    Measure damage parameter (CV,IV, CCE, TCT) and defect properties (TSC, I-DLTS)
    Simulate detector performance (TCAD, TRACS)
    Defect/Material engineering: p/n-type, different resistivity, impurities,…
  LGAD (Low Gain Avalanche Detectors) and APDs (Avalanche Particle Detectors)
    Fast timing applications
    Charge amplification in highly damaged detectors
  3D detectors, CMOS sensors, …
CMS Collaboration & RD50
  Sensor development for the High Granularity Calorimeter (HGC)
Service
  Measurement of sensors for/with external groups
….its all about silicon sensors and their application as HEP detector.
Disclaimer: In following I point out “SSD project leaders” (not the full project teams)!

## Slide 3: Damage & defect parameterization
Lab infrastructure improvements
  Optimization of cryocooler for more accurate temperature reading during temperature scan (20K to 240K in 20min)
    Production of new ceramic PCB (MPT Workshop: Antonio, Rui) & validation in TCT
    Re-design of the mechanical support and connections to reduce thermal loads
    Multi-pin feedthrough installed  injection of carriers using an LED (Collaboration with Manchester University)
    Better readout configuration  Resolution improved to 100 fA
  Addition of functionalities in the controlled temperature chamber (Susi)
    Automatic I-V measurements at different temperature steps, I-T measurements, C-V measurements (in test phase)
Study on leakage current temperature dependence
  Evaluation of activation energy for silicon (work with IRRAD team)
    Wide range of temperature scaling values published in literature
    A value of Ea = 1.20 eV was obtained by our work in agreement of theoretical predictions with midgap defect level
Details: RD50 workshop 6/2016: Isidre for T-scaling of leakage current [link]
From proof of concept to mechanical design + production of ceramic PCB

## Slide 4: Sensors with intrinsic gain
LGAD (Low Gain Avalanche Detectors) [Ultrafast Silicon Detectors – UFSD]
  RD50 collaboration (several institutions); producer CNM and FBK, soon: HPK
  Experiments considering LGAD as option: ATLAS HGT, CMS fast (hermetic) timing, CTPPS
  SSD: Study of gain homogeneity and gain loss after proton irradiation
  Ongoing: TCAD modelling of devices
    Tuning of input parameters (TCAD) and readout chain (spice) using non-irradiated devices
    Test beam of RD50 (no direct SSD involvement):
      50mm sensors of 1.4 mm2 size (reaching 26ps)
      N = number of sensors used for experiment
Details: RD50 workshop 6/2016: Sofia for LGAD [link], Michael for DD-APD [link]
gain approx. 5 before irradiation
..writing publication

## Slide 5: Sensors with intrinsic gain
DD-APD (Deep Diffused Avalanche Particle Detectors) [Hyperfast Detectors]
  Collaboration with some US CMS groups and producer RMD in the US
  Test beams in collaboration with RD51
    Time resolution obtained (non-irradiated): ≤ 20ps
  Homogeneity of response testing in SSD lab and test beam
  Next step: Testing of irradiated devices
    Neutron irradiated DDAD arrived at CERN last week
  Ongoing:
    Unpackaged devices supplied by producer RMD
    New packaging of devices with mesh (150 mm mesh on 50 mm Kapton)
    TCAD simulation of signal [optimization of design parameters]
    Design of transimpedance amplifier (Si-Ge)
Details: RD50 workshop 6/2016: Sofia for LGAD [link], Michael for DD-APD [link]
- 8x8mm2
- 1800V
s = 21ps

## Slide 6: TPA – Two Photon Absorption
Investigation on a new technique for sensor characterization (TPA – TCT)
  Deposition of charge at specific position in detector
  Laser: l  1300 nm; P  50-100 pJ; DT  240 fs
  Proof of principle presented last LHCC
  Example of application:
    HVCMOS sensors (AMS 180nm), 10 ohmcm
    100mm x 100 mm passive pixel, measured at 80V, 20C
Two Photon absorption:
[M.Fernandez-Garcia et al, VCI 2016, Feb.2016]
    Sketch of HVCMOS sensor
    Map of charge collected within 10ns
    Map of collection time needed to get 98% of charge
To be presented on KT innovation day (Tomorrow)

## Slide 7: TPA-TCT after irradiation
Technique can also applied to heavily irradiated sensors!
[M.Fernandez-Garcia, RD50 Workshop, 6/2016]
2D map of collected charge for an irradiated HVCMOS (7×1015 neq/cm2) shows regions with high electric field.
Implant position inferred from collection time and collected charge information.

## Slide 8: TPA-TCT after irradiation
Electric field profiling with TPA:
  Unirradiated detector shows 3 regions of different doping concentration. Implant is only partially depleted.
  Irradiated detector shows depleted implant, pointing to a radiation induced reduction of doping concentration.
DNW
Bulk

## Slide 9: Characterization of Thin Sensors
Use thin sensors (CIS) of various silicon materials to learn about:
  Acceptor Removal (using CV)
    [Relevance: LGAD, APD, CMOS, thin sensors]
  Detrapping close to room temperature (using DLTS)
    [Relevance: Radiation induced signal loss, the killer to all LHC detectors]
  Defect Characterization after high fluences (using TSC)
    [Relevance: defect modelling, TCAD simulation, defect engineering]
First measurements started last week
    If characterization successful: Next step is irradiation of samples.
New sensors!
Wafer layout
Sensors (took 2 years to get them!):
Pad, Ministrip, Spaghetti, e-TCT
Material:
FZ Silicon (10 Kohmcm): 50,100, 150,200,285 mm
CZ Silicon (2 Kohmcm): 50,100,150,200 mm
CZ Silicon (100 ohmcm): 50,100,150,350 mm
EPI Silicon (10,50,250,1000 Wcm): 50 mm
New project!
.. years of work ahead ..

## Slide 10: TRACS – Transient Current Simulator
TRACS
    Developed as Summer Student Project (2014-2016); Julio took up the project in 8/2016
    Finite Element Solver for signal formation in silicon detectors (with focus on edge-TCT measurements)
    Short term aim: Extract E-Field in irradiated silicon sensors by fitting e-TCT measurements
    Long term aim: Extensive simulation and fitting tool for various measurement scenarios
    Progress: Running now on 32 cores in parallel (e-TCT run simulated in 8 min instead of 2 hours)
      easily installable, manual , running on Virtual Machine at CERN; open to RD50 user community (beta version)
TRACS GUI
..using multiple cores
..E-Field parameterization model

## Slide 11: CMS: High Granularity Calorimeter
HGC - Sensors
  600 m2 of silicon sensors (6M channels) exposed up to 1.5x1016 neq/cm2; Structure of sensors: Hexagonal pads
  Radiation tests of sensor structures performed by SSD [Esteban thesis] with Uni HH
  CCE (beta, laser), CV, IV, test beam (with CMS team) on irradiated sensors: (p, n, FZ, EPI, 50 to 300 mm)
Details: IPRD16: Esteban Curras for CMS collaboration (October 2016)
Sensors: p- vs. n-type ; FZ vs. EPI
  Proof of concept: Sensors operational up to highest fluence
  300mm sensors: unclear why n-type is better !?
  120mm sensors: unclear why EPI better than DD-FZ !?
    Very welcome effect: For HPK 8” production no DD-FZ wafers available, will have to use epitaxial wafers!
Timing (test beam data)
    Reaching 20ps time resolution for S/N > 30 (Signal > 20 mips)
dd-FZ 320um
dd-FZ 200um
dd-FZ 120um
Epi 100um
20ps
IR - laser

## Slide 12: CMS HGC : skiroc2
Skiroc2 assets (towards Skiroc2CMS):
  64 Channels. Fully independent
  Preamplifier (adjustable gain)
  High dynamic range (two parallel amplifiers)
    0.5 to 150 MIPs (High Gain amp)
    150 to 2500 MIPs (Low Gain amp)
  Auto trigger + Analog + Digitalization (On chip)
  Token ring read out
Control software developed by Omega
Work status
  Test lab fully deployed
  First measurements on going
  Measurement automatization ongoing
Next steps
  mass measurements to generate statistics
  data analysis of “massive” in-lab data
All 64 channels has its own parameter for trigger and delay, both amplifiers and dedicated SCA memory
x64

## Slide 13: 3D sensors
Project of Laura Franconi (visiting PhD student, Talent) ….writing thesis now
p+ column
n+ column
Sketch of 3D sensor
IV curves before and after proton irradiation at different fluences
Same colour = same 3D diode, before and after irradiation
3.3E13 neq/cm2
1.0E14 neq/cm2
2.5E14 neq/cm2
4.5E14 neq/cm2
2.2E15 neq/cm2
5.0E15 neq/cm2
n+ column
p+ column
Punch through
column
Laser mapping in SSD lab
... good example of collaborative use of the SSD equipment (service)
Red front light gets reflected on the metal lines connecting the n+ and the p+ columns and on the columns themselves: reduced charge collection in these areas.

## Slide 14: Infrastructure & Equipment
Bldgs.28/186 (4 labs, 1 sensor storage area, 4 offices, ..)
  IV/CV [2x], Alibava (CCE) [2x], Beta (CCE), e-TCT, TCT+; I-DLTS, TSC
I-DLTS (Current Deep Level Transient Spectroscopy)
TCT+: TCT (Transient Current Technique)
Cooling to 10K
TSC (Thermally Stimulated Currents)
-70C to 180C
CCE (Charge Collection Efficiency)
Wafer/Sample storage

## Slide 15: 1year outlook – SSD activities
Laboratory and equipment
    Continue working on sample holder fitting on “all characterization stations”, CV/IV in climate chamber
    Continue building up a TSC system for defect characterization (evaluate possibility to get DLTS)
    Prepare TCT+ to measure time resolution with laser beams
    Evaluate possibility for “low-cost” TPA system at CERN
Upcoming & running projects in framework of RD50 with SSD participation
  Nitrogen enriched silicon (RD50-2016-01)
    Status: Material produced in collaboration with TOPSIL, Mask design finalized [CERN SSD  TCT, CCE(Alibava), proton irradiation]
  Gallium doped LGAD sensors (RD50-2016-02)
    Status: First tuning of implantation and diffusion hardware at CNM against TCAD tools finished; First set of detectors with different implant/diffusion ready for distribution to project partners [CERN SSD  TCT, CCE, proton irradiation]
  HVCMOS sensors
    Preparation of RD50 submission ongoing [CERN SSD  e-TCT, TPA-TCT]
  Acceptor removal and defect characterization
    Dedicated production run at CIS, Erfurt for CERN SSD finished, sensors arrived at CERN, next step: testing of sensors and irradiation; then TSC and DLTS measurements [..finally started project]
  Timing with LGAD and APD
    Study of time resolution as function of fluence (Ga-LGAD and DD-APD); TCAD simulations
  TRACS simulation and fitting tool
CMS HGC
    SKIROC [Joaquin] … evaluating test systems for the HGC readout chip
    Finalize CCE study on highly irradiated sensors and test beam studies [Esteban]
    Start evaluating epitaxial silicon [….HPK has no deep diffused 8” possibility!] (no CMS resources)

## Slide 16: KT Innovation Day
Tomorrow: KT Innovation Day
  https://indico.cern.ch/event/575296/timetable/#20161014
EP-DT-DD
EP-DT-DD
EP-DT-DD
EP-DT-EO
Yes, we are the ..
…most innovative section in the whole Department .

## Slide 17: Goodbye Maurice
CERN staff since 1.5.78
1985: LEP-BI
1990: SL-BI
1990: EF-DSM
1992: ECP-MIC-TF
1994: ECP-MIC-SD
1994: ECP-MIC-SD
1998: EP-MIC-SD
2001: EP-TA1-SD
2005: PH-DT2-SD
2008: PH-DT-DI
2004: PH-TA1-SD
2012: PH-DT-DI
2013-16: PH-DT-DD
2011: Retirement in 2013
2012: Hiring Federico
.. Retirement in 2014
… Retirement in 2015
… Retirement in 2016 ?
… we can have another party next year
Never put a sticker like this on your equipment or door! Lifetime is less than 5 years
(i.e. have a vision and plan for the long term)
…lessons learnt from Maurice
Lesson: Maurice will not disappear 
1992 …first irradiations
ROSE 1995
..first evidenced contact with Maurice 2.12.1998 - ROSE meeting
Le Chat Noir Carouge; approx. 3am

## Slide 18: Goodbye Maurice
CERN staff since 1.5.78
2013-16: PH-DT-DD
RD50
2001
2006 Prague
We had many challenges…
… but Maurice mastered them!
..guess who took the photo?
Maurice; .. teaching me French … and 2000 in Paris how to eat oysters
..how to keep workplace tidy
PSI 2000: Don’t put Aluminium blocs into high intensity pion beams; (i.e. never trust reactor people)
2002

## Slide 19: Goodbye Maurice
CERN staff since 1.5.78
2013-16: PH-DT-DD
1992 …first irradiations
RD50
2001
2002
…we had bigger dreams and challenges..
…and huge achievements!!!
…more work …and progress…
Thanks to Maurice
Thank you Maurice! …CERN would be much more efficient, more innovative, better equipped and more friendly place, … if we just could clone you  Enjoy retirement!